Selective etching of silicon nitride over silicon oxide using ClF3/H2 remote plasma

Figure S1. a) RMS surface roughness values and b) images of SiNx and SiOy after etching with ClF3 plasma [same plasma conditions with figure 3a) in the manuscript].

Figure S1 a) and b) show the RMS surface roughness values and the images of surface roughness of SiNx and SiOy after the etching with the conditions in figure 3a), respectively. SiNx and SiOy were etched ~ 400 and ~ 20 nm, respectively. As shown in the figures, the surface roughness of etched SiNx was the highest after the chemical etching with substrate temperature of 100 ℃ (1.5 nm) and it was followed by SiNx after the remote plasma etching without substrate heating (1.3 nm). The lowest surface roughness which is similar to that of the reference SiNx (~ 1 nm) was observed after the plasma etching at substrate heating with 100 ℃ (1.15 nm). Even though there were some differences in the surface roughness after the different etch methods, the differences are considered not significant. In the case of SiOy, possibly due to small etch rates for all of the cases, no significant change in the surface roughness was also observed after the etching with the different methods.

Figure S2. Cross-sectional SEM images of SiNx/SiOy stacks during the etching with ClF3 plasma for a) 1, b) 3, c) 5, and d) 8 min, respectively.

During the process, the structure of SiNx/SiOy stack started to collapse over 4000 Å-width SiNx etch depth as shown in figure S2 d) but no noticeable changes in the remaining SiOy thickness were observed up to 8 min etching.

Figure S3. Cross-sectional SEM images of SiNx/SiOy stacks during the etching with ClF3/H2 (20 %) plasma for a) 1, b) 2, c) 3, and d) 10 min, respectively.

During the etching of SiNx/SiOy stack, the thickness of SiOy was remaining unchanged and no significant change of SiOy thickness between top (which was exposed to the ClF3/H2 remote plasma directly) and underneath layers was observed up to 10 min etching with ClF3/H2 (20 %) plasma (subset of figure d)

| Sample | Atomic percentage (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Si | N | O | F | Cl | C |
| Ref. SiNx | 35.3 | 38 | 19.5 | - | - | 7.2 |
| SiNx (ClF3 only) | 33.9 | 33.3 | 12.1 | 15.6 |  | 5.1 |
| SiNx [ClF3 & H2 (20 %)] | 33.7 | 32.7 | 14.3 | 12.5 | - | 6.8 |
| Ref. SiOy | 32.9 | - | 61.9 | - | - | 5.2 |
| SiOy (ClF3 only) | 31 | - | 59.5 | 5.9 | - | 3.6 |
| SiOy [ClF3 & H2 (20 %)] | 30.5 | - | 59.6 | 5.5 | - | 4.4 |

Table S1. Atomic composition of SiNx and SiNy for different ClF3/H2 etching conditions.

As shown in Table S1, the reference SiNx deposited by PECVD, which is prepared for a stack layer of SiNx/SiOy of 3D NAND device, showed the N/Si ratio of 1.07, therefore, it was a Si-rich compound compared with the stoichiometric silicon nitride (Si3N4; 1.33) while the reference SiOy deposited by PECVD showed O/Si ratio of 1.88 which is close to stoichiometric silicon oxide (SiO2; 1:2)