Supplementary Information

Direct growth of copper oxide nanocubes on graphitic carbon nitrides for aqueous carbon dioxide photoreduction

Byeonghoon Choi,1,3 Chan Kyu Lim,1,3 Minjun Kim,1 Bumjin Park,1 Won-Woo Park,2 Oh-Hoon Kwon,2 Hee-Seung Lee1 & Hyunjoon Song1*

1Department of Chemistry, Korea Advanced Institute of Science and Technology (KAIST), 291 Daehak-ro, Yuseong-gu, Daejeon 34141, Republic of Korea.

2Department of Chemistry, Ulsan National Institute of Science and Technology, Ulsan 44919, Republic of Korea.

3These authors contributed equally: Byunghoon Choi, Chan Kyu Lim

*email: hsong@kaist.ac.kr

Supplementary Figure 1. TEM and HRTEM images of g-C3N4/Cu2O.

Supplementary Figure 2. The histogram for the edge sizes of the Cu2O nanocubes formed on the g-C3N4 surface.

Supplementary Figure 3. Elemental analysis. (a) HAADF image and (b-d) elemental mapping of g-C3N4/Cu2O.
Supplementary Table 1. Comparison of photocatalytic CO2RR performances under the specified reaction conditions without sacrificial reagents.

| Catalyst | Light source | Reaction medium | Product (Selectivity) | Activity | Ref |
| --- | --- | --- | --- | --- | --- |
| g-C3N4/Cu2O | 300 W Xe lamp | Saturated CO2 in water | CH4 (98%) | 5400 μmol gcat-1h-1 QE = 3.7% | this work |
| ZnO-Cu2O | 300 W Xe lamp | Saturated CO2 in water | CH4 (99%) | 1080 μmol gcat-1h-1 QE = 1.5% | Song et al.1 |
| S-doped CoO/Co3O4 | 300 W Xe lamp | Saturated CO2 in water | CH4 (98%) | 10000 μmol gcat-1h-1 QE = 2.3% | Song et al.2 |
| 3DOM CdSQD/NC | 300 W Xe lamp 420 nm ≤ λ | Saturated CO2 in water | CO | 10 μmol gcat-1h-1 4280 μmol gcat-1h-1 (with TEOA) | Wang et al.3 |
| Co2N/BiOBr | 300 W Xe lamp | Saturated CO2 in water | CO | 67.8 μmol gcat-1h-1 | Liu et al.4 |
| Bi12O17Cl2 | 300 W Xe lamp | Saturated CO2 in water | CO | 48.6 μmol gcat-1h-1 QE = 0.14% | Liu et al.5 |
| VBi-BiOBr UNs | 300 W Xe lamp | Saturated CO2 in water | CO | 20.1 μmol gcat-1h-1 | Xia et al.6 |
| (Au/Cu 1:2) TiO2 | 0.21 Wcm−2 Xe lamp 400 nm ≤ λ | Saturated CO2 in water | CH4 | 2200 μmol gcat-1h-1 | Garcia et al.7 |
| PCN-224(Cu)/TiO2 | 300 W Xe lamp 300 nm ≤ λ | Saturated CO2 in water | CO | 37.21 μmol gcat-1h-1 | Wang et al.8 |
| 3D-SiC/2D-MoS2 | 300 W Xe lamp 420 nm ≤ λ | CO2 and H2O vapor | CH4 | 323 μmol gcat-1h-1 QE = 1.75% | Li et al.9 |
| Graphene wrapped Pt/TiO2 | 300 W Xe lamp | CO2 and H2O vapor | CH4 (99%) | 41.3 μmol gcat-1h-1 QE = 1.93% | Zhao et al.10 |

Supplementary Figure 4. XPS spectra of g-C3N4/Cu2O. The spectra in Cu 2p3/2 and Cu LMM regions (a) before and (b) after three repetitive photocatalytic reaction cycles.

Supplementary Figure 5. TEM images of g-C3N4/Cu2O after three repetitive photocatalytic reactions.

Supplementary Figure 6. Control experiments. Photocatalytic CO2RR without CO2, light irradiation, and the catalyst.

Supplementary Figure 7. Photocatalytic CO2RR with isotopes. GC-MS analysis of 13CH4 evolved as the irradiation time from the photocatalytic reduction of 13CO2 with the g-C3N4/Cu2O catalyst.

Supplementary Figure 8. Activity using visible light. Photocatalytic production of CH4 and CO by the irradiation of visible light (λ > 420 nm) using a cut-off filter as a function of irradiation time.

Supplementary Figure 9. Band energy analysis. Tauc plots for (a) g-C3N4 and (b) Cu2O. Mott-Schottky plots for (c) g-C3N4 and (d) g-C3N4/Cu2O.

Supplementary Figure 10. Photoresponses by visible light. Current-time response curves at the visible region of g-C3N4 (black line) and g-C3N4-Cu2O (red line) in 0.1 M phosphate buffer solution.

Supplementary Figure 11. Comparison of photoresponses. Current-time response curves of ZnO-Cu2O (black), ZnO (red), g-C3N4 (blue), and g-C3N4-Cu2O (green) in a 0.1 M phosphate buffer solution by the irradiation in the (a) full-wavelength and (b) visible (λ ≥ 420 nm) regions.

Supplementary Table S2. TCSPC analysis. Fit parameters of TCSPC kinetic profiles in Figure 4d.

|  | A1 (counts) | τ1 (ns) | A2 (counts) | τ2 (ns) | A3 (counts) | τ3 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| g-C3N4 | 3760 [±60] | 18.6 [±0.2] | 38400 [±300] | 4.42 [±0.03] | 70100 [±1000] | 1.23 [±0.02] | 2.91 [±0.04] |
| g-C3N4/ Cu2O | 2350 [±50] | 15.1 [±0.2] | 30200 [±400] | 3.33 [±0.03] | 70600 [±1300] | 0.82 [±0.01] | 1.88 [±0.03] |

Supplementary Figure 12. XPS spectra. (a) g-C3N4 in the N 1s region, (b) Cu2O in the Cu 2p3/2 region, and g-C3N4/Cu2O in the (c) N 1s and (d) Cu 2p3/2 regions.

Supplementary references

1.    	Bae, K.-L., Kim, J., Lim, C. K., Nam, K. M. & Song, H. Colloidal zinc oxide-copper(I) oxide nanocatalysts for selective aqueous photocatalytic carbon dioxide conversion into methane. Nat. Commun. 8, 1156 (2017).

2.    	Choi, J. Y. et al. Surface activation of cobalt oxide nanoparticles for photocatalytic carbon dioxide reduction to methane. J. Mater. Chem. A 7, 15068-15072 (2019).

3.    	Wang, F. et al. Ordered macroporous carbonous frameworks implanted with CdS quantum dots for efficient photocatalytic CO2 reduction. Adv. Mater. 33, 2102690 (2021).

4.    	Di, J. et al. Cobalt nitride as a novel cocatalyst to boost photocatalytic CO2 reduction. Nano Energy 79, 105429 (2021).

5.    	Di, J. et al. Defect-rich Bi12O17Cl2 nanotubes self-accelerating charge separation for boosting photocatalytic CO2 reduction. Angew. Chem. Int. Ed. 57, 14847-14851 (2018).

6.   	Di, J. et al. Bismuth vacancy-tuned bismuth oxybromide ultrathin nanosheets toward photocatalytic CO2 reduction. ACS Appl. Mater. Interfaces 11, 30786-30792 (2019).

7.   	Neaţu, Ş., Maciá-Agulló, J. A., Concepción, P. & Garcia, H. Gold–copper nanoalloys supported on TiO2 as photocatalysts for CO2 reduction by water. J. Am. Chem. Soc. 136, 15969-15976 (2014).

8.    	Wang, L., Jin, P., Huang, J., She, H. & Wang, Q. Integration of copper(II)-porphyrin zirconium metal–organic framework and titanium dioxide to construct Z-scheme system for highly improved photocatalytic CO2 reduction. ACS Sustain. Chem. Eng. 7, 15660-15670 (2019).

9.	Wang, Y. et al. Visible-light driven overall conversion of CO2 and H2O to CH4 and O2 on 3D-SiC@2D-MoS2 heterostructure. J. Am. Chem. Soc. 140, 14595-14598 (2018).

10.  	Zhao, Y. et al. Graphene-wrapped Pt/TiO2 photocatalysts with enhanced photogenerated charges separation and reactant adsorption for high selective photoreduction of CO2 to CH4. Appl. Catal. B 226, 360-372 (2018).