Supplementary Information

Solvation Structure and Interfacial Regulation for Extremely Stable Zinc Metal Anodes Operating in a Wide Range of Temperatures

Peixun Xiong1, Yingbo Kang1, Nan Yao2, Xiang Chen2, Lingxing Zeng4, Qingyun Dou1, Xiaotong Han1, Rana Harpalsinh1, Zhenchuan Tian1, Jeong Hee Park1, Qiang Zhang2, and Ho Seok Park1,3*

1 School of Chemical Engineering, Sungkyunkwan University, Suwon-si, Gyeonggi-do 440-746, Republic of Korea

2 Beijing Key Laboratory of Green Chemical Reaction Engineering and Technology, Department of Chemical Engineering, Tsinghua University, Beijing, 100084, China

3 SKKU Advanced Institute of Nanotechnology (SAINT), College of Engineering & Department of Health Sciences and Technology, Samsung Advanced Institute for Health Sciences and Technology (SAIHST), Sungkyunkwan University, 2066, Seobu-ro, Jangan-gu, Suwon-si, Gyeonggi-do 440-746, Republic of Korea

4 Engineering Research Center of Polymer Green Recycling of Ministry of Education, College of Environmental Science and Engineering, Fujian Normal University, Shangsan Road No.8, Fuzhou, 350007, People’s Republic of China

*Email: phs0727@skku.edu (H. S. Park)

Table of contents

Supplementary Figure 1. Digital of photo of 2M ZnSO4 in H2O/DMF with different volume ratio.	4

Supplementary Figure 2. Snapshot of ZnSO4-H2O-DMF (5:1) during MD simulation.	5

Supplementary Figure 3. Radial distribution functions (RDFs) and coordination number distribution functions.	6

Supplementary Figure 4. Coordination numbers of H2O, DMF, and SO42– around Zn2+ in different electrolytes.	7

Supplementary Figure 5. Different Zn2+[DMF]x[H2O]y[SO42–]z complex ratios in electrolytes.	8

Supplementary Figure 6. 17O NMR spectra in ZnSO4-H2O and ZnSO4-H2O-DMF.	9

Supplementary Figure 7. Cycling performance of Zn||Zn symmetric cells in ZnSO4-H2O-DMF (5:1) electrolyte.	10

Supplementary Figure 8. Ion conductivities of different electrolytes at 25 ℃.	11

Supplementary Figure 9. Cycling performance of Zn||Zn symmetric cells in ZnSO4-H2O-DMF electrolyte.	12

Supplementary Figure 10. Rate performance of Zn||Zn symmetric cell in ZnSO4-H2O.	13

Supplementary Figure 11. Selected charge-discharge profiles of Zn||Cu asymmetric cell in ZnSO4-H2O.	14

Supplementary Figure 12. Corrosion curves of Zn anodes in different electrolytes.	15

Supplementary Figure 13. SEM image of bare Zn anode.	16

Supplementary Figure 14. SEM images of bare Zn anodes after immersion in different electrolytes.	17

Supplementary Figure 15.XRD patterns of bare Zn anodes after immersion in different electrolytes.	18

Supplementary Figure 16. CV curves of Zn||Ti cells with different electrolytes..	19

Supplementary Figure 17. Nyquist plots Zn||Zn symmetric cells in different electrolyte temperatures.	20

Supplementary Figure 18. Chronoamperograms of Zn anodes in different electrolytes.	21

Supplementary Figure 19. TEM image of Zn anode surface.	22

Supplementary Figure 20. XRD patterns of Zn anodes after 20 cycles in different electrolytes.	23

Supplementary Figure 21. pH values of different electrolytes.	24

Supplementary Figure 22. CV curves and galvanostatic charge-discharge profiles of HZICs .	25

Supplementary Figure 23. SEM images of Zn anodes after 500 cycles in different electrolytes.	26

Supplementary Figure 24. DSC curves of different electrolytes at low temperature.	27

Supplementary Figure 25. Ion conductivities of different electrolytes at different temperatures.	28

Supplementary Figure 26. DSC curves of different electrolytes at high temperature.	29

Supplementary Figure 27. Cycling performance of HZICs in different electrolytes.	30

Supplementary Figure 28. Cycling performance of HZICs in different electrolytes.	31

Supplementary Figure 29. Galvanostatic charge-discharge profiles of HZICs in at various temperatures.	32

Supplementary Figure 30. Nyquist plots Zn||Zn symmetric cells at various temperatures in different electrolytes.	33

Supplementary Figure 31. XRD pattern and SEM image of the as-synthesized Zn5(OH)6(CO3)2.	34

Supplementary Figure 32. TGA/DTA curves of the as-synthesized Zn5(OH)6(CO3)2.	35

Supplementary Table 1. Composition of different electrolytes.	36

Supplementary Table 2. Numbers of ions and solvent molecules in MD models.	36

Supplementary Table 3. Radial distribution functions and coordination number of different electrolytes.	36

Supplementary Table 4. Comparison of Zn anodes using electrolyte modification strategy.	37

Supplementary Table 5. Nyquist results of symmetric cells fitting using the equivalent circuit.	38

Supplementary Table 6. Nyquist results of symmetric cells fitting using the equivalent circuit.	38

References	38

Supplementary Movie 1. Operando optical video of Zn anode observed in ZnSO4-H2O.	41

Supplementary Movie 2. Operando optical video of Zn anode observed in ZnSO4-H2O-DMF.	41

Supplementary Figure 1. Digital of photo of 2M ZnSO4 in H2O/DMF with different volume ratio.

Supplementary Figure 2. Snapshot of ZnSO4-H2O-DMF (5:1) during MD simulation.

Supplementary Figure 3. Radial distribution functions (RDFs) and coordination number distribution functions obtained from MD simulations for ZnSO4-H2O-DMF (5:1) electrolyte.

Supplementary Figure 4. Coordination numbers of H2O, DMF, and SO42– around Zn2+ in different electrolytes.

Supplementary Figure 5. Different Zn2+[DMF]x[H2O]y[SO42–]z complex ratios in (a) ZnSO4-H2O, (b) ZnSO4-H2O-DMF (5:1), and (c) ZnSO4-H2O-DMF (4:2) electrolytes obtained from MD simulations.

Supplementary Figure 6. 17O NMR spectra in ZnSO4-H2O and ZnSO4-H2O-DMF.

Supplementary Figure 7. Cycling performance of Zn||Zn symmetric cells in ZnSO4-H2O-DMF (5:1) electrolyte at 1 mA cm–2 for 1 mA h cm–2. The voltage increase at around 450 h is caused by the temperature drop due to power failure of the temperature-controlled equipment.

Supplementary Figure 8. Ion conductivities of different electrolytes at 25 ℃.

Supplementary Figure 9. Cycling performance of Zn||Zn symmetric cells in ZnSO4-H2O-DMF electrolyte at 2 mA cm–2 for 1 mA h cm–2. The voltage increase at around 300 h is caused by the temperature drop due to power failure of the temperature-controlled equipment.

Supplementary Figure 10. Rate performance of Zn||Zn symmetric cell in ZnSO4-H2O at various current densities.

Supplementary Figure 11. Selected charge-discharge profiles of Zn||Cu asymmetric cell in ZnSO4-H2O at 1 mA cm–2 for 1 mA h cm–2.

Supplementary Figure 12. Corrosion curves of Zn anodes in different electrolytes.

Supplementary Figure 13. SEM image of bare Zn anode.

Supplementary Figure 14. SEM images of bare Zn anodes after immersion in (a) ZnSO4-H2O and (b) ZnSO4-H2O-DMF electrolytes for 5 days.

Supplementary Figure 15. XRD patterns of bare Zn anodes after immersion in (a) ZnSO4-H2O and (b) ZnSO4-H2O-DMF electrolytes for 5 days.

Supplementary Figure 16. CV curves of Zn||Ti cells with different electrolytes.

Supplementary Figure 17. Nyquist plots Zn||Zn symmetric cells tested in (a) ZnSO4-H2O and (b) ZnSO4-H2O-DMF under different temperatures. (c) The activation energies obtained from Nyquist plots.

Supplementary Figure 18. Chronoamperograms of Zn anodes in different electrolytes.

Supplementary Figure 19. TEM image of Zn anode surface after 20 cycles in ZnSO4-H2O.

Supplementary Figure 20. XRD patterns of Zn anodes after 20 cycles in different electrolytes.

Supplementary Figure 21. pH values of different electrolytes at 25 ℃.

Supplementary Figure 22. (a) CV curves of HZICs in ZnSO4-H2O at different scan rate. (b) Galvanostatic charge-discharge profiles of HZICs in ZnSO4-H2O at various current densities.

Supplementary Figure 23. SEM images of Zn anodes after 500 cycles in HZICs with (a) ZnSO4-H2O and (b) ZnSO4-H2O-DMF electrolytes.

Supplementary Figure 24. DSC curves of different electrolytes at low temperature.

Supplementary Figure 25. Ion conductivities of different electrolytes at different temperatures.

Supplementary Figure 26. DSC curves of different electrolytes at high temperature.

Supplementary Figure 27. Cycling performance of HZICs at 2 A g–1 in different electrolytes under 60 C.

Supplementary Figure 28. Cycling performance of HZICs at 2 A g–1 in different electrolytes under 70 C.

Supplementary Figure 29. Galvanostatic charge-discharge profiles of HICs cycled in ZnSO4-H2O and tested at 0.5 A g–1 under various temperatures.

Supplementary Figure 30. Nyquist plots Zn||Zn symmetric cells at various temperatures after 20 cycles at 2 mA cm–2 for 1 mA h cm–2 and -20 C in ZnSO4-H2O-DMF electrolyte.

Supplementary Figure 31. (a) XRD pattern and (b) SEM image of the as-synthesized Zn5(OH)6(CO3)2.

Supplementary Figure 32. TGA/DTA curves of the as-synthesized Zn5(OH)6(CO3)2.

Supplementary Table 1. Composition of different electrolytes.

| System (2 mol/L) | ZnSO4 salt | H2O | DMF | Molar ratio (H2O:DMF) |
| --- | --- | --- | --- | --- |
| ZnSO4-H2O | 2 mmol | 55.56 mmol | 0 | -- |
| ZnSO4-H2O-DMF (5:1) | 2 mmol | 49.30 mmol | 2.16 mmol | 22.82:1 |
| ZnSO4-H2O-DMF (4:2) | 2 mmol | 37.04 mmol | 4.32 mmol | 8.57:1 |

Supplementary Table 2. Numbers of ions and solvent molecules in MD models.

| System (2 mol/L) | Number of Zn2+ | Number of SO42- | Number of H2O | Number of DMF |  |
| --- | --- | --- | --- | --- | --- |
| ZnSO4-H2O | 50 | 50 | 1390 |  | 0 |
| ZnSO4-H2O-DMF (5:1) | 50 | 50 | 1226 |  | 54 |
| ZnSO4-H2O-DMF (4:2) | 50 | 50 | 922 |  | 108 |

Supplementary Table 3. Radial distribution functions and coordination number of different electrolytes.

| System | CN of DMF (coordinated/total) | CN of H2O | CN of SO42- |
| --- | --- | --- | --- |
| ZnSO4-H2O | 0.00 (0.0%) | 3.82 | 1.72 |
| ZnSO4-H2O-DMF (5:1) | 0.20 (18.5%) | 3.68 | 1.60 |
| ZnSO4-H2O-DMF (4:2) | 0.44 (20.4%) | 3.48 | 1.56 |

Supplementary Table 4. Comparison of electrochemical properties of the recently reported Zn anodes using electrolyte modification strategy.

| Electrolyte | Current density (mA cm-2)@Capacity (mAh cm-2) | Cycle life (h) | Ref. |
| --- | --- | --- | --- |
| 2M ZnSO4 in H2O:DMF (4:2) | 1@1 | 2500 | This work |
|  | 2@1 | 1400 |  |
|  | 4@1 | 1000 |  |
| 2M ZnSO4 in H2O:DMF (5:1) | 1@1 | 1780 |  |
| 1M Zn(TFSI)2+20M LiTFSI | 0.2@0.068 | ~170 | [1] |
| 1M Zn(SO3CF3) + 1M Li(SO3CF3)2 | 0.5@0.25 | 1500 | [2] |
| 0.5M Zn(CF3SO3)2 in TEP:H2O (7:3) | 1@1 | 220 | [3] |
| LiTFSI:Zn(TFSI)2:urea:water= 1 : 0.05 : 3.8 : 2.0 | 0.1@0.074 | 2400 | [4] |
| 3M Zn(CF3SO3)2 in H2O: diethyl ether (98:2) | 0.2@0.2 | 250 | [5] |
| 2M ZnSO4+0.05mM TBA2SO4 | 2@2 | 300 | [6] |
| 2 M ZnSO4 in ethylene glycol: H2O (40:60) | 2@1 | 145 | [7] |
| 1M Zn(OAc)2+31M KOAc | 5@0.42 | 33.3 | [8] |
| 1M ZnCl2 in H2O: DMSO (17:1) | 0.5@0.5 | 1000 | [9] |
| 1 M ZnSO4 in acetonitrile: H2O (10:90) | 1@2 | 600 | [10] |
| 3M ZnSO4+ 2M LiCl | 0.2@-- | 170 | [11] |
| 1M ZnSO4+ 10mM glucose | 1@1 | 2000 | [12] |
| 1M Zn(CF3SO3)2 +25mM Zn(H2PO4)2 in H2O | 1@1 | 1200 | [13] |
| 4M Zn(TFSI)2+4M P444(201)-TFSI | 1@1 | 850 | [14] |
| 3M Zn(SO3CF3)2+20mM Zn(NO3)2 | 0.5@0.5 | 1200 | [15] |
| 2M Zn(SO3CF3)2 in H2O:DMC (4:1 in molar) | 1@0.5 | 1050 | [16] |
| 2M Zn(SO3CF3)2 in H2O: EG (1:5) | 0.5@0.5 | 600 | [17] |
| 2M ZnSO4 + 0.05M KPF6 | 1@0.5 | 2200 | [18] |
| 2M ZnSO4 + 0.5M NaSO4 | 0.2@-- | 300 | [19] |
| 2M ZnSO4 in glycerol: H2O (1:1) | 1@1 | 1500 | [20] |
| 1M ZnSO4 + 6mM POM in H2O | 10@1 | 114 | [21] |
| 3M ZnSO4 in H2O: ethylene glycol (32:68) | 0.5@0.5 | 2668 | [S22] |
| 2M ZnSO4 + 0.05mg mL-1 Ti3C2Tx | 1@1 | 1000 | [S23] |
| 4M Zn(SO3CF3)2+0.5M Me3EtNOTF | 0.5@0.25 | 6000 | [S24] |

Supplementary Table 5. Nyquist results of symmetric cells fitting using the equivalent circuit.

| Electrolytes | Pristine |  | After 30 min |  | After 10 cycles |  |  | After 20 cycles |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Rs (Ω) | Rct (Ω) | Rs (Ω) | Rct (Ω) | Rs (Ω) | Rint (Ω) | Rct (Ω) | Rs (Ω) | Rint (Ω) | Rct (Ω) |
| ZnSO4-H2O | 0.1 | 420 | 0.1 | 820.3 | 0.5 | 3.2 | 96.1 | 0.3 | 3.3 | 72.4 |
| ZnSO4-H2O-DMF | 1.1 | 198.5 | 1.1 | 362.9 | 1.2 | 2.2 | 58.5 | 1.3 | 2.1 | 46.2 |

Supplementary Table 6. Nyquist results of symmetric cells fitting using the equivalent circuit.

| Temperature (C) | Rs (Ω) | Rint (Ω) | Rct (Ω) |
| --- | --- | --- | --- |
| -20 | 8.6 | 3077 | 12306 |
| 70 | 1.3 | 8.9 | 44.7 |

Equivalent circuit diagram of symmetrical cells in ZnSO4-H2O and ZnSO4-H2O-DMF:

References

- F. Wang, O. Borodin, T. Gao, X. Fan, W. Sun, F. Han, A. Faraone, J. A. Dura, K. Xu, C. Wang. Highly reversible zinc metal anode for aqueous batteries. Nat. Mater. 17, 543–549, (2018).

- J. Hao, J. Long, B. Li, X. Li, S. Zhang, S. Zhang, F. Yang, X. Zeng, Z. Yang, W. Pang, Z. Guo. Toward High-Performance Hybrid Zn-Based Batteries via Deeply Understanding Their Mechanism and Using Electrolyte Additive. Adv. Funct. Mater. 29, 1903605, (2019).

- A. Naveed, H. Yang, J. Yang, Y. Nuli, J. Wang. Highly reversible and rechargeable safe Zn batteries based on a triethyl phosphate electrolyte. Angew. Chem. Int. Ed. 58, 2760–2764, (2019).

- J. Zhao, J. Zhang, W. Yang, B. Chen, Z. Zhao, H. Qiu, S. Dong, X. Zhou, G. Cui, L. Chen. “Water-in-deep eutectic solvent” electrolytes enable zinc metal anodes for rechargeable aqueous batteries. Nano Energy, 57, 625–634, (2019).

- W. Xu, K. Zhao, W. Huo, Y. Wang, G. Yao, X. Gu, H. Cheng, L. Mai, C. Hu, X. Wang. Diethyl ether as self-healing electrolyte additive enabled long-life rechargeable aqueous zinc ion batteries. Nano Energy, 62, 275–281, (2019).

- A. Bayaguud, X. Luo, Y. Fu, C. Zhu. Cationic surfactant-type electrolyte additive enables three-dimensional dendrite-free zinc anode for stable zinc-ion batteries. ACS Energy Lett. 5, 3012–3020, (2020).

- N. Chang, T. Li, R. Li, S. Wang, Y. Yin, H. Zhang, X. Li. An aqueous hybrid electrolyte for low-temperature zinc-based energy storage devices. Energy Environ. Sci. 13, 3527–3535, (2020).

- S. Chen, R. Lan, J. Humphreys, S. Tao. Salt-concentrated acetate electrolytes for a high voltage aqueous Zn/MnO2 battery. Energy Storage Materials, 28, 205–315, (2020).

- L. Gao, D. Li, E. Hu, J. Xu, T. Deng, L. Ma, Y. Wang, X. Yang, C. Wang. Solvation structure design for aqueous Zn metal batteries. J. Am. Chem. Soc. 142, 21404–21409, (2020).

- Z. Hou, H. Tan, Y. Gao, M. Li, Z. Lu, B. Zhang. Tailoring desolvation kinetics enables stable zinc metal anodes. J. Mater. Chem. A, 8, 19367–19374, (2020).

- X. Guo, Z. Zhang, J. Li, N. Luo, G. Chai, T. S. Miller, F. Lai, P. Shearing, D. J. L. Brett, D. Han, Z. Weng, G. He, I. P. Parkin. Alleviation of Dendrite Formation on Zinc Anodes via Electrolyte Additives. ACS Energy Lett. 6, 395–403, (2021).

- P. Sun, L. Ma, W. Zhou, M. Qiu, Z. Wang, D. Chao, W. Mai. Simultaneous Regulation on Solvation Shell and Electrode Interface for Dendrite‐Free Zn Ion Batteries: Achieved by a Low‐Cost Glucose Additive. Angew. Chem. 133, 18395–18403, (2021).

- X. Zeng, J. Mao, J. Hao, J. Liu, S. Liu, Z. Wang, Y. Wang, S. Zhang, T. Zheng, J. Liu, P. Rao, Z. Guo. Electrolyte Design for In Situ Construction of Highly Zn2+-Conductive Solid Electrolyte Interphase to Enable High-Performance Aqueous Zn-Ion Batteries under Practical Conditions. Adv. Mater. 33, 2007416, (2021).

- L. Ma, T. P. Pollard, Y. Zhang, M. A. Schroeder, M. S. Ding, A. V. Cresce, R. Sun, D. R. Baker, B. A. Helms, E. J. Maginn, C. Wang, O. Borodin, K. Xu. Functionalized Phosphonium Cations Enable Zinc Metal Reversibility in Aqueous Electrolytes. Angew. Chem. Int. Ed. 60, 12438–12445, (2021).

- D. Li, L. Gao, T. Deng, S. Liu, C. Wang. Design of a Solid Electrolyte Interphase for Aqueous Zn Batteries. Angew.Chem. Int.Ed. 60, 13035–13041, (2021).

- Y. Dong, L. Mao, G. Ma, S. Di, Y. Wang, L. Wang, J. Xu, N. Zhang. Non-concentrated aqueous electrolytes with organic solvent additives for stable zinc batteries. Chem. Sci. 12, 5843–5852, (2021).

- V. Verma, R. M. Chan, L. Yang, S. Kumar, S. Sattayaporn, R. Chua, Y. Cai, P. Kidkhunthod, W. M. Jr., M. Srinivasan. Chelating Ligands as Electrolyte Solvent for Rechargeable Zinc-Ion Batteries. Chem. Mater. 33, 1330–1340, (2021).

- Y. Zhu, S. Zhang, S. Wu, Z. Hu, G. Cui, J. Luo. In situ built interphase with high interface energy and fast kinetics for high performance Zn metal anodes. Energy Environ. Sci. 14, 3609–3620, (2021).

- Y. Xu, J. Zhu, J. Feng, Y. Wang, X. Wu, P. Ma, X. Zhang, G. Wang, X. Yan. A rechargeable aqueous zinc/sodium manganese oxides battery with robust performance enabled by Na2SO4 electrolyte additive. Energy Storage Materials, 38, 299–308, (2021).

- Y. Zhang, M. Zhu, K. Wu, F. Yu, G. Wang, G. Xu, M. Wu, H. Liu, S. Dou, C. Wu. An in-depth insight of a highly reversible and dendrite-free Zn metal anode in an hybrid electrolyte. J. Mater. Chem. A, 9, 4253–4261, (2021).

- H. Wu, X. Gu, P. Huang, C. Sun, H. Hu. Y. Zhong, C. Lai. Polyoxometalate driven dendrite-free zinc electrodes with synergistic effects of cation and anion cluster regulation. J. Mater. Chem. A, 9, 7025–7033, (2021).

- R. Qin, Y. Wang, M. Zhang, Y. Wang, S. Ding, A. Song, H. Yi, L. Yang, Y. Song, Y. Cui, J. Liu, Z. Wang, S. Li, Q. Zhao, F. Pan. Tuning Zn2+ coordination environment to suppress dendrite formation for high-performance Zn-ion batteries. Nano Energy, 80, 105478, (2021).

- C. Sun, C. Wu, X. Gu, C. Wang, Q. Wang. Interface Engineering via Ti3C2Tx MXene Electrolyte Additive toward Dendrite-Free Zinc Deposition. Nano-Micro Lett. 13, 89, (2021).

- L. Cao, D. Li, T. Pollard, T. Deng, B. Zhang, C. Yang, L. Chen, J. Vatamanu, E. Hu, M. J. Hourwitz, L. Ma, M. Ding, Q. Li, S. Hou, K. Gaskell, J. T. Fourkas, X.-Q. Yang, K. Xu, O. Borodin, C. Wang. Fluorinated interphase enables reversible aqueous zinc battery chemistries. Nat. Nanotechnol. 16, 902–910, (2021).

# Movies

Supplementary Movie 1. Operando optical video of Zn anode observed in symmetric transparent cell with ZnSO4-H2O.

Supplementary Movie 2. Operando optical video of Zn anode observed in symmetric transparent cell with ZnSO4-H2O-DMF.