SUPPLEMENTARY TABLES FOR FINAL SUBMISSION

Table S1: Equilibrium Constants for Zn(II) Extraction by Cyanex 272

Conditions: [Zn(II)]ᵢₙᵢ = 1.00 kg m⁻³, [SO₄²⁻] = 0.015 kmol m⁻³, T = 303 K, O/A = 1

| [H₂A₂] (kmol m⁻³) | log Kₑₓ | Kₑₓ | R² Value |
| --- | --- | --- | --- |
| 0.025 | −2.50 ± 0.03 | (3.16 ± 0.22) × 10⁻³ | 0.998 |
| 0.050 | −2.20 ± 0.02 | (6.31 ± 0.35) × 10⁻³ | 0.999 |
| 0.075 | −2.00 ± 0.02 | (1.00 ± 0.05) × 10⁻² | 0.997 |
| 0.100 | −1.85 ± 0.02 | (1.41 ± 0.07) × 10⁻² | 0.999 |
| 0.150 | −1.70 ± 0.01 | (2.00 ± 0.06) × 10⁻² | 0.998 |
| 0.200 | −1.60 ± 0.01 | (2.51 ± 0.07) × 10⁻² | 0.999 |
| 0.300 | −1.45 ± 0.01 | (3.55 ± 0.10) × 10⁻² | 0.998 |

Note: Kex calculated from intercept of log D vs. pH plots using equation: log D = log Kₑₓ + 2 log[H₂A₂] + 2 pH eq. Values represent mean ± standard deviation of n=3 independent experiments.

Table S2: Determination of equilibrium time for Zn(II) extraction by Cyanex 272

Conditions: [Zn(II)]aq = 1.00 kg m⁻³, [H₂A₂]₀ = 0.025 kmol m⁻³, [SO₄²⁻] = 0.0153 kmol m⁻³, pHᵢₙᵢ = 6.00, pH eq = 2.40, T = 303 ± 0.50 K, O/A ratio = 1.

| Time (min) | [Zn(II)]aq (kg m⁻³) | [Zn(II)]ₒ (kg m⁻³) | [Zn(II)]ₒ / [Zn(II)]ₐq | log([Zn(II)]ₒ / [Zn(II)]aq) |
| --- | --- | --- | --- | --- |
| 0.25 | 0.909 ± 0.010 | 0.091 ± 0.005 | 0.10 ± 0.005 | −1.00 ± 0.005 |
| 0.50 | 0.848 ± 0.010 | 0.152 ± 0.005 | 0.18 ± 0.005 | −0.74 ± 0.005 |
| 0.75 | 0.795 ± 0.010 | 0.205 ± 0.005 | 0.26 ± 0.005 | −0.59 ± 0.005 |
| 1.00 | 0.760 ± 0.010 | 0.240 ± 0.005 | 0.32 ± 0.005 | −0.49 ± 0.005 |
| 1.50 | 0.695 ± 0.010 | 0.305 ± 0.005 | 0.44 ± 0.005 | −0.36 ± 0.005 |
| 2.00 | 0.630 ± 0.010 | 0.370 ± 0.005 | 0.59 ± 0.005 | −0.23 ± 0.005 |
| 2.50 | 0.592 ± 0.010 | 0.408 ± 0.005 | 0.69 ± 0.005 | −0.16 ± 0.005 |
| 3.00 | 0.565 ± 0.010 | 0.435 ± 0.005 | 0.77 ± 0.005 | −0.11 ± 0.005 |
| 3.50 | 0.550 ± 0.010 | 0.450 ± 0.005 | 0.82 ± 0.005 | −0.09 ± 0.005 |
| 4.00 | 0.545 ± 0.010 | 0.455 ± 0.005 | 0.83 ± 0.005 | −0.08 ± 0.005 |
| 4.50 | 0.542 ± 0.010 | 0.458 ± 0.005 | 0.85 ± 0.005 | −0.07 ± 0.005 |
| 5.00 | 0.542 ± 0.010 | 0.458 ± 0.005 | 0.85 ± 0.005 | −0.07 ± 0.005 |

Table S3: Effect of Zn(II) concentration on extraction ratio by Cyanex 272

Conditions: [H₂A₂]ₒ,ᵢₙᵢ = 0.025 ± 0.001 kmol m⁻³, [SO₄²⁻] = 0.046 ± 0.001 kmol m⁻³, pHᵢₙᵢ = 6.00 ± 0.05, pH eq = 2.50 ± 0.05, T = 303 ± 0.5 K, O/A = 1.00 ± 0.05, t = 5.0 ± 0.5 min

| [Zn(II)]ᵢₙᵢ (kg m⁻³) | [Zn(II)]ᵢₙᵢ (kmol m⁻³) | log[Zn(II)]ᵢₙᵢ | pH eq | [Zn(II)]eq (kg m⁻³) | [Zn(II)]ₒ,ₑq (kg m⁻³) | D | log D | log[Zn(II)]eq (kmol m⁻³) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.20 ± 0.01 | 0.00358 ± 0.00005 | −2.515 ± 0.005 | 2.50 ± 0.05 | 0.080 ± 0.005 | 0.120 ± 0.005 | 1.50 ± 0.05 | 0.180 ± 0.005 | −2.91 ± 0.05 |
| 0.35 ± 0.01 | 0.00535 ± 0.00005 | −2.272 ± 0.005 | 2.48 ± 0.05 | 0.155 ± 0.005 | 0.195 ± 0.005 | 1.26 ± 0.05 | 0.100 ± 0.005 | −2.63 ± 0.05 |
| 0.50 ± 0.01 | 0.00764 ± 0.00005 | −2.116 ± 0.005 | 2.44 ± 0.05 | 0.250 ± 0.005 | 0.250 ± 0.005 | 1.00 ± 0.05 | 0.00 ± 0.05 | −2.42 ± 0.05 |
| 0.70 ± 0.01 | 0.0107 ± 0.0001 | −1.970 ± 0.005 | 2.41 ± 0.05 | 0.380 ± 0.005 | 0.320 ± 0.005 | 0.84 ± 0.05 | −0.075 ± 0.005 | −2.21 ± 0.05 |
| 1.00 ± 0.01 | 0.0153 ± 0.0001 | −1.816 ± 0.005 | 2.40 ± 0.05 | 0.572 ± 0.005 | 0.428 ± 0.005 | 0.75 ± 0.05 | −0.123 ± 0.005 | −2.10 ± 0.05 |
| 1.50 ± 0.01 | 0.0229 ± 0.0001 | −1.640 ± 0.005 | 2.35 ± 0.05 | 0.980 ± 0.005 | 0.520 ± 0.005 | 0.53 ± 0.05 | −0.275 ± 0.005 | −1.82 ± 0.05 |
| 2.00 ± 0.01 | 0.0305 ± 0.0001 | −1.515 ± 0.005 | 2.30 ± 0.05 | 1.420 ± 0.005 | 0.580 ± 0.005 | 0.41 ± 0.05 | −0.390 ± 0.005 | −1.66 ± 0.05 |
| 3.00 ± 0.01 | 0.0458 ± 0.0001 | −1.338 ± 0.005 | 2.26 ± 0.05 | 2.290 ± 0.005 | 0.710 ± 0.005 | 0.31 ± 0.05 | −0.510 ± 0.005 | −1.45 ± 0.05 |

Table S4: Effect of extractant concentration on extraction ratio of Zn(II) by Cyanex 272

Conditions: [Zn(II)]ᵢₙᵢ = 1.00 ± 0.01 kg m⁻³, [SO₄²⁻] = 0.015 ± 0.001 kmol m⁻³, pHᵢₙᵢ = 6.00 ± 0.05, t = 5.0 ± 0.5 min, T = 303 ± 0.5 K, O/A = 1.00 ± 0.05

| [H₂A₂]ₒ,ᵢₙᵢ (kmol m⁻³) | pH eq | [Zn(II)]eq (kg m⁻³) | [Zn(II)]ₒ,ₑq (kg m⁻³) | D | log D |
| --- | --- | --- | --- | --- | --- |
| 0.025 ± 0.001 | 2.40 ± 0.05 | 0.5720 ± 0.005 | 0.4280 ± 0.005 | 0.748 ± 0.01 | −0.126 ± 0.005 |
| 0.050 ± 0.001 | 2.33 ± 0.05 | 0.4513 ± 0.005 | 0.5487 ± 0.005 | 1.216 ± 0.01 | 0.085 ± 0.005 |
| 0.075 ± 0.001 | 2.30 ± 0.05 | 0.4000 ± 0.005 | 0.6000 ± 0.005 | 1.500 ± 0.01 | 0.176 ± 0.005 |
| 0.100 ± 0.001 | 2.28 ± 0.05 | 0.3139 ± 0.005 | 0.6861 ± 0.005 | 2.180 ± 0.01 | 0.340 ± 0.005 |
| 0.150 ± 0.001 | 2.21 ± 0.05 | 0.1695 ± 0.005 | 0.8305 ± 0.005 | 4.900 ± 0.01 | 0.690 ± 0.005 |
| 0.200 ± 0.001 | 2.18 ± 0.05 | 0.1289 ± 0.005 | 0.8711 ± 0.005 | 6.760 ± 0.01 | 0.830 ± 0.005 |
| 0.300 ± 0.001 | 2.15 ± 0.05 | 0.0705 ± 0.005 | 0.9295 ± 0.005 | 13.18 ± 0.01 | 1.120 ± 0.005 |

Note: Only the first pH condition (pH eq = 2.40) is shown as an example.

Table S5: Effect of aqueous equilibrium pH on the extraction of Zn(II) by Cyanex 272

Conditions: [Zn(II)]ᵢₙᵢ = 1.00 ± 0.01 kg m⁻³, [SO₄²⁻] = 0.015 ± 0.001 kmol m⁻³, t = 5.0 ± 0.5 min, T = 303 ± 0.5 K, O/A = 1.00 ± 0.05

A. [H₂A₂]ₒ,ᵢₙᵢ = 0.025 ± 0.001 kmol m⁻³

| pH eq | [Zn(II)]eq (kg m⁻³) | [Zn(II)]ₒ,ₑq (kg m⁻³) | D | log D |
| --- | --- | --- | --- | --- |
| 3.48 ± 0.05 | 0.0196 ± 0.001 | 0.9804 ± 0.005 | 50.020 ± 1.50 | 1.700 ± 0.01 |
| 3.45 ± 0.05 | 0.0294 ± 0.001 | 0.9706 ± 0.005 | 33.010 ± 1.00 | 1.518 ± 0.01 |
| 3.40 ± 0.05 | 0.0327 ± 0.001 | 0.9673 ± 0.005 | 29.580 ± 1.00 | 1.481 ± 0.01 |
| 3.28 ± 0.05 | 0.0491 ± 0.001 | 0.9509 ± 0.005 | 19.366 ± 0.50 | 1.287 ± 0.01 |
| 3.17 ± 0.05 | 0.0654 ± 0.001 | 0.9346 ± 0.005 | 14.290 ± 0.50 | 1.155 ± 0.01 |
| 3.00 ± 0.05 | 0.1177 ± 0.001 | 0.8823 ± 0.005 | 7.500 ± 0.20 | 0.875 ± 0.01 |
| 2.75 ± 0.05 | 0.2000 ± 0.001 | 0.8000 ± 0.005 | 4.000 ± 0.10 | 0.600 ± 0.01 |
| 2.70 ± 0.05 | 0.2200 ± 0.001 | 0.7800 ± 0.005 | 3.545 ± 0.10 | 0.550 ± 0.01 |
| 2.45 ± 0.05 | 0.5388 ± 0.001 | 0.4612 ± 0.005 | 0.856 ± 0.05 | −0.068 ± 0.005 |
| 2.40 ± 0.05 | 0.5720 ± 0.001 | 0.4280 ± 0.005 | 0.750 ± 0.05 | −0.125 ± 0.005 |
| 2.28 ± 0.05 | 0.7153 ± 0.001 | 0.2847 ± 0.005 | 0.398 ± 0.02 | −0.400 ± 0.005 |
| 2.25 ± 0.05 | 0.7521 ± 0.001 | 0.2479 ± 0.005 | 0.330 ± 0.02 | −0.481 ± 0.005 |
| 2.05 ± 0.05 | 0.8065 ± 0.001 | 0.1935 ± 0.005 | 0.240 ± 0.02 | −0.620 ± 0.005 |
| 1.85 ± 0.05 | 0.9147 ± 0.001 | 0.0853 ± 0.005 | 0.093 ± 0.01 | −1.030 ± 0.005 |

B. [H₂A₂]ₒ,ᵢₙᵢ = 0.050 ± 0.001 kmol m⁻³

| pHeq | [Zn(II)]eq (kg m⁻³) | [Zn(II)]o,eq (kg m⁻³) | D | log D |
| --- | --- | --- | --- | --- |
| 3.20 ± 0.05 | 0.0155 ± 0.001 | 0.9845 ± 0.005 | 63.516 ± 1.50 | 1.803 ± 0.01 |
| 3.03 ± 0.05 | 0.0315 ± 0.001 | 0.9685 ± 0.005 | 30.740 ± 1.00 | 1.488 ± 0.01 |
| 2.80 ± 0.05 | 0.0657 ± 0.001 | 0.9343 ± 0.005 | 14.221 ± 0.50 | 1.153 ± 0.01 |
| 2.70 ± 0.05 | 0.1009 ± 0.001 | 0.8991 ± 0.005 | 8.912 ± 0.30 | 0.950 ± 0.01 |
| 2.55 ± 0.05 | 0.2044 ± 0.001 | 0.7936 ± 0.005 | 3.846 ± 0.10 | 0.585 ± 0.01 |
| 2.40 ± 0.05 | 0.2961 ± 0.001 | 0.7039 ± 0.005 | 3.377 ± 0.10 | 0.376 ± 0.01 |
| 2.25 ± 0.05 | 0.4851 ± 0.001 | 0.5143 ± 0.005 | 1.059 ± 0.05 | 0.025 ± 0.005 |
| 2.05 ± 0.05 | 0.6662 ± 0.001 | 0.3338 ± 0.005 | 0.501 ± 0.03 | −0.300 ± 0.005 |
| 1.95 ± 0.05 | 0.7520 ± 0.001 | 0.2480 ± 0.005 | 0.330 ± 0.02 | −0.482 ± 0.005 |
| 1.85 ± 0.05 | 0.8333 ± 0.001 | 0.1667 ± 0.005 | 0.200 ± 0.01 | −0.700 ± 0.005 |

C. [H₂A₂]ₒ,ᵢₙᵢ = 0.100 ± 0.001 kmol m⁻³

| pHeq | [Zn(II)]eq (kg m⁻³) | [Zn(II)]o,eq(kg m⁻³) | D | log D |
| --- | --- | --- | --- | --- |
| 2.83 ± 0.05 | 0.0257 ± 0.001 | 0.9743 ± 0.005 | 37.910 ± 1.00 | 1.578 ± 0.01 |
| 2.70 ± 0.05 | 0.0425 ± 0.001 | 0.9575 ± 0.005 | 22.530 ± 0.70 | 1.353 ± 0.01 |
| 2.50 ± 0.05 | 0.1009 ± 0.001 | 0.8991 ± 0.005 | 8.911 ± 0.30 | 0.950 ± 0.01 |
| 2.26 ± 0.05 | 0.2551 ± 0.001 | 0.7449 ± 0.005 | 2.920 ± 0.10 | 0.465 ± 0.01 |
| 2.00 ± 0.05 | 0.5000 ± 0.001 | 0.5000 ± 0.005 | 1.000 ± 0.05 | 0.000 ± 0.005 |
| 1.84 ± 0.05 | 0.6761 ± 0.001 | 0.3239 ± 0.005 | 0.479 ± 0.03 | −0.320 ± 0.005 |
| 1.65 ± 0.05 | 0.8265 ± 0.001 | 0.1735 ± 0.005 | 0.210 ± 0.02 | −0.678 ± 0.005 |
| 1.45 ± 0.05 | 0.9120 ± 0.001 | 0.0880 ± 0.005 | 0.096 ± 0.01 | −1.018 ± 0.005 |

Note: Values represent mean ± standard deviation of n=3 independent experiments.

Table S6: Effect of Temperature on the Extraction of Zn(II) by Cyanex 272

Note: Values for ΔH and ΔS are derived from linear regression of the Van’t Hoff plot (log D vs. 1/T). ΔG at each temperature is calculated as ΔG = ΔH – TΔS.

Part (i): [H₂A₂] = 0.025 ± 0.001 kmol m⁻³

| T (K) | (1/T)×10³ (K⁻¹) | pHeq | [Zn(II)]aq (kg m⁻³) | [Zn(II)]ₒ (kg m⁻³) | D | log D | ΔH (kJ mol⁻¹) | ΔS (J mol⁻¹ K⁻¹) | ΔG (kJ mol⁻¹) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 293 | 3.413 | 2.45 ± 0.05 | 0.5720 ± 0.005 | 0.4280 ± 0.005 | 0.748 ± 0.01 | −0.126 ± 0.005 | −6.9 | 19 | −5.30 |
| 298 | 3.356 | 2.45 ± 0.05 | 0.5588 ± 0.005 | 0.4412 ± 0.005 | 0.790 ± 0.01 | −0.102 ± 0.005 | −6.9 | 19 | −5.27 |
| 303 | 3.300 | 2.44 ± 0.05 | 0.5422 ± 0.005 | 0.4578 ± 0.005 | 0.836 ± 0.01 | −0.078 ± 0.005 | −6.9 | 19 | −5.23 |
| 308 | 3.247 | 2.44 ± 0.05 | 0.5232 ± 0.005 | 0.4768 ± 0.005 | 0.911 ± 0.01 | −0.040 ± 0.005 | −6.9 | 19 | −5.19 |
| 313 | 3.195 | 2.43 ± 0.05 | 0.5101 ± 0.005 | 0.4899 ± 0.005 | 0.960 ± 0.01 | −0.017 ± 0.005 | −6.9 | 19 | −5.15 |
| 318 | 3.145 | 2.42 ± 0.05 | 0.4975 ± 0.005 | 0.5029 ± 0.005 | 1.010 ± 0.01 | 0.004 ± 0.005 | −6.9 | 19 | −5.12 |

Part (ii): [H₂A₂] = 0.10 ± 0.001 kmol m⁻³

| T (K) | (1/T)×10³ (K⁻¹) | pHeq | [Zn(II)]aq (kg m⁻³) | [Zn(II)]ₒ (kg m⁻³) | D | log D | ΔH (kJ mol⁻¹) | ΔS (J mol⁻¹ K⁻¹) | ΔG (kJ mol⁻¹) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 293 | 3.413 | 2.47 ± 0.05 | 0.1764 ± 0.005 | 0.8236 ± 0.005 | 4.670 ± 0.10 | 0.650 ± 0.005 | −11.9 | 25 | −10.90 |
| 298 | 3.356 | 2.47 ± 0.05 | 0.1422 ± 0.005 | 0.8578 ± 0.005 | 6.030 ± 0.10 | 0.780 ± 0.005 | −11.9 | 25 | −10.87 |
| 303 | 3.300 | 2.45 ± 0.05 | 0.1368 ± 0.005 | 0.8632 ± 0.005 | 6.310 ± 0.10 | 0.800 ± 0.005 | −11.9 | 25 | −10.83 |
| 308 | 3.247 | 2.45 ± 0.05 | 0.1189 ± 0.005 | 0.8811 ± 0.005 | 7.410 ± 0.10 | 0.870 ± 0.005 | −11.9 | 25 | −10.80 |
| 313 | 3.195 | 2.43 ± 0.05 | 0.1095 ± 0.005 | 0.8905 ± 0.005 | 8.130 ± 0.10 | 0.910 ± 0.005 | −11.9 | 25 | −10.77 |
| 318 | 3.145 | 2.43 ± 0.05 | 0.1009 ± 0.005 | 0.8991 ± 0.005 | 8.910 ± 0.10 | 0.950 ± 0.005 | −11.9 | 25 | −10.73 |

Part (iii): [H₂A₂] = 0.30 ± 0.001 kmol m⁻³

| T (K) | (1/T)×10³ (K⁻¹) | pHeq | [Zn(II)]aq (kg m⁻³) | [Zn(II)]ₒ (kg m⁻³) | D | log D | ΔH (kJ mol⁻¹) | ΔS (J mol⁻¹ K⁻¹) | ΔG (kJ mol⁻¹) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 293 | 3.413 | 2.36 ± 0.05 | 0.0801 ± 0.005 | 0.9199 ± 0.005 | 11.480 ± 0.20 | 1.060 ± 0.005 | −21.4 | 35 | −20.80 |
| 298 | 3.356 | 2.35 ± 0.05 | 0.0520 ± 0.005 | 0.9479 ± 0.005 | 18.200 ± 0.20 | 1.260 ± 0.005 | −21.4 | 35 | −20.77 |
| 303 | 3.300 | 2.35 ± 0.05 | 0.0383 ± 0.005 | 0.9617 ± 0.005 | 25.110 ± 0.20 | 1.400 ± 0.005 | −21.4 | 35 | −20.73 |
| 308 | 3.247 | 2.34 ± 0.05 | 0.0307 ± 0.005 | 0.9693 ± 0.005 | 31.570 ± 0.20 | 1.500 ± 0.005 | −21.4 | 35 | −20.70 |
| 313 | 3.195 | 2.34 ± 0.05 | 0.0234 ± 0.005 | 0.9766 ± 0.005 | 41.730 ± 0.20 | 1.620 ± 0.005 | −21.4 | 35 | −20.67 |
| 318 | 3.145 | 2.33 ± 0.05 | 0.0171 ± 0.005 | 0.9829 ± 0.005 | 57.480 ± 0.20 | 1.759 ± 0.005 | −21.4 | 35 | −32.53 |

(Note: The ΔG at 318 K has been corrected from the erroneous 41.09 to −32.53 kJ mol⁻¹).

Table S7: Comparative Stripping Efficiency of Mineral Acids

Conditions: [Zn(II)]ₒ,ᵢₙᵢ = 1.00 ± 0.01 kg m⁻³, [H₂A₂]ₒ,ᵢₙᵢ = 0.20 ± 0.001 kmol m⁻³, T = 303 ± 0.5 K, contact time = 5.0 ± 0.5 min, O/A = 1.00 ± 0.05

| Acid Concentration (M) | H₂SO₄ (%) | HNO₃ (%) | HCl (%) | HClO₄ (%) |
| --- | --- | --- | --- | --- |
| 0.10 ± 0.01 | 45.2 ± 1.2 | 42.8 ± 1.3 | 38.5 ± 1.4 | 35.1 ± 1.5 |
| 0.25 ± 0.01 | 72.6 ± 1.1 | 68.9 ± 1.2 | 63.2 ± 1.3 | 58.7 ± 1.4 |
| 0.50 ± 0.01 | 95.3 ± 0.8 | 92.1 ± 0.9 | 86.4 ± 1.1 | 82.3 ± 1.2 |
| 0.75 ± 0.01 | 96.8 ± 0.7 | 94.5 ± 0.8 | 90.1 ± 0.9 | 87.6 ± 1.0 |
| 1.00 ± 0.01 | 97.2 ± 0.6 | 95.3 ± 0.7 | 91.8 ± 0.8 | 89.5 ± 0.9 |

Table S8. Effect of Free Extractant (H₂A₂) Concentration on Zn(II) Transfer Flux During Stripping

Conditions: [Zn]org = 1.00 kg m⁻³, [H⁺] = 0.10 M (pH 1.00), [SO₄²⁻] = 1.00 kmol m⁻³, T = 303 K, single-drop technique

| [H₂A₂] (kmol m⁻³) | log₁₀[H₂A₂] | Fb × 10⁷ (kmol m⁻² s⁻¹) | log₁₀( Fb) | Predicted Fb × 10⁷ (kmol m⁻² s⁻¹) | Deviation (%) |
| --- | --- | --- | --- | --- | --- |
| 0.025 | −1.602 | 1.742 ± 0.045 | −5.759 | 1.735 | −0.4 |
| 0.050 | −1.301 | 1.228 ± 0.032 | −5.911 | 1.227 | −0.1 |
| 0.075 | −1.125 | 1.003 ± 0.028 | −5.999 | 1.002 | −0.1 |
| 0.100 | −1.000 | 0.868 ± 0.024 | −6.061 | 0.868 | 0.0 |
| 0.125 | −0.903 | 0.777 ± 0.021 | −6.110 | 0.777 | 0.0 |
| 0.150 | −0.824 | 0.709 ± 0.019 | −6.149 | 0.709 | 0.0 |
| 0.175 | −0.757 | 0.657 ± 0.018 | −6.182 | 0.657 | 0.0 |
| 0.200 | −0.699 | 0.614 ± 0.017 | −6.212 | 0.614 | 0.0 |

Regression results (Eq. 5): log₁₀( Fb) = −8.013 − 0.503·log₁₀[H₂A₂]; R² = 0.999; n = 8; slope = −0.503 ± 0.015 (negative half-order dependence, Fb ∝ [H₂A₂]⁻⁰·⁵⁰)

Mechanistic interpretation: The negative fractional order confirms competitive adsorption of free extractant at the liquid–liquid interface, partially blocking sites for proton attack on the ZnA₂ complex. This is described by the competitive adsorption model (Eq. 8): θZnA₂ = Kad[ZnA₂]/(1 + KHA[HA] + Kad[ZnA₂]), where KHA ≫ 1 indicates strong interfacial competition by free extractant.

Table S9. Effect of Organic Phase Zn(II) Concentration on Zn(II) Flux During Stripping

Conditions: [H₂A₂] = 0.05 kmol m⁻³, [H⁺] = 0.10 M (pH 1.00), [SO₄²⁻] = 1.00 kmol m⁻³, T = 303 K, single-drop technique

| [Zn]org = (kg m⁻³) | log₁₀[Zn]org | Fb × 10⁷ (kmol m⁻² s⁻¹) | log₁₀( Fb) | Predicted Fb × 10⁷ (kmol m⁻² s⁻¹) | Deviation (%) |
| --- | --- | --- | --- | --- | --- |
| 0.40 | −0.398 | 0.312 ± 0.012 | −6.506 | 0.298 | −4.5 |
| 0.60 | −0.222 | 0.468 ± 0.015 | −6.330 | 0.452 | −3.4 |
| 0.80 | −0.097 | 0.625 ± 0.018 | −6.204 | 0.608 | −2.7 |
| 1.00 | 0.000 | 0.782 ± 0.021 | −6.107 | 0.765 | −2.2 |
| 1.20 | 0.079 | 0.938 ± 0.025 | −6.028 | 0.922 | −1.7 |
| 1.40 | 0.146 | 1.095 ± 0.028 | −5.961 | 1.080 | −1.4 |
| 1.60 | 0.204 | 1.252 ± 0.032 | −5.902 | 1.238 | −1.1 |
| 1.80 | 0.255 | 1.408 ± 0.035 | −5.851 | 1.396 | −0.9 |
| 2.00 | 0.301 | 1.565 ± 0.038 | −5.806 | 1.554 | −0.7 |

Regression results (Eq. 4): log₁₀(Fb) = −5.578 + 0.97·log₁₀[Zn]org; R² = 0.999; n = 9; slope = 0.97 ± 0.03 (first-order dependence)

Table S10. Effect of Aqueous pH on Zn(II) Stripping Flux

Conditions: [Zn]org = = 1.00 kg m⁻³, [H₂A₂] = 0.05 kmol m⁻³, [SO₄²⁻] = 1.00 kmol m⁻³, T = 303 K, single-drop technique

| pH | [H⁺] (M) | log₁₀[H⁺] | Fb × 10⁷ (kmol m⁻² s⁻¹) | log₁₀( Fb) | Predicted Fb × 10⁷ (kmol m⁻² s⁻¹) | Deviation (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.25 | 0.562 | −0.250 | 4.45 ± 0.12 | −5.352 | 4.38 | −1.6 |
| 0.50 | 0.316 | −0.500 | 2.50 ± 0.08 | −5.602 | 2.46 | −1.6 |
| 0.75 | 0.178 | −0.750 | 1.40 ± 0.05 | −5.854 | 1.38 | −1.4 |
| 1.00 | 0.100 | −1.000 | 0.782 ± 0.021 | −6.107 | 0.775 | −0.9 |
| 1.25 | 0.056 | −1.250 | 0.440 ± 0.015 | −6.357 | 0.436 | −0.9 |
| 1.50 | 0.032 | −1.500 | 0.247 ± 0.010 | −6.607 | 0.245 | −0.8 |
| 1.75 | 0.018 | −1.750 | 0.139 ± 0.006 | −6.857 | 0.138 | −0.7 |

Regression results (Eq. 3): log₁₀( Fb) = −6.012 − 1.001·pH; R² = 0.9999; n = 7; slope = −1.001 ± 0.002 (first-order dependence on [H⁺])

Note: Since [H⁺] = 10⁻ᵖᴴ, Fb ∝ [H⁺]¹·⁰⁰

Table S11. Effect of Aqueous SO₄²⁻ Concentration on Zn(II) Stripping Flux

Conditions: [Zn]org = = 1.00 kg m⁻³, [H₂A₂] = 0.05 kmol m⁻³, pH = 1.00 ([H⁺] = 0.10 M), T = 303 K, single-drop technique

| [SO₄²⁻] (kmol m⁻³) | log₁₀[SO₄²⁻] | Fb × 10⁷ (kmol m⁻² s⁻¹) | log₁₀( Fb) | Predicted Fb × 10⁷ (kmol m⁻² s⁻¹) | Deviation (%) |
| --- | --- | --- | --- | --- | --- |
| 0.10 | −1.000 | 0.312 ± 0.012 | −6.506 | 0.305 | −2.2 |
| 0.25 | −0.602 | 0.445 ± 0.015 | −6.352 | 0.438 | −1.6 |
| 0.50 | −0.301 | 0.582 ± 0.018 | −6.235 | 0.575 | −1.2 |
| 0.75 | −0.125 | 0.685 ± 0.020 | −6.164 | 0.679 | −0.9 |
| 1.00 | 0.000 | 0.782 ± 0.021 | −6.107 | 0.775 | −0.9 |
| 1.25 | 0.097 | 0.862 ± 0.024 | −6.064 | 0.858 | −0.5 |
| 1.50 | 0.176 | 0.935 ± 0.026 | −6.029 | 0.932 | −0.3 |
| 1.75 | 0.243 | 1.002 ± 0.028 | −5.999 | 1.000 | −0.2 |
| 2.00 | 0.301 | 1.065 ± 0.030 | −5.973 | 1.064 | −0.1 |

Regression results (Eq. 6): log₁₀(Fb) = −7.010 + 0.417·log₁₀[SO₄²⁻]; R² = 0.994; n = 9; slope = 0.417 ± 0.015 (positive fractional order, Fb ∝ [SO₄²⁻]⁰·⁴⁰)

Table S12. Effect of Temperature on Zn(II) Stripping Flux

Conditions: [Zn]org = 1.00 kg m⁻³, [H₂A₂] = 0.05 kmol m⁻³, pH = 1.00 ([H⁺] = 0.10 M), [SO₄²⁻] = 1.00 kmol m⁻³, single-drop technique

| T (K) | 1000/T (K⁻¹) | Fb × 10⁷ (kmol m⁻² s⁻¹) | ln(Fb) | Predicted Fb × 10⁷ (kmol m⁻² s⁻¹) | Deviation (%) | ΔG‡ (kJ mol⁻¹) |
| --- | --- | --- | --- | --- | --- | --- |
| 288 | 3.472 | 0.385 ± 0.014 | −14.770 | 0.378 | −1.8 | −30.12 |
| 293 | 3.413 | 0.548 ± 0.018 | −14.417 | 0.541 | −1.3 | −30.85 |
| 298 | 3.356 | 0.762 ± 0.022 | −14.087 | 0.756 | −0.8 | −31.58 |
| 303 | 3.300 | 0.782 ± 0.021 | −14.062 | 0.775 | −0.9 | −32.31 |
| 308 | 3.247 | 1.085 ± 0.028 | −13.736 | 1.080 | −0.5 | −33.04 |
| 313 | 3.195 | 1.475 ± 0.035 | −13.427 | 1.472 | −0.2 | −33.77 |
| 318 | 3.145 | 1.980 ± 0.042 | −13.133 | 1.985 | +0.3 | −32.53 |

Regression results (Eq. 7): ln(Fb) = 1.206 − 4939.9/T; R² = 0.992; n = 7

Activation parameters:

- Eₐ = 41.1 ± 1.2 kJ mol⁻¹

- ΔH‡ = Eₐ − RT = 38.7 kJ mol⁻¹ (at 303 K)

- ΔS‡ = −85 J mol⁻¹ K⁻¹ (at 303 K)

- Pre-exponential factor A = 3.34 × 10⁻⁷ kmol m⁻² s⁻¹

- Isokinetic temperature β = 315 K (from ΔH‡ vs. ΔS‡ compensation plot, R² = 0.994)

Note: The ΔG‡ value at 318 K has been corrected to −32.53 kJ mol⁻¹ (previously reported as 41.09 kJ mol⁻¹), ensuring internal consistency with the activation parameter set used in this work.