Enrichment of Luminescence via Incorporation of Fluxes in La2Zr2O7:Tb3+ Nanophosphors: One Material, Many Possibilities-Latent Fingerprint Visualization, Anti-counterfeiting, Luminescent Flexible Films

D.R. Lavanya1, G.P. Darshan2, *, J. Malleshappa1, H.B. Premkumar2, S.C. Sharma3, S.A. Hariprasad4, H. Nagabhushana5, #

1Department of Physics, University College of Science, Tumkur University,

Tumkur 572 103, India

2Department of Physics, FMPS, M. S. Ramaiah University of Applied Sciences, Bengaluru 560 054, India

3Honarory Professor, Jain Deemed to be University, Bengaluru 562 112, India

4Department of Electronics and Communication, Faculty of Engineering and Technology, Jain Global Campus, Bengaluru 562 112, India

5Prof. C.N.R. Rao Centre for Advanced Materials, Tumkur University,

Tumkur 572 103, India

Corresponding Authors: G.P. Darshan (Email Id.: darshubavimane@gmail.com) and

H. Nagabhushana (bhushanvlc@gmail.com).

Figure S1 (a) Schematic illustration showing the followed synthesis procedure of the LZO:Tb3+ (7 mol %) NPs by solution combustion route; (b) Graphic view of the LFPs development and visualization protocol adopted in the present work; (c) Schematic representation of the data encryption and decoding procedure developed by screen printing technique using prepared NPs as a security ink.

Figure S2. DR spectra of the prepared (a) LZO:Tb3+ (1-9 mol %) NPs; (b)LZOT: NH4Cl, NH4F, NaBr (1 wt. %) NPs and LZOT: NH4Cl (4 wt. %) NPs.

Figure S3 (a-f) SEM micrographs of LZO:Tb3+ (1-9 mol %) NPs prepared by solution combustion route using urea as a fuel; SEM micrographs of various fluxes (g) NaBr (1 wt. %), (h) NH4F (1 wt. %), (i) NH4Cl (1 wt. %) conjugated LZOT NPs; TEM images of the (j) LZOT NPs, (k) LZOT: NH4Cl (4 wt. %) NPs; (l) HRTEM image of the LZOT: NH4Cl (4 wt. %) NPs and its enlarged portion, which representing the interplanar lattice spacing of (222) plane (Inset: SAED pattern of the optimized NPs).

Figure S4. Schematic illustration for the energy level diagram of Tb3+ ions in the LZO lattice.

Figure S5. Visualized FPs developed on the glass surface under UV 254 nm light illumination and revealing various well-defined ridge details.

Figure S6. AC label on the foam irradiated with UV 254 nm light with different time periods (a) 0 h; (b) 2 h; (c) 3 h; (d) 4 h; (f) 5 h.

Figure S7. AC label on the ceramic tile maintained at various temperatures (a) 32 °C; (b) 40 °C; (c) 50 °C; (d) 60 °C; (f) 70 °C.

Figure S8. Developed AC label using fabricated security ink on the aluminium foil stirred ultrasonically at 30 kHz at different time periods (a) without treatment; (b) 10 min; (c) 20 min; (d) 30 min; (e) 40 min; (f) 50 min.

Table S1: The estimated average crystallite size of the prepared Tb3+ doped LZO NPs.

| Tb3+ Conc. (mol %) | Crystallite size (nm) |  | Strain (ε x 10-3) | Energy band gap (Eg in eV) |
| --- | --- | --- | --- | --- |
|  | Scherrer’s relation | W-H plot |  |  |
| LZO | 7.19 | 8.11 | 4.82 | 3.505 |
| 1 | 7.51 | 9.36 | 4.62 | 3.492 |
| 3 | 6.94 | 9.92 | 5.01 | 3.488 |
| 5 | 7.48 | 8.17 | 4.63 | 3.484 |
| 7 | 7.09 | 7.40 | 4.89 | 3.480 |
| 9 | 7.69 | 8.14 | 4.52 | 3.478 |
| LZOT NPs |  |  |  |  |
| NH4F (1 wt. %) | 7.94 | 11.51 | 5.24 | 3.483 |
| NaBr (1 wt. %) | 7.53 | 8.04 | 5.61 | 3.477 |
| NH4Cl (1 wt. %) | 7.52 | 7.83 | 4.75 | 3.477 |
| NH4Cl (2 wt. %) | 7.85 | 8.93 | 4.67 | 3.476 |
| NH4Cl (3 wt. %) | 7.44 | 9.27 | 4.88 | 3.476 |
| NH4Cl (4 wt. %) | 7.97 | 8.71 | 4.94 | 3.475 |
| NH4Cl (5 wt. %) | 6.64 | 8.73 | 5.14 | 3.473 |

Table S2: Photometric properties (CIE, CCT and CP) of the LZO:Tb3+ (1-9 mol %) NPs.

| Tb3+ Conc. (mol %) | CIE values |  | CCT (K) | CP (%) |
| --- | --- | --- | --- | --- |
|  | X | Y |  |  |
| 1 | 0.3471 | 0.5262 | 5219 | 71 |
| 3 | 0.3415 | 0.5747 | 5351 | 89 |
| 5 | 0.3421 | 0.5686 | 5338 | 87 |
| 7 | 0.3418 | 0.5612 | 5339 | 84 |
| 9 | 0.3251 | 0.5424 | 5649 | 77 |
| LZOT NPs |  |  |  |  |
| NH4F (1 wt. %) | 0.3231 | 0.6088 | 5662 | 81 |
| NaBr (1 wt. %) | 0.3236 | 0.6084 | 5654 | 80 |
| NH4Cl (1 wt. %) | 0.2587 | 0.5658 | 6970 | 90 |
| NH4Cl (2 wt. %) | 0.2793 | 0.5775 | 6500 | 92 |
| NH4Cl (3 wt. %) | 0.2704 | 0.5866 | 6652 | 96 |
| NH4Cl (4 wt. %) | 0.2549 | 0.5835 | 6979 | 97 |
| NH4Cl (5 wt. %) | 0.2633 | 0.5812 | 6488 | 95 |

Table S3: Previous literature of photometric properties of Tb3+ ions doped various hosts.

| Sample | CIE |  | CCT (K) | CP (%) | QE (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
|  | X | Y |  |  |  |  |
| TiO2 | 0.35 | 0.48 | --- | 73 | --- | Zikriya et al. [80] |
| Y2O3 | 0.32 | 0.53 | --- | --- | --- | Yadav et al. [81] |
| LiBaB9O15 | 0.31 | 0.62 | --- | --- | --- | Singh et al. [82] |
| GdAlO3 | 0.319 | 0.597 | 4624 | --- | --- | Jisha et al. [83] |
| BaLu2Si3O10 | 0.155 | 0.083 | --- | --- | 72 | Li et al. [84] |
| LaAlGe2O7 | 0.204 | 0.434 | --- | 92 | --- | Ding et al. [85] |
| Y3Al5O12 | 0.396 | 0.552 | --- | --- | --- | Xing et al. [86] |
| Ca9LiMn(PO4)7 | 0.368 | 0.350 | 4196 | 90 | 51 | Zhang et al. [87] |
| CaWO4 | 0.299 | 0.449 | 6721 | --- | --- | Neto et al. [88] |
| CdSiO3 | 0.384 | 0.511 | 4513 | 84 | 80 | Basavaraj et al. [89] |
| WO3 | 0.304 | 0.444 | 4835 | --- | --- | Kavitha et al. [90] |
| La2Hf2O7 | 0.357 | 0.475 | 4930 | --- | --- | Gupta et al. [91] |
| Bi2O3 | 0.287 | 0.419 | 7393 | --- | 91 | Ashwini et al. [92] |
| Sr3B2O | 0.25 | 0.68 | 6753 | --- | --- | Khursheed et al. [93] |
| Na3Y(PO4)2 | 0.221 | 0.360 | --- | --- | 94 | Dahiya et al. [94] |
| Y3Al5O12 | 0.172 | 0.556 | --- | --- | --- | Singh et al. [95] |
| NaBiF4 | 0.328 | 0.580 | --- | 62.4 | --- | Du et al. [96] |
| YBO3 | 0.290 | 0.442 | --- | --- | --- | Srivastava et al. [97] |
| LaGaO3 | 0.26 | 0.38 | --- | --- | 69 | Samuel et al. [98] |
| La2Zr2O7 | 0.2549 | 0.5835 | 6979 | 97 | --- | Present work |