Supplementary Information

Molecular origin of the extreme mechanical strength of an ester bond containing pathogen surface protein

Lei et al.

Supplementary Information

Molecular origin of the extreme mechanical strength of an ester bond containing pathogen surface protein

Hai Lei1,2#, Quan Ma1#, Wenfei Li1#, Jing Wen3, Haibo Ma3, Meng Qin1, Wei Wang1 and Yi Cao1,2*

1Collaborative Innovation Center of Advanced Microstructures, National Laboratory of Solid State Microstructure, Department of Physics, Nanjing University, Nanjing, China 210093

2Chemistry and Biomedicine innovation center, Nanjing University, Nanjing, China 210093

3Key Laboratory of Mesoscopic Chemistry of MOE, School of Chemistry and Chemical Engineering, Institute of Theoretical and Computational Chemistry, Nanjing University, Nanjing, China 210023

#equal contribution.

*E-mail: caoyi@nju.edu.cn

Supplementary Figures

Supplementary Figure 1. Single molecule force spectroscopy experiments on the C1WT containing polyprotein, Spytag-(GB1-C1WT)4-cys, using the Sypcatcher/Spytag chemistry. a, Schematic of the single molecular force spectroscopy experiment. b, Typical force-distance traces. Worm-like chain (black) was used to fit the saw-tooth peaks. The last peak may be due to the rupture of the maleimide-thiol adduct for surface covalent linking. c, Unfolding force distribution of the fingerprint maker GB1 proteins. Gaussian fitting shows the average unfolding force of 205.68 ± 45.47 pN. (mean ± S.D.) d, The detaching forces of the polyprotein either from the substrate or the cantilever shows an average force of 1167.9 ± 473.5 pN. (mean ± S.D.)

Supplementary Figure 2. Mutual interplay between the ester bond and the local structure of its surrounding residues under pulling forces. a, Cartoon representation of the native structure of the C1WT. The residues immediately surrounding the ester bond (including K10, T12, H133, D138, and A140) were shown by sphere representation. These residues form a barrel-like structure preventing the water molecules from attacking the ester bond. The two residues forming the ester bond (T11 and N141) were shown by stick representation. b, Distributions of the rmsd of the local structure surrounding the ester bond (involving the residues K10, T12, H133, D138, A140, T11, and N141) compared to that in the native structure for the C1WT and C1CP under different pulling forces. c, Representative MD trajectories showing the number of accessible water molecules to the ester bond (NW) as a function of time for the simulations with the covalent-bonding interactions arising from the ester bond deleted (non-bond) at different pulling forces. For comparison, the result with the ester bond formed (bond) at the pulling force of 1.5 nN was also shown. d-e, Same as (c) but showing the distance between the two Cα atoms of the ester bond forming residues (d) and the rmsd of the local structure surrounding the ester bond (e) as a function of time.

Supplementary Figure 3. Mechanical unfolding of ParV and its mutant (mParv). a, Sequence alignment of C1 from C. perfringens and ParV from Parvinmonas sp.. In both proteins, the ester forming residues Thr (Cyan) and Gln (Red) are conserved. b, Predicted structure of ParV, which is similar to the C1 structure. c, Representative force-extension curves of pulling Fg-(ParV-GB1)2-cys by a SdrG-cys modified cantilever. Force-extension curves only display two unfolding events which are attributed to the unfolding of GB1. d, Representative force-extension curves of pulling Fg-(mParV-GB1)2-cys by a SdrG-cys modified cantilever. The two peaks (colored in green) with ΔLc of 46 nm correspond to the unfolding of mParV domains; the next two peaks (colored in blue) correspond to the unfolding of GB1; and the last peak correspond to the rupture of the Fg/SdrG complex.

Supplementary methods

The sequence of individual protein domains/tags

Fgβ

NEEGFFSARGHRPLD

Spytag

AHIVMVDAYKPTK

GB1 (PDB 3MP9)

MDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTE

C1WT domain of Cpe0147 (PDB:4MKM & 4NI6)

MPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVE

Parv (EGV09726 Cna B-type domain protein from Parvimonas sp.)

GEIKTTVMAGGKTSTENEVATLKAKDIEGGVEVSDKITYKGLYPNEKYDVIGKIYEVKDGELVNPGHPVSVVNSGDDLKADTTGKGEWTLNFGKLNLEAGKSYVVFETVVSMENVIDTDGDGKPDKKQELTHEDPNDKSQTFRI

Full polyprotein construct sequences

All constructs were cloned into pET22B or pQE80L vectors containing a 6×HIS (HHHHHH) tag for purification.

SdrG-Cys-6×HIS (PDB:1R17)

MKLGSEQGSNVNHLIKVTDQSITEGYDDSDGIIKAHDAENLIYDVTFEVDDKVKSGDTMTVNIDKNTVPSDLTDSFAIPKIKDNSGEIIATGTYDNTNKQITYTFTDYVDKYENIKAHLKLTSYIDKSKVPNNNTKLDVEYKTALSSVNKTITVEYQKPNENRTANLQSMFTNIDTKNHTVEQTIYINPLRYSAKETNVNISGNGDEGSTIIDDSTIIKVYKVGDNQNLPDSNRIYDYSEYEDVTNDDYAQLGNNNDVNINFGNIDSPYIIKVISKYDPNKDDYTTIQQTVTMQTTINEYTGEFRTASYDNTIAFSTSSGQGQGDLPPEKTRSCGTEFAAALEHHHHHH

6×HIS-Cys-SpyCatcher (PDB:4MLI)

MRGSHHHHHHGSCMVDTLSGLSSEQGQSGDMTIEEDSATHIKFSKRDEDGKELAGATMELRDSSGKTISTWISDGQVKDFYLYPGKYTFVETAAPDGYEVATAITFTVNEQGQVTVNGKATKGDAHIDRS

Fgβ-linker-(GB1)2-C1WT-(GB1)2-Cys-6×HIS

MKLGSNEEGFFSARGHRPLDGSGSGSGSAGTGSGRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVERSDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSCGTEFAAALEHHHHHH

6×HIS-Spytag-(GB1-C1WT)4-Cys

MRGSHHHHHHGSAHIVMVDAYKPTKRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVERSC

Fgβ-linker-(GB1)2-C1T11A-(GB1)2-Cys-6×HIS

MKLGSNEEGFFSARGHRPLDGSGSGSGSAGTGSGRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKATVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKAQTLIVERSDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSCGTEFAAALEHHHHHH

Fgβ-linker-(GB1)2-C1CP-(GB1)2-Cys-6×HIS

MKLGSNEEGFFSARGHRPLDGSGSGSGSAGTGSGRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSDTKQVVKHEDKNDKAQTLIVEVPGVGVPGVGVPGEGVPGVGVPGVGVPGVGVPGVGVPGEGVPGVGVPGGLMPEVKEGTLKTTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELRSDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSCGTEFAAALEHHHHHH

Fgβ-linker-(GB1)2-C1-df-(GB1)2-Spytag-6×HIS

MKLGSNEEGFFSARGHRPLDGSGSGSGSAGTGSGRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMPEVKEGTLKCTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELDTKQVVKHEDKNDKACTLIVERSDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSAHIVMVDAYKPTKRSGTEFAAALEHHHHHH

Fgβ-linker-(GB1)2-C1CP-df-(GB1)2- Spytag -6×HIS

MKLGSNEEGFFSARGHRPLDGSGSGSGSAGTGSGRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSDTKQVVKHEDKNDKACTLIVEVPGVGVPGVGVPGEGVPGVGVPGVGVPGVGVPGVGVPGEGVPGVGVPGGLMPEVKEGTLKCTVAADGVNGSSEKEALVSFENSKDGVDVKDTIDYKDLVANEKYNLTGKLMHVKDDGSLEEVATKTTEVTAVENGSGQWELDFGNQKLQVGEKYVVFENAESVENLIDTDNNYELRSDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSAHIVMVDAYKPTKRSGTEFAAALEHHHHHH

6×HIS-Spytag-(GB1-Parv)2-Cys

MRGSHHHHHHGSAHIVMVDAYKPTKRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSGEIKTTVMAGGKTSTENEVATLKAKDIEGGVEVSDKITYKGLYPNEKYDVIGKIYEVKDGELVNPGHPVSVVNSGDDLKADTTGKGEWTLNFGKLNLEAGKSYVVFETVVSMENVIDTDGDGKPDKKQELTHEDPNDKSQTFRIRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSGEIKTTVMAGGKTSTENEVATLKAKDIEGGVEVSDKITYKGLYPNEKYDVIGKIYEVKDGELVNPGHPVSVVNSGDDLKADTTGKGEWTLNFGKLNLEAGKSYVVFETVVSMENVIDTDGDGKPDKKQELTHEDPNDKSQTFRIRSC

Fgβ-linker- (GB1-mParv)2-Cys-6×HIS

MKLGSNEEGFFSARGHRPLDGSGSGSGSAGTGSGRSMDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSGEIKATVMAGGKTSTENEVATLKAKDIEGGVEVSDKITYKGLYPNEKYDVIGKIYEVKDGELVNPGHPVSVVNSGDDLKADTTGKGEWTLNFGKLNLEAGKSYVVFETVVSMENVIDTDGDGKPDKKQELTHEDPNDKSQTFRIRSDTYKLILNGKTLKGETTTEAVDAATAEKVFKQYANDNGVDGEWTYDDATKTFTVTERSGEIKATVMAGGKTSTENEVATLKAKDIEGGVEVSDKITYKGLYPNEKYDVIGKIYEVKDGELVNPGHPVSVVNSGDDLKADTTGKGEWTLNFGKLNLEAGKSYVVFETVVSMENVIDTDGDGKPDKKQELTHEDPNDKSQTFRIRSCGTEFAAALEHHHHHH