Electronic supplementary material for article: “Insigths of sphalerite weathering under simulated acidic, circumneutral and alkaline conditions to account for mineral activity and potential Zn release”

Fabiola S. Sosa-Rodrígueza, Jorge Vázquez-Arenasb, Patricia Ponce-Peñac, Antonio Aragón-Piñad, Martine Mallete, Gabriel Trejo-Córdovaf, Diola M. Núñez-Ramírezc, Miguel A. Escobedo-Bretadoc, René H. Larac, *

a Research Area of Growth and Environment, Metropolitan Autonomous University (UAM), Azcapotzalco, Av. San Pablo 180, Mexico City, 02200, Mexico.

b Conacyt-Departament of Chemistry, Metropolitan Autonomous University (UAM), Iztapalapa, Av. San Rafael Atlixco No 186, 09340, Mexico City, Mexico.

c Department of Materials Science, Faculty of Chemical Sciences, Universidad Juárez del Estado de Durango (UJED), Av. Veterinaria S/N, Circuito Universitario, 34120, Durango, DGO, Mexico.

d Institute of Metallurgy, Autonomous University of San Luis Potosí (UASLP), Av. Sierra Leona 550, Lomas 2da, 78210, San Luis Potosi, SLP, Mexico.

e Université de Lorraine, CNRS, LCPME, F-54000 Nancy, France.

f Centro de Investigación y Desarrollo Tecnológico en Electroquímica (CIDETEQ), Parque Tecnológico Sanfandila, Querétaro, 76703, Mexico.

Fig. S1. Massive mineral specimens: (a) low-Fe bearing and Pb-bearing sphalerite sample (i.e., PbS-ZnS crystal); (b) marmatite-like sample (i.e., FeZnS crystal); (c) and (d) 2D SEM images for the PbS-ZnS sample (<106 m). Carbon paste electrodes (CPE) were constructed using these mineral samples. Solid phases identification was carried out under EDS basis (n= 10 analyses).

Fig. S2. Teflon-coated stainless steel electrode system with hole to be loaded with carbon paste containing the PbS-ZnS and/or FeZnS grain samples (50 wt. %, <106 m).

Table S1. Summary of Raman transitions in terms of sulfur, zinc and lead species used to identify main secondary compounds on altered sphalerite samples (vi, indicates the transition order).

| Chemical compound | Raman peak position, cm-1 | References |
| --- | --- | --- |
| Polysulfides (Sn2-) | from 443 to 475, main at 470 (v1) | Mycroft et al. 1990 This study |
| Elemental sulfur (S0) | 155 (v3), 220 (v2), 470 (v1) | Karimi et al., 2017 Mycroft et al. 1990 Ward, 1968 |
| Sphalerite (FeZnS) | 180 (v2), 220 (v2), 298 (v1), 330 (v1), 349 (v1) | Karimi et al., 2017 Kharbish, 2007 Osadchii and Gorbaty, 2010 Buzatu et al. 2013 This study |
| Galena (PbS) | Not any active peak due to cubic structure | Shapter et al. 2000 |
| Anglesite (PbSO4) | 968 (v2), 1054 (v1) | Shapter et al. 2000 Batonneau et al. 2000 This study |
| Zinc sulfate (ZnSO4) | 982 (v1) | Hayes et al. 1984 |

Table S2. Summary of XPS (S2p3/2 and Zn2p3/2) binding energy (BE) positions of chemical species for pristine and leached surfaces of sphalerite.

| Chemical species | Binding energy (BE) |  |  | Reference |
| --- | --- | --- | --- | --- |
| Sphalerite (monosulfide, S2-) Disulphide (S22-) | ~161.2 to ~161.6 ~162.2 |  | Harmer et al., 2008 Fornassiero et al. 2006 Buckley and Woods, 1989 Mikhlin et al., 2016 Harmer et al., 2008 Schaufuβ et al. 1998 Pratt et al. 1994, 1998 Mikhlin et al. 2000 |  |  |
| Polysulfides (Sn2-) Elemental sulfur (S0) Undetermined sulfoxyspecies (SOx2-) to SO32- Sulfate (SO42-) Zn(II)-S2- | ~162.5 to 163.3 ~163.3 to 164.6 ~163.5 to 164.3 ~168.5 1021.2 to ~1022.1 |  | Mycroft et al. 1990 Sandström et al. 2005 Mikhlin et al., 2016 Fornassiero et al., 2006 Mikhlin et al. 1998, 2000 Mycroft et al. 1990 Eggleston et al. 1996 Buckley and Woods, 1989 Tonniazo et al. 1999 Nesbitt et al. 1998a,b Mycroft et al. 1990 Eggleston et al. 1996 Nesbitt et al. 1995, 1998a Schaufuβ et al. 1998 Tonniazo et al. 1999 Mullet et al. 2007 Buckley and Woods 1987 Nesbitt and Muir 1994 Tonniazo et al. 1999 Mullet et al. 2007 Nowak and Laahajaleto 2000 Fornassiero et al., 2006 Thomas et al. 2003 Nowak and Laajalehto 2000 Richardson and Vaughan 1989 Nesbitt et al. 1995 Nesbitt and Muir 1998 Fornassiero et a., 2006 Harmer et al., 2008 Buckley and Woods, 1989 Mikhlin et al., 2016 |  |  |

Fig. S3. 3D SEM images of pristine (a) and leached sphalerite (i.e., PbS-ZnS) samples obtained from simulated leaching devices in 0.1 M NaNO3 (b), 0.1 M HClO4 (c) and 0.1 M H2SO4 (d) conditions. Secondary phases identification was carried out under EDS basis (data, n= 10) where it was indicated the analyzed points in Figure. ZnS= sphalerite.

Fig. S4. Raman spectrum obtained on altered free-galena particle in 0.1 M H2SO4 solution from the PbS-ZnS weathering system. Raman peaks corresponded to anglesite (i.e., PbSO4)-like compound. Galena has no known Raman peaks according to specific crystalline structure.

Fig. S5. XPS S2p (a) and Pb4d (b) high-resolution spectra obtained from leached PbS-ZnS samples after 240 h in 0.1 M H2SO4 solution. Quiescent and ambient conditions.

Fig. S6. Cyclic voltammograms initiated into the positive scans (i, black curves) and negative scans (ii, red curves) direction using CPE-marmatite-like sample (50 wt. %) under different simulated weathering conditions. 5 mV· s-1. Ambient conditions. Quiescent systems. The inert response of the CPE without mineral species (100 % graphite) was included for comparison purposes (iii, gray curve).

Fig. S7. Cyclic voltammograms (positive scans) using CPE-marmatite-like sample (50  wt. %) under different simulated conditions. Scan rate= 5 mV· s-1. Ambient conditions. Quiescent system.

Fig. S8. Potential vs Current curves obtained from Chronopotentiometric (CP) experiments using the CPE-PbS-ZnS sample (50 wt. %) and CPE-FeZnS sample (50 wt. %) under different simulated weathering conditions. Selected time was 600 s. Current pulses were applied based on Cyclic voltammetry. Ambient conditions. Quiescent systems.

Fig. S9. Current vs Potential curves obtained from Chronoamperometric (CA) experiments using CPE-FeZnS sample (50 wt. %) under different simulated weathering conditions. Potential pulses were applied based on Cyclic voltammetry results. Ambient and quiescent conditions.

Fig. S10. Current vs Potential curves obtained from Chronoamperometric (CA) experiments using CPE-PbS-ZnS sample (50 wt. %) under different simulated weathering conditions. Potential pulses were applied based on Cyclic voltammetry. Ambient and quiescent conditions.

Fig. S11. Comparison of Tafel plots obtained using CPE-PbS-ZnS sample (50 wt. %) under different simulated weathering conditions. 1 mV· s-1. Ambient conditions. Stirring conditions= 300 rpm.

Fig. S12. Comparison of Tafel plots obtained using CPE-FeZnS sample (50 wt. %) under different simulated weathering conditions. 1 mV· s-1. Ambient conditions. Stirring conditions= 300 rpm.

The Buttler-Volmer equation was utilized to elucidate Tafel parameters under the following general procedure (an example is given in Fig. S15, see below):

Anodic branch

I= nFkf*CRbexpαAnFRTE       αA=1-αC  (1)

i0, exchange current

η, overpotential

αA, B, transfer charge coefficient anodic(A) or cathodic (B)

n, transfered electron number for the limitant step

log⁡(I)= log⁡(nFkf*CRbexpαAnFRTE)       αA=1-αC

log(a*b)=log(a)+log(b)

logI=lognFkf*CRb+2.303αAnFRTE

Catodic branch

I=-nFkb*CObexp-αCnFRTE

log⁡(I)= log⁡(-nFkb*CObexp-αCnFRTE)

log(a*b)=log(a)+log(b)

logI=log-nFkb*COb+-2.303αCnFRTE

Recall that the definition of the exchange current (i0) is the current when one is located at the equilibrium potential (Eeq), and the oxidation and reduction currents are the same:

i0=nFkf*CRbexpαAnFRTEeq=-nFkb*CObexp-αCnFRTEeq (2)

CRb, bulk concentration of reduced species

COb, bulk concentration of oxidized species

kf, rate constant for oxidation

kb, rate constant for reduction

The definition of the overpotential is known:

η=E-Eeq    (3)

If (2) is substituted in (1) to avoid dealing with overpotentials and simultaneously definition of overpotential in eq. (3), remains of the following shape:

I= nFkf*CRbexpαAnFRTE-nFkb*CObexp-αCnFRTE            (4)

Particular assumptions for the PbS-ZnS and FeZnS samples analysis (Eqs. 1 to 4):

- The difference E-Eeq is minor for E beyond equilibrium; accordingly, catodic branch is easily omitted from Tafel analysis.

I≈-nFkb*CObexp-αCnFRTE            (5)

- Aforementioned processes are kinetically controlled, whereby the following approach can be drawn for practical purposes:

I≈-nFk'b*COsexp-αCnFRTE            (6)

Fig. S13. General procedure for obtaining Tafel parameters. Scan rate of 1 mV· s-1. Ambient conditions. Stirring conditions= 300 rpm. The Tafel plot was acquired for the CPE-inert system in this figure.

From the Figure 8:

CPE-Marmatite-like in 0.1 M H2SO4 conditions:

2.303αAnFRT=3.5912          lognFkf*CRb=-3.6689, whereby

αA=0.04 for n=1             kf*CRb=2.22x10-09 mol/s →  cm3s*molcm3

Ecorr=0.07 V

CPE-ZnS-PbS in 0.1 M H2SO4 conditions:

αA=0.12 for n=1             kf*CRb=4.97x10-10 mol/s →  cm3s*molcm3

Ecorr=0.13 V

CPE-Marmatite-like in 0.1 M NaOH conditions:

αA=0.04 for n=1             kf*CRb=3.14x10-8 mol/s →  cm3s*molcm3

Ecorr=-0.164 V

CPE-ZnS-PbS in 0.1 M NaOH conditions:

αA=0.05 for n=1             kf*CRb=1.07x10-7 mol/s →  cm3s*molcm3

Ecorr=-0.165 V

CPE-Marmatite-like in 0.1 M NaNO3 conditions:

αA=0.02 for n=1             kf*CRb=1.19x10-9 mol/s →  cm3s*molcm3

Ecorr=0.11 V

CPE-ZnS-PbS in 0.1 M NaNO3 conditions:

αA=0.05 for n=1             kf*CRb=4.15x10-10 mol/s →  cm3s*molcm3

Ecorr=0.1 V

CPE-Marmatite-like in 0.1 M HClO4 conditions:

αA=0.02 for n=1             kf*CRb=2.11x10-9 mol/s →  cm3s*molcm3

Ecorr=0.07 V

CPE-ZnS-PbS in 0.1 M HClO4 conditions:

αA=0.05 for n=1             kf*CRb=4.02x10-10 mol/s →  cm3s*molcm3

Ecorr=0.05 V

Fig. S14. Pourbaix diagram of the Zn-S-H2O system.