Supporting information

A recycling alternative for expanded polystyrene residues using natural esters

Luisa V. García-Barreraa,b, Dafne L. Ortega-Solísb, Gabriela Soriano-Gilesb, Nazario Lópezc, Fernando Romero-Romeroa,b, Eric Reinheminerdd, Victor Varela-Guerreroa,b*, María F. Ballesteros-Rivasa,b*

a Universidad Autónoma del Estado de México. Facultad de Química. Paseo Colón esq. Paseo Tollocan s/n, 50120, Toluca, México, CP 50120, México

b Centro Conjunto de Investigación en Química Sustentable UAEM-UNAM, Carretera Toluca-Atlacomulco km 14.5, 50200, Mexico

c Centro de Investigaciones Químicas, IICBA, Universidad Autónoma del Estado de Morelos, Av. Universidad 1001, Col. Chamilpa, Cuernavaca, Morelos 62209, Mexico

dRigaku Americas Corporation. 9009 New Trails Drive. The Woodlands, TX 77381. USA

*Corresponding authors at: Centro Conjunto de Investigación en Química Sustentable UAEM-UNAM, Carretera Toluca-Atlacomulco km 14.5, 50200, Mexico.

E-mail addresses: vvarelag@uaemex.mx (V. Varela-Guerrero), mfballesterosr@uaemex.mx (M.F. Ballesteros-Rivas).

Contents

Table S1. Time required to dissolve WEP

Table S2. Main bands of the esters

Table S3. Characteristic bands of WEP compared to WEP recovered from esters

Fig.S1. Infrared spectroscopy of omega-3

Fig.S2. Infrared spectroscopy of glyceryl tributyrate

Fig.S3. Infrared spectroscopy of ethyl butyrate

Fig.S4. FTIR of esters: (a) omega-3, (b) glyceryl tributyrate and (c) ethyl butyrate

Fig.S5. Differential Scanning Calorimetry of untreated WEP

Fig.S6. Differential Scanning Calorimetry at 50% WEP solution using omega-3

Fig.S7. Differential Scanning Calorimetry at 50% WEP solution using glyceryl tributyrate

Fig.S8. Differential Scanning Calorimetry at 50% WEP solution using ethyl butyrate

Fig.S9. Thermogravimetric analysis of untreated WEP

Fig.S10. Thermogravimetric analysis at a 50% solution of WEP using omega-3

Fig.S11. Thermogravimetric Analysis at 50% WEP solution using glyceryl tributyrate

Fig.S12. Thermogravimetric analysis at a 50% solution of WEP using ethyl butyrate

Fig.S13. Degree of advance α for the calculation of the activation energy of the WEP without treatment using the Friedman model with heating rate β = 20°C/min (293.15 K / min)

Fig.S14. Linear regression for the calculation of the activation energy of the WEP without treatment using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S15. Degree of advancement α for the calculation of the activation energy of the WEP recovered with omega-3 using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S16. Linear regression for the calculation of the activation energy of the WEP recovered with omega-3 using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S17. Degree of advancement α for the calculation of the activation energy of the WEP recovered with glyceryl tributyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S18. Linear regression for the calculation of the activation energy of the WEP recovered with glyceryl tributyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S19. Degree of advancement α for the calculation of the activation energy of the WEP recovered with ethyl butyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S20. Linear regression for the calculation of the activation energy of the WEP recovered with ethyl butyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S21. Scanning electron micrograph of untreated WEP (a) outer layer (b) inner layer

Fig.S22. Experimentation process for WEP recycling a) WEP-Omega 3 mixing, b) and c) WEP dissolution process, d) WEP precipitation, e) and f) recovered WEP

| Omega-3 |  | Glyceryl tributyrate |  | Ethyl butyrate |  |
| --- | --- | --- | --- | --- | --- |
| Co (w/w) | Time (min) | Co (w/w) | Time (min) | Co (w/w) | Time (min) |
| 10.123 | 4.21111 | 10.08558 | 4.41667 | 10.02133 | 0.86667 |
| 20.02485 | 6.09444 | 20.00796 | 8.15833 | 19.9277 | 2 |
| 30.0033 | 6.56111 | 30.04303 | 11.73333 | 30.00269 | 2.31111 |
| 39.99868 | 7.2 | 40.03082 | 17.25 | 39.97742 | 2.44445 |
| 49.96054 | 7.94445 | 50.02479 | 24.325 | 50.01294 | 2.46667 |
| 59.97404 | 10.05 | 60.02682 | 30.44167 | 59.98019 | 3.32222 |
| 69.96818 | 15.30833 | 70.00197 | 40.65833 | 70.1271 | 3.48889 |
| 79.99804 | 24.05 | 79.97312 | 52.84167 | 80.1 | 3.59 |
| 89.97957 | 28.05 | 90.02584 | 73.5 | 90.02312 | 3.96667 |
| 99.9967 | 31.23333 | 100.00497 | 130.5 | 100.14142 | 7.40556 |

Table S1. Time required to dissolve WEP

Table S2. Main bands of the esters

| Omega-3 |  |  |  |  | Glyceryl tributyrate |  |  |  |  | Ethyl Butyrate |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Vibration | Frequency (cm-1) | Intensity | Shape |  | Vibration | Frequency (cm-1) | Intensity | Shape |  | Vibration | Frequency (cm-1) | Intensity | Shape |
| = C-H (of the unsaturations present in the chain) | 3011 | w | Narrow |  | C-H | 2965 2936 2877 | w | Narrow |  | C-H | 2964 2937 2877 | w | Narrow |
| C-H | 2959 2926 2855 | m | Narrow |  | C = O (from the ester) | 1735 | s | Acute |  | C = O (from the ester) | 1735 | s | Acute |
| C = O (from the ester) | 1735 | s | Acute |  | C-O (from alkyl ester) | 1164 | m | Narrow-Acute |  | C-O (from alkyl ester) | 1161 | m | Narrow-Acute |
| C-O (from alkyl ester) | 1177 1161 | m | Narrow |  | - | - | - | - |  | - | - | - | - |

Table S3. Characteristic bands of WEP compared to WEP recovered from esters

| WEP untreated |  |  |  | RE-OME3 |  |  | RE-GT |  |  | RE-EB |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Vibration | Frequency (cm-1) | Intensity |  | Frequency (cm-1) | Intensity |  | Frequency (cm-1) | Intensity |  | Frequency (cm-1) | Intensity |
| = C-H (from the aromatic ring) | 3026 | w |  | 3026 | w |  | 3026 | w |  | 3026 | w |
| -CH2- | 2921 2849 | m |  | 2922 2849 | m |  | 2925 2850 | m |  | 2923 2849 | m |
| -C = C- (from the aromatic ring) | 1601 1493 1450 | m |  | 1600 1494 1452 | m |  | 1601 1493 1452 | m |  | 1601 1493 1452 | m |
| = C-H oop (out-of-plane twist) | 752 695 | s |  | 754 693 | s |  | 756 695 | s |  | 755 695 | s |

WEP: Waste Expanded Polystyrene

RE-OME3: WEP recovered from Omega 3

RE-GT: WEP recovered from Glyceryl Tributyrate

RE-EB: WEP recovered from Ethyl Butyrate

Fig.S1 Infrared spectroscopy of omega-3

Fig.S2 Infrared spectroscopy of glyceryl tributyrate

Fig.S3 Infrared spectroscopy of ethyl butyrate

Fig.S4 FTIR of esters: (a) omega-3, (b) glyceryl tributyrate and (c) ethyl butyrate

Fig.S5 Differential Scanning Calorimetry of untreated WEP

Fig.S6 Differential Scanning Calorimetry at 50% WEP solution using omega-3

Fig.S7 Differential Scanning Calorimetry at 50% WEP solution using glyceryl tributyrate

Fig.S8 Differential Scanning Calorimetry at 50% WEP solution using ethyl butyrate

Fig.S9 Thermogravimetric analysis of untreated WEP

Fig.S10 Thermogravimetric analysis at a 50% solution of WEP using omega-3

Fig.S11 Thermogravimetric Analysis at 50% WEP solution using glyceryl tributyrate

Fig.S12 Thermogravimetric analysis at a 50% solution of WEP using ethyl butyrate

Fig.S13 Degree of advance α for the calculation of the activation energy of the WEP without treatment using the Friedman model with heating rate β = 20°C/min (293.15 K / min)

Fig.S14 Linear regression for the calculation of the activation energy of the WEP without treatment using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S15 Degree of advancement α for the calculation of the activation energy of the WEP recovered with omega-3 using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S16 Linear regression for the calculation of the activation energy of the WEP recovered with omega-3 using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S17 Degree of advancement α for the calculation of the activation energy of the WEP recovered with glyceryl tributyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S18 Linear regression for the calculation of the activation energy of the WEP recovered with glyceryl tributyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S19 Degree of advancement α for the calculation of the activation energy of the WEP recovered with ethyl butyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

Fig.S20 Linear regression for the calculation of the activation energy of the WEP recovered with ethyl butyrate using the Friedman model with heating rate β=20°C/min (293.15 K/min)

(b)

(a)

Fig.S21 Scanning electron micrograph of untreated WEP (a) outer layer (b) inner layer

Fig.S22 Experimentation process for WEP recycling a) WEP-Omega 3 mixing, b) and c) WEP dissolution process, d) WEP precipitation, e) and f) recovered WEP