Supporting Information

pH-regulated carbon dots fluorescence sensor array detection of multiple heavy metal ions under stepwise prediction

Yuying Liu a, Jiao Chena, Xiyuan Wang a, Hao Liu a, Tingting Yuanb, Qingdong Shia, Zijun Xuac*, Jianjie Weid*

a College of Resources and Environment Sciences, Xin Jiang University, Urumqi 830046, PR China

b Tianjin Geological Engineering Survey and Design Institute Co. LTD

c College of Resources and Environment Sciences, China Agricultural University, Beijing 100193, PR China

d College of Mathematics and System Science, Xinjiang University, Urumqi 830046, China

Address:

College of Resources and Environment Sciences, Xinjiang University, Shengli Road, Tianshan District, Urumqi, China, 830046.

*Corresponding author:

E-mail address: xuzijun511@163.com

Tel: 0991-2111429

EXPERIMENTAL SECTION

1.1 Fluorescence quantum yield measurement. The aqueous solution of quinine sulfate in 0.1 M H2SO4 with the about 54% QY were used as reference standard solutions. The corresponding absorbance values (A) of solutions with different concentrations were determined at 370 nm UV light and the A should be no more than 0.05 and greater than 0.01. By scanning the fluorescence spectra of standard reference quinine sulfate and sample solution respectively, the integrated fluorescence intensity (i.e., the area of the fluorescence spectrum) was recorded by the software of the fluorometer. The refractive index of deionized water and 0.1 mol/L H2SO4 were tested respectively, and then substituted into the following equation to calculate the QY of CPC-CDs:

ΦX=ΦST (kx / kST) (η2X / η2ST)

Where: ΦST is QY of reference material, kx and kST indicate respectively the slope of the linear fitting line, ηX and ηST refer to the refractive index.

List of Figures

Figure. S1. Fluorescence excitation (black line) and emission (red line) spectra of CPC-CDs (Inset: the photographs of CPC solution under irradiation by 370 nm UV light ).

Figure. S2. The ratio of integrated area of fluorescence peak to absorption value :

(A) CPC-CDs;  (B) the Quinine sulfate .

Figure. S3. Absorption spectra of four metal chelates （XO-Cr6+, XO-Fe3+, XO-Fe2+, XO-Hg2+）and fluorescence excitation spectra of CPC-CDs.

Figure. S4. The UV absorption spectrum of CPC-CDs, four metal complexes, CPC-CDs+metal complexes, CPC-CDs and metal complexes and the sum of quantity.

Figure. S5. Fluorescence response of CPC-CDs and CPC-CDs/XO in different pH buffer solutions.

Figure. S6. Fluorescence spectra of CPC-CDs, CPC-CDs/XO and the reacton of CDs/XO with different metal ions（Cr6+、Fe2+、Fe3+、Hg2+）.

Figure. S7. (a) Fluorescence responses of metal ions reacting with sensor array systems in different pH environments ; (b) Fluorescence responses of Cr6+ reacting with sensor array systems in different pH environments ; (c) Fluorescence responses of Fe3+ reacting with sensor array systems in different pH environments ; (d) Fluorescence responses of Fe2+ reacting with sensor array systems in different pH environments ; (e) Fluorescence responses of Hg2+ reacting with sensor array systems in different pH environments.

Figure. S8. The fluorescence intensity ratios of the CPC-CDs/XO aqueous solutions in the presence of 10 μM of various anions and metal ions. (pH=7.4).

Figure. S9. Optimization of XO concentration in Tris-HCl buffer solution. (pH=7.4).

Figure. S10. Optimization of reaction time between CPC-CDs and XO in Tris-HCl buffer solution.(pH=7.4).

Figure. S11. Optimization of reaction time between XO/CDs and Cr6+ in Tris-HCl buffer solution.(pH=7.4).

Figure S1. Fluorescence excitation (black line) and emission (red line) spectra of CPC-CDs (Insert: photos of the novel CPC-CDs solution irradiated by natural light (right) and 365 nm ultraviolet light (left)).

Figure S2. The ratio of integrated area of fluorescence peak to absorption value : (A) CPC-CDs; (B) the Quinine sulfate .

Figure S3. Absorption spectra of four metal chelates（XO-Cr6+, XO-Fe3+, XO-Fe2+, XO-Hg2+）and fluorescence excitation spectra of CPC-CDs.

Figure S4. The UV absorption spectrum of CPC-CDs, four metal complexes, CPC-CDs+metal complexes, CPC-CDs and metal complexes and the sum of quantity.

Figure S5. Fluorescence response of CPC-CDs and CPC-CDs/XO in different pH buffer solutions.

Figure S6. Fluorescence spectra of CPC-CDs, CPC-CDs/XO and the reacton of CPC-CDs/XO with different metal ions（Cr6+、Fe2+、Fe3+、Hg2+）.

Figure S7. a. Fluorescence responses of metal ions reacting with sensor array systems in different pH environments(pH 7.4 on the left, 8.8 on the right).

Figure S7. b. Fluorescence responses of Cr6+ reacting with sensor array systems in different pH environments.

Figure S7. c. Fluorescence responses of Fe3+ reacting with sensor array systems in different pH environments.

Figure S7. d. Fluorescence responses of Fe2+ reacting with sensor array systems in different pH environments.

Figure S7. e. Fluorescence responses of Hg2+ reacting with sensor array systems in different pH environments.

Figure S8. The fluorescence intensity ratios of the CPC-CDs/XO aqueous solutions in the presence of 10 μM of various anions and metal ions.(pH=7.4).

F Figure S9. Optimization of XO concentration in Tris-HCl buffer solution (pH=7.4).

F Figure S10. Optimization of reaction time between CPC-CDs and XO in Tris-HCl buffer solution.(pH=7.4).

F Figure S11. Optimization of reaction time between CPC-CDs/XO and Cr6+ in Tris-HCl buffer solution(pH=7.4).

List of Tables

Table S1. Classification accuracy of four metal ions in deionized water samples for unknown samples

Table S2. Concentration accuracy of four metal ions in deionized water samples for unknown samples

Table S3. Classification accuracy of four metal ions in lake water for unknown samples

Table S4. Concentration accuracy of four metal ions in lake water for unknown samples

Table S5. Classification accuracy of binary mixtures in deionized water sample for unknown samples

Table S6. Concentration accuracy of binary mixtures in deionized water sample for unknown

samples

Table S7. Classification accuracy of binary mixtures in lake water for unknown samples

Table S8. Concentration accuracy of binary mixtures in lake water for unknown samples

Table S9. Detection of Cr6+ in lake water Using CPC-CDs/XO Sensor Array

Table S1. Classification accuracy of four metal ions in deionized water samples for unknown samples

| Data Types Class | Total samples | correct prediction samples | Accuracy |
| --- | --- | --- | --- |
| Category Data | 22 | 21 | 95.45% |

Table S2. Concentration accuracy of four metal ions in deionized water samples for unknown sample

| Data Types Class | Total samples | Accuracy |
| --- | --- | --- |
| concentration data | 22 | 100.00% |

Table S3. Classification accuracy of four metal ions in lake water for unknown sample.

| Data Types Class | Total samples | correct prediction samples | Accuracy |
| --- | --- | --- | --- |
| Category Data | 15 | 15 | 100.00% |

Table S4. Concentration accuracy of four metal ions in lake water for unknown samples

| Data Types Class | Total samples | Accuracy |
| --- | --- | --- |
| concentration data | 15 | 100.00% |

| Data Types Class | Total samples | correct prediction samples | Accuracy |  |
| --- | --- | --- | --- | --- |
| Category Data | 22 | 21 |  | 95.45% |

Table S5. Classification accuracy of binary mixtures in deionized water sample for unknown samples

Table S6. Concentration accuracy of binary mixtures in deionized water sample for unknown

| Data Types Class | Total samples | Accuracy 1 | Accuracy 2 |
| --- | --- | --- | --- |
| concentration data | 22 | 100.00% | 100.00% |

Table S7. Classification accuracy of binary mixtures in lake water for unknown samples

| Data Types Class | Total samples | correct prediction samples | Accuracy |  |
| --- | --- | --- | --- | --- |
| Category Data | 11 | 10 |  | 90.90% |

Table S8. Concentration accuracy of binary mixtures in lake water for unknown samples

| Data Types Class | Total samples | Accuracy 1 | Accuracy 2 |
| --- | --- | --- | --- |
| concentration data | 11 | 100.00% | 100.00% |

Table S9. Detection of Cr6+ in lake water Using CPC-CDs/XO Sensor Array

| Added (μM) | ICP-MS (μM) | CPC-CDs/XO (μM) |
| --- | --- | --- |
| 1 | 0.98 | 1 |
| 10 | 11.42 | 10 |