Ion exchange capacity of LTL zeolite: a promising way for cerium recovery

Giorgia Confalonieri* 1, Giovanna Vezzalini2, Laura Maletti2, Francesco Di Renzo3, Vittorio Gozzoli2, Rossella Arletti*2

1 ID22, Structure of Materials European Synchrotron Radiation Facility 71, avenue des Martyrs,384043 Grenoble, France giorgia.confalonieri@esrf.fr

2 Dipartimento di Scienze Chimiche e Geologiche, Università degli Studi di Modena e Reggio Emilia, Via Giuseppe Campi, 103, 41125 Modena rossella.arletti@unimore.it

3 ICGM, University of Montpellier, CNRS, ENSCM, Place Eugène Bataillon, 34095, Montpellier, France

Table S1. Residual nitrogen (%) from elemental analysis, and calculated NH4+ amount (%), in the Ce-exchanged NH4-LTL samples.

| Name | N (%) | NH4+ (%) |
| --- | --- | --- |
| Ce-30 | 3.27 | 4.21 |
| Ce-60 | 3.06 | 3.94 |
| Ce-90 | 2.77 | 3.57 |
| Ce-180 | 2.48 | 3.19 |
| Ce-290 | 2.30 | 2.96 |
| Ce-750 | 2.21 | 2.85 |

Table S2. SEM-EDS analysis - expressed as oxide - and standard deviations (esd) of the Ce-exchanged NH4-LTL samples recalculated with the amount of H2O from TG and NH4 from elemental analysis (see Table S1).

| Name | H2O (%) | (NH4)2O (%) | Al2O3 (%) | SiO2 (%) | K2O (%) | Ce2O3 (%) | Al2O esd | SiO2 esd | K2O esd | Ce2O3 esd |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ce-30 | 11.70 | 6.08 | 17.47 | 59.76 | 3.76 | 1.11 | 0.15 | 0.26 | 0.21 | 0.08 |
| Ce-60 | 11.70 | 5.69 | 17.28 | 59.21 | 3.80 | 2.24 | 0.08 | 0.11 | 0.11 | 0.02 |
| Ce-90 | 12.40 | 5.15 | 16.94 | 58.44 | 3.70 | 3.25 | 0.08 | 0.29 | 0.08 | 0.06 |
| Ce-180 | 12.80 | 4.61 | 16.71 | 57.16 | 3.55 | 5.12 | 0.11 | 0.16 | 0.11 | 0.15 |
| Ce-290 | 12.90 | 4.28 | 16.83 | 57.21 | 3.31 | 5.43 | 0.29 | 0.48 | 0.13 | 0.60 |
| Ce-750 | 12.90 | 4.11 | 16.89 | 57.15 | 3.18 | 5.67 | 0.11 | 0.28 | 0.08 | 0.32 |

Table S3. Ce3+ ICP analysis of the exchange solutions where the zeolite was put in contact for 72 h with the same solution. The table reports for each sample: i) the starting Ce3+ content (mg) of the solution; ii) the Ce3+ (mg) drawn from the solution (i.e. exchanged by the zeolite) after 24, 48, 72 h of contact with the solution; iii) the % of Ce exchanged (calculated as percentage of Ce amount in solution every day) after 24, 48, 72 h of contact with the solution; iv) the total exchange %.

| Sample | Starting Ce3+ in sol. (mg) | Ce3+ exchanged (drawn from the solution) (mg) |  |  | 24 h (%) | 48 h (%) | 72 h (%) | Total (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 24 h | 48 h | 72 h |  |  |  |  |
| Ce-30 | 8 | 8 | 0 | 0 | 100 | 0 | 0 | 100 |
| Ce-60 | 17 | 17 | 0 | 0 | 100 | 0 | 0 | 100 |
| Ce-90 | 25 | 25 | 0 | 0 | 100 | 0 | 0 | 100 |
| Ce-180 | 51 | 39 | 1 | 0 | 77 | 8 | 0 | 78 |
| Ce-290 | 82 | 44 | 4 | 1 | 54 | 11 | 3 | 60 |
| Ce-750 | 211 | 51 | -3* | 1 | 24 | -2* | 1 | 23 |

* this sample shows a slight release of the incorporated cerium after 48 h.

Table S4. SEM-EDS analysis, and standard deviations (esd), of NH4-LTL samples after Ce3+ release.

| Name | Al2O3 (%) | SiO2 (%) | K2O (%) | Ce2O3 (%) | Al2O esd | SiO2 esd | K2O esd | Ce2O3 esd |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Rev-Ce-30 | 21.40 | 74.23 | 4.19 | 0.16 | 0.06 | 0.13 | 0.07 | 0.11 |
| Rev-Ce-60 | 21.44 | 74.26 | 4.10 | 0.15 | 0.13 | 0.14 | 0.05 | 0.05 |
| Rev-Ce-90 | 21.02 | 74.32 | 4.17 | 0.35 | 0.57 | 0.36 | 0.07 | 0.32 |
| Rev-Ce-180 | 21.56 | 74.29 | 4.10 | 0.29 | 0.10 | 0.22 | 0.08 | 0.12 |
| Rev-Ce-290 | 21.94 | 74.25 | 4.16 | 0.23 | 0.09 | 0.10 | 0.03 | 0.10 |
| Rev-Ce-750 | 21.34 | 74.36 | 4.04 | 0.20 | 0.12 | 0.11 | 0.05 | 0.10 |

Table S5. Nitrogen % from elemental analysis in the Ce-exchanged NH4-LTL samples and in the same samples after Ce3+ release.

|  | N % |  | N % |
| --- | --- | --- | --- |
| NH4-LTL [1] | 3.59 |  |  |
| Ce-30 | 3.27 | Rev-Ce-30 | 3.50 |
| Ce-60 | 3.06 | Rev-Ce-60 | 3.47 |
| Ce-90 | 2.77 | Rev-Ce-90 | 3.72 |
| Ce-180 | 2.48 | Rev-Ce-180 | 3.51 |
| Ce-290 | 2.3 | Rev-Ce-290 | 3.57 |
| Ce-750 | 2.21 | Rev-Ce-750 | 3.52 |