Table 1. 3D modeling and output of 3D-printed auxetic lattice 4 type structures.

| Sample | Auxetic lattice repeat unit | Modeling images | g-code | Weight (g) | Optical images |
| --- | --- | --- | --- | --- | --- |
| TR |  |  |  | 6.3 |  |
| HN |  |  |  | 7.1 |  |
| CT |  |  |  | 7.4 |  |
| RE |  |  |  | 8.4 |  |

Table 2. Optical images for up to 5th cycle coatings of auxetic lattice 4 type structures.

| Sample | Cycle times |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Non coating | First | Second | Third | Fourth | Fifth |
| TR |  |  |  |  |  |  |
| HN |  |  |  |  |  |  |
| CT |  |  |  |  |  |  |
| RE |  |  |  |  |  |  |

Table 4. Strain images and Poisson’s ratio of auxetic lattice TR patterns up to 60% elongation.

| Description | Strain (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0 | 1 | 3 | 5 | 10 | 15 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | - | 0 | 0 | 0 | 0 | 0.067 |
| - | 20 | 25 | 30 | 40 | 50 | 60 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | 0.107 | 0.105 | 0.100 | 0.119 | 0.105 | 0.091 |

Table 5. Strain images and Poisson’s ratio of auxetic lattice HN patterns up to 60% elongation.

| Description | Strain (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0 | 1 | 3 | 5 | 10 | 15 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | - | 0 | 0 | 0 | 0 | 0.059 |
| - | 20 | 25 | 30 | 40 | 50 | 60 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | 0.102 | 0.143 | 0.126 | 0.100 | 0.097 | 0.112 |

Table 6. Strain images and Poisson’s ratio of auxetic lattice CT patterns up to 60% elongation.

| Description | Strain (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0 | 1 | 3 | 5 | 10 | 15 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | - | 0 | 0 | 0 | -0.102 | -0.073 |
| - | 20 | 25 | 30 | 40 | 50 | 60 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | -0.064 | -0.054 | -0.044 | -0.070 | -0.062 | -0.051 |

Table 7. Strain images and Poisson’s ratio of auxetic lattice RE patterns up to 60% elongation.

| Description | Strain (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0 | 1 | 3 | 5 | 10 | 15 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | - | 0 | 0 | 0 | -0.145 | -0.068 |
| - | 20 | 25 | 30 | 40 | 50 | 60 |
| Images |  |  |  |  |  |  |
| Poisson’s ratio | -0.063 | -0.056 | -0.046 | -0.038- | -0.027 | -0.026 |