Supporting information

Chitosan-silanol groups functional magnetic nanoparticles for heavy metals and bacteria removal

Qibo Liua, Yonghui Wang b,1, Xueli Liub, Shuang Lib, shuyue Renb, Zhixian Gao b, Tie Han b, Zhangrun Xua,*, Huanying Zhoub,*

a Research Center for Analytical Sciences, Northeastern University, Shenyang 110819, China.

b Tianjin Key Laboratory of Risk Assessment and Control Technology for Environment and Food Safety, Tianjin Institute of Environmental and Operational Medicine, Tianjin 300050, China.

* Corresponding Authors:

E-mail addresses: xuzr@mail.neu.edu.cn (Prof. Zhangrun Xu); zhouhytj@163.com (Prof. Huanying Zhou).

1 These authors contributed equally to this work.

CONTENTS

Fig.S1. Schematic diagram of Fe3O4@Si-OH@CS.

Fig.S2. Zeta potential distribution of Fe3O4@Si-OH and Fe3O4@Si-OH@CS.

Fig.S3. Magnetization curves of Fe3O4@Si-OH@CS (Inset:Magnetic separation).

Table.S1. BET results of Fe3O4, Fe3O4@Si-OH, and Fe3O4@Si-OH@CS.

Table.S2. Comparison of adsorption capacity for removing heavy metal with different adsorbents.

Fig.S1. Schematic diagram of Fe3O4@Si-OH@CS.

Fig.S2. Zeta potential distribution of Fe3O4@Si-OH and Fe3O4@Si-OH@CS.

Fig.S3. Magnetization curves of Fe3O4@Si-OH@CS (Inset:Magnetic separation).

Table.S1. BET results of Fe3O4, Fe3O4@Si-OH, and Fe3O4@Si-OH@CS.

|  | Fe3O4 | Fe3O4@Si-OH | Fe3O4@Si-OH@CS |
| --- | --- | --- | --- |
| SBET m2/g | 141.86 | 21.82 | 27.34 |
| Pore volume cm3/g | 0.693 | 0.068 | 0.098 |
| Pore size/nm | 19.55 | 12.46 | 14.35 |

Table.S2. Comparison of adsorption capacity for removing heavy metal with different adsorbents.

| Adsorbent(mg/g) | QCr(Ⅵ) (mg/g) | QAs (mg/g) | QHg (mg/g) | QSe (mg/g) | References |
| --- | --- | --- | --- | --- | --- |
| SBA-APTES | 51.0 | 36.0 | / | 79.0 | Dobrzyńska, J. 2021 |
| SBA-TMPED | 55.0 | 24.0 | / | 78.0 | Dobrzyńska, J. 2021 |
| SBA-MPTMS | 55.0 | / | / | 31.0 | Dobrzyńska, J. 2021 |
| CTF-1 | / | 28.6 | 32.8 | / | K. Leus et al 2018 |
| CMCH | 49.0 | / | 28.2 | / | Wu et al., 2017 |
| Amino-Magnetic-GO | 28.0 | / | 23.0 | / | Guo et al., 2014 |
| A-MLS | 54.2 | 53.1 | / | / | Popovic et al., 2020 |
| Monodispersed Gamma-AlOOH / Fe(OH)3 | 13.1 | 43.8 | / | / | Zhang et al., 2016 |
| Fe3O4@Si-OH@CS | 82.5 | 53.9 | 54.3 | 130.0 | This work |

/ The work was not mentioned.