Supplementary information

Bottom-up Growth of Graphene Nanospears and Nanoribbons

Haibin Sun1,2,+, Fengning Liu1,3,+, Leining Zhang1,+, Ben McLean1, Hao An1,3, Ming Huang1, Marc-Georg Willinger4, Rodney Ruoff1,3,5,6, Zhujun Wang4,7,,  & Feng Ding1,3

1Center for Multidimensional Carbon Materials, Institute for Basic Science, Ulsan 44919, Republic of Korea

2Key Laboratory of Microelectronics and Energy of Henan Province, College of Physics and Electronic Engineering, Xinyang Normal University, Xinyang 464000, China

3Department of Materials Science and Engineering, Ulsan National Institute of Science and Technology, Ulsan 44919, Republic of Korea

4Scientific Center for Optical and Electron Microscopy, ETH Zurich, Otto-Stern-Weg 3, 8093 Zurich, Switzerland

5Department of Chemistry, Ulsan National Institute of Science and Technology (UNIST), Ulsan, 44919, Republic of Korea

6School of Energy and Chemical Engineering, Ulsan National Institute of Science and Technology (UNIST), Ulsan, 44919, Republic of Korea

7School of Physical Science and Technology, Shanghai Tech University, Shanghai 200031, China

Correspondence and requests for materials should be addressed to Z.-J.W (email: wangzhj3@shanghaitech.edu.cn) or to F.D. (email: f.ding@unist.ac.kr)

[+] These authors contributed equally to this work.

Supplementary Fig. 1 (a) Temperature-time profile for the CVD growth of graphene with the diluted CH4 gas (1%). (b) Temperature-time profile for the CVD growth of graphene with the purified CH4 gas (100%).

Supplementary Fig. 2 The optical images of graphene islands grown on the Cu surface with varying shapes, under the growth condition of Figure S1(a).

Supplementary Fig. 3 SEM images of graphene islands grown on the Cu surface with varying shapes, under the growth condition of Figure S1(a).

Supplementary Fig. 4 Characteristics of particles on Cu substrate annealed at 1050 ℃ for 60min with 500 sccm of Ar and 200 sccm of H2 using the quartz tube. a-b SEM images of the Cu surface: a A large number of particles can be observed. b The enlarged SEM image of a. c-d XPS spectra of the Cu surface.

Supplementary Fig. 5 SEM images of GNSs grown on Cu foils, under the growth condition of Figure S1(b).