SUPPLEMENTARY INFORMATION

Life Cycle Assessment (LCA) as a support decision-making tool in nanocomposite material additive manufacturing sector

Foteini Petrakli, Anastasia Gkika, Anestis Vlysidis, Panagiotis Karayannis, Natalia Sieti, Elias Koumoulos*

IRES—Innovation in Research & Engineering Solutions, Rue Koningin Astritlaan 59B, 1780 Wemmel, Belgium

*Contact: epk@innovation-res.eu

Table S1 Environmental impacts in all (16) impact categories of 1 g CNTs, GNPs and GO

| Impact category | Unit | CNTs | GNPs | GO |
| --- | --- | --- | --- | --- |
| Climate change | kg CO2 eq | 0.246 | 0.0745 | 0.343 |
| Ozone depletion | kg CFC-11 eq | 3.10E-08 | 9.13E-09 | 1.78E-07 |
| Human toxicity, non-cancer effects | CTUh | 8.60E-08 | 2.50E-08 | 2.42E-07 |
| Human toxicity, cancer effects | CTUh | 3.38E-08 | 6.24E-09 | 3.76E-08 |
| Particulate matter | kg PM2.5 eq | 9.89E-05 | 3.02E-05 | 0.0003 |
| Ionizing radiation HH | kBq U235 eq | 0.128 | 0.040225 | 0.094 |
| Ionizing radiation E (interim) | CTUe | 3.31E-07 | 1.04E-07 | 2.62E-07 |
| Photochemical ozone formation | kg NMVOC eq | 0.0006 | 0.000167 | 0.0013 |
| Acidification | molc H+ eq | 0.0013 | 0.000412 | 0.0046 |
| Terrestrial eutrophication | molc N eq | 0.0021 | 0.000642 | 0.0043 |
| Freshwater eutrophication | kg P eq | 0.0002 | 7.27E-05 | 0.0002 |
| Marine eutrophication | kg N eq | 0.0002 | 7.14E-05 | 0.0005 |
| Freshwater ecotoxicity | CTUe | 3.337 | 1.010782 | 14.546 |
| Land use | kg C deficit | 0.189 | 0.057344 | 0.572 |
| Water resource depletion | m3 water eq | 0.003 | 0.000738 | 0.004 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 2.18E-06 | 6.27E-07 | 2.05E-05 |

Table S2 Environmental impacts in all (16) impact categories of 1 g PP, PA and PLA raw materials

| Impact category | Unit | PA | PLA | PP |
| --- | --- | --- | --- | --- |
| Climate change | kg CO2 eq | 8.034 | 0.934 | 1.848 |
| Ozone depletion | kg CFC-11 eq | 2.38E-09 | 2.2E-07 | 3.86E-08 |
| Human toxicity, non-cancer effects | CTUh | 1.05E-07 | 8.96E-07 | 2.21E-07 |
| Human toxicity, cancer effects | CTUh | 2.26E-07 | 1.8E-07 | 6.17E-08 |
| Particulate matter | kg PM2.5 eq | 0.003 | 0.002 | 0.001 |
| Ionizing radiation HH | kBq U235 eq | 0.001 | 0.255787 | 0.106 |
| Ionizing radiation E (interim) | CTUe | 4.45E-09 | 9.15E-07 | 2.84E-07 |
| Photochemical ozone formation | kg NMVOC eq | 0.020 | 0.012 | 0.006 |
| Acidification | molc H+ eq | 0.036 | 0.0220 | 0.007 |
| Terrestrial eutrophication | molc N eq | 0.067 | 0.067 | 0.013 |
| Freshwater eutrophication | kg P eq | 0.0004 | 0.001 | 0.0003 |
| Marine eutrophication | kg N eq | 0.014 | 0.008 | 0.001 |
| Freshwater ecotoxicity | CTUe | 13.310 | 66.453 | 19.205 |
| Land use | kg C deficit | 0.043 | 9.230 | 0.531 |
| Water resource depletion | m3 water eq | 0.037 | 0.074 | 0.007 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 1.35E-05 | 6E-05 | 2.73E-05 |

Table S3 Impact of 1 kg filament production (in different combinations among polymers and NMs loading) on climate change category (kgCO2eq.)

|  | 0.5 wt% | 1 wt% | 2 wt% | 3 wt% | 4 wt% | 5 wt% | 7.5 wt% | 10 wt% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PA -CNT | 5.914 | 7.132 | 9.568 | 12.005 | 14.441 | 16.878 | 22.969 | 29.060 |
| PA -GNP | 5.026 | 5.357 | 6.018 | 6.679 | 7.341 | 8.002 | 9.655 | 11.309 |
| PA -GO | 6.367 | 8.038 | 11.380 | 14.722 | 18.064 | 21.407 | 29.762 | 38.118 |
| PP -CNT | 3.161 | 4.410 | 6.908 | 9.407 | 11.905 | 14.403 | 20.649 | 26.895 |
| PP -GNP | 2.273 | 2.635 | 3.358 | 4.081 | 4.804 | 5.528 | 7.336 | 9.144 |
| PP -GO | 3.615 | 5.316 | 8.720 | 12.124 | 15.528 | 18.932 | 27.443 | 35.953 |
| PLA -CNT | 3.792 | 5.046 | 7.553 | 10.061 | 12.568 | 15.076 | 21.345 | 27.613 |
| PLA -GNP | 2.904 | 3.270 | 4.003 | 4.735 | 5.468 | 6.200 | 8.031 | 9.862 |
| PLA -GO | 4.245 | 5.952 | 9.365 | 12.778 | 16.191 | 19.605 | 28.138 | 36.671 |

Table S4 Impact of 1 kg PLA -CNT/GNPs/GO 0.5, 3 & 5 wt% in all categories

| 1 kg PLA -CNT 0.5% |  |  |
| --- | --- | --- |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 3.792366 |
| Ozone depletion | kg CFC-11 eq | 4.18E-07 |
| Human toxicity, non-cancer effects | CTUh | 2.26E-06 |
| Human toxicity, cancer effects | CTUh | 4.22E-07 |
| Particulate matter | kg PM2.5 eq | 0.002795 |
| Ionizing radiation HH | kBq U235 eq | 1.071822 |
| Ionizing radiation E (interim) | CTUe | 3.03E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.015863 |
| Acidification | molc H+ eq | 0.030604 |
| Terrestrial eutrophication | molc N eq | 0.081791 |
| Freshwater eutrophication | kg P eq | 0.002765 |
| Marine eutrophication | kg N eq | 0.009257 |
| Freshwater ecotoxicity | CTUe | 160.9097 |
| Land use | kg C deficit | 10.45794 |
| Water resource depletion | m3 water eq | 0.093451 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 7.70E-05 |
| 1 kg PLA -CNT 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 10.06119 |
| Ozone depletion | kg CFC-11 eq | 1.19E-06 |
| Human toxicity, non-cancer effects | CTUh | 4.39E-06 |
| Human toxicity, cancer effects | CTUh | 1.26E-06 |
| Particulate matter | kg PM2.5 eq | 0.00521 |
| Ionizing radiation HH | kBq U235 eq | 4.25334 |
| Ionizing radiation E (interim) | CTUe | 1.13E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.02982 |
| Acidification | molc H+ eq | 0.063186 |
| Terrestrial eutrophication | molc N eq | 0.132619 |
| Freshwater eutrophication | kg P eq | 0.008576 |
| Marine eutrophication | kg N eq | 0.014946 |
| Freshwater ecotoxicity | CTUe | 242.5539 |
| Land use | kg C deficit | 14.93233 |
| Water resource depletion | m3 water eq | 0.169469 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.00013 |
| 1 kg PLA -CNT 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 15.07624 |
| Ozone depletion | kg CFC-11 eq | 1.80E-06 |
| Human toxicity, non-cancer effects | CTUh | 6.09E-06 |
| Human toxicity, cancer effects | CTUh | 1.93E-06 |
| Particulate matter | kg PM2.5 eq | 0.007142 |
| Ionizing radiation HH | kBq U235 eq | 6.798554 |
| Ionizing radiation E (interim) | CTUe | 1.78E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.040986 |
| Acidification | molc H+ eq | 0.089253 |
| Terrestrial eutrophication | molc N eq | 0.173281 |
| Freshwater eutrophication | kg P eq | 0.013224 |
| Marine eutrophication | kg N eq | 0.019498 |
| Freshwater ecotoxicity | CTUe | 307.8693 |
| Land use | kg C deficit | 18.51185 |
| Water resource depletion | m3 water eq | 0.230283 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000172 |
| 1 kg PLA -GNP 0.5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 2.9047829 |
| Ozone depletion | kg CFC-11 eq | 3.08E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.96E-06 |
| Human toxicity, cancer effects | CTUh | 2.84E-07 |
| Particulate matter | kg PM2.5 eq | 0.002451783 |
| Ionizing radiation HH | kBq U235 eq | 0.63447226 |
| Ionizing radiation E (interim) | CTUe | 1.90E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.013844543 |
| Acidification | molc H+ eq | 0.02603062 |
| Terrestrial eutrophication | molc N eq | 0.074482566 |
| Freshwater eutrophication | kg P eq | 0.001958836 |
| Marine eutrophication | kg N eq | 0.008435735 |
| Freshwater ecotoxicity | CTUe | 149.27896 |
| Land use | kg C deficit | 9.8023597 |
| Water resource depletion | m3 water eq | 0.081551261 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 6.92E-05 |
| 1 kg PLA -GNP 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 4.7356908 |
| Ozone depletion | kg CFC-11 eq | 5.30E-07 |
| Human toxicity, non-cancer effects | CTUh | 2.56E-06 |
| Human toxicity, cancer effects | CTUh | 4.35E-07 |
| Particulate matter | kg PM2.5 eq | 0.003149031 |
| Ionizing radiation HH | kBq U235 eq | 1.6292418 |
| Ionizing radiation E (interim) | CTUe | 4.47E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.017710024 |
| Acidification | molc H+ eq | 0.035748425 |
| Terrestrial eutrophication | molc N eq | 0.088766611 |
| Freshwater eutrophication | kg P eq | 0.003736509 |
| Marine eutrophication | kg N eq | 0.010020935 |
| Freshwater ecotoxicity | CTUe | 172.76946 |
| Land use | kg C deficit | 10.998858 |
| Water resource depletion | m3 water eq | 0.098071381 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 8.33E-05 |
| 1 kg PLA -GNP 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 6.2004171 |
| Ozone depletion | kg CFC-11 eq | 7.07E-07 |
| Human toxicity, non-cancer effects | CTUh | 3.04E-06 |
| Human toxicity, cancer effects | CTUh | 5.55E-07 |
| Particulate matter | kg PM2.5 eq | 0.003706829 |
| Ionizing radiation HH | kBq U235 eq | 2.4250575 |
| Ionizing radiation E (interim) | CTUe | 6.53E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.020802409 |
| Acidification | molc H+ eq | 0.04352267 |
| Terrestrial eutrophication | molc N eq | 0.10019385 |
| Freshwater eutrophication | kg P eq | 0.005158646 |
| Marine eutrophication | kg N eq | 0.011289096 |
| Freshwater ecotoxicity | CTUe | 191.56187 |
| Land use | kg C deficit | 11.956056 |
| Water resource depletion | m3 water eq | 0.11128748 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 9.46E-05 |
| 1 kg PLA -GO 0.5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 4.245249 |
| Ozone depletion | kg CFC-11 eq | 1.15E-06 |
| Human toxicity, non-cancer effects | CTUh | 3.04E-06 |
| Human toxicity, cancer effects | CTUh | 4.41E-07 |
| Particulate matter | kg PM2.5 eq | 0.00399 |
| Ionizing radiation HH | kBq U235 eq | 0.904499 |
| Ionizing radiation E (interim) | CTUe | 2.69E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.019518 |
| Acidification | molc H+ eq | 0.047011 |
| Terrestrial eutrophication | molc N eq | 0.093033 |
| Freshwater eutrophication | kg P eq | 0.002781 |
| Marine eutrophication | kg N eq | 0.010464 |
| Freshwater ecotoxicity | CTUe | 216.9548 |
| Land use | kg C deficit | 12.37695 |
| Water resource depletion | m3 water eq | 0.095809 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000168 |
| 1 kg PLA -GO 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 12.77849 |
| Ozone depletion | kg CFC-11 eq | 5.61E-06 |
| Human toxicity, non-cancer effects | CTUh | 9.07E-06 |
| Human toxicity, cancer effects | CTUh | 1.38E-06 |
| Particulate matter | kg PM2.5 eq | 0.012379 |
| Ionizing radiation HH | kBq U235 eq | 3.249403 |
| Ionizing radiation E (interim) | CTUe | 9.20E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.051749 |
| Acidification | molc H+ eq | 0.161628 |
| Terrestrial eutrophication | molc N eq | 0.200072 |
| Freshwater eutrophication | kg P eq | 0.008668 |
| Marine eutrophication | kg N eq | 0.022192 |
| Freshwater ecotoxicity | CTUe | 578.8245 |
| Land use | kg C deficit | 26.44637 |
| Water resource depletion | m3 water eq | 0.183619 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000678 |
| 1 kg PLA -GO 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 19.60507 |
| Ozone depletion | kg CFC-11 eq | 9.17E-06 |
| Human toxicity, non-cancer effects | CTUh | 1.39E-05 |
| Human toxicity, cancer effects | CTUh | 2.13E-06 |
| Particulate matter | kg PM2.5 eq | 0.019091 |
| Ionizing radiation HH | kBq U235 eq | 5.125325 |
| Ionizing radiation E (interim) | CTUe | 1.44E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.077535 |
| Acidification | molc H+ eq | 0.253322 |
| Terrestrial eutrophication | molc N eq | 0.285702 |
| Freshwater eutrophication | kg P eq | 0.013379 |
| Marine eutrophication | kg N eq | 0.031574 |
| Freshwater ecotoxicity | CTUe | 868.3203 |
| Land use | kg C deficit | 37.70191 |
| Water resource depletion | m3 water eq | 0.253867 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.001086 |

Table S5 Impact of 1 kg PP -CNT/GNPs/GO 0.5, 3 & 5 wt% in all categories

| 1 kg PP -CNT 0.5% |  |  |
| --- | --- | --- |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 3.161167 |
| Ozone depletion | kg CFC-11 eq | 2.25E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.13E-06 |
| Human toxicity, cancer effects | CTUh | 2.55E-07 |
| Particulate matter | kg PM2.5 eq | 0.001183 |
| Ionizing radiation HH | kBq U235 eq | 0.898971 |
| Ionizing radiation E (interim) | CTUe | 2.36E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.007007 |
| Acidification | molc H+ eq | 0.012807 |
| Terrestrial eutrophication | molc N eq | 0.021748 |
| Freshwater eutrophication | kg P eq | 0.001745 |
| Marine eutrophication | kg N eq | 0.002496 |
| Freshwater ecotoxicity | CTUe | 68.72444 |
| Land use | kg C deficit | 1.639716 |
| Water resource depletion | m3 water eq | 0.02173 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 2.79E-05 |
| 1 kg PP -CNT 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 9.407149 |
| Ozone depletion | kg CFC-11 eq | 9.98E-07 |
| Human toxicity, non-cancer effects | CTUh | 3.27E-06 |
| Human toxicity, cancer effects | CTUh | 1.10E-06 |
| Particulate matter | kg PM2.5 eq | 0.003633 |
| Ionizing radiation HH | kBq U235 eq | 4.084245 |
| Ionizing radiation E (interim) | CTUe | 1.06E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.021114 |
| Acidification | molc H+ eq | 0.045767 |
| Terrestrial eutrophication | molc N eq | 0.073944 |
| Freshwater eutrophication | kg P eq | 0.00758 |
| Marine eutrophication | kg N eq | 0.008346 |
| Freshwater ecotoxicity | CTUe | 151.5499 |
| Land use | kg C deficit | 6.331578 |
| Water resource depletion | m3 water eq | 0.099442 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 8.18E-05 |
| 1 kg PP -CNT 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 14.40393 |
| Ozone depletion | kg CFC-11 eq | 1.62E-06 |
| Human toxicity, non-cancer effects | CTUh | 4.99E-06 |
| Human toxicity, cancer effects | CTUh | 1.77E-06 |
| Particulate matter | kg PM2.5 eq | 0.005592 |
| Ionizing radiation HH | kBq U235 eq | 6.632464 |
| Ionizing radiation E (interim) | CTUe | 1.72E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.032401 |
| Acidification | molc H+ eq | 0.072135 |
| Terrestrial eutrophication | molc N eq | 0.115701 |
| Freshwater eutrophication | kg P eq | 0.012247 |
| Marine eutrophication | kg N eq | 0.013027 |
| Freshwater ecotoxicity | CTUe | 217.8102 |
| Land use | kg C deficit | 10.08507 |
| Water resource depletion | m3 water eq | 0.161612 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000125 |
| 1 kg PP -GNP 0.5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 2.2735844 |
| Ozone depletion | kg CFC-11 eq | 1.15E-07 |
| Human toxicity, non-cancer effects | CTUh | 8.26E-07 |
| Human toxicity, cancer effects | CTUh | 1.17E-07 |
| Particulate matter | kg PM2.5 eq | 0.000839276 |
| Ionizing radiation HH | kBq U235 eq | 0.4616213 |
| Ionizing radiation E (interim) | CTUe | 1.23E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.004988214 |
| Acidification | molc H+ eq | 0.008233733 |
| Terrestrial eutrophication | molc N eq | 0.014439251 |
| Freshwater eutrophication | kg P eq | 0.000938551 |
| Marine eutrophication | kg N eq | 0.001675129 |
| Freshwater ecotoxicity | CTUe | 57.093693 |
| Land use | kg C deficit | 0.98413677 |
| Water resource depletion | m3 water eq | 0.009830716 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 2.01E-05 |
| 1 kg PP -GNP 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 4.0816525 |
| Ozone depletion | kg CFC-11 eq | 3.41E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.44E-06 |
| Human toxicity, cancer effects | CTUh | 2.71E-07 |
| Particulate matter | kg PM2.5 eq | 0.001571722 |
| Ionizing radiation HH | kBq U235 eq | 1.4601468 |
| Ionizing radiation E (interim) | CTUe | 3.81E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.00900401 |
| Acidification | molc H+ eq | 0.01832864 |
| Terrestrial eutrophication | molc N eq | 0.03009161 |
| Freshwater eutrophication | kg P eq | 0.002740512 |
| Marine eutrophication | kg N eq | 0.003421066 |
| Freshwater ecotoxicity | CTUe | 81.765409 |
| Land use | kg C deficit | 2.3981045 |
| Water resource depletion | m3 water eq | 0.028044826 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 3.51E-05 |
| 1 kg PP -GNP 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 5.5281069 |
| Ozone depletion | kg CFC-11 eq | 5.22E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.94E-06 |
| Human toxicity, cancer effects | CTUh | 3.94E-07 |
| Particulate matter | kg PM2.5 eq | 0.002157679 |
| Ionizing radiation HH | kBq U235 eq | 2.2589672 |
| Ionizing radiation E (interim) | CTUe | 5.89E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.012216646 |
| Acidification | molc H+ eq | 0.026404565 |
| Terrestrial eutrophication | molc N eq | 0.042613497 |
| Freshwater eutrophication | kg P eq | 0.00418208 |
| Marine eutrophication | kg N eq | 0.004817815 |
| Freshwater ecotoxicity | CTUe | 101.50278 |
| Land use | kg C deficit | 3.5292786 |
| Water resource depletion | m3 water eq | 0.042616113 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 4.70E-05 |
| 1 kg PP -GO 0.5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 3.61405 |
| Ozone depletion | kg CFC-11 eq | 9.61E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.91E-06 |
| Human toxicity, cancer effects | CTUh | 2.74E-07 |
| Particulate matter | kg PM2.5 eq | 0.002378 |
| Ionizing radiation HH | kBq U235 eq | 0.731648 |
| Ionizing radiation E (interim) | CTUe | 2.02E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.010661 |
| Acidification | molc H+ eq | 0.029214 |
| Terrestrial eutrophication | molc N eq | 0.03299 |
| Freshwater eutrophication | kg P eq | 0.001761 |
| Marine eutrophication | kg N eq | 0.003704 |
| Freshwater ecotoxicity | CTUe | 124.7695 |
| Land use | kg C deficit | 3.558722 |
| Water resource depletion | m3 water eq | 0.024089 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000119 |
| 1 kg PP -GO 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 12.12445 |
| Ozone depletion | kg CFC-11 eq | 5.42E-06 |
| Human toxicity, non-cancer effects | CTUh | 7.96E-06 |
| Human toxicity, cancer effects | CTUh | 1.21E-06 |
| Particulate matter | kg PM2.5 eq | 0.010802 |
| Ionizing radiation HH | kBq U235 eq | 3.080308 |
| Ionizing radiation E (interim) | CTUe | 8.55E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.043043 |
| Acidification | molc H+ eq | 0.144208 |
| Terrestrial eutrophication | molc N eq | 0.141397 |
| Freshwater eutrophication | kg P eq | 0.007672 |
| Marine eutrophication | kg N eq | 0.015592 |
| Freshwater ecotoxicity | CTUe | 487.8205 |
| Land use | kg C deficit | 17.84562 |
| Water resource depletion | m3 water eq | 0.113593 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.00063 |
| 1 kg PP -GO 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 18.93276 |
| Ozone depletion | kg CFC-11 eq | 8.98E-06 |
| Human toxicity, non-cancer effects | CTUh | 1.28E-05 |
| Human toxicity, cancer effects | CTUh | 1.96E-06 |
| Particulate matter | kg PM2.5 eq | 0.017542 |
| Ionizing radiation HH | kBq U235 eq | 4.959235 |
| Ionizing radiation E (interim) | CTUe | 1.38E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.068949 |
| Acidification | molc H+ eq | 0.236204 |
| Terrestrial eutrophication | molc N eq | 0.228122 |
| Freshwater eutrophication | kg P eq | 0.012402 |
| Marine eutrophication | kg N eq | 0.025103 |
| Freshwater ecotoxicity | CTUe | 778.2612 |
| Land use | kg C deficit | 29.27513 |
| Water resource depletion | m3 water eq | 0.185196 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.001039 |

Table S6 Impact of 1 kg PA - GNPs/GO/ CNT 0.5, 3 & 5 wt% in all categories

| 1 kg PA -GNP 0.5% |  |  |
| --- | --- | --- |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 5.0263537 |
| Ozone depletion | kg CFC-11 eq | 9.91E-08 |
| Human toxicity, non-cancer effects | CTUh | 7.74E-07 |
| Human toxicity, cancer effects | CTUh | 1.90E-07 |
| Particulate matter | kg PM2.5 eq | 0.001900364 |
| Ionizing radiation HH | kBq U235 eq | 0.41516499 |
| Ionizing radiation E (interim) | CTUe | 1.10E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.011282084 |
| Acidification | molc H+ eq | 0.020971262 |
| Terrestrial eutrophication | molc N eq | 0.038660219 |
| Freshwater eutrophication | kg P eq | 0.001016382 |
| Marine eutrophication | kg N eq | 0.007188911 |
| Freshwater ecotoxicity | CTUe | 54.470777 |
| Land use | kg C deficit | 0.76667356 |
| Water resource depletion | m3 water eq | 0.023214515 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 1.40E-05 |
| 1 kg PA -GNP 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 6.6797718 |
| Ozone depletion | kg CFC-11 eq | 3.26E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.39E-06 |
| Human toxicity, cancer effects | CTUh | 3.40E-07 |
| Particulate matter | kg PM2.5 eq | 0.002573198 |
| Ionizing radiation HH | kBq U235 eq | 1.4163004 |
| Ionizing radiation E (interim) | CTUe | 3.70E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.014944292 |
| Acidification | molc H+ eq | 0.030350577 |
| Terrestrial eutrophication | molc N eq | 0.052951849 |
| Freshwater eutrophication | kg P eq | 0.00281397 |
| Marine eutrophication | kg N eq | 0.008625084 |
| Freshwater ecotoxicity | CTUe | 79.289849 |
| Land use | kg C deficit | 2.1928583 |
| Water resource depletion | m3 water eq | 0.040676726 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 2.93E-05 |
| 1 kg PA -GNP 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 8.0025063 |
| Ozone depletion | kg CFC-11 eq | 5.08E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.89E-06 |
| Human toxicity, cancer effects | CTUh | 4.60E-07 |
| Particulate matter | kg PM2.5 eq | 0.003111466 |
| Ionizing radiation HH | kBq U235 eq | 2.2172087 |
| Ionizing radiation E (interim) | CTUe | 5.77E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.017874057 |
| Acidification | molc H+ eq | 0.03785403 |
| Terrestrial eutrophication | molc N eq | 0.064385154 |
| Freshwater eutrophication | kg P eq | 0.004252041 |
| Marine eutrophication | kg N eq | 0.009774023 |
| Freshwater ecotoxicity | CTUe | 99.145106 |
| Land use | kg C deficit | 3.3338061 |
| Water resource depletion | m3 water eq | 0.054646495 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 4.15E-05 |
| 1 kg PA -GO 0.5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 6.366819 |
| Ozone depletion | kg CFC-11 eq | 9.45E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.86E-06 |
| Human toxicity, cancer effects | CTUh | 3.47E-07 |
| Particulate matter | kg PM2.5 eq | 0.003439 |
| Ionizing radiation HH | kBq U235 eq | 0.685192 |
| Ionizing radiation E (interim) | CTUe | 1.89E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.016955 |
| Acidification | molc H+ eq | 0.041951 |
| Terrestrial eutrophication | molc N eq | 0.057211 |
| Freshwater eutrophication | kg P eq | 0.001838 |
| Marine eutrophication | kg N eq | 0.009217 |
| Freshwater ecotoxicity | CTUe | 122.1466 |
| Land use | kg C deficit | 3.341259 |
| Water resource depletion | m3 water eq | 0.037472 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000113 |
| 1 kg PA -GO 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 14.72257 |
| Ozone depletion | kg CFC-11 eq | 5.40E-06 |
| Human toxicity, non-cancer effects | CTUh | 7.91E-06 |
| Human toxicity, cancer effects | CTUh | 1.28E-06 |
| Particulate matter | kg PM2.5 eq | 0.011804 |
| Ionizing radiation HH | kBq U235 eq | 3.036461 |
| Ionizing radiation E (interim) | CTUe | 8.43E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.048984 |
| Acidification | molc H+ eq | 0.15623 |
| Terrestrial eutrophication | molc N eq | 0.164257 |
| Freshwater eutrophication | kg P eq | 0.007746 |
| Marine eutrophication | kg N eq | 0.020796 |
| Freshwater ecotoxicity | CTUe | 485.3449 |
| Land use | kg C deficit | 17.64037 |
| Water resource depletion | m3 water eq | 0.126224 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000624 |
| 1 kg PA -GO 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 21.40716 |
| Ozone depletion | kg CFC-11 eq | 8.97E-06 |
| Human toxicity, non-cancer effects | CTUh | 1.27E-05 |
| Human toxicity, cancer effects | CTUh | 2.03E-06 |
| Particulate matter | kg PM2.5 eq | 0.018495 |
| Ionizing radiation HH | kBq U235 eq | 4.917477 |
| Ionizing radiation E (interim) | CTUe | 1.37E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.074606 |
| Acidification | molc H+ eq | 0.247654 |
| Terrestrial eutrophication | molc N eq | 0.249894 |
| Freshwater eutrophication | kg P eq | 0.012472 |
| Marine eutrophication | kg N eq | 0.030059 |
| Freshwater ecotoxicity | CTUe | 775.9036 |
| Land use | kg C deficit | 29.07966 |
| Water resource depletion | m3 water eq | 0.197226 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.001033 |
| 1 kg PA -CNT 0.5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 5.913936 |
| Ozone depletion | kg CFC-11 eq | 2.09E-07 |
| Human toxicity, non-cancer effects | CTUh | 1.08E-06 |
| Human toxicity, cancer effects | CTUh | 3.28E-07 |
| Particulate matter | kg PM2.5 eq | 0.002244 |
| Ionizing radiation HH | kBq U235 eq | 0.852515 |
| Ionizing radiation E (interim) | CTUe | 2.23E-06 |
| Photochemical ozone formation | kg NMVOC eq | 0.0133 |
| Acidification | molc H+ eq | 0.025544 |
| Terrestrial eutrophication | molc N eq | 0.045969 |
| Freshwater eutrophication | kg P eq | 0.001823 |
| Marine eutrophication | kg N eq | 0.00801 |
| Freshwater ecotoxicity | CTUe | 66.10152 |
| Land use | kg C deficit | 1.422253 |
| Water resource depletion | m3 water eq | 0.035114 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 2.18E-05 |
| 1 kg PA -CNT 3% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 12.00527 |
| Ozone depletion | kg CFC-11 eq | 9.83E-07 |
| Human toxicity, non-cancer effects | CTUh | 3.22E-06 |
| Human toxicity, cancer effects | CTUh | 1.17E-06 |
| Particulate matter | kg PM2.5 eq | 0.004634 |
| Ionizing radiation HH | kBq U235 eq | 4.040398 |
| Ionizing radiation E (interim) | CTUe | 1.05E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.027055 |
| Acidification | molc H+ eq | 0.057789 |
| Terrestrial eutrophication | molc N eq | 0.096804 |
| Freshwater eutrophication | kg P eq | 0.007653 |
| Marine eutrophication | kg N eq | 0.01355 |
| Freshwater ecotoxicity | CTUe | 149.0743 |
| Land use | kg C deficit | 6.126332 |
| Water resource depletion | m3 water eq | 0.112074 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 7.60E-05 |
| 1 kg PA -CNT 5% |  |  |
| Impact category | Unit | Total |
| Climate change | kg CO2 eq | 16.87833 |
| Ozone depletion | kg CFC-11 eq | 1.60E-06 |
| Human toxicity, non-cancer effects | CTUh | 4.94E-06 |
| Human toxicity, cancer effects | CTUh | 1.84E-06 |
| Particulate matter | kg PM2.5 eq | 0.006546 |
| Ionizing radiation HH | kBq U235 eq | 6.590705 |
| Ionizing radiation E (interim) | CTUe | 1.71E-05 |
| Photochemical ozone formation | kg NMVOC eq | 0.038058 |
| Acidification | molc H+ eq | 0.083584 |
| Terrestrial eutrophication | molc N eq | 0.137473 |
| Freshwater eutrophication | kg P eq | 0.012317 |
| Marine eutrophication | kg N eq | 0.017983 |
| Freshwater ecotoxicity | CTUe | 215.4525 |
| Land use | kg C deficit | 9.889595 |
| Water resource depletion | m3 water eq | 0.173643 |
| Mineral, fossil & ren resource depletion | kg Sb eq | 0.000119 |

Table S7 Impact on climate change of the composite filaments produced by PA and GO as a filler in different loadings and EoL management routes (cradle-to-gate)

| Impact category | Climate change (kg CO2 eq/ kg of filament) |
| --- | --- |
| PA -GO 0.5% 100%incinerated | 11.3 |
| PA -GO 0.5% 100%landfilled | 10.73 |
| PA -GO 0.5% 100%recycling | 2.42 |
| PA -GO 1% 100%incinerated | 12.98 |
| PA -GO 1% 100%landfilled | 12.4 |
| PA -GO 1% 100%recycling | 4.09 |
| PA -GO 2% 100%incinerated | 16.32 |
| PA -GO 2% 100%landfilled | 15.74 |
| PA -GO 2% 100%recycling | 7.44 |
| PA -GO 3% 100%incinerated | 18.15 |
| PA -GO 3% 100%landfilled | 17.58 |
| PA -GO 3% 100%recycling | 9.27 |

Table S8 Electrical conductivity of various polymers with different nano-fillers based loadings

| Thermoplastic + Filler (wt. %) | Conductivity (S/m) | Reference |
| --- | --- | --- |
| PEEK/1% MWCNT | 3.19E-06 | Gonçalves et al. |
| PEEK/2% MWCNT | 3.08E-05 | Gonçalves et al. |
| PEEK/3% MWCNT | 1.15E+00 | Gonçalves et al. |
| PEEK/4% MWCNT | 1.24E+01 | Gonçalves et al. |
| PEEK/5% MWCNT | 1.48E+01 | Gonçalves et al. |
| PEEK/6% MWCNT | 2.22E+01 | Gonçalves et al. |
| PLA/1.5% GNP | 2.51E-08 | Ivanov et al |
| PLA/3% GNP | 9.90E-08 | Ivanov et al |
| PLA/6% GNP | 8.35E-03 | Ivanov et al |
| PLA/1.5% MWCNT | 1.40E-08 | Ivanov et al |
| PLA/3% MWCNT | 7.86E-04 | Ivanov et al |
| PLA/6% MWCNT | 2.10E-02 | Ivanov et al |
| ABS/4.76% MWCNT | 4.00E-01 | Podsiadły et al |
| ABS/9.09% MWCNT | 6.67E+00 | Podsiadły et al |
| PLA/0.5% rGO | 8.00E-10 | Gomez et al |
| PLA/1% rGO | 4.00E-07 | Gomez et al |
| PLA/2% rGO | 1.00E-03 | Gomez et al |
| PA12/1% MWCNT | 1.00E-12 | Socher et al 2011 |
| PA12/3% MWCNT | 1.70E-02 | Socher et al 2011 |

* approximated values from graph

References

Electrically Conductive Polyetheretherketone Nanocomposite Filaments: From Production to Fused Deposition Modeling. Gonçalves, Jordana, Patrícia Lima, Beate Krause, Petra Pötschke, Ugo Lafont, José R. Gomes, Cristiano S. Abreu, Maria C. Paiva, and José A. Covas. 8, s.l. : Polymers , 2018, Vol. 10. 10.3390/polym10080925.

PLA/Graphene/MWCNT Composites with Improved Electrical and Thermal Properties Suitable for FDM 3D Printing Applications. Ivanov, Evgeni, Rumiana Kotsilkova, Hesheng Xia, Yinghong Chen, Ricardo K. Donato, Katarzyna Donato, Anna P. Godoy, Rosa Di Maio, Clara Silvestre, Sossio Cimmino, and Verislav Angelov. s.l. : Applied Sciences , 2019, Vol. 9. 10.3390/app9061209.

Carbon Nanotube-Based Composite Filaments for 3D Printing of Structural and Conductive Elements. Podsiadły, Bartłomiej, Piotr Matuszewski, Andrzej Skalski, and Marcin Słoma. 3, s.l. : Applied Sciences , 2021, Vol. 11. 10.3390/app11031272.

Preparation of electrically conductive PLA/rGO nanocomposite filaments. Gómez, Julio & Villaro, Elvira & Pérez, Javier & Haidar, Bojan. s.l. : Graphene Technology, 2020, Vol. 5. 10.1007/s41127-020-00031-3.

Electrical and thermal properties of polyamide 12 composites with hybrid fillers systems of multiwalled carbon. Robert Socher, Beate Krause, Sylvia Hermasch, Roland Wursche, Petra Pötschke. 8, s.l. : Composites Science and Technology, Elsevier, 2011, Vol. 71. hal-00753187.