# Supplementary Information

Surface constrained electron-hole rich species active in the electrocatalytic water splitting

J. J. Velasco-Vélez1,2,*, E. Carbonio2,3, C.H. Chuang4, Cheng-Jhih Hsu4, Jyh-Fu Lee5, R. Arrigo6, M. Hävecker1,2, R. Wang7, M. Plodinec2,8, A. Centeno9, A. Zurutuza9, L. Falling2, R. Mom2, S. Hofmann7, R. Schlögl1,2, A. Knop-Gericke1,2, T. Jones2*

# *Corresponding author: velasco@fhi-berlin.mpg.de, trjones@fhi-berlin.mpg.de

1Department of Heterogeneous Reactions, Max Planck Institute for Chemical Energy Conversion, Mülheim an der Ruhr 45470, Germany

2Department of Inorganic Chemistry, Fritz-Haber-Institut der Max-Planck-Gesellschaft, Berlin 14195, Germany

# 3Helmholtz-Center Berlin for Materials and Energy, BESSY II, Berlin 12489, Germany

4Department of Physics, Tamkang University, New Taipei City 25137, Taiwan

# 5National Synchrotron Radiation Research Center, Hsinchu 30076, Taiwan

6School of Sciences, University of Salford, Environment and Life, Cockcroft building, M5 4WT, Manchester, U.K.

7Department of Engineering, University of Cambridge, Cambridge CB3 0FA, United Kingdom

8Rudjer Boskovic Institute, Bijenicka 54, HR-10000 Zagreb, Croatia

9Graphenea, San Sebastian 20018, Spain

# Fig. S1

SEM image of the BLG coating the Si3N4 grid with holes of 1 µm diameter: (A) 10 µm and (B) 1 µm  scales. (C) Raman spectra of different graphitic materials.

# Fig. S2

(A) Sketch and picture of the EC cell used for the hard X-ray measurements in the Ir L3-edge. (B) Sketch and picture of the liquid flow cell used for the PES measurements: The blue arrows indicate the electrolyte flow. The cell has three electrodes: counter, working and reference. The working electrode is transferred directly onto the grid.

Fig. S3

Structure of bulk Ir2O5 (A) and bulk IrO3 (B).

Fig. S4

The surface terminations considered for IrO2 (111). In (A) all surface µ2-O and µ1-O are hydroxylated. The µ2-OH sites are progressively hydroxlated from (B) to (E), where in (E) the surface has µ2-O and µ1-OH. In (F) µ2-O and µ1-O are present, while further oxidation to (G) produces µ2-O and µ1-OOH before the most oxidized surface (H) is reached, with µ2-O and µ1-OO.

Fig. S5

The surface terminations considered for IrO2 (001). In (A) all surface µ2-O and µ1-O are hydroxylated. The µ2-OH sites are progressively hydroxlated from (B) to (C), where in (C) the surface has µ2-O and µ1-OH. In (D) µ1-OH and µ1-O are present, while further oxidation to (E) produces µ2-O. Two µ1-OOH species are shown in (F), and µ2-O and µ1-OO in (G).

Table S1: Computed Ir 4f binding energies of iridium bound to µ1-O(H) for IrO2 (110) and (111) surfaces with varying degrees of surface oxidation. All µ2-sites are O.

| µ1-site | (110) Ir 4f / eV | (111) Ir 4f / eV | (001) Ir 4f / eV | (210) Ir 4f |
| --- | --- | --- | --- | --- |
| OH | 61.8 | 62.5 | 62.4 | 61.8 |
| O | 62.5 | 63.3 | 62.8a, 63.5b | 62.5 |
| OOH | 61.9 | 62.4 | 62.4 |  |
| OO | 61.6 | 62.0 | 61.8 |  |

aFor the (001) surface the surface Ir is bound to one µ1-OH and one µ1-OH.

bFor the (001) surface the surface Ir is bound to two µ1-O.

Fig. S6

Correlation between Ir formal oxidation state and Ir 4f shift

Fig. S7

# Correlation between Ir formal oxidation state and satellite position.

Table S2: Parameters used for fitting the in situ collected spectra depending on the applied potential.

| Potential | Peak | Peak possition | Peak Shape | fwhm |
| --- | --- | --- | --- | --- |
| +1.6 V vs. Ag/AgCl | µ1-OH(111)/µ1-O(110) | 62.5 eV | DS(0.1;400) | 1.1 |
|  | Satµ1-OH(111)/µ1-O(110) 1 | 63.3 eV | GL(30) | 1.1 |
|  | Satµ1-OH(111)/µ1-O(110) 2 | 64.1 eV | GL(30) | 1.1 |
| +1.0 V vs. Ag/AgCl | µ1-OH(111)/µ1-O(110) | 62.5 eV | DS(0.1;400) | 1.1 |
|  | Satµ1-OH(111)/µ1-O(110) 1 | 63.3 eV | GL(30) | 1.1 |
|  | Satµ1-OH(111)/µ1-O(110) 2 | 64.1 eV | GL(30) | 1.1 |
|  | µ1-OH(110)/ | 61.8 eV | DS(0.1;400) | 1.1 |
|  | Satµ1-OH(110) 1 | 62.6 eV | GL(30) | 1.1 |
|  | Satµ1-OH(110) 2 | 63.4 eV | GL(30) | 1.1 |
| +0.7 V vs. Ag/AgCl | IrIII | 62.3 eV | GL(30) | 1.8 |
| OCV | IrIII | 62.3 eV | GL(30) | 1.8 |
| HV (reference) | Ir0 | 61.2 eV | DS(0.1;400) | 1.1 |