Supplementary Information For

Layered double hydroxide membrane with high hydroxide conductivity and ion selectivity for energy storage device

by Hu et al.

Supplementary Figure 1. The environmental transmission electron microscopy (ETEM) images of LDHs. a, The ETEM image of LDHs. b, The high resolution ETEM image of the area circled by the white frame in a.

Supplementary Figure 2. Particle size distribution of LDHs.

Supplementary Figure 3. SEM images of Base membrane. a, Surface morphology of Base membrane. b, Cross-section morphology of Base membrane.

Supplementary Figure 4. SEM images of LDH-M membrane. a, Surface morphology of LDH-M membrane. b, magnified surface morphology of LDH-M membrane.

Supplementary Figure 5. The permeability of cationic ions and Fe(CN)63−. Comparison of cationic ions and Fe(CN)63− for a, Base membrane and b, LDH-M membrane.

Supplementary Figure 6. The membrane resistance measured by EIS in 3 mol L−1 sodium hydroxide solution. a, The EIS plot of different numbers of LDH-M stacked layer-by-layer. Inset: The magnified EIS plot, The EIS plot shift to right with the number of membrane increases. b, The change of the resistance with the numbers of Base. The resistance of one membrane was calculated from the slope of the linear fit of the resistance vs. the numbers of membranes stacked layer-by-layer. As a result, the membrane resistance is 0.07846 Ω for this sample. The conductivity and area resistance of a membrane is calculated by equation (1). The effective area is 1.766 cm2 and the thickness of Base membrane is 105 μm measured with a micrometer caliper. As a result, the conductivity of Base is 0.076 S cm −1 and the area resistance is 0.138 Ω cm2. c,d,e,f, The change of the resistance with the numbers of LDH-M (c) Nf115 (d) Nf212 (e) and PBI (f) . The membrane conductivity of the membranes were measured and calculated with the same procedure as Base.

Supplementary Figure 7. The visual experiment of the white precipitate of silver chloride verifies that the chloride ion is exchanged after soaking MgAl-Cl-LDH in 3 mol L−1 NaOH solution. a, The pure 3 mol L−1 NaOH solution supernatant, by adjusting the pH to acidity with 3 mol L−1 nitric acid, then adding 1 mol L−1 AgNO3 into above solution, finally no white precipitation of AgCl was observed. b, In contrast, taking the NaOH supernatant which soaked with MgAl-Cl-LDH, by adjusting the pH to acidity with 3 mol L−1 nitric acid, then adding 1 mol L−1 AgCl into above solution , finally a white precipitate appears, which proves that there exists exchanged Cl− in the supernatant.

Supplementary Figure 8. The ETEM images of prepared samples. The red cycle represent the selected area for (003) plane diffraction of a, MgAl-Cl-LDH and b, MgAl-OH-LDH.

Supplementary Figure 9. The XPS survey spectra of MgAl-Cl-LDH and MgAl-OH-LDH samples. Note that the disappearance of Cl element could be observed for MgAl-OH-LDH sample.

Supplementary Figure 10. The FT-IR spectra of prepared MgAl-Cl-LDH and MgAl-OH-LDH samples.

Supplementary Figure 11. Optimized structures for layered double hydroxide. a, model-0 (3 × 3 × 1 supercells of Mg2Al(OH)6Cl·2H2O); b, model-1 (model-0 structure with Cl− substituted by OH− with the addition of two water molecules per layer), c, model-2 (model-0 structure with two Cl− substituted by one Zn(OH)42− and other Cl− substituted by OH−), and d model-3 (model-0 structure with four Cl− substituted by one Fe(CN)64− and other Cl− substituted by OH−). Mg atoms of hydrotalcite layer were shown in orange octahedra, Al atoms of hydrotalcite layer were shown in iceblue octahedra, Cl anions were shown in green balls, Zn atom was shown in yellow ball, Fe atom was shown in pink ball, N atoms were shown in blue balls, C atoms were shown in tan balls, O atoms in hydroxide ions and water molecules were shown in red balls, O atoms of LDHs were shown in red stick, H atoms in hydroxide ions and water molecules were shown in white balls, and H atoms of LDHs were shown in white sticks, respectively.

Supplementary Figure 12. Contact angle of prepared membranes using 3M NaOH as feeding solution. Contact angle of a, Base membrane and b, LDH-M membrane. As time processes, the contact angle values decreases, while LDH-M shows better wettability with NaOH solution than Base.

Supplementary Figure 13. Electrochemical performance of the alkaline zinc-iron flow battery employing LDH-M membrane and Base at the current density of 80 mA cm−2. a, Cycling performance of AZIFB with LDH-M. b, The comparison of discharge capacity for AZIFB with LDH-M and Base.

Supplementary Figure 14 . The electrolytes cross over images of alkaline zinc iron flow battery with Base and LDH-M at the current density of 80 mA cm−2. a, The negative and positive electrolytes image at the end of 5th discharge for AZIFB with Base. The obvious color change of negative electrolyte can be found, indicating the cross-over of the electrolyte. b, The negative and positive electrolytes image at the end of 5th discharge for AZIFB with LDH-M.

Supplementary Figure 15. The SEM images of the LDH-M membrane after nearly 400 cycles charging-discharging test at the current density of 200 mA cm-2. a, The cross-section and b, surface morphology of LDH-M.

Supplementary Figure 16. Electrochemical performance of the alkaline zinc-iron flow battery employing LDH-M membrane. a, The open-cell voltage (OCV) versus state-of-charge (SOC) of AZIFB. b, The polarization curves of AZIFB at 90% SOC, 60% SOC, and 30% SOC.