Table 1 | Substrate scoping investigations. Comparison of the catalytic performance of electrooxidation of benzyl alcohol derivatives and alcohols with vicinal C=C, C=O and -OH groups over CoOOH and Au/CoOOH catalysts.

| Entry | Reactant | CoOOH vs. Au/CoOOH |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Charge transfer (C cm−2 h−1) | Production rate (mmol cm−2 h−1) |  | FEtotal (%) |
|  |  |  | aldehyde | acid |  |
| 1 |  | 74.5/1207.2 | 0.054/0.44 | 0.16/2.86 | 97/98 |
| 2 |  | 116.2/1020.1 | 0.13/0.86 | 0.20/1.81 | 88/85 |
| 3 |  | 71.8/1148.2 | 0.10/2.70 | 0.12/1.30 | 91/89 |
| 4 |  | 81.0/638.1 | 0.037/0.085 | 0.19/1.58 | 99/99 |
| 5 |  | 71.2/891.7 | 0.20/3.23 | 0.083/0.61 | 99/96 |
| 6 |  | 43.3/110.2 | 0.00/0.00 | 0.11/0.29 | 98/100 |
| 7 |  | 26.1/61.2 | 0.068/0.12 | 0.030/0.090 | 95/95 |
| 8 |  | 62.7/651.9 | 0.014/0.52 | 0.15/1.45 | 97/100 |
| 9 |  | 135.1/255.5 | 0.00/0.00 | 0.037/0.71a | 85/85 |
| 10 |  | 38.2/322.9 | 0.00/0.00 | 0.12/0.90b | 97/98 |
| 11 |  | 13.4/253.2 | 0.00/0.00 | 0.041/0.77c | 97/96 |
| 12 |  | 44.3/406.2 | 0.00/0.00 | 0.17/1.38d | 98/91 |

Note. Entries 1-7 were reacted in 1 M KOH with 0.1 M reactant at 60 ºC, Entries 8-12 were reacted in 1 M KOH with 0.3 M reactant at r.t. aThe total productivity of pyruvic acid, acetic acid and formic acid. bThe total productivity of glycolic acid and formic acid. cThe total productivity of lactic acid, acetic acid and formic acid. dThe total productivity of glyceric acid, lactic acid, glycolic acid and formic acid.