Fluorescent Indolo[2,3-b]quinoxalin-2-yl)(phenyl)methanone Dyes: Photophysical, AIE activity, Electrochemical, and Theoretical studies

Deepali N. Kanekara, Sudhakar S. Dhanawadea, Anand B. Jadhava, Mohmmed Ghadiyalib, Sajeev Chackob and  Rajesh M. Kamblea*

aDepartment of Chemistry, University of Mumbai, Santacruz (E), Mumbai 400 098, India

bDepartment of Physics, University of Mumbai, Santacruz (E), Mumbai 400 098, India

e-mail: kamblerm@chem.mu.ac.in

| Sr. No. |  | Pg. No. |
| --- | --- | --- |
|  | Enlarged Emission spectra of dyes | 3 |
| 2. | Aggregation Induced Emission study of dye 2 in THF−water mixture (10-5 M) | 4 |
| 3. | Absorption spectra of 1 and 2 in THF/Water mixture (0‒100%) | 5 |
| 4. | Cyclic voltammetry (CV) of compounds 1‒4 in anhydrous dichloromethane | 6 |
| 5. | MALDI-TOF Spectra of compounds 1‒4 | 7‒8 |
| 6. | FTIR Spectra of compounds 1‒4 | 9‒10 |
| 7. | 1H and 13C NMR Spectra of compounds 1‒4 | 11‒14 |
| 8. | Optimized structures of compounds 1‒4 | 15‒16 |
| 9. | Frontier molecular orbitals of compound 1‒4 | 17‒20 |
| 10. | Cartesian coordinates and Charges (Mulliken and Lowdin) of compounds 1‒4 | 21‒25 |
| A) | Table S1. Cartesian coordinates of optimized structure of compound 1 |  |
| B) | Table S2. Cartesian coordinates of optimized structure of compound 2 |  |
| C) | TableS3. Cartesian coordinates of optimized structure of compound 3 |  |
| D) | TableS4. Cartesian coordinates of optimized structure of compound 4 |  |
| 11. |  |  |
| a. | Main vertical electronic transition of 1‒4 in gas, toluene, chloroform and DMSO | 26‒30 |
| b. | Simulated absorption spectra of 1‒4 in gas, toluene, chloroform and DMSO | 31 |

- Enlarged Emission spectra of dyes

Figure S1. Enlarged Emission spectra of dyes 1‒4 toluene (a), ethyl acetate (b), chloroform (c) and DMSO(d).

- Aggregation Induced Emission study of Dye 2

Figure S2. Fluorescence image of 2 in THF‒water mixture with subsequently increasing water fractions (10-5 M) by 10% up to 80% and by 5% from 80% to 100% under UV‒Visible light (a); Fluorescence spectra of 2 in THF−water mixture (10-5 M) with increasing water fractions (ƒw) (b); plots of PL intensity and peak wavelength versus ƒw (c) and DLS plot of 2 obtained for nano-aggregates formed in fw = 95% of THF−water mixture (d).

- Absorption Spectra of AIE studies in THF−water Mixture

Figure S3. Absorption spectra of 1 (a) and 2 (b) (10-5 M) in THF−water mixture with increasing water fractions (ƒw).

- Cyclic voltammetry (CV) of compounds 1, 2 and 4 in anhydrous dichloromethane

Figure S4: Cyclic voltammetry of compounds 1, 2 and 4.

- MALDI-TOF spectra of compounds 1‒4

Figure S5: MALDI-TOF mass of 1.

Figure S6: MALDI-TOF mass of 2.

Figure S7: MALDI-TOF mass of 3.

Figure S8: MALDI-TOF mass of 4.

- FTIR spectra of compounds 1‒4

Figure S9: FTIR Spectra of 1.

Figure S10: FTIR Spectra of 2.

Figure S11: FTIR Spectra of 3.

Figure S12: FTIR Spectra of 4.

- 1H and 13C NMR spectra of compounds 1‒4

Figure S13: 1H-NMR (above) and 13C-NMR (below) spectra in CDCl3 of compound 1.

Figure S14: 1H-NMR (above) and 13C-NMR (below) spectra in CDCl3 of compound 2.

Figure S15: 1H-NMR (above) and 13C-NMR (below) spectra in CDCl3 of compound 3

Figure S16: 1H-NMR spectra in CDCl3 of compound 4.

- Optimized structures of compounds 1‒4

Figure S17: Optimized structures of compound 1.

Figure S18: Optimized structures of compound 2.

Figure S19: Optimized structures of compound 3.

Figure S20: Optimized structures of compound 4.

- Frontier molecular orbitals of compounds 1‒4

Figure S21: Frontier molecular orbital of compound 1.

Figure S22: Frontier molecular orbital of compound 2.

Figure S23: Frontier molecular orbital of compound 3.

Figure S24: Frontier molecular orbital of compound 4.

- Cartesian coordinates and charges (Mulliken and Lowdin) of compounds 1‒4.

- Table S1: Cartesian coordinates of optimized structure of compound 1.

Total Energy: – 1087.159 Hartrees

| Atoms | X | Y | Z | Mulliken | Lowdin |
| --- | --- | --- | --- | --- | --- |
| C | -4.42247 | -2.28742 | -0.31272 | -0.30429 | -0.04167 |
| C | -4.92745 | -1.47033 | 0.70045 | -0.29702 | -0.03152 |
| C | -4.10038 | -0.53183 | 1.31458 | -0.21868 | -0.04437 |
| C | -2.77564 | -0.39453 | 0.90482 | -0.97112 | -0.02848 |
| C | -2.26165 | -1.21079 | -0.11088 | 1.35008 | -0.09321 |
| C | -3.09471 | -2.16803 | -0.70607 | 0.35190 | -0.00050 |
| C | -0.82229 | -1.16105 | -0.53473 | -1.50180 | 0.02312 |
| C | -0.06935 | 0.13504 | -0.47271 | 1.35124 | -0.09428 |
| C | -0.69757 | 1.39141 | -0.69042 | -0.89434 | -0.02062 |
| C | 0.03212 | 2.55579 | -0.69299 | -0.29322 | -0.02473 |
| C | 1.42723 | 2.53467 | -0.45588 | -0.08771 | -0.03613 |
| C | 2.06982 | 1.26817 | -0.23249 | 0.06812 | -0.05961 |
| C | 1.29651 | 0.08819 | -0.26357 | 0.03678 | 0.03349 |
| N | 2.12389 | 3.71084 | -0.44876 | -0.05110 | -0.06131 |
| C | 3.40199 | 3.57352 | -0.22179 | -0.00176 | -0.02826 |
| C | 4.06605 | 2.30364 | 0.00890 | 0.08509 | -0.03810 |
| N | 3.41453 | 1.17089 | 0.00404 | 0.06882 | -0.01285 |
| N | 4.33719 | 4.58036 | -0.15835 | 0.05534 | -0.05529 |
| C | 5.58719 | 4.01292 | 0.10641 | 0.19015 | -0.01867 |
| C | 5.46673 | 2.60548 | 0.21807 | 0.64852 | -0.07022 |
| C | 6.81775 | 4.64759 | 0.25549 | -0.44127 | -0.05679 |
| C | 7.92885 | 3.84665 | 0.51939 | -0.33351 | -0.02135 |
| C | 7.82247 | 2.45336 | 0.63214 | -0.39441 | -0.05826 |
| C | 6.59014 | 1.82368 | 0.48193 | -0.64444 | 0.00308 |
| O | -0.26821 | -2.17537 | -0.92627 | -0.18668 | -0.16202 |
| C | 4.06339 | 5.99323 | -0.34130 | -0.33418 | 0.02597 |
| H | -5.06359 | -3.02085 | -0.78861 | 0.17593 | 0.05580 |
| H | -5.96095 | -1.56957 | 1.01329 | 0.16089 | 0.05489 |
| H | -4.48519 | 0.09211 | 2.11332 | 0.18070 | 0.05567 |
| H | -2.13570 | 0.33012 | 1.39370 | 0.17491 | 0.06897 |
| H | -2.68103 | -2.81092 | -1.47354 | 0.21328 | 0.07294 |
| H | -1.76231 | 1.42893 | -0.88456 | 0.17768 | 0.07001 |
| H | -0.43669 | 3.51506 | -0.87805 | 0.18403 | 0.06814 |
| H | 1.79586 | -0.86193 | -0.11905 | 0.26197 | 0.08675 |
| H | 6.91657 | 5.72295 | 0.17148 | 0.15333 | 0.06348 |
| H | 8.89852 | 4.31647 | 0.63980 | 0.17578 | 0.05633 |
| H | 8.70869 | 1.86494 | 0.83736 | 0.16985 | 0.05510 |
| H | 6.49451 | 0.74768 | 0.56598 | 0.18317 | 0.06985 |
| H | 4.33275 | 6.55950 | 0.55479 | 0.17423 | 0.05946 |
| H | 2.99680 | 6.10678 | -0.52773 | 0.18750 | 0.07547 |
| H | 4.62053 | 6.38852 | -1.19547 | 0.17626 | 0.05970 |

- Table S2: Cartesian coordinates of optimized structure of compound 2.

Total Energy: – 1126.486 Hartrees

| Atoms | X | Y | Z | Mulliken | Lowdin |
| --- | --- | --- | --- | --- | --- |
| C | -4.44194 | -2.27347 | 0.31290 | -0.34419 | -0.04190 |
| C | -4.90127 | -1.50969 | -0.76173 | -0.24381 | -0.03186 |
| C | -4.04687 | -0.60328 | -1.38655 | -0.28580 | -0.04449 |
| C | -2.74092 | -0.44433 | -0.92723 | -0.84527 | -0.02828 |
| C | -2.27262 | -1.20757 | 0.14985 | 1.31634 | -0.09320 |
| C | -3.13213 | -2.13351 | 0.75664 | 0.37393 | -0.00077 |
| C | -0.85218 | -1.13507 | 0.63072 | -1.78015 | 0.02279 |
| C | -0.09826 | 0.15808 | 0.53717 | 1.40056 | -0.09512 |
| C | -0.73548 | 1.42131 | 0.67484 | -0.75698 | -0.02122 |
| C | -0.00743 | 2.58641 | 0.65166 | -0.43541 | -0.02514 |
| C | 1.39544 | 2.55871 | 0.46561 | 0.18427 | -0.03653 |
| C | 2.04705 | 1.28516 | 0.32228 | -0.06903 | -0.06008 |
| C | 1.27430 | 0.10572 | 0.37936 | 0.08825 | 0.03292 |
| N | 2.09005 | 3.73532 | 0.43036 | -0.04836 | -0.06215 |
| C | 3.37589 | 3.59213 | 0.25457 | 0.09583 | -0.02842 |
| C | 4.04972 | 2.31412 | 0.10409 | 0.06253 | -0.03719 |
| N | 3.39929 | 1.18098 | 0.13723 | 0.07655 | -0.01398 |
| N | 4.31084 | 4.59677 | 0.17876 | 0.04464 | -0.05547 |
| C | 5.57012 | 4.01840 | -0.01710 | 0.23592 | -0.02082 |
| C | 5.45614 | 2.61037 | -0.07014 | 0.15796 | -0.06487 |
| C | 6.80898 | 4.63926 | -0.15288 | -0.22939 | -0.04911 |
| C | 7.92310 | 3.82475 | -0.34303 | -0.62088 | -0.02314 |
| C | 7.83849 | 2.42003 | -0.40108 | 0.30957 | -0.09939 |
| C | 6.58830 | 1.81803 | -0.26116 | -0.84903 | -0.00371 |
| O | -0.31514 | -2.12869 | 1.09288 | -0.18555 | -0.16229 |
| C | 4.03092 | 6.01572 | 0.28705 | -0.32682 | 0.02566 |
| C | 9.08511 | 1.59370 | -0.61499 | -0.36611 | -0.06098 |
| H | -5.10428 | -2.98193 | 0.79751 | 0.17460 | 0.05570 |
| H | -5.92043 | -1.62543 | -1.11352 | 0.16075 | 0.05480 |
| H | -4.39575 | -0.02096 | -2.23187 | 0.18005 | 0.05560 |
| H | -2.07920 | 0.25520 | -1.42364 | 0.17862 | 0.06910 |
| H | -2.75302 | -2.73628 | 1.57298 | 0.21537 | 0.07282 |
| H | -1.80676 | 1.46480 | 0.82785 | 0.18351 | 0.06991 |
| H | -0.48361 | 3.55176 | 0.77669 | 0.17758 | 0.06798 |
| H | 1.77970 | -0.84852 | 0.29562 | 0.26235 | 0.08645 |
| H | 6.91351 | 5.71681 | -0.11362 | 0.14981 | 0.06373 |
| H | 8.89599 | 4.29411 | -0.45073 | 0.16946 | 0.06149 |
| H | 6.48618 | 0.73917 | -0.29909 | 0.17252 | 0.07235 |
| H | 4.33477 | 6.54129 | -0.62278 | 0.17232 | 0.05903 |
| H | 2.95802 | 6.13629 | 0.42732 | 0.19322 | 0.07526 |
| H | 4.55503 | 6.45078 | 1.14296 | 0.17499 | 0.05928 |
| H | 9.83275 | 1.79192 | 0.15914 | 0.15753 | 0.05274 |
| H | 8.85915 | 0.52598 | -0.59440 | 0.15398 | 0.04921 |
| H | 9.55009 | 1.81700 | -1.58052 | 0.16375 | 0.05330 |

- Table S3: Cartesian coordinates of optimized structure of compound 3.

Total Energy: – 3660.700 Hartrees

| Atoms | X | Y | Z | Mulliken | Lowdin |
| --- | --- | --- | --- | --- | --- |
| C | -4.42306 | -2.28564 | -0.29897 | -0.31264 | -0.04097 |
| C | -4.91349 | -1.47782 | 0.72871 | -0.28869 | -0.03047 |
| C | -4.07818 | -0.54407 | 1.33894 | -0.24997 | -0.04388 |
| C | -2.75969 | -0.40237 | 0.91115 | -0.89498 | -0.02823 |
| C | -2.26023 | -1.20957 | -0.11903 | 1.34890 | -0.09392 |
| C | -3.10132 | -2.16206 | -0.71067 | 0.35444 | 0.00017 |
| C | -0.82785 | -1.15466 | -0.56300 | -1.73799 | 0.02308 |
| C | -0.07253 | 0.14077 | -0.49160 | 1.41847 | -0.09230 |
| C | -0.70107 | 1.39955 | -0.69576 | -0.88673 | -0.01825 |
| C | 0.02847 | 2.56376 | -0.69225 | -0.24252 | -0.02367 |
| C | 1.42463 | 2.53980 | -0.46115 | -0.38627 | -0.03499 |
| C | 2.06736 | 1.27056 | -0.25034 | 0.15993 | -0.05842 |
| C | 1.29344 | 0.09054 | -0.28851 | 0.11659 | 0.03455 |
| N | 2.12196 | 3.71499 | -0.44736 | -0.04123 | -0.05859 |
| C | 3.40064 | 3.57554 | -0.22581 | 0.09545 | -0.02809 |
| C | 4.06289 | 2.30429 | -0.00711 | 0.07718 | -0.03926 |
| N | 3.41190 | 1.17147 | -0.01894 | 0.07749 | -0.00883 |
| N | 4.33709 | 4.58233 | -0.15759 | 0.05606 | -0.05370 |
| C | 5.58517 | 4.01200 | 0.09971 | 0.08399 | -0.01952 |
| C | 5.46459 | 2.60446 | 0.20123 | 0.61887 | -0.06204 |
| C | 6.81869 | 4.63969 | 0.25220 | -0.44107 | -0.04545 |
| C | 7.93183 | 3.84092 | 0.50927 | -0.19799 | -0.05757 |
| C | 7.80611 | 2.45028 | 0.60933 | -0.09830 | -0.25393 |
| C | 6.58170 | 1.81169 | 0.45799 | -0.66563 | -0.03361 |
| O | -0.27860 | -2.16149 | -0.97885 | -0.18342 | -0.15978 |
| C | 4.06367 | 5.99737 | -0.32828 | -0.33575 | 0.02729 |
| Br | 9.37386 | 1.40349 | 0.96697 | -0.19555 | 0.26371 |
| H | -5.07073 | -3.01525 | -0.77180 | 0.17687 | 0.05612 |
| H | -5.94222 | -1.58052 | 1.05574 | 0.16236 | 0.05521 |
| H | -4.45164 | 0.07247 | 2.14868 | 0.17986 | 0.05591 |
| H | -2.11314 | 0.31818 | 1.39744 | 0.18422 | 0.06890 |
| H | -2.69863 | -2.79774 | -1.48988 | 0.21524 | 0.07316 |
| H | -1.76684 | 1.43870 | -0.88402 | 0.18229 | 0.07066 |
| H | -0.44083 | 3.52459 | -0.86735 | 0.18904 | 0.06870 |
| H | 1.79308 | -0.86096 | -0.15450 | 0.26181 | 0.08739 |
| H | 6.92591 | 5.71469 | 0.17698 | 0.15802 | 0.06648 |
| H | 8.90402 | 4.30014 | 0.63308 | 0.23447 | 0.06207 |
| H | 6.48933 | 0.73627 | 0.53528 | 0.26394 | 0.07558 |
| H | 4.33555 | 6.55586 | 0.57180 | 0.17570 | 0.06006 |
| H | 2.99657 | 6.11250 | -0.51050 | 0.18974 | 0.07615 |
| H | 4.61799 | 6.39894 | -1.18121 | 0.17779 | 0.06030 |

- Table S4: Cartesian coordinates of optimized structure of compound 4.

Total Energy: – 1291.722 Hartrees

| Atoms | X | Y | Z | Mulliken | Lowdin |
| --- | --- | --- | --- | --- | --- |
| C | -4.43576 | -2.28179 | -0.26240 | -0.35966 | -0.03979 |
| C | -4.88020 | -1.51009 | 0.81293 | -0.24396 | -0.02865 |
| C | -4.02041 | -0.59298 | 1.41430 | -0.27904 | -0.04304 |
| C | -2.72361 | -0.43169 | 0.93108 | -0.87651 | -0.02776 |
| C | -2.27023 | -1.20286 | -0.14705 | 1.31396 | -0.09511 |
| C | -3.13509 | -2.13903 | -0.73071 | 0.39719 | 0.00137 |
| C | -0.86108 | -1.12681 | -0.65368 | -1.71172 | 0.02316 |
| C | -0.09945 | 0.16521 | -0.55350 | 1.40053 | -0.08819 |
| C | -0.73063 | 1.43062 | -0.69959 | -0.82296 | -0.01511 |
| C | 0.00042 | 2.59368 | -0.67507 | -0.42886 | -0.02159 |
| C | 1.40102 | 2.55906 | -0.47798 | 0.15599 | -0.03366 |
| C | 2.04673 | 1.28287 | -0.32462 | -0.03423 | -0.05552 |
| C | 1.26999 | 0.10492 | -0.38462 | 0.08600 | 0.03551 |
| N | 2.10244 | 3.73214 | -0.44103 | -0.04278 | -0.05275 |
| C | 3.38330 | 3.58120 | -0.25361 | 0.09030 | -0.02745 |
| C | 4.04746 | 2.30673 | -0.09260 | -0.00199 | -0.03926 |
| N | 3.39538 | 1.17496 | -0.12740 | 0.08297 | -0.00357 |
| N | 4.32654 | 4.58947 | -0.17286 | 0.05075 | -0.04685 |
| C | 5.57204 | 4.01664 | 0.03621 | 0.16723 | -0.00269 |
| C | 5.45418 | 2.60111 | 0.09439 | 0.80383 | -0.05772 |
| C | 6.80914 | 4.64807 | 0.18230 | -0.44359 | -0.03995 |
| C | 7.92556 | 3.84913 | 0.38892 | -0.18382 | 0.02236 |
| C | 7.79793 | 2.45525 | 0.44546 | -0.60154 | -0.06639 |
| C | 6.57422 | 1.80844 | 0.30039 | -0.66766 | 0.04996 |
| O | -0.33048 | -2.10903 | -1.14408 | -0.17886 | -0.15575 |
| C | 4.04423 | 6.01027 | -0.29081 | -0.31452 | 0.03027 |
| N | 9.00689 | 1.64561 | 0.66811 | -0.17947 | 0.15630 |
| O | 10.07502 | 2.23608 | 0.79445 | -0.00441 | -0.18708 |
| O | 8.87728 | 0.42786 | 0.71504 | 0.00156 | -0.17988 |
| H | -5.10254 | -2.99843 | -0.72831 | 0.17751 | 0.05666 |
| H | -5.89227 | -1.62815 | 1.18373 | 0.16297 | 0.05577 |
| H | -4.35781 | -0.00494 | 2.26022 | 0.18254 | 0.05630 |
| H | -2.05744 | 0.27499 | 1.41123 | 0.17303 | 0.06879 |
| H | -2.76724 | -2.74680 | -1.54844 | 0.21685 | 0.07358 |
| H | -1.80087 | 1.47649 | -0.85917 | 0.18695 | 0.07172 |
| H | -0.47117 | 3.56024 | -0.80667 | 0.18200 | 0.06959 |
| H | 1.77121 | -0.85099 | -0.29543 | 0.26644 | 0.08847 |
| H | 6.90668 | 5.72526 | 0.13887 | 0.17465 | 0.06911 |
| H | 8.90687 | 4.28659 | 0.50957 | 0.26474 | 0.08244 |
| H | 6.51017 | 0.73008 | 0.34850 | 0.28039 | 0.09463 |
| H | 4.33810 | 6.53874 | 0.61977 | 0.17727 | 0.06209 |
| H | 2.97233 | 6.12561 | -0.44096 | 0.19951 | 0.07730 |
| H | 4.57433 | 6.43977 | -1.14491 | 0.18041 | 0.06237 |

- Main vertical electronic transition of 1‒4 in gas, toluene, chloroform and DMSO

Compound 1

Table S5: Electronic transition of 1 in gas phase

| 1 | 404.6nm ( 3.1eV) | 0.0404 | (HOMO -> LUMO ) (96%) |
| --- | --- | --- | --- |
| 2 | 357.1nm ( 3.5eV) | 0.0032 | (HOMO-2 -> LUMO ) (47%) |
| 3 | 348.9nm ( 3.6eV) | 0.0037 | (HOMO-3 -> LUMO ) (92%) |
| 4 | 345.9nm ( 3.6eV) | 0.0906 | (HOMO-1 -> LUMO ) (59%) |
| 5 | 315.8nm ( 3.9eV) | 0.7610 | (HOMO -> LUMO+1) (59%) |
| 6 | 311.1nm ( 4.0eV) | 0.0572 | (HOMO-4 -> LUMO ) (44%) |
| 7 | 295.6nm ( 4.2eV) | 0.0082 | (HOMO-4 -> LUMO ) (45%) |
| 8 | 290.3nm ( 4.3eV) | 0.0716 | (HOMO-1 -> LUMO+1) (79%) |
| 9 | 287.2nm ( 4.3eV) | 0.0080 | (HOMO-5 -> LUMO ) (87%) |
| 10 | 282.0nm ( 4.4eV) | 0.0330 | (HOMO-6 -> LUMO ) (82%) |

Table S6: Electronic transition of 1 in toluene

| 1 | 415.4nm ( 3.0eV) | 0.0692 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 354.6nm ( 3.5eV) | 0.1034 | (HOMO-1 -> LUMO ) (49%) |
| 3 | 349.1nm ( 3.6eV) | 0.1114 | (HOMO-2 -> LUMO ) (38%) |
| 4 | 346.5nm ( 3.6eV) | 0.0115 | (HOMO-3 -> LUMO ) (58%) |
| 5 | 327.4nm ( 3.8eV) | 1.0217 | (HOMO -> LUMO+1) (67%) |
| 6 | 310.9nm ( 4.0eV) | 0.0040 | (HOMO-2 -> LUMO ) (31%) |
| 7 | 295.1nm ( 4.2eV) | 0.1307 | (HOMO-1 -> LUMO+1) (85%) |
| 8 | 293.1nm ( 4.2eV) | 0.0102 | (HOMO-4 -> LUMO ) (28%) |
| 9 | 289.9nm ( 4.3eV) | 0.0094 | (HOMO-5 -> LUMO ) (86%) |
| 10 | 280.6nm ( 4.4eV) | 0.0554 | (HOMO-6 -> LUMO ) (70%) |

Table S7: Electronic transition of 1 in chloroform

| 1 | 422.0nm ( 2.9eV) | 0.0895 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 357.7nm ( 3.5eV) | 0.2329 | (HOMO-1 -> LUMO ) (71%) |
| 3 | 347.4nm ( 3.6eV) | 0.1501 | (HOMO-2 -> LUMO ) (38%) |
| 4 | 345.2nm ( 3.6eV) | 0.0264 | (HOMO-4 -> LUMO ) (73%) |
| 5 | 333.4nm ( 3.7eV) | 0.9925 | (HOMO -> LUMO+1) (65%) |
| 6 | 311.3nm ( 4.0eV) | 0.0052 | (HOMO-3 -> LUMO ) (37%) |
| 7 | 297.8nm ( 4.2eV) | 0.1730 | (HOMO-1 -> LUMO+1) (87%) |
| 8 | 293.3nm ( 4.2eV) | 0.0162 | (HOMO-3 -> LUMO ) (32%) |
| 9 | 291.2nm ( 4.3eV) | 0.0154 | (HOMO-5 -> LUMO ) (61%) |
| 10 | 279.5nm ( 4.4eV) | 0.0661 | (HOMO-6 -> LUMO ) (59%) |

Table S8: Electronic transition of 1 in DMSO

| 1 | 430.7nm ( 2.9eV) | 0.1181 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 362.8nm ( 3.4eV) | 0.4158 | (HOMO-1 -> LUMO ) (82%) |
| 3 | 347.3nm ( 3.6eV) | 0.6154 | (HOMO -> LUMO+1) (44%) |
| 4 | 343.9nm ( 3.6eV) | 0.0304 | (HOMO-4 -> LUMO ) (81%) |
| 5 | 337.8nm ( 3.7eV) | 0.4955 | (HOMO -> LUMO+1) (34%) |
| 6 | 312.1nm ( 4.0eV) | 0.0108 | (HOMO-2 -> LUMO ) (38%) |
| 7 | 301.3nm ( 4.1eV) | 0.2270 | (HOMO-1 -> LUMO+1) (88%) |
| 8 | 295.5nm ( 4.2eV) | 0.0195 | (HOMO-5 -> LUMO ) (52%) |
| 9 | 292.4nm ( 4.2eV) | 0.0385 | (HOMO-3 -> LUMO ) (30%) |
| 10 | 277.9nm ( 4.5eV) | 0.0853 | (HOMO-6 -> LUMO ) (45%) |

Compound 2

Table S9: Electronic transition of 2 in gas

| 1 | 416.6nm ( 3.0eV) | 0.0337 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 357.1nm ( 3.5eV) | 0.0031 | (HOMO-2 -> LUMO ) (40%) |
| 3 | 350.0nm ( 3.5eV) | 0.0563 | (HOMO-1 -> LUMO ) (43%) |
| 4 | 348.8nm ( 3.6eV) | 0.0163 | (HOMO-4 -> LUMO ) (74%) |
| 5 | 320.4nm ( 3.9eV) | 0.8341 | (HOMO -> LUMO+1) (55%) |
| 6 | 314.2nm ( 3.9eV) | 0.0006 | (HOMO-2 -> LUMO ) (38%) |
| 7 | 295.8nm ( 4.2eV) | 0.0016 | (HOMO-3 -> LUMO ) (47%) |
| 8 | 291.7nm ( 4.3eV) | 0.0621 | (HOMO-1 -> LUMO+1) (80%) |
| 9 | 285.8nm ( 4.3eV) | 0.0050 | (HOMO-5 -> LUMO ) (88%) |
| 10 | 280.7nm ( 4.4eV) | 0.0398 | (HOMO-6 -> LUMO ) (83%) |

Table S10: Electronic transition of 2 in toluene

| 1 | 429.2nm ( 2.9eV) | 0.0533 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 358.2nm ( 3.5eV) | 0.0876 | (HOMO-1 -> LUMO ) (52%) |
| 3 | 349.7nm ( 3.5eV) | 0.1020 | (HOMO-2 -> LUMO ) (38%) |
| 4 | 346.6nm ( 3.6eV) | 0.0102 | (HOMO-4 -> LUMO ) (87%) |
| 5 | 333.1nm ( 3.7eV) | 1.0328 | (HOMO -> LUMO+1) (57%) |
| 6 | 314.2nm ( 3.9eV) | 0.0016 | (HOMO-2 -> LUMO ) (46%) |
| 7 | 296.5nm ( 4.2eV) | 0.1156 | (HOMO-1 -> LUMO+1) (87%) |
| 8 | 292.6nm ( 4.2eV) | 0.0158 | (HOMO-3 -> LUMO ) (51%) |
| 9 | 288.7nm ( 4.3eV) | 0.0075 | (HOMO-5 -> LUMO ) (87%) |
| 10 | 279.7nm ( 4.4eV) | 0.0687 | (HOMO-6 -> LUMO ) (71%) |

Table S11: Electronic transition of 2 in Chloroform

| 1 | 436.7nm ( 2.8eV) | 0.0662 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 361.9nm ( 3.4eV) | 0.1502 | (HOMO-1 -> LUMO ) (61%) |
| 3 | 348.5nm ( 3.6eV) | 0.3710 | (HOMO-2 -> LUMO ) (29%) |
| 4 | 345.3nm ( 3.6eV) | 0.0347 | (HOMO-4 -> LUMO ) (88%) |
| 5 | 338.8nm ( 3.7eV) | 0.8309 | (HOMO -> LUMO+1) (45%) |
| 6 | 314.6nm ( 3.9eV) | 0.0038 | (HOMO-2 -> LUMO ) (50%) |
| 7 | 299.3nm ( 4.1eV) | 0.1539 | (HOMO-1 -> LUMO+1) (88%) |
| 8 | 292.4nm ( 4.2eV) | 0.0275 | (HOMO-3 -> LUMO ) (47%) |
| 9 | 290.5nm ( 4.3eV) | 0.0181 | (HOMO-5 -> LUMO ) (74%) |
| 10 | 279.1nm ( 4.4eV) | 0.0784 | (HOMO-6 -> LUMO ) (58%) |

Table S12: Electronic transition of 2 in DMSO

| 1 | 446.4nm ( 2.8eV) | 0.0838 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 366.9nm ( 3.4eV) | 0.2737 | (HOMO-1 -> LUMO ) (71%) |
| 3 | 352.8nm ( 3.5eV) | 1.0685 | (HOMO -> LUMO+1) (58%) |
| 4 | 343.9nm ( 3.6eV) | 0.0132 | (HOMO-4 -> LUMO ) (89%) |
| 5 | 339.8nm ( 3.6eV) | 0.1946 | (HOMO-2 -> LUMO ) (27%) |
| 6 | 315.7nm ( 3.9eV) | 0.0105 | (HOMO-2 -> LUMO ) (54%) |
| 7 | 302.8nm ( 4.1eV) | 0.2043 | (HOMO-1 -> LUMO+1) (90%) |
| 8 | 294.5nm ( 4.2eV) | 0.0206 | (HOMO-5 -> LUMO ) (53%) |
| 9 | 292.0nm ( 4.2eV) | 0.0616 | (HOMO-5 -> LUMO ) (31%) |
| 10 | 278.8nm ( 4.4eV) | 0.0861 | (HOMO-2 -> LUMO+1) (40%) |

Compound 3

Table S13: Electronic transition of 3 in gas

| 1 | 418.3nm ( 3.0eV) | 0.0310 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 360.0nm ( 3.4eV) | 0.0019 | (HOMO-2 -> LUMO ) (49%) |
| 3 | 350.5nm ( 3.5eV) | 0.0023 | (HOMO-4 -> LUMO ) (92%) |
| 4 | 346.6nm ( 3.6eV) | 0.0708 | (HOMO-1 -> LUMO ) (57%) |
| 5 | 321.5nm ( 3.9eV) | 0.0050 | (HOMO-3 -> LUMO ) (40%) |
| 6 | 316.9nm ( 3.9eV) | 0.9085 | (HOMO -> LUMO+1) (53%) |
| 7 | 302.7nm ( 4.1eV) | 0.0262 | (HOMO-3 -> LUMO ) (45%) |
| 8 | 293.3nm ( 4.2eV) | 0.0030 | (HOMO-5 -> LUMO ) (91%) |
| 9 | 288.7nm ( 4.3eV) | 0.0094 | (HOMO-6 -> LUMO ) (76%) |
| 10 | 286.2nm ( 4.3eV) | 0.0383 | (HOMO-1 -> LUMO+1) (69%) |

Table S14: Electronic transition of 3 in toluene

| 1 | 426.9nm ( 2.9eV) | 0.0524 | (HOMO -> LUMO ) (97%) |
| --- | --- | --- | --- |
| 2 | 354.5nm ( 3.5eV) | 0.0165 | (HOMO-2 -> LUMO ) (25%) |
| 3 | 351.0nm ( 3.5eV) | 0.1520 | (HOMO-1 -> LUMO ) (47%) |
| 4 | 348.4nm ( 3.6eV) | 0.0135 | (HOMO-4 -> LUMO ) (75%) |
| 5 | 328.4nm ( 3.8eV) | 1.1793 | (HOMO -> LUMO+1) (60%) |
| 6 | 320.5nm ( 3.9eV) | 0.0076 | (HOMO-2 -> LUMO ) (44%) |
| 7 | 299.5nm ( 4.1eV) | 0.0011 | (HOMO-3 -> LUMO ) (50%) |
| 8 | 295.4nm ( 4.2eV) | 0.0105 | (HOMO-5 -> LUMO ) (77%) |
| 9 | 290.6nm ( 4.3eV) | 0.0557 | (HOMO-1 -> LUMO+1) (76%) |
| 10 | 286.0nm ( 4.3eV) | 0.0465 | (HOMO-6 -> LUMO ) (69%) |

Table S15: Electronic transition of 3 in Chloroform

| 1 | 432.4nm ( 2.9eV) | 0.0676 | (HOMO -> LUMO ) (98%) |
| --- | --- | --- | --- |
| 2 | 356.0nm ( 3.5eV) | 0.1594 | (HOMO-1 -> LUMO ) (59%) |
| 3 | 350.0nm ( 3.5eV) | 0.1608 | (HOMO-2 -> LUMO ) (35%) |
| 4 | 347.2nm ( 3.6eV) | 0.0249 | (HOMO-5 -> LUMO ) (45%) |
| 5 | 334.5nm ( 3.7eV) | 1.1813 | (HOMO -> LUMO+1) (61%) |
| 6 | 320.4nm ( 3.9eV) | 0.0046 | (HOMO-2 -> LUMO ) (47%) |
| 7 | 298.8nm ( 4.2eV) | 0.0017 | (HOMO-3 -> LUMO ) (46%) |
| 8 | 296.6nm ( 4.2eV) | 0.0242 | (HOMO-4 -> LUMO ) (44%) |
| 9 | 293.0nm ( 4.2eV) | 0.0908 | (HOMO-1 -> LUMO+1) (82%) |
| 10 | 284.4nm ( 4.4eV) | 0.0497 | (HOMO-6 -> LUMO ) (62%) |

Table S16: Electronic transition of 3 in DMSO

| 1 | 439.8nm ( 2.8eV) | 0.0896 | (HOMO -> LUMO ) (98%) |
| --- | --- | --- | --- |
| 2 | 360.4nm ( 3.4eV) | 0.3446 | (HOMO-1 -> LUMO ) (75%) |
| 3 | 349.3nm ( 3.5eV) | 0.6221 | (HOMO -> LUMO+1) (34%) |
| 4 | 346.0nm ( 3.6eV) | 0.0488 | (HOMO-5 -> LUMO ) (82%) |
| 5 | 339.4nm ( 3.7eV) | 0.6701 | (HOMO -> LUMO+1) (37%) |
| 6 | 320.6nm ( 3.9eV) | 0.0090 | (HOMO-2 -> LUMO ) (51%) |
| 7 | 299.9nm ( 4.1eV) | 0.0154 | (HOMO-4 -> LUMO ) (45%) |
| 8 | 297.2nm ( 4.2eV) | 0.0525 | (HOMO-3 -> LUMO ) (32%) |
| 9 | 296.2nm ( 4.2eV) | 0.1271 | (HOMO-1 -> LUMO+1) (81%) |
| 10 | 282.3nm ( 4.4eV) | 0.0635 | (HOMO-6 -> LUMO ) (50%) |

Compound 4

Table S17: Electronic transition of 4 in gas

| 1 | 393.4nm ( 3.2eV) | 0.0681 | (HOMO -> LUMO ) (91%) |
| --- | --- | --- | --- |
| 2 | 362.4nm ( 3.4eV) | 0.0020 | (HOMO-2 -> LUMO ) (52%) |
| 3 | 354.6nm ( 3.5eV) | 0.0600 | (HOMO -> LUMO+1) (68%) |
| 4 | 350.4nm ( 3.5eV) | 0.0030 | (HOMO-5 -> LUMO ) (77%) |
| 5 | 333.1nm ( 3.7eV) | 0.3555 | (HOMO-1 -> LUMO ) (60%) |
| 6 | 326.4nm ( 3.8eV) | 0.0000 | (HOMO-7 -> LUMO+1) (80%) |
| 7 | 322.0nm ( 3.9eV) | 0.0813 | (HOMO-1 -> LUMO+1) (52%) |
| 8 | 316.3nm ( 3.9eV) | 0.2474 | (HOMO-1 -> LUMO+1) (32%) |
| 9 | 305.1nm ( 4.1eV) | 0.0587 | (HOMO-4 -> LUMO ) (44%) |
| 10 | 302.8nm ( 4.1eV) | 0.0038 | (HOMO-3 -> LUMO ) (89%) |

Table S18: Electronic transition of 4 in toluene

| 1 | 400.0nm ( 3.1eV) | 0.1634 | (HOMO -> LUMO ) (87%) |
| --- | --- | --- | --- |
| 2 | 369.6nm ( 3.4eV) | 0.1572 | (HOMO -> LUMO+1) (82%) |
| 3 | 355.7nm ( 3.5eV) | 0.0317 | (HOMO-2 -> LUMO ) (42%) |
| 4 | 348.8nm ( 3.6eV) | 0.0084 | (HOMO-5 -> LUMO ) (62%) |
| 5 | 343.8nm ( 3.6eV) | 0.3582 | (HOMO-1 -> LUMO ) (78%) |
| 6 | 333.1nm ( 3.7eV) | 0.3695 | (HOMO-1 -> LUMO+1) (89%) |
| 7 | 321.1nm ( 3.9eV) | 0.0000 | (HOMO-8 -> LUMO+1) (61%) |
| 8 | 316.4nm ( 3.9eV) | 0.3324 | (HOMO -> LUMO+2) (41%) |
| 9 | 308.5nm ( 4.0eV) | 0.2798 | (HOMO-4 -> LUMO ) (20%) |
| 10 | 304.6nm ( 4.1eV) | 0.0368 | (HOMO-3 -> LUMO ) (59%) |

Table S19: Electronic transition of 4 in Chloroform

| 1 | 405.1nm ( 3.1eV) | 0.2601 | (HOMO -> LUMO ) (81%) |
| --- | --- | --- | --- |
| 2 | 378.6nm ( 3.3eV) | 0.1995 | (HOMO -> LUMO+1) (80%) |
| 3 | 353.5nm ( 3.5eV) | 0.1179 | (HOMO-1 -> LUMO ) (35%) |
| 4 | 348.6nm ( 3.6eV) | 0.1537 | (HOMO-1 -> LUMO ) (34%) |
| 5 | 347.0nm ( 3.6eV) | 0.0861 | (HOMO-5 -> LUMO ) (28%) |
| 6 | 340.0nm ( 3.6eV) | 0.4880 | (HOMO-1 -> LUMO+1) (91%) |
| 7 | 318.5nm ( 3.9eV) | 0.0002 | (HOMO-8 -> LUMO ) (50%) |
| 8 | 318.0nm ( 3.9eV) | 0.5337 | (HOMO -> LUMO+2) (66%) |
| 9 | 310.2nm ( 4.0eV) | 0.1580 | (HOMO-4 -> LUMO ) (18%) |
| 10 | 305.5nm ( 4.1eV) | 0.0145 | (HOMO-3 -> LUMO ) (47%) |

Table S20: Electronic transition of 4 in DMSO

| 1 | 413.4nm ( 3.0eV) | 0.4364 | (HOMO -> LUMO ) (77%) |
| --- | --- | --- | --- |
| 2 | 390.0nm ( 3.2eV) | 0.1798 | (HOMO -> LUMO+1) (76%) |
| 3 | 357.4nm ( 3.5eV) | 0.2287 | (HOMO-1 -> LUMO ) (85%) |
| 4 | 348.1nm ( 3.6eV) | 0.6562 | (HOMO-1 -> LUMO+1) (88%) |
| 5 | 347.1nm ( 3.6eV) | 0.0145 | (HOMO-5 -> LUMO+1) (33%) |
| 6 | 345.2nm ( 3.6eV) | 0.0323 | (HOMO-5 -> LUMO+1) (26%) |
| 7 | 322.3nm ( 3.8eV) | 0.6455 | (HOMO -> LUMO+2) (79%) |
| 8 | 315.7nm ( 3.9eV) | 0.0000 | (HOMO-8 -> LUMO ) (66%) |
| 9 | 311.4nm ( 4.0eV) | 0.0606 | (HOMO-4 -> LUMO+1) (24%) |
| 10 | 306.9nm ( 4.0eV) | 0.0196 | (HOMO-2 -> LUMO ) (35%) |

- Simulated absorption spectra of compounds 2‒4 in gas, toluene, chloroform and DMSO

Figure S25: Simulated absorption spectra of compounds 2 (A), 3 (B) and 4 (C) in gas, toluene, chloroform and DMSO.