Supplementary Materials for

Parachute structure trisiloxane surfactant: synthesis and its use in reverse flotation of iron ore

Zhi-qiang Huang,1*† Shi-yong Zhang,1† Vladimir E. Burov2†, Hong-ling Wang,3 Ru-kuan Liu,4 Chen Cheng,1 Shu-yi Shuai,1 Wen-yuan Li,1 Xin-yang Yu,1 Gui-chun He,1 Weng Fu5, Vladimir Z. Poilov2*

1 Jiangxi Province Key Laboratory of Mining Engineering, Jiangxi University of Science and Technology, Ganzhou, Jiangxi, 34100, China

2 Department of Chemical Engineering, Perm National Research Polytechnic University, Perm, 614990, Russia

3 Guangdong Institute of Resources Comprehensive Utilization, Guangzhou, 510650, China

4 Hunan Academy of Forestry, Changsha, Hunan, 410004, China

5 School of Chemical Engineering, The University of Queensland, St Lucia, 4072 QLD, Australia

† These authors contributed equally to this work.

* Corresponding author: zhiqiang@jxust.edu.cn (Z. Huang); vladimirpoilov@mail.ru (V.Z. Poilov)

# Supplementary Table 1 Chemical component of magnetite ore

| Composition | Content/% |
| --- | --- |
| TFe | 51.42 |
| SiO2 | 20.56 |
| Al2O3 | 4.93 |
| MnO | 1.85 |
| MgO | 7.27 |
| Na2O | 5.09 |
| K2O | 1.28 |
| CaO | 3.58 |
| P | 0.25 |
| S | 2.12 |
| Ig | 1.65 |

Supplementary Table 2 The industrial prices of agents

| Agent | Formula weight (g/mol) | Price (USD/t) |
| --- | --- | --- |
| N-(β-aminoethyl)-γ-aminopropyl methyl dimethoxy silane | 206.36 | 4,010 |
| Hexamethyldisiloxane | 162.38 | 5,500 |
| DA | 185.35 | 4,200 |
| AAT | 322.24 | — |

Supplementary Figs. 1. Structural characterization of AAT. a and b, 1H and 13C NMR spectrum of AAT. c, Infrared spectrogram of AAT.

Supplementary Figs. 2. Mineral purity and flotation process. a and b, XRD spectrum of pure magnetite and quartz. c, Pure mineral flotation process. d, Flowsheet of magnetite ore ﬂotation tests.