Supporting information

Anhydrous Grotthuss mechanism for fast proton transport in a dense oxide-ion array of α-MoO3

Zihan Ma1‡, Xiang-Mei Shi1‡, Shin-ichi Nishimura1, Seongjae Ko1, Masashi Okubo2, Atsuo Yamada1,*

1Department of Chemical System Engineering, School of Engineering, The University of Tokyo, Hongo 7-3-1, Bunkyo-ku, Tokyo 113-8656, Japan.

2 Department of Electrical Engineering and Bioscience, School of Advanced Science and Engineering, Waseda University, Okubo 3-4-1, Shinjuku-ku, Tokyo 169-8555, Japan.

*e-mail address of corresponding author: yamada@chemsys.t.u-tokyo.ac.jp

‡These authors contributed equally.

Figure S1. Synchrotron XRD pattern of α-MoO3.

Figure S2. Raman spectra of three ZnCl2-based aqueous electrolytes: conventional Zn2+ electrolyte (3 mol kg‒1 ZnCl2/H2O), superconcentrated Zn2+ electrolyte (32 mol kg‒1 ZnCl2/H2O), and superconcentrated dual-ion (Zn2+/H+) electrolytes (32 mol kg‒1 ZnCl2 and 1 mol kg‒1 P2O5/H2O). The Raman bands observed in the range of 2800–4000 cm-1 correspond to the O–H stretching modes of water molecules. The broad bands in the range of 2900 -3700 cm-1 are attributed to clusters of water molecules with various hydrogen-bonding environments. The peak at 3464 cm-1 (gray dashed line) is attributed to Zn2+ solvated water molecules that are not clustered through hydrogen bonding.

Figure S3. Zn stripping and plating at 0.5 mA cm-2 on Ti foil in a 32 m ZnCl2 + 1 m P2O5 aqueous electrolyte. Inset: coulombic efficiency in three ZnCl2-based aqueous electrolytes: conventional Zn2+ electrolyte (3 mol kg‒1 ZnCl2/H2O, gray dot), superconcentrated Zn2+ electrolyte (32 mol kg‒1 ZnCl2/H2O, orange dot), and superconcentrated dual-ion (Zn2+/H+) electrolytes (32 mol kg‒1 ZnCl2 and 1 mol kg‒1 P2O5/H2O, red dot).

Figure S4. XRF spectra of MoO3 electrodes: (1) pristine, (2) soaked for 1 day, and (3) discharged in a 32 m ZnCl2 + 1 m P2O5 aqueous electrolyte. The soaked electrode and discharged electrode were carefully extracted from electrolyte, rinsed with water, dried with acetone. The green dashed lines at 8-10 keV corresponds to zinc and the gray dashed lines at 17-20 keV corresponds to molybdenum. The zinc peak intensity did not increase after soaking or discharged, indicating no zinc ion intercalation.

Figure S6. X-ray photoelectron spectroscopy (XPS) spectra of the zinc metal anode cycled in three ZnCl2-based aqueous electrolytes after 20 cycles: conventional Zn2+ electrolyte (3 mol kg‒1 ZnCl2/H2O), superconcentrated Zn2+ electrolyte (32 mol kg‒1 ZnCl2/H2O), and superconcentrated dual-ion (Zn2+/H+) electrolytes (32 mol kg‒1 ZnCl2 and 1 mol kg‒1 P2O5/H2O). The peaks in conventional Zn2+ electrolyte correspond to Mo(0).

Figure S7. Charge/discharge curves of a MoO3-zinc cell with (a) galvanostatic (CC) charging mode and (b) galvanostatic + potentiostatic (CC-CV) charging mode in a 32 m ZnCl2 + 1 m P2O5 aqueous electrolyte. The “irreversible capacity” in CC charging mode can be recovered by a 3h-constant voltage step.

Figure S8. Galvanostatic intermittent titration technique (GITT) curves of a MoO3-zinc cell in a 32 m ZnCl2 + 1 m P2O5 aqueous electrolyte. Even under the GITT condition, a voltage hysteresis of approximately 0.5 V remains, indicating different routes upon protonation and deprotonation.

Figure S9. Potentiostatic intermittent titration technique (PITT) results of a MoO3–zinc cell in a 32 m ZnCl2 + 1 m P2O5 aqueous electrolyte. (a) Current and voltage respose versus time. (b) Diffusion coefficient (D) normalized by the diffusion length (L).

Figure S10. Rate capability of MoO3 in a 32 m ZnCl2 + 1 m P2O5 aqueous electrolyte with (a) activated charcoal as a counter electrode and Ag/AgCl as a reference electrode, and (b) zinc metal as both counter and reference electrodes. The capacity at the rates of 1-8 A g‒1 is identical in both systems while the capacity for the cell with zinc anode at the rate of 16 A g‒1 is much lower than that with an activated charcoal counter electrode, indicting the overpotential of zinc anode is rate-limiting in the proposed MoO3-Zn battery.

Figure S11. galvanostatic + potentiostatic (CC-CV)  charge/discharge curves of a MoO3–zinc cell in (a) 3 m ZnCl2, and (b) 32 m ZnCl2 electrolytes.

Figure S12. Capacity retention of MoO3–zinc cells using a conventional Zn2+ aqueous electrolyte (3 mol kg‒1 ZnCl2/H2O), a superconcentrated Zn2+ aqueous electrolyte (32 mol kg‒1 ZnCl2/H2O), and a superconcentrated dual-ion (Zn2+/H+) aqueous electrolytes (32 mol kg‒1 ZnCl2 and 1 mol kg‒1 P2O5/H2O) with galvanostatic charge.

Figure S13. Snapshots of simulated (a) pristine, (b) water inserted and (c) hydronium inserted structures.

Figure S14. Schematic representation of three different types of oxygen in MoO3 structure: the terminating oxygen coordinated to one Mo (O1), the bridging oxygen coordinated to two Mo (O2) and the oxygen shared with three Mo (O3).

Figure S15. Snapshot of calculated protonated H2.5MoO3 structure via DFT simulation.

Figure S16. (a) Convex hull of discharge and charge process. (b) Simulated voltage curve compared with an experimental curve.

Figure S17. Protonation energy barrier in H0.5MoO3 with O-O length of 2.71 Å

Figure S18. Statistics of the shortest O-O distances in lattice oxygen in different deprotonation states.

Figure S19. Deprotonation energy barrier in a channel in H2.5MoO3  with O-O length of 3.17 Å. The channel in gray plane is the same with that in figure 5d.

Figure S20. Simulated structure of charged HMoO3. No long-range 1D proton transfer channel can be found in the structure, therefore, the Grotthuss-type proton transport is disrupted.

Figure S21. Deprotonation energy barrier in HMoO3.

Figure S22. Structure evolution via DFT simulation.

Figure S23. Regan plot: comparison of the energy density and power density of this work to other zinc-ion or proton batteries.

References

[1] Ma, L. et al. Achieving Both High Voltage and High Capacity in Aqueous Zinc-Ion Battery for Record High Energy Density. Advanced Functional Materials 29, 1906142 (2019).

[2] Qiu, W. et al. High-performance flexible quasi-solid-state Zn–MnO2 battery based on MnO2 nanorod arrays coated 3D porous nitrogen-doped carbon cloth. J. Mater. Chem. A 5, 14838–14846 (2017).

[3] Yan, M. et al. Water-Lubricated Intercalation in V2O5·nH2O for High-Capacity and High-Rate Aqueous Rechargeable Zinc Batteries. Advanced Materials 30, 1703725 (2018).

[4] Kundu, D., Adams, B. D., Duffort, V., Vajargah, S. H. & Nazar, L. F. A high-capacity and long-life aqueous rechargeable zinc battery using a metal oxide intercalation cathode. Nature Energy 1, 1–8 (2016).

[5] Zhang, L., Chen, L., Zhou, X. & Liu, Z. Towards High-Voltage Aqueous Metal-Ion Batteries Beyond 1.5 V: The Zinc/Zinc Hexacyanoferrate System. Advanced Energy Materials 5, 1400930 (2015).

[6] Zhang, N. et al. Rechargeable aqueous zinc-manganese dioxide batteries with high energy and power densities. Nature Communications 8, 405 (2017).

[7] Li, H. et al. MoS2 nanosheets with expanded interlayer spacing for rechargeable aqueous Zn-ion batteries. Energy Storage Materials 19, 94–101 (2019).

[8] Zhang, N. et al. Cation-Deficient Spinel ZnMn2O4 Cathode in Zn(CF3SO3)2 Electrolyte for Rechargeable Aqueous Zn-Ion Battery. J. Am. Chem. Soc. 138, 12894–12901 (2016).

[9] Hu, P. et al. Zn/V2O5 Aqueous Hybrid-Ion Battery with High Voltage Platform and Long Cycle Life. ACS Appl. Mater. Interfaces 9, 42717–42722 (2017).

[10] Zhang, H. et al. Interlayer Engineering of α-MoO3 Modulates Selective Hydronium Intercalation in Neutral Aqueous Electrolyte. Angewandte Chemie International Edition 60, 896–903 (2021).