Supplementary Information

TiO2 Nanosheet Supported MnCeOx: A Remarkable Catalyst with Enhanced Low-Temperature Catalytic Activity in o-DCB Oxidation

Xu He,†12 Haiwei Guo,†1 Xiaoyao Liu,1 Jiaxin Wen,1 Gengbo Ren,1 Xiaodong Ma1*

1 School of Energy and Environmental Engineering, Hebei University of Technology, Tianjin 300401 (China)

2 School of Chemistry and Chemical Engineering, Xingtai University, Xingtai 054000 (China)

†These authors contributed equally.

* Corresponding author. E-mail: maxd@hebut.edu.cn (X. Ma)

- Catalyst preparation

Synthesis of TiO2-NS

Anatase TiO2 exposing {001} facet was synthesized by the hydrothermal method.(Wang et al. 2012) The hydrofluoric acid solution was added into C16H36O4Ti solution with agitation for 0.5 h, the mixed solution followed by transferring into the 50 mL Teflon reactor with hydrothermal treatment at 200 oC for 24 h. Hereafter the suspension was centrifuged and then washed with deionized water and anhydrous ethanol, respectively. The obtained precipitates were dried at 80 oC for 12 h and subsequently calcined at 500 ℃ for 2 h. Obtained samples were designated as TiO2-NS.

Synthesis of TiO2-NTO

The TiO2-NTO were all synthesized by the hydrothermal method using ammonium titanate nanowire precursor as the titanium source.(Li et al. 2010) 0.8 g P25 was added to 10 M KOH by continuous stirring for 0.5 h. The mixture was was introduced to a 50 mL Teflon autoclave, held at 200 oC for hydrothermal treatment for 24 h. The resultant precipitates were centrifuged and alternately washed with deionized water and absolute ethanol until the supernatant pH was below 10. Then the precipitates were mixed with 0.1 M NH4NO3 aqueous solution for ion exchange (6 h) and were subsequently centrifuged to obtain the precipitate, which was repeated 3 times. After that, the precipitates were dried at 60 oC for 12 h to obtain ammonium titanate nanowire. Finally, the ammonium titanate nanowire was used as a precursor to obtain the TiO2-NTO by a similar method aforementioned.

Synthesis of MnOx/TiO2

TiMnx catalysts were prepared by an impregnation method. In a typical synthesis, the calculated amounts of Mn(NO3)2 and 100 mg of TiO2 samples were added into 25 mL deionized water and stirred magnetically for 0.5 h. The suspensions were held at room temperature for 24 h and dried at 100 oC for 5 h, and the final powder was calcined in air at 500 oC for 2 h. Obtained samples were labeled as TiMnx（where x represents the molar ratio of Mn/(Mn+Ti)). The nominal content of Mn was 10, 15, and 20 mol%.

Synthesis of MnCeOx/TiO2

Series of TiMn15Cey catalysts were prepared through the impregnation method based on the TiMn15 with the introduction of the different molar proportions of Mn/(Mn+Ce). Specifically, the calculated amounts of Mn(NO3)2 and Ce(NO3)3·6H2O were mixed into 25 mL deionized water. Then 100 mg of TiO2 supports were added into the aqueous solution, then stirred for 0.5 h followed by aging for 48 h. The precipitates were dried at 100 ℃ for 5 h and calcined at 500 ℃ for 2 h. The resulting samples were labeled as TiMn15Cey, where y refers to molar ratios of Mn/(Mn+Ce) which were 15, 30, and 45 mol%, respectively.

- Catalyst characterization

SEM produced by Jsm-7800, Japan electronics CO, Ltd was used to characterize the morphology of catalysts. TEM images were given by JEM-2100 F transmission electronic microscopies. The XRD measurements were performed to investigate the crystal phases of the samples by an advanced diffractometer with the Cu-Ka radiation. The physical properties of catalysts such as specific surface area and pore size distribution of the materials were tested using the N2-adsorption/desorption instrument (ASAP 2460) at 77 K. H2-TPR analysis, evaluating the reduction properties of materials was operated on a dynamic adsorption reactor (TPDRO 1100 SERIES) with 5% H2/N2 mixed gas, 50 mL/min gas flow rate, and 10 ℃/min of temperature rise rate. The XPS was tested by a Kratos Axis Ultra DLD spectrometer using a monochromated Al-Kα X-ray (1486.6 eV). Every spectrum was modified by the C1s signal at 284.6 eV.

The in situ DRIFT experiments were conducted using a PerkinElmer 2000 FT-IR spectrometer by accumulating 128 scans at a resolution of 2 cm-1. A DRIFT cell equipped with ZnSe window was used for the gas flow system. Before the test, the catalyst was held at 350 oC in N2 for 1 h and cooled to 50 oC. The background spectra were collected at desired temperatures which were subtracted from the sample spectra. Thereafter, a mixture of o-DCB and 10% O2/N2 was introduced into the reactor. After stability, FT-IR spectra were recorded.

3. Figures and tables

Fig. S1. The SEM images of (a) TiMn15Ce30-NS and (b) TiMn15Ce30-NTO.

Fig. S2. XRD patterns of TiMn15-NS.

Fig. S3. Light-off curves for the catalytic oxidation of o-DCB over TiMnx-NS and TiMn15Cey-NS.

Table S1. Crystallite sizes of TiO2-NTO, TiO2-NS, TiMn15Ce30-NTO, TiMn15Ce30-NS and TiMn15-NS, Full-width-at-half maximum (FWHM) of TiMn15Ce30-NTO and TiMn15Ce30-NS.

| Samples | Average Crystallite Size [a] (nm) | FWHM (o) |  |
| --- | --- | --- | --- |
|  |  | (004) 2θ (o) | (200) 2θ (o) |
| TiO2-NTO | 37.9 | - | - |
| TiO2-NS | 43.8 | - | - |
| TiMn15-NS | 44.1 | - | - |
| TiMn15Ce30-NTO | 40.0 | 0.192 | 0.227 |
| TiMn15Ce30-NS | 34.2 | 0.312 | 0.223 |

[a] Calculated by Scherrer equation based on the (101) diffraction peak.

References

Li JM, Yu YX, Chen QW, Li JJ, Xu DS (2010) Controllable synthesis of TiO2 single crystals with tunable shapes using ammonium-exchanged titanate nanowires as precursors. Cryst Growth Des 10: 2111-2115. https://doi:org/10.1021/cg9012087

Wang W, Lu CH, Su MX, Ni YR, Xu ZZ (2012) Synthesis, characterization, and nitrogen concentration depended visible-light photoactivity of nitrogen-doped TiO2 nanosheets with dominant (001) facets. Chin J Catal 33: 629-636. https://doi:org/10.1016/s1872-2067(11)60348-3