Supplementary information

Quantized wrinkles and fracture of stiff membranes on soft films

Yancheng Meng, Henggao Xiang, Jianqiang Zhang, Zhili Hu, Jun Yin, Liqiang Li*, Zhuhua Zhang* and Wanlin Guo*

Email: wlguo@nuaa.edu.cn, chuwazhang@nuaa.edu.cn, lilq@tju.edu.cn

I.  Materials and Methods

- PDMS film fabrications

- O2 plasma treatments

- Peeling treatments

- Finite element simulations

II. Supplementary theoretical analysis

- A beam model for evaluating the strain in soft microfilms

- The correction of the beam model

- The evaluation of the deformation of stiff membrane

Ⅲ. figures S1 to S13

- Figure S1: Schematic illustration of the bending region of the microfilm under peeling.

- Figure S2: Analytical results calculated with a corrected beam model.

- Figure S3: Buckling behaviors due to lateral compression induced by the Poisson’s effect under uniaxial stretch along the vertical direction.

- Figure S4: The morphology of the fold-collapse.

- Figure S5: Front view of buckling patterns in bending regions of a series of SiO1.8/PDMS bilayers with different ts and constant tm of 155 nm.

- Figure S6: The dependence of fracture periods (W) on ts and the dependence of critical thickness (tsN) of soft microfilm on tm.

- Figure S7: Patterned fracture with a period of 8λ0.

- Figure S8. Relationships of the ribbon width W with the membrane thickness tm for the fracture periods of 1λ0, 2λ0 and 4λ0.

- Figure S9: Buckling and fracture behaviors of SiO1.8/PDMS bilayer films under the peeling with a bending angle of less than 90°.

- Figure S10: Integrated compressive strains that are transferred to the stiff membrane within a period length of 1λ0 () and 2λ0 ().

- Figure S11: The surface perimeter of different folds (single, double, and quadruple folds) as a function of ts from finite element simulations.

- Figure S12: Side view of buckling patterns in the bending region of peeling bilayers with different ts and a constant tm of 155 nm from finite element simulations.

- Figure S13: Order fracture/groove in other bilayers after the peeling treatments.

IV. Supplementary References

Materials and Methods

PDMS film fabrications

PDMS films are fabricated as in ref. S1. The bonding interaction between the PDMS film and the substrate was controlled by the coated layer of trichloro (1H, 1H, 2H, 2H-perﬂuorooctyl) silane (JKChemical, China) that was deposited on Si wafer before spinning the PDMS layer.

O2 plasma treatments

After fabrication, the PDMS films on the Si wafer were immediately exposed to oxygen plasma in the reactor (PLAUX-PR40L from Kunshan Plaux Electronics Technology Co., Ltd. China). Treatments were performed at a pressure of 30 Pa of oxygen and a frequency of 40 kHz. The thickness of the stiff membrane (SiO1.8) was controlled by varying duration and power of the plasma treatment.

Peeling treatments

After plasma treatment, the sample was first chopped into strips. Then, one end of the strip was attached by tape. Finally, the strips were peeled off using a clamp (blunt-ended forceps) at a uniform speed and a bending angle of 90°. Through keeping the peeling speed, the profile of the bending region was maintained and the buckling structures were created in the bending region. Suddenly stopping the peeling treatment and fixed the end of peeled strip, the buckling patterns can be frozen in the bending region. The front and side views of the buckling patterns were obtained via scanning electron microscope (SEM) and confocal laser microscopy. The cross sections of the buckling patterns were milled and captured by focused ion beam technology (FIB)S2.

Finite element simulations

To better understand the quantized buckling patterns and fracture in bilayers, we set up finite element to model the stiff membrane and soft microfilm with software packages ABAQUS 6.14. Since the substrate is PDMS, we consider the soft microfilm as a Mooney-Rivlin material in a plane-strain state. The stiff membrane and soft microfilm were modeled with hybrid quadrilateral elements (CPE4H), as implemented in ABAQUS. The quasi-static method was adopted and a very small initial geometric imperfection was introduced into the model for post-buckling analysisS3. The thicknesses of the membrane and microfilm were set according to experimental results. The displacement-controlled loading condition was used to apply the stretch to the film-substrate system along an inclined angle of 45°, as indicated by a yellow arrow in Fig. 2d in the main text.

Supplementary theoretical analysis

A beam model for evaluating the strain in soft microfilms

The deformation in the stiff membrane was determined by estimating the compressive strain in the soft microfilm, because the adhesion between the stiff and soft layers is strong enough to avoid delamination. Therefore, the determination of the strain in the soft microfilm is a key issue. To calculate the compressive stain in the whole bending region of the bilayer, we approximated the bending film as a cantilever beam with large deflectionS4, as shown in Fig. S1.

Fig. S1 | Schematic illustration of the bending region of the microfilm under peeling. s and θ are the arc length and the angular deflection of the beam, respectively;  is the peeling angle; X and Y are the horizontal and vertical coordinates of the bending beam, respectively. f0 is the adhesive force per unit width between the soft microfilm and rigid substrate; L is the total length of the part with compressive strain in the whole bending region, marked with a dashed blue arc. l is the total length of the straight beam before peeling. Es is the Young’s modulus and I is the moment of inertia of the beam. s = 0.16 ts is the deviation lengths of the maximal curvature, corresponding to the maximal compressive strain, from the clamped point (s = 0). ts is the thickness of the beam.

The study in Ref. S4 provides a normalized expression of the large deflection of a Euler-Bernoulli cantilever beam. For ease of calculations, we implemented denormalization of the large deflection expression as below,

(S1)

where = /2 and a is equal to (f0L2/EsI)1/2, with f0 = 10 N/m and Es = 1.8 MPa (the Young’s modulus of the PDMS film).

The correction of the beam model

According to the beam model, the compressive strain,, on the inner surface of the bending region can be expressed as

,                                    (S2)

where  is the curvature of the bending region and can be written as

.                           (S3)

The strain profile in the deflected beam can be calculated by Eqs. S1-S3 in principle. The calculations show that the strain increases with moving away from the free end and reaches a maximum at the clamped point. That is, the maximum strain appears at the clamped point (s = 0) with the maximal curvature and can be written as

,                            (S4)

.                        (S5)

However, the beam model cannot correctly describe the strain distribution in the region near the clamped end since the strain must be continuous across the clamped point. In fact, the maximum strain always deviates from the clamped point, as schematically illustrated by the blue solid line in Fig. S2a. The deviation lengths are determined in experiment through measuring the distance between the maximal deformation of the stiff film and the clamped point (i.e. the very peeling front), which are in a range 0.12ts-0.18ts and an average of 0.16ts. In the strain profile calculated from the beam model, we take the value at s = 0.16ts as the maximal strain. The as-corrected maximal strain  is about 0.93 times of the value at the clamped point , because = 0.93.

Figure S2b shows the calculated bending profiles of a series of micro-PDMS films with different thicknesses according to the corrected beam model. In addition, Fig. S2c shows a comparison between calculated and experimental profiles of three bending bilayers (with ts = 36, 62, and 112 μm). The experiments are in good agreement with the corrected model. We ignore the effect of stiff SiO1.8 nano-membranes on the bending profile of the microfilm. Figure S2d shows the strain distribution and the corrected maximal strains in these bending microfilms.

Fig. S2 | Analytical results calculated with a corrected beam model. a, Schematic illustration of the correction of maximum strain in the strain profile. Red dotted line is the strain profile of bending beam calculated by ideal beam model. Blue solid line represents practical distribution of compressive strain in the bending region. The segment of practical strain profile between “a” to “b” can be calculated and provided by an ideal beam model correctly. The practical maximum strain is at the point “a”. Inset, ts-dependent deviation length between the maximal deformation point in the stiff membrane and the clamped point, which are in a range 0.12ts-0.18ts and an average of 0.16ts. b, Calculated profiles of bending microfilms with different thicknesses. c, Comparison for calculated (cal) and experimental (exp) profiles of the bending region of beams. d, Distribution of strain in a bending beam. The corrected maximal strains in the beams with different ts are the intersection points of the corresponding strain profiles with the gray line; 0.16 ts is the average deviation distance between the maximum strain point and the clamped point (i.e., the very peeling front) for all the analyzed beams.

The evaluation of the deformation of stiff membrane

The integration of maximum strain () in a region with a length of nλ0 (n = 1, 2, and 4) reads as,

,                                (S6)

where is the as-corrected maximum strain on the inner surface of the bending region and equal to , and l is the length of the flat microfilm prior to buckling instability. Note that were normalized by λ0 in the main text and denoted as Δn.

Meanwhile, the critical wavelength for the wrinkling instability λ0 can be expressed asS5

,                           (S7)

where i = Ei/(1-μi2) with i = m or s; μm and μs are the Poisson ratios of stiff membrane and soft microfilm, respectively; and tm is the thickness of the stiff membrane. Therefore, λ0 is proportional to the membrane thickness and independent of the thickness of soft microfilm.

Combining Eqs. S4, S5 and S7 with Eq. S6 and considering the correction of the maximal strain and curvature, we have

,             (S8)

To determine , we measured tsN (N = 1, 2) with five groups of SiO1.8/PDMS bilayers. The thicknesses of stiff SiO1.8 membranes for the five groups of samples are 138, 155, 194, 232 and 281 nm, respectively. Each group contains 15-20 samples, in which the thickness of soft microfilm varies from 20 to 300 µm. Based on experimentally measured tsN, we can obtain the critical for fracture of the nth-order pattern, denoted as  (n =1, 2, and 4), according to Eq. S8. The statistic average of the calculated / is equal to 0.96, close to 1 (fig. S10A). Therefore, is independent of n, and thus can be written as  (corresponds to  that is normalized by λ0 in the main text). and  are shown to monotonically increases with tm (fig. S10A). Fitting this monotonic dependence shows that and  are proportional to the square root of tm (fig. S10B), expressed as

,                                   (S9)

where cn is approximately equal to10-3/2 m-1/2, where “m” is the meter. Substituting  in Eq. S8 with Eq. S9, we obtain

.              (S10)

Then, it is easy to have

.                                 (S11)

Because there is peeling treating, ts relates to compressive strain.

,                    (S12)

Therefore, Eq. S10 can be further transformed into a universal relation about the strain and mechanical properties of the bilayer films.

.     (S13)

The equivalent strain () is defined as follows

.             (S14)

Fig. S3 | Buckling behaviors due to lateral compression induced by the Poisson effect under uniaxial stretch along the vertical direction. Top panel, SEM images showing front views of the buckling structures under compression of different magnitudes; lower panel, focused ion beam (FIB) images, showing the cross-sections of the locations that are marked by red dashed lines in the top panels. C-x% represents a x% compressive strain along the lateral direction.

Fig. S4 | The morphology of the fold-collapse. a, SEM images, showing the front view of a fold-collapse. b, side view of the fold-collapse. c, FIB images, showing the cross-sections of this fold-collapse and enlarged view of its bottom, white dotted line represents the profile of the fold-collapse. “Pt” represents platinum film, needed to mill the cross-section by focused ion beam.

Fig. S5 | Front view of buckling patterns in bending regions of a series of SiO1.8/PDMS bilayers with different ts and constant tm of 155 nm. a, Schematically illustration of the detection of the buckling patterns in scanning electron microscope (SEM). b-g, SEM images, various buckling patterns. The thicknesses of microfilms are 33 μm (b), 36 μm (c), 62 μm (d), 90 μm (e), 112 μm (f) and 142 μm (g), respectively. 36 and 112 μm are two critical thicknesses of the soft microfilms, corresponding to ts1 and ts2, respectively. 1, 2, and 4λ0 represent fold-collapse (or fracture) appeared in wrinkle (single fold, s-f-c), double (d-f-c), and quadruple folds (q-f-c), respectively. The difference of the period of one kind of fold-collapse is mainly attributed to the varying curvature in the bending region which causes same region with different lengths in the front view images. The scale bar is 20 μm.

Fig. S6 | The dependence of fracture periods (W) on ts and the dependence of critical thickness (tsN) of the soft microfilm on tm. a, The fracture period in a series of bilayers with different ts yet a given tm = 155 nm and λ0 = 12.81 μm. Vertical bars represent standard error here and below. b, The fracture period in a series of bilayers with a given tm = 281 nm and λ0 = 23.01 μm. The thickness of soft microfilm in these two series of bilayers are both ranging from 20 µm to 300 µm. c, Experimental ts2 and ts1 (first two critical thickness of soft microfilm, as marked in a and b) in five series of SiO1.8/PDMS bilayers and calculated dependence of ts2 and ts1 on tm; The thicknesses of stiff SiO1.8 films for the five groups of samples are 138, 155, 194, 232 and 281 nm, respectively. Each group contains 15-20 samples, in which the thickness of soft microfilm varies from 20 µm to 300 µm. d, Normalized ts2 and ts1 by the corresponding λ0 (squares), along with two fitting lines (dotted lines).

Fig. 7 | Patterned fracture with a period of 8λ0. The thickness of stiff SiO1.8 membrane is tm = 108 nm, the thickness of the soft film is ts = 366 μm, λ0 = 8.93 μm, and ts/λ0 = 41.

Fig. 8 | Relationships of the ribbon width W with the membrane thickness tm for the fracture periods of 1λ0, 2λ0 and 4λ0. The dotted data are from experiments while the solid lines are from theory.

Fig. S9 | Buckling and fracture behaviors of SiO1.8/PDMS bilayer films under the peeling with a bending angle of less than 90°. a, Schematic illustration of the peeling treatment. b, SEM image, showing nonperiodic fractures in the peeled region away from the peeling front. c, A pattern of gradually changed wrinkles around the peeling front (i.e., the bending region). The scale bar is 20 µm.

Fig. S10 | Integrated compressive strains that are transferred to the stiff membrane within a period length of 1λ0 () and 2λ0 (). a, (solid squares) and  (solid circles) as functions of tm based on measured ts1 and ts2 in five series of bilayers. The variation of / with tm is shown by olive spheres, with a statistic average of 0.96. b, Normalized and by the square root of 0.93tm/1000. Note that were normalized by λ0 in the main text and denoted as; the integration of compressive strain within a period length of nλ0 is right the shortened length of the microfilm in the same region upon the corresponding fold-collapse.

Fig. S11 | The surface perimeter of different folds (single, double, and quadruple folds) as a function of ts from finite element simulations. Here, tm = 155 nm.

Fig. S12 | Side view of buckling patterns in the bending region of peeling bilayers with different ts and a constant tm of 155 nm from finite element simulations. a, Wrinkles gradually evolve into single folds in a bilayer with ts=30 µm. b, Wrinkles and double folds in a bilayer with ts=60 µm. c, Wrinkles, double folds, quadruple folds and quadruple-fold collapses simultaneously appear in the bilayer with ts=150 µm; inset, a zooming-in image of the cross-section of quadruple-fold collapses.

Fig. S13 | Order fracture/groove in other bilayers after the peeling treatments. a, Aligned micro-ribbons made from a fractured PMMA membrane (tm = 3.2 μm). b, A stripped Au nanomembrane (tm = 300 nm) with nanoscale troughs. c, Aligned micro-ribbons made from a fractured graphene monolayer. All the stiff layers are bound onto soft PDMS microfilms.

Supplementary References

S1.	Meng, Y., Gong, X., Huang, Y. & Li, L. Mechanically tunable opacity effect in transparent bilayer film: Accurate interpretation and rational applications. Appl. Mater. Today 16, 474-481, (2019).

S2.	Cairney, J. M., Munroe, P. R. & Hoffman, M. The application of focused ion beam technology to the characterization of coatings. Surf. Coat. Tech. 198, 165-168, (2005)

S3.	Jin, L., Takei, A. & Hutchinson, J. W. Mechanics of wrinkle/ridge transitions in thin film/substrate systems. J. Mech. Phys. Solids 81, 22-40 (2015).

S4.	Tari, H., Kinzel, G. L. & Mendelsohn, D. A. Cartesian and piecewise parametric large deflection solutions of tip point loaded Euler–Bernoulli cantilever beams. Int. J. Mech. Sci. 100, 216-225, (2015).

S5.	Zhuo, L. & Zhang, Y. The mode-coupling of a stiff film/compliant substrate system in the post-buckling range. Int. J. Solids Struct. 53, 28-37, (2015).