Supplementary Information for:

Ultra-Broadband Dispersion-Manipulated Dielectric Metalenses by Nonlinear Dispersive Phase Compensation

Yueqiang Hu1,2, Yuting Jiang1, Yi Zhang1, Jiajie Lai1, Peng He1, Xiangnian Ou1, Ling Li1 and Huigao Duan1,2,3*

1National Research Center for High-Efficiency Grinding, College of Mechanical and Vehicle Engineering, Hunan University, Changsha 410082, P.R. China

2Advanced Manufacturing Laboratory of Micro-Nano Optical Devices, Shenzhen Research Institute, Hunan University, Shenzhen, 518000, P.R. China

3 Innovation Institute of the Greater Bay Area, Hunan University, Guangzhou, 511300, P.R. China

*Corresponding authors. Email: duanhg@hnu.edu.cn

Section 1: Theoretical derivation of wavenumber and effective refractive index

The formula S1 expresses the relationship between the wavenumber and the effective refractive index (ERI) in the one-dimensional equivalent medium theory.

neff=(1-Fnair2+FnTiO22)-1/2	(S1)

where F is the duty cycle. neff is the effective refractive index. nair is the refractive index of air. nTio2 is the experimentally measured refractive index of titanium dioxide. Figure S1 shows the relationship between the wavenumber and the effective refractive index derived from the formula S1 when F = 0.5.

Figure S1. The relationship between wavenumber and effective refractive index is derived from the one-dimensional equivalent medium theory.

Section 2: Optical constant of TiO2

Figure S2 shows the experimentally measured n and k values of TiO2 in the 210 nm-1650 nm band.

Figure S2. The optical constant of TiO2.

Section 3: Meta-units libraries

First, the ERIs of 14 kinds of meta-units are simulated by the Lumerical MODE Solutions. The period of meta-units was set as 500 nm. Considering the constraints of experimental conditions and period size, we set the minimum and maximum size constraints of the nanostructures to be 50 nm and 450 nm, respectively. Nanostructures with different cross-sectional shapes are shown in Figure 2a. For the simulation, the boundary conditions of the simulation was set to periodic boundary conditions. The refractive index of the TiO2 was the measurement result by ellipsometer. We used eigenmodes to analyze and calculate nanostructures with different wavelengths and different cross-sectional shapes, and obtain the equivalent refractive index neff.

Then we calculated the phase at different wavelengths (400 nm, 450 nm, 550 nm, 650 nm, 750 nm, 850 nm, 900 nm, 1000 nm) when the height is 600 nm according to formula 1. We calculated the phase φ0, at the largest wavelength (λ = 1000 nm) and dispersion, ∆φ=φ-φ0, for the chosen ∆φ (i.e., λ = 400–1000 nm) of each meta-units. The calculation results is shown in Figure S3. In the process of matching the structure, we found that it is difficult to achieve ultra-broadband achromatic with these meta-units libraries. In order to obtain better matching results, we changed the structure height to 1000 nm to obtain greater phase compensation. The calculation results is shown in Figure S4.

Figure S3. Meta-units libraries, the height is 600nm. a. λ = 400 nm. b. λ = 450 nm.

c. λ = 550 nm. d. λ = 650 nm. e. λ = 750 nm. f. λ = 850 nm. g. λ = 900 nm.

Figure S4. Meta-units libraries, the height is 1000nm. a. λ = 400 nm. b. λ = 450 nm.

c. λ = 550 nm. d. λ = 650 nm. e. λ = 750 nm. f. λ = 850 nm. g. λ = 900 nm.

Section 4: The intrinsic phase dispersion response of nanostructures.

The relationship between the wavenumber and phase of six meta-units is shown in Figure S5, which proves that the nanostructures have nonlinear phase dispersion.

Figure S5. The intrinsic phase dispersion response of nanostructures.

Section 5: Matching results of ultra-broadband achromatic metalenses with different numerical apertures (NA).

First, we designed ultra-broadband achromatic metalenses with different NA (0.0665, 0.0830, 0.0995, 0.1159) in the 400 nm to 1000 nm band by linear dispersive phase compensation methods. The first step is to calculate the expected phase φconstruct_0, at the largest wavelength (λ = 1000 nm) and expected dispersion, ∆φconstruct=φconstruct-φconstruct_0, for the chosen ∆φconstruct (i.e., λ = 400–1000 nm) of each meta-units. Then we matched the structures at different r0, and chosen the r0 with the smallest error. The error here can be expressed by formula S2, where ∆φconstruct is the expected dispersion, ∆φmetaunit is the dispersion of the chosen meta-units. rmax is the farthest position of the meta-unit on the layout, nλ is the different wavelength.

Error=i=1nλr=1rmax(∆φconstruct-∆φmetaunit)2	（S2）

Figure S5 shows the matching results of the linear dispersion phase compensation method. In order to obtain a smaller matching error, we have proposed a nonlinear dispersion phase compensation method (rλ is different at different wavelength) in the design of ultra-broadband achromatic metalens. Figure S6 shows the matching results of the nonlinear dispersion phase compensation method.

Figure S6. The linear dispersion phase compensation method matching results.

a. NA = 0.0665. b. NA = 0.0830. c. NA = 0.0995. d. NA = 0.1159.

Figure S7. The nonlinear dispersion phase compensation method matching results.

a. NA = 0.0665. b. NA = 0.0830. c. NA = 0.0995. d. NA = 0.1159.

Section 6: Device fabrication.

The fabrication process of the device is shown in Figure S8. First, a 1000-nm-thick polymethyl methacrylate (PMMA) electron-beam resist layer was spin coated at 2000 rpm on the transparent glass substrate with ITO film layer and baked on a hot plate for 4 min at 180 °C. Then, the sample was exposed through electron-beam lithography (EBL) with a 100-KV voltage and a beam current of 200 pA. Subsequently, the sample was developed in a mixed solution of methyl isobutyl ketone (MIBK) and isopropanol (IPA) (MIBK: IPA = 1:3) for 1 minute, and fixed in the IPA for 1 minute. Later, we used the atomic layer deposition (ALD) system to fill the exposed area with 230 nm TiO2. After this process, a layer of 230 nm Tio2 will remain on the top of the entire sample. We etched the TiO2 on the top layer by ion beam etching (IBE) in the next process. Then, we used reactive ion etching (RIE) to remove the photoresist. Finally, the TiO2 structures with a high aspect ratio are obtained.

Figure S8. Fabrication process of TiO2 structure based on conformal filling process.

Section 7: Optical characterization.

In order to verify the performance of ultra-broadband achromatic and arbitrary dispersion controlled metalenses, we designed two optical setups to characterize the focal length and imaging effect, respectively.

The optical setup used to verify the ultra-broadband achromatic metalens and the arbitrary dispersion control metalenses is shown in Figure S9. The laser beam is emitted by a supercontinuum laser source, and we can obtain the target wavelength after the laser beam passes through the color filter. The laser beam is imaged on the CCD through the metalens and the objective lens. Finally, the translation stage moved from the position where the sample surface is imaged, and the camera acquired an imaging pattern every 1 μm until it stops at 800 μm from the starting position.

In the imaging experiment, we replaced the super continuum laser source with a halogen lamp. We placed the resolution target in front of the ultra-broadband achromatic metalens and obtained the imaging result at the focal point of the lens. Finally, we judged the imaging quality of the ultra-broadband achromatic metalens by comparing images of different wavelengths.

Figure S9. The optical characterization system. a. Schematic diagram of optical setup for verifying the performance of fabricated ultra-broadband achromatic metalens and arbitrary dispersion control metalenses. CF: color filter. ML: metalenses. OL: objective lens. b. Schematic diagram of optical setup for imaging with broadband achromatic metalenses. RT: resolution target.

Section8: Simulation results from 400-1000 nm band.

Because of the limitation of the experimental conditions, in the article we only show the simulation and experimental results from the 420-1000 nm band. Figure S10 shows the simulation results from 400-1000 nm band.

Figure S10. Simulation results from 400-1000 nm band.

Section 9: The effects of processing errors.

In fact, some errors will inevitably be introduced in every step of sample preparation. Therefore, for the processing plan used in this article, we had selected two locations where errors are most likely to occur and performed corresponding simulations. First, we simulated the overexposure caused by the large dose in the electron beam exposure process. The left side of Fig. S10 a, b, c, d is the simulation result with normal structure size, and the result on the right is the simulation result after all the structure sizes are increased by 40 nm. We also simulated the loss of the structure height during the ion beam etching process. The left side of Fig. S11 a, b, c, d is the simulation result when the height of the nanostructure is 1000 nm, and the right side is the simulation result when the structure height is reduced to 800 nm.

In the process of comparing these two sets of simulation results, it can be found that whether the size of the nanostructure increases or the height decreases, the focal length will have a larger deviation at a short wavelength, while the impact will be less at a long wavelength. Part of the reason is that nanostructures need to provide greater phase compensation at shorter wavelengths, and the deviation of the structure will cause a bigger phase change, which will cause a change in the focal length.

Figure S11. Simulation of the impact of overexposure on the focusing effect.

a. b. c. d. Comparison of simulation results when λ =450 nm. 550 nm. 650 nm. 750 nm.

Figure S12. Simulation of the impact of overetching on the focusing effect.

a. b. c. d. Comparison of simulation results when λ =450 nm. 550 nm. 650 nm. 750 nm.