Supplementary Materials for

# Novel structure of active platinum-bismuth site for oxidation of carbon monoxide

Bing Nan,1, 5 Qiang Fu,2 Miao Shu,1 Lulu Zhou,2 Weiwei Wang,2 Chun-Jiang Jia,2* Chao Ma,3* Jun-Xiang Chen,4 Lina Li,1, 6 Rui Si,1, 6*

*Correspondence to: Email: sirui@sinap.ac.cn (R.S.); cma@hnu.edu.cn (C.M.); jiacj@sdu.edu.cn (C.-J.J.)

Supplementary Fig. 1 Nitrogen adsorption measurements of fresh Pt/PtBi-SiO2 samples: (a) adsorption-desorption isotherm and (b) BJH pore size distribution.

Supplementary Fig. 2 TEM (a,d,g), HRTEM (b,e,h) and aberration-corrected HAADF-STEM (c,f,i) images of fresh Pt/PtBi-SiO2 samples: (a,b,c) 1Pt-SiO2; (d,e,f) 1Pt2Bi-SiO2; (g,h,i) 1Pt5Bi-SiO2.

Supplementary Fig. 3. Diameter histograms on oxide cluster of fresh (a) and used (b) Pt/PtBi-SiO2 samples on the basis of HAADF-STEM data.

Supplementary Fig. 4 The XRD patterns of fresh Pt/PtBi-SiO2 samples with a “slow-scan” mode (scanning rate of 1° min−1) from 35 to 55°.

Supplementary Fig. 5 X-ray photoelectron spectroscopy profiles of PtBi-SiO2 samples: (a) fresh; (b) used.

Supplementary Fig. 6 In-situ DRIFTS study of (a,c) CO adsorption, (b,d) N2 purging on fresh 1Pt-SiO2-400 (a,b) and 1Pt2Bi-SiO2 (c,d). The catalysts were pretreated in situ at 300 °C under O2 flow in the DRIFTS reaction cell before data collection (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C)

Supplementary Fig. 7 TEM/HRTEM (a,b) images; XRD profile (c) and diameter histograms on oxide clusters (d) for fresh 1Pt-SiO2-400.

Supplementary Fig. 8 CO oxidation light-off experiments for Pt/PtBi-SiO2 samples with pretreatment at 300 °C under air ( 1% CO/20% O2/79% N2, 134,000 mL gcat−1 h−1).

Supplementary Fig. 9 (a) the “light-off” experiments over Pt/PtBi-SiO2 samples; (b) the catalytic performance of 1Pt-SiO2 and 1Pt-SiO2-400; and (c) the cyclic stability of the 1Pt2Bi-SiO2 alternatingly tested at 500 and 200 °C (2% CO/1% O2/He, 10 mg of catalyst, GHSV: 300, 000 mL·gcat−1·h−1)

Supplementary Fig. 10 TEM and HRTEM images of used Pt/PtBi-SiO2 samples: (a,b,c) 1Pt-SiO2; (d,e,f) 1Pt2Bi-SiO2; (g,h,i) 1Pt5Bi-SiO2.

Supplementary Fig. 11 Representative aberration-corrected HAADF-STEM images (a,b,c) and STEM-EDS elemental mapping images (d) of used 1Pt2Bi-SiO2.

Supplementary Fig. 12 The EXAFS fitting results in R space of PtBi-SiO2 samples after hydrogen reduction at 210 °C for 30 mins without air exposure until finishing XAFS experiments: (a) only PtO and metallic PtPt shells and (b) PtO, metallic PtPt and PtOBi shells for EXAFS fitting.

We have conducted the XAFS tests for Bi-doped samples after hydrogen reduction at 210 °C without air exposure, well consistent with the pretreatment condition before CO oxidation “light off” experiment to detect structural evolution of active site. Firstly, we supposed that the hydrogen reduction destroyed Pt−[O]x−Bi structure completely with metallic Pt−Pt shell (small-size metallic Pt clusters or particles) plus a minor Pt−O shell. However, the fitting results with only Pt−Pt and Pt−O shells in Supplementary Fig. 12a were not well consistent with EXAFS data, especially in ~3.0 Å lacking a specific shell. Therefore, we appended an additional Pt−O−Bi shell for Bi-promoted samples, in which the fitting curves could match EXAFS data pretty well. It indicated that after hydrogen reduction the active site was composed of metallic Pt phase plus Pt−[O]x−Bi structure.

Supplementary Fig. 13 The comparison of different shells over EXAFS fitting results in R space for 1Pt2Bi-SiO2.

In order to require more reliable local structure for used Bi-promoted samples, we firstly conducted the EXAFS fitting process with PtO and metallic PtPt shells. Although we can obtain the relatively reasonable coordination number and bond distance for PtO and metallic PtPt shells, the fitting curves were not consistent with EXAFS profiles very well, especially in 3.03.5 Å. After addition of PtOBi shell, we can acquire the most suitable EXAFS fitting results in Supplementary Fig. 13.

Supplementary Fig. 14 Pt L3–edge EXAFS fitting results in R space for (a) fresh and (b) used 1Pt-SiO2-400.

As a reference, 1Pt-SiO2-400 calcinated at 400 °C possesses almost identical local coordination structure and active site size with Bi-promoted samples except for Pt–[O]x–Bi structure. After CO oxidation, the Pt active site is in a low oxidized state for 1Pt-SiO2-400 (+0.9) sample and EXAFS results indicate the Pt–O (R ≈ 2.00 Å, CN ≈ 2.0) and metallic Pt–Pt (R ≈ 2.75 Å, CN ≈ 5.8) shell about ~1 nm nanoparticle with surface partial oxide platinum site.

Supplementary Fig. 15 H2TPR profiles of fresh (a) and used (b) Pt/PtBi-SiO2 catalysts. The H2-TPR for used samples was conducted after CO oxidation without exposing to air.

For used samples, the reducible oxygen in 1Pt-SiO2 has been taken away by hydrogen pretreatment at 210 °C, being metallic platinum particle. However, a low temperature reduction peaks for used Bi-promoted samples further confirmed the maintaining of Pt[O]xBi structure. We calculated the hydrogen consumption of 1Pt2Bi-SiO2 (78μmol/g) and 1Pt5Bi-SiO2 (95μmol/g) for Pt[O]xBi structure, which was much less than that of fresh Bi-promoted samples. It indicated that the most Pt[O]xBi structure was destroyed. Moreover, no temperature shift occurred on peaks for isolated BiOx cluster (350−400 °C), revealing that BiOx cluster structure could be maintained after hydrogen reduction and make no contribution on improvement of CO oxidation activity.

Supplementary Fig. 16 COTPR profiles of (a,b) fresh (pretreatment condition: 300 ºC for 30 min in 5 vol.% O2/He) and (c,d) used (after CO oxidation without air exposure) Pt/PtBi-SiO2 samples, (5 vol.% CO/He, 20 cm3 min-1, with ramping rate at 5 °C min-1)

The amount of surface oxygen was calculated by following formula:

Active oxygen quantity: R = (V × 0.05 × Con.) / (22.4 × M) × 1000 × t            (1)

V: gas flow rate      Con.: conversion of 5%CO/He     M: mass of catalyst      t: time of first peak for CO-TPR        0.05: 5%CO/He

Supplementary Fig. 17 In-situ DRIFTS study of (a, b) CO adsorption, (c, d) N2 purging, (e, f) CO resorption, and (g, h) O2 removal on (a, c, e, g) 1Pt-SiO2 and (b, d, f, h) 1Pt2Bi-SiO2. The catalysts were pretreated in situ at 210 °C under 5 vol.% H2/N2 flow in the DRIFTS reaction cell before data collection (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C).

Supplementary Fig. 18 In-situ DRIFTS study of (a) CO adsorption, (b) N2 purging on 1Pt-SiO2-400. The catalysts were pretreated in situ at 210 °C under 5 vol.% H2/N2 flow in the DRIFTS reaction cell before data collection (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C)

Supplementary Fig. 19 In-situ DRIFTS study of CO adsorption on 2Bi-SiO2 with different pretreatment condition. The catalysts were pretreated in situ (a) at 300 °C under air and (b) at 210 °C under 5 vol.% H2/N2 flow in DRIFTS reaction cell before data collection (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C)

Supplementary Fig. 20 In-situ DRIFTS study of CO absorption on different doping of bismuth species. (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C).

Supplementary Fig. 21 Frequencies of a CO adsorbate on the Pt@PtOx model without (a-d) and with (e-h) Bi dopant. The teal blue, gray, red and purple spheres represent Pt, C, O, and Bi atoms, respectively.

Supplementary Fig. 22 Density of states (DOS) for the d electrons of the Pt atom on which the CO molecule adsorbs. The red and blue lines correspond to the models in Supplementary Figs. 20c (without Bi atom) and 20f (with Bi atom), respectively. The Fermi level is set to 0 (black dash line).

Supplementary Fig. 23 In-situ DRIFTS in the mode: “CO adsorption → reaction conditions (1% CO/ 20% O2/N2 flow) at 200°C → CO adsorption” on 1Pt-SiO2 without catalyst replacement and air exposure, (CO flow rate: 30 mL min−1; catalyst mass: 20 mg).

Supplementary Table 1: Bulk Pt and Bi concentration, BET specific surface areas (SBET), BJH pore volume (Vp), average cluster sizes (D) for Pt/PtBi-SiO2 and SiO2 samples.

| Sample | Pt (wt.%)a | Bi (wt.%)a | TR (°C) | H2 (μmol g−1)b | SBET (m2/g)c | Vp (cm3/g)c | D (nm)d |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SiO2 | — | — | — | — | 430 | 1.322 | — |
| 1Pt-SiO2 | 0.8 | — | 101 | 157α, 82β | 400 | 1.225 | 1.7±0.4 3.0±0.6e |
| 1Pt2Bi-SiO2 | 0.9 | 2.3 | 162, 248, 349 | 254α, 247β | 424 | 1.352 | 1.6±0.5 1.8±0.3e |
| 1Pt5Bi-SiO2 | 0.9 | 6.1 | 197, 278, 371 | 657α, 529β | 405 | 1.286 | 1.7±0.3 2.0±0.4e |

a Determined by ICP-AES; b Actual value of H2 consumptions (α) and theoretical values of H2 consumption calculated according to Pt4+ → Pt0 and Bi3+ → Bi0 (β); c From N2 adsorption/desorption experiments; d Statistic data of cluster on the basis of TEM images; e after CO oxidation.

Supplementary Table 2: Oxidation state of platinum (δ) and Pt L3-edge EXAFS fitting results (R: distance; CN: coordination number; σ2: Debye-Waller factor a; △E0: inner potential correction b) of Pt/PtBi-SiO2 samples.

| Sample | δ | Pt-O |  | Pt-Pt(metal) |  | Pt-O-Pt/Bi |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | R (Å) | CN | R (Å) | CN | R (Å) | CN |
| 1Pt-SiO2 (fresh) | 1.8 | 2.01±0.01 | 2.4±0.3 | 2.78±0.01 | 6.4±0.8 | 3.09±0.02 | 2.7±1.0 |
| 1Pt-SiO2-400 (fresh) | 3.2 | 2.00±0.01 3.78±0.03 | 4.5±0.2 2.4±1.0 | — | — | 3.10±0.04 | 1.2±0.6 |
| 1Pt2Bi-SiO2 (fresh) | 3.0 | 2.00±0.01 3.77±0.04 | 4.9±0.1 2.4±1.7 | — | — | 3.03±0.02 | 3.0±0.7 |
| 1Pt5Bi-SiO2 (fresh) | 3.5 | 2.00±0.01 3.80±0.03 | 5.7±0.3 1.7±0.7 | — | — | 3.05±0.04 | 4.0±1.0 |
| 1Pt2Bi-SiO2 (hydrogenc) | 0.2 | 2.06±0.03 | 0.6±0.2 | 2.73±0.01 | 6.8±1.4 | 2.90±0.04 | 2.6±1.2 |
| 1Pt5Bi-SiO2 (hydrogenc) | 0.4 | 2.00±0.01 | 2.0±0.2 | 2.72±0.01 | 5.0±1.2 | 2.90±0.04 | 1.4±0.9 |
| 1Pt-SiO2 (used) | 0.4 | — | — | 2.76±0.01 | 9.4±1.0 | — | — |
| 1Pt-SiO2-400 (used) | 0.9 | 1.97±0.01 | 2.0±0.2 | 2.75±0.01 | 5.8±0.5 | — | — |
| 1Pt2Bi-SiO2 (used) | 0.7 | 1.99±0.01 | 1.0±0.1 | 2.77±0.01 | 8.4±1.7 | 2.99±0.02 | 2.2±0.8 |
| 1Pt5Bi-SiO2 (used) | 1.3 | 1.99±0.01 | 2.5±0.1 | 2.70±0.01 | 4.7±1.0 | 2.96±0.03 | 2.2±0.6 |

aσ2 = 0.0030, 0.008 and 0.008Å2 for all the analyzed PtO, PtPt and PtBi shells, respectively; b△E0 = 11.2, 13.3 and 14.1 eV for fresh 1Pt-SiO2, 1Pt2Bi-SiO2 and 1Pt5Bi-SiO2, respectively, which were obtained from the linear combination fits on XANES profiles and the fitting results of Pt foil (△E0 = 8.3  1.2 eV) and PtO2 (△E0 = 15.0  0.9 eV) standards; △E0 = 7.4  1.8 eV for all used samples; c the samples was reduced with 5 vol. %H2/N2 at 210 °C for 30 min.

Supplementary Table 3: Temperature of 50% (T50%) and 90% (T90%) CO conversion, rates normalized by catalyst weight (rw), rates normalized by platinum amount (rPt) and apparent activation energies (Ea) for the carbon monoxide oxidation reaction over Pt/PtBi-SiO2 samples.

| Sample | T50% | T90% | rw (molCO·gcat-1·s-1) |  |  | rPt (mmolCO·molPt-1·s-1) |  |  | Ea(kJ/mol) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 90C | 100C | 110C | 90C | 100C | 110C |  |
| 1Pt-SiO2 | 144 | 150 | 0.2 | 0.3 | 0.7 | 4.8 | 7.3 | 17.1 | 704 |
| 1Pt2Bi-SiO2 | 85 | 96 | 1.7 | 3.1 | 3.9 | 41.4 | 75.5 | 95.1 | 524 |
| 1Pt5Bi-SiO2 | 103 | 117 | 0.9 | 1.5 | 2.2 | 21.9 | 36.6 | 53.6 | 563 |

Supplementary Table 4: Testing conditions of Arrhenius plots (rw) for Pt/PtBi-SiO2 samples.

| 1Pt-SiO2 | 60,000 mL·gcat-1·h-1 |  | 1Pt2Bi-SiO2 | 224,000 mL·gcat-1·h-1 |  |
| --- | --- | --- | --- | --- | --- |
|  | Conv.(%) | rw(molCO·gcat-1·s-1) |  | Conv.(%) | rw(molCO·gcat-1·s-1) |
| 90°C | 2.7 | 0.2 | 90°C | 5.0 | 1.7 |
| 100°C | 4.3 | 0.3 | 100°C | 10.0 | 3.1 |
| 110°C | 8.9 | 0.7 | 110°C | 15.2 | 3.9 |
| 1Pt5Bi-SiO2 | 100,000 mL·gcat-1·h-1 |  |  |  |  |
|  | Conv.(%) | rw(molCO·gcat-1·s-1) |  |  |  |
| 90°C | 3.3 | 0.9 |  |  |  |
| 100°C | 5.4 | 1.5 |  |  |  |
| 110°C | 7.9 | 2.2 |  |  |  |

Supplementary Table 5: H2-TPR peak temperature (TR), and experiment hydrogen consumption (H2) over Pt/PtBi-SiO2 samples.

| Sample | TR (°C) |  | H2 (μmol g−1) for first peak |  |
| --- | --- | --- | --- | --- |
|  | fresh | used | fresh | used |
| 1Pt-SiO2 | 101 |  | 107 | 0 |
| 1Pt2Bi-SiO2 | 162, 248, 349 | 90, 250, 349 | 185 | 78 |
| 1Pt5Bi-SiO2 | 197, 278, 371 | 120, 310, 363 | 199 | 95 |