Supplementary Information

Large-area synthesis of nanoscopic catalyst-decorated conductive MOF film using microfluidic-based solution shearing

Jin-Oh Kim1,4,Won-Tae Koo1,2,4, Hanul Kim3, Chungseong Park1,2,, Calvin Andreas Hutomo1, Siyoung Q. Choi3, Il-Doo Kim1,2, and Steve Park1

1Department of Materials Science and Engineering, Korea Advanced Institute of Science and Technology (KAIST), 291 Daehak-ro, Yuseong-gu, Daejeon 34141, Republic of Korea

2Membrane Innovation Center for Anti-virus & Air-quality Control, KAIST Institute for Nanocentury, 291, Daehak-ro, Yuseong-gu, Daejeon 34141, Republic of Korea

3Department of Chemical and Biomolecular Engineering, Korea Advanced Institute of Science and Technology (KAIST), Daejeon 34141, Korea

4These authors contributed equally: Jin-Oh Kim, Won-Tae Koo.

Corresponding authors: I.-D.K (idkim@kaist.ac.kr), S.P. (stevepark@kaist.ac.kr)

Table of Contents

- Supplementary Table 1. Summary of various fabrication methods of ultrathin C–MOFs.

- Supplementary Table 2. Mixing index and the concentration distribution of ligand for 10 microfluidic cycles without Pt solution’s flow.

- Supplementary Table 3. 3D surface and 2D cross sectional concentration distribution of ligand for 10 microfluidic cycles without Pt solution’s flow.

- Supplementary Table 4. Mixing index and the concentration distribution of ligand for 15 microfluidic cycles with Pt solution’s flow.

- Supplementary Table 5. 3D surface and 2D cross sectional concentration distribution of ligand for 15 microfluidic cycles with Pt solution’s flow.

- Supplementary Table 6. The weight ratio of Cu and Pt in Pt@Cu3(HHTP)2 at various flow rates of Pt precursors.

- Supplementary Table 7. Summary of the reaction rate constants of the sensors.

- Supplementary Table 8. Summary of sensing properties of 2D material-based NO2 sensors.

- Supplementary Fig. 1. Fabrication of microfluidic blade.

- Supplementary Fig. 2. Computational fluid dynamics simulation of microfluidic blade

- Supplementary Fig. 3. Effect of mixing time on the degree of mixing at various flow rates.

- Supplementary Fig. 4. Surface roughness profile measurement of Pt@Cu3(HHTP)2 thin-film.

- Supplementary Fig. 5. XRD patterns of Pt@Cu3(HHTP)2 after MiCS process, and only after microfluidic synthesis process without solution shearing.

- Supplementary Fig. 6. TEM images of Pt@Cu3(HHTP)2

- Supplementary Fig. 7. HRTEM image of Pt@Cu3(HHTP)2 under different synthesis processes.

- Supplementary Fig. 8. AFM topographic images of a manually scratched Pt@Cu3(HHTP)2 films at various shearing speeds.

- Supplementary Fig. 9. N2 adsorption and desorption isotherms of the Cu3(HHTP)2 and Pt@Cu3(HHTP)2 samples at 77 K.

- Supplementary Fig. 10. Comparison of electrical properties of films fabricated through MiCS process and conventional solution shearing process.

- Supplementary Fig. 11. Responses of Pt@Cu3(HHTP)2 thin-film at different ratios of Pt NPs.

- Supplementary Fig. 12. Response traces of the sensors to 0.1–1 ppm of NO2.

- Supplementary Fig. 13. Response times of the sensors to 0.1–3 ppm of NO2.

- Supplementary Fig. 14. Additional sensing results.

- Supplementary Fig. 15. Exponential fitting curves of the sensors.

- References

Supplementary Table 1. Summary of various fabrication methods of C-MOF-based films

| Methods | Example materials | Process times | THKa | Pros | Cons | Refb |
| --- | --- | --- | --- | --- | --- | --- |
| Drop casting | Cu3(HITP)2 | 1. Synthesis: ~2 days 2. Deposition: ~30 min | ≥ µm | Facile processes Applicable to various supports | Poor uniformity High surface roughness Difficult to produce ultra-thin layers Long processing time Difficult to synthesize at large-scale with high uniformity | 1, 2, 3 |
|  | Ni3(HHTP)2 |  |  |  |  |  |
|  | Cu3(HHTP)2 |  |  |  |  |  |
|  | Co3(HHTP)2 |  |  |  |  |  |
| Layer-by-layer (LbL) growth | Cu3(HHTP)2 | 1. Preparing substrates: ~1 days 2. LbL growth: ~1 min/cycle | ~2 nm/ cycle | High uniformity Accurate control of film THK Ultra-thin structure | Need of chemical modification on substrates Sequential LbL steps that can lead to long processing time | 1, 4 |
| Liquid-liquid interfacial reaction | Ag3BHT2 | 30 min | ~280 nm | Fast synthesis High uniformity | Difficult to control THK of films Difficult to synthesize at large-scale with high uniformity | 5 |
|  | Au3BHT2 | 6.5 h | ~320 nm |  |  |  |
| Microfluidic-based solution shearing (MiCS) | Cu3(HHTP)2 | 10 min | ~100 nm | Facile synthesis Ultra-fast synthesis High uniformity Accurate control of film THK Ultra-thin structure Large scale synthesis Simultaneous incorporation of nanocatalyst in the pores. |  | This work |

THKa is the thickness of the C-MOF-based films. Refb is reference.

Supplementary Table 2. Mixing index and the concentration distribution of ligand for 10 microfluidic cycles without Pt solution’s flow.

Supplementary Table 3. 3D surface and 2D cross sectional concentration distribution of ligand for 10 microfluidic cycles without Pt solution’s flow.

Supplementary Table 4. Mixing index and the concentration distribution of ligand for 15 microfluidic cycles with Pt solution’s flow.

Supplementary Table 5. 3D surface and 2D cross sectional concentration distribution of ligand for 15 microfluidic cycles with Pt solution’s flow.

Supplementary Table 6. The weight ratio of Cu and Pt in Pt@Cu3(HHTP)2 at various flow rates of Pt precursors.

| Flow rate (L/min) | Cu (Weight ratio %) | Pt (Weight ratio %) |
| --- | --- | --- |
| 50 | 20.1 | 0.9 |
| 100 | 20.0 | 2.3 |
| 150 | 20.2 | 2.7 |
| 200 | 20.4 | 3.5 |

Supplementary Table 7. Summary of the reaction rate constants of the sensors.

|  | kads (ppm-1 s-1) | kdes (s-1) | K (kads/kdes, ppm-1) |
| --- | --- | --- | --- |
| Cu3(HHTP)2 powder | 8.77 ± 0.26 × 10-3 | 8.60 ± 0.08 × 10-5 | 10.2 ± 0.3 |
| Cu3(HHTP)2 thin-film | 1.51 ± 0.03 × 10-3 | 2.60 ± 0.05 × 10-5 | 58.2 ± 1.2 |
| Pt@Cu3(HHTP)2 thin-film | 2.34 ± 0.22 × 10-3 | 4.83 ± 0.49 × 10-5 | 48.5 ± 4.6 |

kads is adsorption rate constant, kdes is desorption rate constant, and K is the equilibrium constant.

Supplementary Table 8. Summary of sensing properties of 2D material-based NO2 sensors operated at room temperature in air.

| Materials | Measurement | Reponse definition | Humidity | Response | Detection limit | Ref.a |
| --- | --- | --- | --- | --- | --- | --- |
| Pt@Cu3(HHTP)2 thin-film | Resistance | ΔRg/R0 | Dry | 89.9% to 3 ppm | 0.1 ppm | This work |
| Cu3(HHTP)2 thin-film | Resistance | ΔRg/R0 | Dry | 53.7% to 3 ppm | 0.1 ppm | This work |
| Cu3(HHTP)2 powder | Resistance | ΔRg/Ra | Dry | 11.8% to 3 ppm | 1 ppm | This work |
| Pd@Cu3(HHTP)2 powder | Resistance | ΔRg/Ra | Dry | 42.8% to 3 ppm | 1 ppm | 6 |
| MOF-templated PdO-Co3O4 | Resistance | ΔRg/Ra | Dry | 5% to 5 ppm | 1 ppm | 7 |
| MOF-derived carbons | Resistance | ΔRg/Ra | Dry | 1% to 5 ppm | 0.1 ppm | 8 |
| Scrolled graphene | Resistance | ΔRg/Ra | Dry | 67.9% to 3 ppm | 1 ppm | 9 |
| Sulfonated RGOb | Resistance | ΔRg/Ra | Dry | 58% to 10 ppm | 0.12 ppm | 10 |
| In2O3/RGO | Resistance | ΔRg/Ra | Dry | 50% at 10 ppm | 1 ppm | 11 |
| MoS2 nanosheets | Resistance | ΔRg/Ra | Dry | 15% at 5 ppm | 1.5 ppm | 12 |
| WS2/Ag nanowire | Resistance | ΔRg/Ra | Dry | 58% at 25 ppm | 1 ppm | 13 |
| WS2 nanosheets | Resistance | ΔRg/Ra | Dry | 38 % at 2 ppm | 0.1 ppm | 14 |
| CdTe/MoS2 | Resistance | ΔRg/Ra | Dry | 27% at 5 ppm | 0.1 ppm | 15 |
| RGO/MoS2 | Conductance | ΔGg/Ga | Dry | 28% at 4 ppm | 1 ppm | 16 |

Ref.a: the reference number in the manuscript. RGOb is the reduced graphene oxide.

Supplementary Fig. 1 Fabrication of microfluidic blade. (a) CAD image of the microfluidic blade channel design, (b) Photo image of laser-ablated polyimide film with microchannel design on each layer. (c) Photo image of fabricated microfluidic blade and (d) Photo image of solution shearing process with the fabricated microfluidic blade.

Supplementary Fig. 2 Computational fluid dynamics simulation of microfluidic channels.

Supplementary Fig. 3 Effect of mixing time on the degree of mixing at various flow rates.

Supplementary Fig. 4 Surface roughness profile measurement of Pt@Cu3(HHTP)2 thin-film fabricated by (a) MiCS and (b) conventional solution shearing at 150 oC (shearing speed: 5 mm/s). (Ra values: (a) 2.8 nm, (b) 92.3 nm)

Supplementary Fig. 5 XRD patterns of Pt@Cu3(HHTP)2 after MiCS process, and only after microfluidic synthesis process without solution shearing.

Supplementary Fig. 6 (a) TEM image of Pt@Cu3(HHTP)2, (b) HRTEM image of Pt@Cu3(HHTP)2, (c) STEM image of Pt@Cu3(HHTP)2 and (d) TEM-EDS mapping of Pt@Cu3(HHTP)2.

Supplementary Fig. 7 HRTEM images of Pt@Cu3(HHTP)2 under different synthesis processes.: (a) synthesized using bulk synthetic technique, (b) synthesized using microfluidic-based solution shearing process.

Supplementary Fig. 8 AFM topographic images of a manually scratched Pt@Cu3(HHTP)2 films at various shearing speeds.

Supplementary Fig. 9 N2 adsorption and desorption isotherms of the Cu3(HHTP)2 and Pt@Cu3(HHTP)2 samples at 77 K.

Supplementary Fig. 10 Comparison of electrical properties of C-MOF films fabricated through MiCS process and conventional solution shearing process: Optical images of C-MOF films fabricated by (a) MiCS process and (b) conventional solution shearing process. (c) Comparison of electrical properties of C-MOF films fabricated using MiCS process and conventional solution shearing process. Coefficient of variation (%) for each process is italicized.

Supplementary Fig. 11 Responses of Pt@Cu3(HHTP)2 thin-film to different flow rates of Pt precursor solution.

Supplementary Fig. 12 Response traces of the sensors to 0.1–1 ppm of NO2: (a) 0.1, (b) 0.2, (c) 0.4, (d) 0.6, (e) 0.8, and (f) 1 ppm of NO2. The shaded area indicates the standard deviation of the sensors (N ≥ 4).

Supplementary Fig. 13 Response times of the sensors to 0.1–3 ppm of NO2.

Supplementary Fig. 14 Additional sensing results. (a) Response traces of Pt@Cu3(HHTP)2 thin-film to multiple exposures of NO2 0.1 ppm. (b) Response traces of the sensors to NO2 1 ppm in dry and humid air. The shaded area in each graph presents the standard deviation of the sensors (N ≥ 4).

Supplementary Fig. 15 Exponential fitting curves of the sensors. Response traces of the sensors to 1 ppm of NO2: (a) Cu3(HHTP)2 powder, (b) Cu3(HHTP)2 thin-film, and (c) Pt@Cu3(HHTP)2 thin-film. Reaction rate constants were calculated by the exponential fitting of response traces.

In detail, NO2 reaction rate constants of the sensors were calculated by (1) the mass action law of NO2 reactions and (2) the assumption that response is proportional to the amounts of adsorbed NO2 molecules2,3. The reaction rate constants were obtained from the exponential fitting of the response trace curves [R(t)] using following equations.

Rt for NO2 adsorption=Rmax∙CgK1+CgK(1-exp-1+CgKK∙kads∙t)             (1)

Rt for NO2 desorption=R0exp⁡[-kdes∙t]                                 (2)

where K is the equilibrium constant, kads is the adsorption rate constant, and Kdes is the desorption rate constant, Rmax is the maximum response, and Cg is the concentration of gas (NO2) molecules.

References

1.	Ko, M., Mendecki, L., Mirica. K.A. Conductive two-dimensional metal-organic frameworks as multifunctional materials. Chem. Commun. 54, 7873-7891 (2018).

2.	Campbell, M.G., Sheberla, D., Liu, S.F., Swager, T.M., Dinca, M. Cu3(hexaiminotriphenylene2: an electrically conductive 2D metal-organic framework for chemiresistive sensing. Angew. Chem., Int. Ed. 54, 4349-4352 (2015).

3.	Mendecki, L., Mirica, K.A. Conductive metal-organic frameworks as ion-to-electron transducers in potentiometric sensors. ACS Appl. Mater. Interfaces 10, 19248-19257 (2018).

4.	Yao, M.S. et al. Layer‐by‐layer assembled conductive metal–organic framework nanofilms for room‐temperature chemiresistive sensing. Angew. Chem., Int. Ed. 56, 16510-16514 (2017).

5.	Chen, I.-F., Lu, C.-F., Su, W.-F. Highly conductive 2D metal–organic framework thin film fabricated by liquid–liquid interfacial reaction using one-pot-synthesized benzenehexathiol. Langmuir 34, 15754-15762 (2018).

6.	Koo, W.-T., Kim, S.-J., Jang, J.-S., Kim, D.-H., Kim, I.-D. Catalytic metal nanoparticles embedded in conductive metal–organic frameworks for chemiresistors: highly active and conductive porous materials. Adv. Sci. 6, 1900250 (2019).

7.	Choi, S.-J., Choi, H.-J., Koo, W.-T., Huh, D., Lee, H., Kim, I.-D. Metal-organic framework-templated PdO-Co3O4 nanocubes functionalized by SWCNTs: improved NO2 reaction kinetics on flexible heating film. ACS Appl. Mater. Interfaces 9, 40593-40603 (2017).

8.	Rui, K. et al. Dual-function metal-oganic framework-based wearable fibers for gas probing and energy storage. ACS Appl. Mater. Interfaces 10, 2837-2842 (2018).

9.	Chen, Z. et al. Mimicking a dog's nose: scrolling graphene nanosheets. ACS Nano 12, 2521-2530 (2018).

10.	Yuan, W., Liu, A., Huang, L., Li, C., Shi, G. High-performance NO2 sensors based on chemically modified graphene. Adv. Mater. 25, 766-771 (2013).

11.	Yang, W., Wan, P., Zhou, X., Hu, J., Guan, Y., Feng, L. Additive-free synthesis of In2O3 cubes embedded into graphene sheets and their enhanced NO2 sensing performance at room temperature. ACS Appl. Mater. Interfaces 6, 21093-21100 (2014).

12.	Cho, B. et al. Charge-transfer-based gas sensing using atomic-layer MoS2. Sci. Rep. 5, 8052 (2015).

13.	Ko, K.Y. et al. Improvement of gas-sensing performance of large-area tungsten disulfide nanosheets by surface functionalization. ACS Nano 10, 9287-9296 (2016).

14.	Xu, T. et al. The ultra-high NO2 response of ultra-thin WS2 nanosheets synthesized by hydrothermal and calcination processes. Sens. Actuators, B 259, 789-796 (2018).

15.	Jaiswal, J., Sanger, A., Tiwari, P., Chandra, R. MoS2 hybrid heterostructure thin film decorated with CdTe quantum dots for room temperature NO2 gas sensor. Sens. Actuators, B 305, 127437 (2020).

16.	Zhou, Y., Liu, G., Zhu, X., Guo, Y. Ultrasensitive NO2 gas sensing based on rGO/MoS2 nanocomposite film at low temperature. Sens. Actuators, B 251, 280-290 (2017).