Supplementary Information

Jia-Wei Wang et al.

Experimental Section

Materials

CuBCP,1 CuBCP',1 BIH,2 CoTSPc (deprotonated and protonated),3 CoTCPc,4,5 and pbcp ligand6 were prepared following the previously reported methods. Milli-Q ultrapure water (> 18 MΩ) was utilized unless otherwise stated. [Cu(CH3CN)4]PF6 (97%, Innochem), bis[(2-diphenyl-phosphino)phenyl]ether (DPEphos; 97%, Innochem), 9,9-dimethyl-4,5-bis(diphenylphosphino)xanthene (xantphos; 97%, Innochem), 2,9-dimethyl-4,7-diphenyl-1,10-phenanthroline (bathocuproine, bcp; 97%, Innochem), CoPc (97%, β-form, Aldrich), CoTAPc (95%, Jilin Chinese Academy of Sciences-Yanshen Technology Co., Ltd.), CH3CN (Superdry, >99.5%, Acros), NMP (Superdry, >99.5%, Acros), TEA (Superdry, >99.5%, Energy Chemical Co., Ltd.), phenol (99.5%, Aladdin), 2,2,2-trifluoroethanol (TFE, 99.5%, Aladdin), CO2 (99.999%), N2 (99.999%), 13CO2 (99.9%) and other chemicals were commercially available and used without further purification.

Characterization

1H NMR and 1H-1H 2D NMR correlation spectroscopy (COSY) spectra were obtained on a Bruker advance III instrument (400 MHz). Electrochemical measurements were carried out using an electrochemical workstation (CHI 620E). All potentials were referenced against ferrocenium/ferrocene (Fc+/Fc) as an internal standard. Unless otherwise stated, all potentials were footnoted as vs. normal hydrogen electrode (NHE) by adding 0.64 V based on the potentials vs. Fc+/Fc. The irradiation experiments were carried out with a blue LED light (Zolix, MLED4). Gas chromatographic analysis was conducted on an Agilent 7820A gas chromatography equipped with a thermal conductivity detector (TCD) and a TDX-01 packed column, where the oven temperature was held constant at 60 °C, the inlet and detector temperature were set at 80 °C and 200 °C, respectively. The isotopic labeling experiment was conducted under 13CO2 atmosphere and the gas in the headspace was analyzed by a quantitative mass spectrometer attached Agilent 7890A gas chromatography. The liquid phase of the reaction system was analyzed by an ion chromatograph (Metrohm, 930 Compact IC Flex, Supp 5 anion column, Na2CO3/NaHCO3 aqueous eluent) to detect the presence of formate. UV–vis spectra were collected on a Shimadzu UV-3600 spectrophotometer. The emission experiments were conducted on a modular fluorescent life and steady-state fluorescence spectrometer (FLSP1000, Edinburgh Instruments LTD.). The TA spectroscopy was carried out on a laser flash photolysis instrument (LP980, Edinburgh Instruments LTD.). All experiments were operated at room temperature (24~25 °C) unless otherwise stated.

Synthesis of CoTDMAPc

CoTAPc (0.79 mmol, 0.5 g) and iodomethane (3 mL) were stirred at room temperature in DMF (20 mL) for 24 h. After the reaction, diethyl ether was added to the mixture. The precipitate was collected by centrifugation with ethanol for five times and water for five times, respectively. The final product was dried in oven at 373 K as a blue-green solid. MALDI-TOF: CoTDMAPc (measured: 743.249; simulated: 743.251).

Synthesis of CuPBCP/CuPBCP'

The synthesis follows a similar procedure for preparing heteroleptic Cu(I) PSs.7 In a 50 mL Schlenk tube, [Cu(CH3CN)4]PF6 (186 mg, 0.5 mmol) and DPEphos (279 mg, 0.5 mmol) or xantphos (289 mg, 0.5 mmol) are dissolved in 10 mL dry DCM at room temperature under N2 and darkness. The resulting solution is stirred at 40 °C for 2 h. The reaction mixture is then added with the pbcp ligand (180 mg, 0.5 mmol) under N2 flow. The resulting mixture is then heated at 45 °C for 2 h. The reaction mixture was then allowed to cool to room temperature and the solvent was evaporated under reduced pressure. Then a minimal volume of dry DCM (ca. 5 mL) was added to dissolve most the orange residue, which was filtrated via a 0.45 μM nylon membrane, followed by the addition of excess xantphos (ca. 70 mg) into the filtrate to prevent the formation of [Cu(pbcp)2]+. Finally, excess dry hexane (50 mL) was added to precipitate CuPBCP/CuPBCP' as yellow powder (46%/55% yield). It should be noted that the presence of trace water will make the product oily. The yellow prism crystals were obtained by the gaseous diffusion of ether into dry CH3CN solutions of the Cu(I) PSs. Q-TOF ESI-MS(+): [Cu(xantphos)(pbcp)]+ (measured: 1003.2767; simulated: 1003.2756); [Cu(DPEphos)(pbcp)]+ (measured: 963.2444; simulated: 963.2437).

DFT Calculation on CoPc complexes

Cobalt phthalocyanine with varied substituents have been optimized by Perdew-Burke-Ernzerhof hybrid functional (PBE0)8 method and def2-SVP basis set with ultrafine integration grids and Grimme’s DFT-D3(BJ) empirical dispersion correction9 by Gaussian 09 package.10 Harmonic vibrational frequency was performed at the same level to guarantee that there is no imaginary frequency in the molecules, i.e. they locate on the minima of potential energy surface. The Hirshfeld population11 was gained from Gaussian, while the electron density at cobalt center were yielded from Multiwfn 3.812 whose input files were extracted from Gaussian format checkpoint.

X-ray Crystallography

Single-crystal X-ray diffraction data were collected at 150 K on an Agilent Technologies Supernova system with Cu/Kα (λ = 1.54178 Å) radiation. The empirical absorption corrections were applied using spherical harmonics, implemented in SCALE3 ABSPACK scaling algorithm. The structure was solved using direct method and refined by the full-matrix least-squares method on F2, which yielded the positions of all non-hydrogen atoms. These were refined first isotropically and then anisotropically. All the hydrogen atoms of the ligand were placed in calculated positions with fixed isotropic thermal parameters and included in the structure factor calculations in the final stage of full-matrix least-squares refinement. All the calculations were performed using the SHELX-97 program.13 CCDC number: CuPBCP (2092595) and CuPBCP' (2043973).

Determination of Binding Constant

Binding isotherms for the NMR titration were calculated from a global proton shift analysis using Bindfit with the shift differences (δ - δ0) taken to obtain a binding isotherm.14 The fitting is based on the shift difference between the host-only data and the data at varying guest concentrations. The Equations used for these analyses are available in the review by Thordarson.15 Nelder-Mead (Simplex) method was used as the optimal search algorithm. The error of binding constant, the root mean square and the covariance of the fit (variance of the residuals divided by the variance in the data) were used to conclude the models that best describe the binding between CuPBCP and CoTCPc. Specific discussion on the choices of the models is included in the table captions. It should be noted that the non-cooperative mode means that each of the multiple binding process does not interfere with each other, in which the second binding constant (K12 or K21) will be equivalent to the first binding constant (K11). For the choices of protons in binding fits, we observed that most protons at the pbcp ligand in CuPBCP underwent significant relaxation with the addition of CoTCPc and thus disappeared, presumably due to the coordinative interaction with paramagnetic Co(II) center. We thus only utilized the shifted but not vanished protons G, H, J1-J4 and K1-K4 of CuPBCP for binding fits, which still afforded reliable binding constants that are consistent with our previous works on coordinative interaction.16

Cyclic Voltammetry

Cyclic voltammetry was performed in a 25 mL gas-tight three-neck flask with a three-electrode system, where a 3 mm glassy carbon disc electrode, a platinum wire auxiliary electrode, and a platinum wire pseudo-reference electrode were placed in a 0.1 M tetrabutylammonium hexafluorophosphate (TBAPF6) NMP solution (8.0 mL) or NMP/TEA (v:v = 5:1; 9.6 mL). Prior to experiments, the working electrode was polished in turn with 0.3 and 0.05 μm Al2O3 slurry for 3 min to obtain a mirror surface, then sonicated in water for ~60 seconds to remove debris, and finally rinsed with water. The solution was bubbled with N2/CO2 for 15 min prior to each experiment. Scan rate is 100 mV/s.

Photocatalytic Experiments

The photocatalytic reduction of CO2 to CO was conducted in a 17 mL home-made reactor upon successive addition of catalyst, proton source, a CH3CN solution containing Cu PS, corresponding diphosphine ligand and BIH, and finally TEA, under 1 atm CO2 atmosphere at 293±2 K. Phenol was placed in a N2-saturated Schlenk flask and molten at 70 °C prior to use. After the reaction system purged with CO2 for 10 min, the photocatalytic reaction was initiated by irradiation under an LED light. The generated gases in the headspace were analyzed by a gas chromatography, and the possible products in the solution were analyzed by an ion chromatograph.

Determination of Φ for CO Production

A reported method17 was used to determine Φ. A typical experiment employed a mixture of CoTCPc (0.05 mM), CuBCP (0.5 mM), xantphos (1.0 mM), phenol (5.0 v%), and BIH (50 mM) in 4.0 mL CH3CN/TEA (v:v = 5:1) for evaluation. The temperature was kept at 25 °C. The light source is an LED light set-up (λ = 425 ± 5 nm, light intensity = 40 mW·cm−2, irradiated area is 1.5 cm2). The photon flux is determined to be 2.39 × 10-7 einstein s-1.18 Under these conditions, the light entering the reaction solution was considered to be fully absorbed by PS without scattering, suggesting the evaluated Φ is a lower limit. The 5 min of light irradiation is consistent with the total number of photons np = 7.18 × 10-5 einstein.

The Φ with BIH as the two-electron reductant was evaluated by the Equation19 for two-electron reduction of CO2.

Φ = n(CO) / np                                                                           (S1)

A typical Φ of 63.5% was determined by the measured n(CO) = 45.6 μmol by GC-TCD after 5 min of irradiation.

Determination of Quenching Rate (kq)

A reported method19 was followed to calculate the kq, where the fluorescence intensity of photo-excited Cu(I) PS in the presence of quencher was measured and fitted to the Stern-Volmer Equation,

I0I=1+K[Q]=1+kqτ0[Q]                                                                 (S2)

In this Equation, I0 and I are the fluorescence intensity values in the absence and presence of the quencher, K is the Stern-Volmer constant for dynamic quenching, kq is the apparent rate of bimolecular quenching, τ0 is the lifetime of the excited state without quencher, and [Q] is the concentration of the quencher.

In the time-resolved fluorescent quenching experiments, the calculation Equation should be

τ0τ=1+kq'τ0[Q]                                                                           (S3)

Here kq' is the dynamic quenching rate.

Determination of Second-Order Reaction Rate (kr) for the Excited States

A reported method20 was followed to calculate the kr, where the lifetime of reduced Cu(I) PS in the presence of quencher was measured and fitted to the following Equation S4,

τ1τ=1+krτ1[Q]                                                                           (S4)

In this Equation, τ1 and τ are the lifetimes in the absence and presence of the quencher, and [Q] is the concentration of the quencher.

Extended X-ray Absorption Fine Structure (EXAFS) Analysis

Athena software21 was used for data processing. The energy scale for each scan was normalized using copper metal standard. Data in energy space were pre-edge corrected, normalized, deglitched (if necessary), and background corrected. The processed data were next converted to the photoelectron wave vector (k) space and weighted by k2. The electron wave number is defined as. E0 is the energy origin or the threshold energy. K-space data were truncated near the zero crossings k = 2 to 11.674 Å-1 for the CuBCP and CuPBCP ground states and k = 2 to 9 Å-1 for the reconstructed excited states in the Cu EXAFS Fourier transformation. The k-space data were transferred into the Artemis Software for curve fitting. In order to fit the data, the Fourier peaks were isolated separately, grouped together, or the entire (unfiltered) spectrum was used. The individual Fourier peaks were isolated by applying a Hanning window to the first and last 15% of the chosen range, leaving the middle 70% untouched. Curve fitting was performed using ab initio-calculated phases and amplitudes from the FEFF822 program from the University of Washington. Ab initio-calculated phases and amplitudes were used in the EXAFS Equation (Equation S5),

|  | (S5) |
| --- | --- |

where Nj is the number of atoms in the jth shell; Rj the mean distance between the absorbing atom and the atoms in the jth shell; (,k, Rj ) is the ab initio amplitude function for shell j, and the Debye-Waller term accounts for damping due to static and thermal disorder in absorber-backscatterer distances. The mean free path term  reflects losses due to inelastic scattering, where λj(k), is the electron mean free path. The oscillations in the EXAFS spectrum are reflected in the sinusoidal term , where is the ab initio phase function for shell j. This sinusoidal term shows the direct relation between the frequency of the EXAFS oscillations in k-space and the absorber-backscatterer distance. S02 is an amplitude reduction factor.

The EXAFS equation23 (Equation S5) was used to fit the experimental Fourier isolated data (q-space) as well as unfiltered data (k-space) and Fourier transformed data (R-space) using N, S02, E0, R, and 2 as variable parameters (Supplementary Table 11). N refers to the number of coordination atoms around Cu for each shell. The quality of fit was evaluated by R-factor and the reduced Chi2 value. The deviation in E0 ought to be less than or equal to 10 eV. R-factor less than 2% denotes that the fit is good enough. R-factor between 2 and 5% denotes that the fit is correct within a consistently broad model. The reduced Chi2 value is used to compare fits as more absorber-backscatter shells are included to fit the data. A smaller reduced Chi2 value implies a better fit. Similar results were obtained from fits in k, q, and R-spaces.

Steady-State and Time-Resolved XAS Measurements

Steady-state and time-resolved X-ray absorption spectra were collected at 11 ID-D24 beamlines at the Advanced Photon Source using undulator radiation at electron energy 8.98 keV in solvent grade acetonitrile. The samples were circulated through a stainless-steel nozzle into a free-flowing cylindrical jet inside an airtight aluminum chamber, and continuously degassed with nitrogen. This sample handling technique ensures proper sample recovery such that the subsequent laser pulse can hit a “fresh” sample position.

Cooled running water from a chiller was additionally circulated around the jacketed sample flask to prevent heating damage of the complexes by radiation. The X-ray fluorescence signals were collected with two avalanche photodiodes (APDs) positioned at 90˚ on both sides of the liquid jet, and a combination of Z-1 filters and soller slits with conical geometry were used to reduce the background from elastically scattered X-rays.

The experiments were carried out using the 24-bunch timing mode of APS (in top up mode with a constant 102 mA ring current) which consists of a train of X-rays separated by 153 ns. This mode easily allows for gateable detectors that selects X-ray pulses. This timing mode was suitable for this type of experiments in which the separation between adjacent X-ray pulses is long enough for the Avalanche Photodiode (APD) detector to resolve individual X-ray pulses.

The time-resolved experiments were carried out by pumping the samples at 400 nm wavelength using a regenerative amplified laser with 10 kHz repetition rate 5 ps-FWHM pulse length and laser power of 630 mW at the sample. The X-ray and laser beam was spatially overlapped with an X-ray spot size of 100 µm (V) × 450 µm (H) and laser spot size of 170 µm (V) × 550 µm (H). With a liquid flow speed of around 4.5 m s-1, the pumped laser volume was calculated to move out of the FWHM laser pulse region in around 20 µs. This temporal range ensured that the excited state volume was probed more at the center and less at the edges where the excitation fraction would be less, due to movement of the sample. Beamline 11 ID-D has an automated data digitization system which allows for all X-ray pulses after laser excitation to be collected. Such a system, together with the larger X-ray beam spot size, was very useful for our experiments, as multiple X-ray pulses after laser excitation were averaged to monitor the dynamics for the formation and decay of triplet states for the CuBCP and CuPBCP as PSs in the nano-microsecond time regime.

The delay between the pump and X-ray pulses was adjusted by a programmable delay line (PDL-100A-20NS, Colby Instruments). A Cu metal foil was placed between two ionization chambers downstream to the X-ray beam, and its transmission recorded with each scan for energy calibration.

Ground and Excited-State DFT Calculations

The DFT optimization calculations were performed using the ORCA (Version 4.2.0) program package developed by Neese25 and co-workers. The geometry optimizations of the ground state structures were carried out using the BP86 exchange-correlation functional26,27 in combination with the triple zeta valance polarization functions (def2-TZVP),28 and the atom-pairwise dispersion correction with the Becke-Johnson damping scheme (D3BJ).29,30 The ground state structures for the complexes in solution were furthermore optimized at the BP86 level with the def2-TZVP triple-zeta basis sets, the atom-pairwise dispersion correction D3BJ and after considering solvent effect of acetonitrile by the PCM31 method.

The excited-state geometries were by contrast optimized using the B3LYP32,33 as functional with the def2-TZVP triple-zeta28 basis sets and once again with the Becke-Johnson damping scheme (D3BJ)29,30 and the PCM31 method. The RI34,35 and RIJCOSX36 approximations were used to accelerate Coulomb and exchange integrals for the ground and excited state calculations respectively. The default GRID settings were further employed for the self-consistent field iterations and for the final energy evaluation. The calculated structures were confirmed to be minima based on a check of the energies and the absence of imaginary frequencies from frequency calculations carried out on the optimized geometries.

Supporting Figures

Supplementary Figure 1. MALDI-TOF HR MS spectrum of CoTCPc dissolved in NMP.

Supplementary Figure 2. MALDI-TOF HR MS spectrum of CoTSPc dissolved in NMP.

Supplementary Figure 3. MALDI-TOF HR MS spectrum of CoTDMAPc dissolved in NMP.

Supplementary Figure 4. UV-vis spectra of 25 μM CoPc derivatives in NMP.

Supplementary Figure 5. CVs of 0.5 mM CoTCPc in 0.1 M nBu4NPF6 NMP/TEA (v:v = 5:1) solution under N2 (deep red), CO2 (medium red) or CO2 (pale red) with 5 v% phenol at a scan rate of 0.1 V s-1.

Supplementary Figure 6. CVs of (a) 0.1 mM CoTSPc (limited solubility), (b) 0.5 mM CoPc, (c) 0.5 mM CoTAPc or (d) 0.5 mM CoTDMAPc in 0.1 M nBu4NPF6 NMP/TEA (v:v = 5:1) solution under N2 (deep color), CO2 (medium color) or CO2 (pale color) with 5 v% phenol (PhOH) at a scan rate of 0.1 V s-1.

Supplementary Figure 7. (a,b) 1H and (c) 2D COSY NMR spectra of CuPBCP in CD3CN with proton assignments.

Supplementary Figure 8. (a,b) 1H and (c) 2D COSY NMR spectra of CuPBCP' in CD3CN with proton assignments.

Supplementary Figure 9. Q-TOF HR MS spectrum of CuPBCP dissolved in CH3CN.

Supplementary Figure 10. Q-TOF HR MS spectrum of CuPBCP' dissolved in CH3CN.

Supplementary Figure 11. Crystal structure of the cation of CuPBCP. Counter anions and solvent molecules are omitted for clarity. Possibility = 50%.

Supplementary Figure 12. Crystal structure of the cation of CuPBCP'. Counter anions and solvent molecules are omitted for clarity. Possibility = 50%.

Supplementary Figure 13. Excited-state lifetime measurements of Cu(I) PSs, including (a) CuBCP (pink), (b) CuBCP' (azure), (c) CuPBCP (orange) and (d) CuPBCP' (turquoise). Deaerated 50 μM CH3CN solutions of Cu(I) PSs were used.

Supplementary Figure 14. (a) Reduction and (b) oxidation CVs of 0.5 mM CuBCP (pink), CuPBCP (orange), CuBCP’ (azure) or CuPBCP’ (turquoise) in 0.1 M nBu4NPF6 CH3CN solution under N2 with 1.0 mM Fc as the internal reference.

Supplementary Figure 15. Time profiles and TONs of photocatalytic CO and H2 yields from a mixture of CuBCP (0.5 mM), xantphos ligand (1.0 mM), phenol (5.0 v%), and BIH (20 mM) in 4 mL CH3CN/TEA (v:v = 5:1) within 1 h of 450-nm LED irradiation under 1 atm CO2 with the concentration of CoTCPc as (a) 0.2 μM, (b) 2.0 μM, (c) 20 μM, (d) 50 μM, (e) 100 μM or (f) 200 μM.

Supplementary Figure 16. UV-vis spectra of 50 μM CuBCP (magenta), 10 μM CoTCPc (red) and 10 μM BIH (volet) in CH3CN.

Supplementary Figure 17. Time profiles of photocatalytic CO and H2 yields from a mixture of CuBCP (0.5 mM), xantphos ligand (1.0 mM), CoTCPc (0.05 mM), and BIH (20 mM) in 4 mL CH3CN/TEA (v:v = 5:1) under 1 atm CO2 without proton souce (violet) or with 5.0 v% of phenol (PhOH, orange), TFE (red) or H2O (pink).

Supplementary Figure 18. Mass spectra analyses via gas chromatography on the generated gas from a mixture of CuBCP (0.5 mM), xantphos ligand (1.0 mM), CoTCPc (0.05 mM), phenol (5.0 v%), and BIH (20 mM) in 4 mL CH3CN/TEA (v:v = 5:1) within 1 h of 450-nm LED irradiation under 1 atm CO2.

Supplementary Figure 19. (a,b) 1H and (c) 2D COSY NMR spectra of CuPBCP in d7-DMF with proton assignments.

Supplementary Figure 20. 1H NMR titration of CoTCPc into a 0.50 mM DMF-d7 solution of CuPBCP.

Supplementary Figure 21. 1H NMR titration of CoTCPc into a 0.50 mM DMF-d7 solution of CuBCP. The magnified area clearly show that no shift of the aromatic proton signals took place when increasing concentration of CoTCPc was added in the solution of CuBCP, indicative of no interaction.

Supplementary Figure 22. UV-vis spectra of 10 μM CH3CN solution of CoTCPc in the absence (red) or presence (crimson) of 16.7 v% TEA. The enhanced absorbance and narrowed peak of the Q band indicate the diminished staking of CoTCPc, consistent with the coordination of TEA to isolate each molecule.

Supplementary Figure 23. 1H NMR titration of CoTCPc into a 0.50 mM DMF-d7 solution of CuPBCP in the absence of presence of 5 v% TEA. It should be noted that the addition of TEA volume ratio higher than 5% will enhance the difficulties of shimming during NMR titration, and 5 v% is already excessive to the concentration of guest/host.

Supplementary Figure 24. Proposed catalytic mechanism of CoTCPc for CO2 reduction.

Supplementary Figure 25. Transient fluorescent spectra of a CH3CN solution containing 0.1 mM CuBCP, in the absence and presence of varying concentrations of quencher (a) BIH or (c) CoTCPc, respectively. Ratio of lifetimes versus (b) [BIH] with linear fitting or (d) [CoTCPc].

Supplementary Figure 26. Nanosecond TA spectroscopic results of (a,b) CuBCP and (c,d) CuPBCP. (a) TA spectra of 0.03 mM CuBCP with 0.15 mM CoTCPc. (b) Plot of (τ1 / τ - 1) versus [CoTCPc] with linear fitting for the CuBCP system. or (c) 0.03 mM CuPBCP with 0.05 mM CoTCPc. (d) Plot of (τ1 / τ - 1) versus [CoTCPc] with linear fitting for the CuPBCP system.

Supplementary Figure 27. (a) Normalized Cu K-edge XANES of CuBCP (black) and CuPBCP (red). (b) Fourier transforms of k2-weighted Cu EXAFS for CuBCP (black) and CuPBCP (red). (c) Simulated EXAFS spectra for CuBCP (black) and CuPBCP (red) using atomic coordinates obtained from DFT simulations.

Supplementary Figure 28. Fourier transforms of k2-weighted Cu EXAFS for (a) ground-state CuBCP (solid black line) and its corresponding fit (Fit 2, Supplementary Table 9, dotted black line), (b) reconstructed excited-state CuBCP (solid magenta line) and its corresponding fit (Fit 5, Supplementary Table 9, dashed red line), (c) ground-state CuPBCP (solid red line) and its corresponding fit (Fit 4, Supplementary Table 9, dashed green line) and (d) reconstructed excited-state CuPBCP (solid green line) and its corresponding fit (Fit 6, Supplementary Table 9, dashed blue line).

Supplementary Figure 29. Stacked spectra between laser and X-ray pulses for (a) 0.8 mM CuBCP in CH3CN, at a series of time delays between 100 ps to 1.07 µs and (b) 0.8 mM CuPBCP in CH3CN between 100 ps to 306 ns. The dotted lines represent the raw data and the solid lines represent smoothened spectra, respectively.

Supporting Tables

Supplementary Table 1. Elemental analysis results of Cu PSs and several CoPc derivatives.

| Complexes | Calculated formula | Calculated value (%) |  |  | Measured value (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | C | H | N | C | H | N |
| CuBCP | CuC65.5H53F6N2P3OCl (CuBCP·0.5CH2Cl2) | 66.11 | 4.49 | 2.35 | 66.45 | 4.44 | 2.18 |
| CuPBCP | CuC63H50F6N2P3OCl (CuPBCP) | 65.82 | 4.38 | 4.87 | 66.01 | 4.42 | 4.96 |
| CuBCP' | CuC62H49F6N2P3O1.5 (CuBCP'·0.5H2O) | 66.70 | 4.42 | 2.51 | 67.24 | 4.37 | 2.53 |
| CuPBCP' | CuC60H46F6N4P3O (CuPBCP') | 64.95 | 4.18 | 5.05 | 65.14 | 4.41 | 5.07 |
| CoTCPc | CoC36H28Cl2N8Na2O14 (CoTCPc·6H2O·2NaCl) | 44.46 | 2.90 | 11.52 | 44.42 | 3.02 | 11.86 |
| CoTSPc | CoC32H14Cl2N8NaO13S4 (CoTSPc4-·H2O·NaCl) | 36.39 | 1.34 | 10.61 | 36.82 | 1.31 | 10.84 |
| CoTDMAPc | C45H47CoI5N13Na5O2 (CoTDMAPc·NMP·H2O·5NaI) | 33.56 | 2.94 | 11.31 | 33.75 | 2.85 | 11.01 |

Supplementary Table 2. 1H NMR results and proton assignments of Cu(I) PSs.

| Entry | Compounds | Solvent | Assignments |
| --- | --- | --- | --- |
| 1 | CuBCP | CD3CN | 1H-NMR (CD3CN, 400 MHz, 25 °C): δ [ppm] =7.77 (d, J = 7.8 Hz, 2H), 7.73 (s, 2H), 7.59 (t, J = 6.5 Hz, 6H), 7.53 (d, J = 8.9 Hz, 6H), 7.33-7.23 (m, 6H), 7.21-7.03 (m, 18H), 2.33 (s, 6H), 1.74 (s, 6H). |
| 2* | CuPBCP | CD3CN | 1H-NMR (CD3CN, 400 MHz, 25 °C): δ [ppm] = 8.82 (dd, 4H, J = 4.4, 1.6, py-H), 7.80 (dd, 2H, J = 7.9, 1.3 Ar-H), 7.69 (s, 2H, phen-H), 7.58 (s, 2H, phen-H), 7.51 (dd, 4H, J = 4.4, 1.6 py-H), 7.35-7.27 (m, 6H, Ar-H), 7.20-7.06 (m, 18H, Ar-H), 2.37 (s, 6H, CH3), 1.76 (s, 6H, CH3). |
| 3 | CuBCP' | CD3CN | 1H-NMR (CD3CN, 400 MHz, 25 °C): δ [ppm] =7.79 (s, 2H), 7.61 (d, J = 7.0 Hz, 6H), 7.59-7.53 (m, 6H), 7.43 (dd, J = 17.6, 9.9 Hz, 4H), 7.29 (t, J = 7.4 Hz, 2H), 7.23 (t, J = 6.9 Hz, 4H), 7.13-7.02 (m, 18H), 2.50 (s, 6H). |
| 4* | CuPBCP' | CD3CN | 1H-NMR (CD3CN, 400 MHz, 25 °C): δ [ppm] = 8.81 (d, J = 4.5 Hz, 4H, py-H), 7.73 (s, 2H, phen-H), 7.60 (s, 2H, phen-H), 7.51 (d, J = 4.6 Hz, 4H, py-H), 7.44 (dd, J = 16.8, 8.2 Hz, 4H, Ar-H), 7.30 (t, J = 7.5 Hz, 2H, Ar-H), 7.23 (t, J = 6.8 Hz, 4H, Ar-H), 7.13-6.98 (m, 18H, Ar-H), 2.51 (s, 6H, CH3). |
| 5 | CuBCP | d7-DMF | 1H-NMR (d7-DMF, 400 MHz, 25 °C): δ [ppm] = 7.93 (d, J = 7.6 Hz, 2H), 7.85 (s, 2H), 7.77 (s, 2H), 7.70-7.61 (m, 10H), 7.39 (t, J = 7.6 Hz, 6H), 7.28-7.18 (m, 16H), 7.16-7.10 (m, 2H), 2.47 (s, 6H), 1.79 (s, 6H). |
| 6* | CuPBCP | d7-DMF | 1H-NMR (d7-DMF,, 400 MHz, 25 °C): δ [ppm] = 8.88 (d, J = 4.6 Hz, 4H, py-H), 7.95 (d, J = 7.8 Hz, 2H, Ar-H), 7.87 (s, 2H, phen-H), 7.83 (s, 2H, phen-H), 7.69 (d, J = 4.5 Hz, 4H, py-H), 7.40 (t, J = 7.2 Hz, 6H, Ar-H), 7.29-7.12 (m, 18H, Ar-H), 2.50 (s, 6H, CH3), 1.79 (s, 6H, CH3). |

*More detailed assignments have been made with the references of 1H-1H 2D NMR correlation spectroscopy (COSY) spectra (Figures S7, S8, and S19).

Supplementary Table 3. Crystallographic data for CuPBCP and CuPBCP'.

| Complex | CuPBCP | CuPBCP'·(C2H5)2O·H2O |
| --- | --- | --- |
| Formula | C63H50CuF6N4OP3 | C64H56CuF6N4O3P3 |
| CCDC number | 2092595 | 2043973 |
| Formula weight | 1149.52 | 1199.57 |
| Crystal system | triclinic | monoclinic |
| Space group | P-1 | Cc |
| Z | 2 | 4 |
| a / Å | 11.0218(2) | 24.1468(17) |
| b / Å | 13.2401(3) | 10.3466(7) |
| c / Å | 24.7771(9) | 23.3639(16) |
| α / ° | 97.109(2) | 90 |
| β / ° | 97.344(2) | 102.528(3) |
| γ / ° | 97.8986(16) | 90 |
| V / Å3 | 3515.07(16) | 5698.2(7) |
| ρcalcd / g m-3 | 1.086 | 1.398 |
| μ / mm-1 | 1.524 | 0.538 |
| Crystal size / mm | 0.25 × 0.18 × 0.12 | 0.18 × 0.15 × 0.12 |
| 2Θ range for data collection / ° | 6.81 / 145.86 | 3.456 / 54.36 |
| Reflns collected / Independent | 25680 / 13644 | 41445 / 12330 |
| Rint | 0.0361 | 0.0543 |
| Parameters refined | 711 | 737 |
| F(000) | 1184.0 | 2480.0 |
| GOF on F2 | 1.020 | 1.115 |
| Final R indices [I > 2sigma(I)] | R1a = 0.0650 wR2b = 0.1736 | R1a = 0.0967 wR2b = 0.2593 |
| R indices (all data) | R1 = 0.0720 wR2 = 0.1804 | R1 = 0.1123 wR2 = 0.2781 |
| Largest diff. peak and hole / e Å-3 | 1.79 / -0.45 | 0.88 / -2.03 |

aR1 = ∑||F0| - |Fc||/∑F0. bwR2 = {[∑(F02-Fc2)/∑w (F02)2]}1/2, w = 1/[s2(Fo2) + (0.2000P)2 + 0.0000P]; where P = (Fo2 + 2Fc2)/3

Supplementary Table 4. Measured geometrical, photophysical and redox properties of Cu(I) PSs in deareated CH3CN.a

| Cu PS | Dihedral angle (°) | λem (nm) | λab (nm) | ε450 (M-1 cm-2) | Φemb | τb (ns) | Ered (V) | Eox (V) | Isosbestic point (nm) | E0-0 (V) | Eq, red (V) | Eq, ox (V) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CuBCP | 95.0 | 580 | 388 | 766 | 0.58% | 280.0 ns τ1 = 12.4 ns, 2% τ2 = 285.4 ns, 98% | -1.36 | 0.86 | 460 | 2.70 | 1.34 | -1.84 |
| CuPBCP | 94.2 | 550 | 395 | 885 | 0.23% | 74.2 ns τ1 = 2.8 ns, 28% τ2 = 38.6 ns, 50% τ3 = 240.5 ns, 22% | -1.37 | 0.92 | 430 | 2.88 | 1.51 | -1.96 |
| CuBCP' | 91.3 | 620 | 393 | 608 | 0.60% | 256.8 ns τ1 = 2.9 ns, 2% τ2 = 257.9 ns, 98% | -1.38 | 0.95 | 469 | 2.64 | 1.26 | -1.69 |
| CuPBCP' | 89.3 | 591 | 385 | 809 | 0.44% | 63.8 ns τ1 = 3.1 ns, 34% τ2 = 32.2 ns, 44% τ3 = 220.4 ns, 22% | -1.40 | 0.92, 0.99 | 475 | 2.61 | 1.21 | -1.69 |

[a] Potentials are versus Fc+/0.

[b] Excitation wavelength is 450 nm.

Supplementary Table 5. Photocatalytic CO2 reduction to CO by CuBCP/CoTCPc in the absence of certain component.*

| Entry | Conditions | n(CO) (μmol) | n(H2) (μmol) |
| --- | --- | --- | --- |
| 1 | No CoTCPc | N.D. | 1.20±0.40 |
| 2 | No CuBCP | N.D. | N.D. |
| 3 | Under N2 instead of CO2 | N.D. | N.D. |
| 4 | No irradiation | N.D. | N.D. |
| 5 | No BIH | 0.60±0.10 | 1.10±0.20 |

*Standard condition: CuBCP (0.5 mM), xantphos ligand (1.0 mM), CoTCPc (0.05 mM), phenol (5.0 v%), and BIH (20 mM) in 4 mL CH3CN/TEA (v:v = 5:1) within 1 h of 450-nm LED irradiation under 1 atm CO2.

Supplementary Table 6. Bindfit results for CuPBCP/CoTCPc.

| Host:Guest Model | Flavor | Applicable? Y/N | K (M-1) | K error (%) | Total root mean square | Total covariance | Optimal model* |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1:1 | None | N | N.A. |  |  |  |  |
| 1:2 | None | Y | K11 = 7069 K12 = 754 | ±76.8 ±12.4 | 0.00106 | 0.00105 |  |
| 1:2 | Non-cooperative | Y | K11 = 3795 | ±3.1 | 0.00107 | 0.00106 | √ |
| 2:1 | None | N | N.A. |  |  |  |  |
| 2:1 | Non-cooperative | Y | K11 = 911 | ±8.5 | 0.00109 | 0.00111 |  |

*Three models are applicable with the fitted data. Considering the K errors to be within ±10%, the non-cooperative 1:2 and non-cooperative 2:1 models are more reasonable. By comparison, with the smaller total root mean square, total covariance and K error, the non-cooperative 1:2 binding model should be the optimal model to afford the 1:1 binding constant (K11) of 3795±118 M-1.

Supplementary Table 7. Bindfit results for CuPBCP/CoTCPc/TEA.

| Host:Guest Model | Flavor | Applicable? Y/N | K (M-1) | K error (%) | Total root mean square | Total covariance | Optimal model* |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1:1 | None | N | N.A. |  |  |  |  |
| 1:2 | None | Y | K11 = 210638 K12 = 196 | ±1498.3 ±9.6 | 0.00118 | 0.00100 |  |
| 1:2 | Non-cooperative | Y | K11 = 1611 | ±2.8 | 0.00120 | 0.00103 | √ |
| 2:1 | None | N | N.A. |  |  |  |  |
| 2:1 | Non-cooperative | Y | K11 = 530 | ±11.7 | 0.00119 | 0.00102 |  |

*Three models are applicable with the fitted data. Considering the K errors to be within ±10%, the non-cooperative 1:2 model is considered as the optimal model to afford the 1:1 binding constant (K11) of 1611±45 M-1.

Supplementary Table 8. The optimized structures and Gibbs free energies of *COOH and *CO intermediates from the CoPc families. The white, gray, blue, red, yellow and pink colors denote H, C, N, O, S and Co atoms.

| Complexes | *COOH species | ΔG(*COOH) (eV) | *CO species | ΔG(*CO) (eV) |
| --- | --- | --- | --- | --- |
| CoTSPc |  | 1.123817 |  | -0.11355 |
| CoTCPc |  | 1.126483 |  | -0.11021 |
| CoPc |  | 1.129477 |  | -0.11377 |
| CoTAPc |  | 1.111136 |  | -0.13034 |
| CoTDMAPc |  | 1.10349 |  | -0.18819 |

Supplementary Table 9. Overview of the applied EXAFS fit parameters.

| Sample | Fit | Shell, N | R, Å | E0 | ss.2 (10-3) | R-factor | Reduced Chi-square |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CuBCP | 1 | Cu-N/P, 4 | 2.11 | 11.0 | 5.2 | 0.0262 | 711 |
|  | 2 | Cu-N, 2 Cu-P, 2 | 2.08 2.30 | 3.8 | 4.4 8.9 | 0.0026 | 112 |
| CuPBCP | 3 | Cu-N/P, 4 | 2.12 | 11.8 | 4.8 | 0.0325 | 1971 |
|  | 4 | Cu-N, 2 Cu-P, 2 | 2.09 2.30 | 4.2 | 4.5 7.6 | 0.0006 | 48 |
| Reconstructed CuBCP | 5 | Cu-N, 2 Cu-P, 2 | 2.01 2.39 | 5.9 | 9.6 5.7 | 0.0076 | 20 |
| Reconstructed CuPBCP | 6 | Cu-N, 2 Cu-P, 2 | 1.99 2.43 | 5.8 | 1.4 11.1 | 0.0273 | 215 |

*The fit was carried out between 1/1.3 - 3 Å, in apparent distance scale for the ground and reconstructed laser on states. The reconstructed excited states of CuBCP and CuPBCP correspond to the subtraction of the EXAFS data of the “Laser on” states from the ground/ “Laser off” states. CuBCP and CuPBCP show a proportion of excited states of ~35% and 27%, respectively, as described in the main text. 65% and 73% of the ground-state EXAFS spectra were subtracted accordingly from the “Laser on” states of CuBCP and CuPBCP, respectively, to gain their reconstructed excited states.

Supplementary Table 10. Stick figures of XRD and DFT calculated structures calculated in gas phase.

| XRD stick figures | DFT stick figures |
| --- | --- |
| CuBCP | CuBCP |
| CuPBCP | CuPBCP |

Supplementary Table 11. Comparison of the solid-state XRD measurements with DFT optimized coordinates using the BP-86 functional and def2-TZVP triple-zeta basis sets, together with atom-pairwise Grimme dispersion correction with D3BJ in gas phase.

| Heteroleptic [(P^P) Cu(N^N)]PF6 | XRD CuBCP | XRD CuPBCP | DFT ground-state CuBCP | DFT ground-state CuPBCP |
| --- | --- | --- | --- | --- |
| Cu-N1 | 2.06416 | 2.10718 | 2.06540 | 2.06662 |
| Cu-N2 | 2.09832 | 2.08182 | 2.06857 | 2.07029 |
| Cu-P1 | 2.24247 | 2.24416 | 2.22856 | 2.23100 |
| Cu-P2 | 2.30480 | 2.30179 | 2.26153 | 2.26250 |
| Cu-O | 3.20538 | 3.20754 | 3.16865 | 3.16493 |
| Cu-N3 | N.A. | 9.13659 | N.A. | 9.15401 |
| Cu-N4 | N.A. | 9.15058 | N.A. | 9.13441 |
| N1-Cu-N2 | 80.423 | 79.917 | 81.209 | 81.149 |
| P1-Cu-P2 | 119.680 | 119.357 | 119.183 | 119.242 |
| Torsional Angle | 85.0063° | 85.7550° | 86.3227° | 86.2064° |

Supplementary Table 12. Stick figures of CuBCP’s and CuPBCP’s ground- and excited-state structures in solution.

| Ground-state DFT stick figures | Excited-state DFT stick figures |
| --- | --- |
| CuBCP C1-C2-C3: 178.247° C4-C5-C6: 178.066° | CuBCP C1-C2-C3: 178.130° ΔC1-C2-C3: -0.117° C4-C5-C6: 177.906° ΔC4-C5-C6: -0.160° |
| CuPBCP C1-C2-N3: 178.370° C4-C5-N4: 178.109° | CuPBCP C1-C2-N3: 177.641° ΔC1-C2-N3: -0.729° C1-C2-N3: 177.880° ΔC1-C2-N3:-0.229° |

Reference:

1.	DiSalle, B. F. & Bernhard, S. Orchestrated photocatalytic water reduction using surface-adsorbing iridium photosensitizers. J. Am. Chem. Soc. 133, 11819-11821 (2011).

2.	Zhu, X. Q., Zhang, M. T., Yu, A., Wang, C. H. & Cheng, J. P. Hydride, hydrogen atom, proton, and electron transfer driving forces of various five-membered heterocyclic organic hydrides and their reaction intermediates in acetonitrile. J. Am. Chem. Soc. 130, 2501-2516 (2008).

3.	Weber, J. H. & Busch, D. H. Complexes derived from strong field ligands. Xix. Magnetic properties of transition metal derivatives of 4,4',4",4'''-tetrasulfophthalocyanine. Inorg. Chem. 4, 469-471 (1965).

4.	Kobayashi, N. & Nishiyama, Y. Catalytic electroreduction of molecular oxygen using iron or cobalt 4,4',4",4'"-tetracarboxyphthalocyanine. J. Phys. Chem. 89, 1167-1170 (1985).

5.	Kumar, A., Prajapati, P. K., Aathira, M. S., Bansiwal, A., Boukherroub, R. & Jain, S. L. Highly improved photoreduction of carbon dioxide to methanol using cobalt phthalocyanine grafted to graphitic carbon nitride as photocatalyst under visible light irradiation. J. Colloid Interface Sci. 543, 201-213 (2019).

6.	Li, C., et al. A phenanthroline derivative as exciton blocking material for organic solar cells. Dyes Pigm. 97, 258-261 (2013).

7.	Luo, S. P., et al. Photocatalytic water reduction with copper-based photosensitizers: A noble-metal-free system. Angew. Chem. Int. Ed. 52, 419-423 (2013).

8.	Adamo, C. & Barone, V. Toward reliable density functional methods without adjustable parameters: The PBE0 model. J. Chem. Phys. 110, 6158-6170 (1999).

9.	Goerigk, L. & Grimme, S. Efficient and accurate double-hybrid-meta-gga density functionals-evaluation with the extended gmtkn30 database for general main group thermochemistry, kinetics, and noncovalent interactions. J. Chem. Theory Comput. 7, 291-309 (2011).

10.	Frisch, M. J., et al. Gaussian 09, Revision C.01 (Gaussian, Inc., 2009)

11.	Hirshfeld, F. L. Bonded-atom fragments for describing molecular charge densities. Theor. Chim. Acta 44, 129-138 (1977).

12.	Lu, T. & Chen, F. Multiwfn: A multifunctional wavefunction analyzer. J. Comput. Chem. 33, 580-592 (2012).

13.	Sheldrick, G. M. A short history of SHELX. Acta Crystallogr., Sect. A: Found. Crystallogr. 64, 112-122 (2008).

14.	Bindfit.  (ed^(eds). v0.5 edn.

15.	Thordarson, P. Determining association constants from titration experiments in supramolecular chemistry. Chem. Soc. Rev. 40, 1305-1323 (2011).

16.	Wang, J. W., Jiang, L., Huang, H. H., Han, Z. & Ouyang, G. Rapid electron transfer via dynamic coordinative interaction boosts quantum efficiency for photocatalytic CO2 reduction. Nat. Commun. 12, 4276 (2021).

17.	Li, H., Li, F., Zhang, B., Zhou, X., Yu, F. & Sun, L. Visible light-driven water oxidation promoted by host-guest interaction between photosensitizer and catalyst with a high quantum efficiency. J. Am. Chem. Soc. 137, 4332-4335 (2015).

18.	Kuhn, H., Braslavsky, S. & Schmidt, R. Chemical actinometry (IUPAC technical report). Pure Appl. Chem. 76, 2105-2146 (2004).

19.	Thoi, V. S., Kornienko, N., Margarit, C. G., Yang, P. & Chang, C. J. Visible-light photoredox catalysis: Selective reduction of carbon dioxide to carbon monoxide by a nickel N-heterocyclic carbene-isoquinoline complex. J. Am. Chem. Soc. 135, 14413-14424 (2013).

20.	Wang, P., et al. A broadband and strong visible-light-absorbing photosensitizer boosts hydrogen evolution. Nat. Commun. 10, 3155 (2019).

21.	Ravel, B. & Newville, M. Athena, artemis, hephaestus: Data analysis for X-ray absorption spectroscopy using ifeffit. J. Synchrot. Radiat. 12, 537-541 (2005).

22.	Rehr, J. J., Albers, R. C. & Zabinsky, S. I. High-order multiple scattering calculations of X-ray-absorption fine structure. Phys. Rev. Lett. 69, 3397-3400 (1992).

23.	Koningsberger, D. C. & Prins, R. X-ray absorption: Principles, applications, techniques of EXAFS, SEXAFS and XANES. John Wiley & Sons (1988).

24.	Chen, L. X. & Zhang, X. Photochemical processes revealed by X-ray transient absorption spectroscopy. J. Phys. Chem. Lett. 4, 4000-4013 (2013).

25.	Neese, F. The ORCA program system. Wiley Interdisciplinary Reviews: Computational Molecular Science 2, 73-78 (2012).

26.	Perdew, J. P. Density-functional approximation for the correlation energy of the inhomogeneous electron gas. Phys. Rev. B 33, 8822-8824 (1986).

27.	Becke, A. D. Density-functional exchange-energy approximation with correct asymptotic behavior. Phys. Rev. A Gen. Phys. 38, 3098-3100 (1988).

28.	Weigend, F. & Ahlrichs, R. Balanced basis sets of split valence, triple zeta valence and quadruple zeta valence quality for h to rn: Design and assessment of accuracy. Phys. Chem. Chem. Phys. 7, 3297-3305 (2005).

29.	Grimme, S., Ehrlich, S. & Goerigk, L. Effect of the damping function in dispersion corrected density functional theory. J. Comput. Chem. 32, 1456-1465 (2011).

30.	Grimme, S., Antony, J., Ehrlich, S. & Krieg, H. A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements h-pu. J Chem Phys 132, 154104 (2010).

31.	Mennucci, B. & Tomasi, J. Continuum solvation models: A new approach to the problem of solute’s charge distribution and cavity boundaries. J. Chem. Phys. 106, 5151-5158 (1997).

32.	Stephens, P. J., Devlin, F. J., Chabalowski, C. F. & Frisch, M. J. Ab initio calculation of vibrational absorption and circular dichroism spectra using density functional force fields. J. Phys. Chem. 98, 11623-11627 (1994).

33.	Becke, A. D. Density‐functional thermochemistry. iii. The role of exact exchange. J. Chem. Phys. 98, 5648-5652 (1993).

34.	Eichkorn, K., Treutler, O., Öhm, H., Häser, M. & Ahlrichs, R. J. C. P. Auxiliary basis sets to approximate coulomb potentials. Chem. Phys. 242, 652 (1995).

35.	Weigend, F. Accurate coulomb-fitting basis sets for H to Rn. Phys. Chem. Chem. Phys. 8, 1057-1065 (2006).

36.	Kossmann, S. & Neese, F. Efficient structure optimization with second-order many-body perturbation theory: The rijcosx-mp2 method. J. Chem. Theory Comput. 6, 2325-2338 (2010).

Appendix I: DFT calculation data on CoPc and its derivatives

The Hirshfeld atomic charges (e) of studied molecules. The number denotes the atomic labels.

| Molecules | Atoms | Charge | Atoms | Charge |
| --- | --- | --- | --- | --- |
| CoPc | C1 | -0.0282 | C29 | -0.0223 |
|  | C2 | -0.0352 | C30 | -0.0282 |
|  | C3 | -0.0351 | C31 | -0.0352 |
|  | C4 | -0.0282 | C32 | -0.0352 |
|  | C5 | -0.0223 | C33 | -0.0282 |
|  | C6 | 0.1020 | C34 | -0.0223 |
|  | N7 | -0.1533 | C35 | 0.1019 |
|  | C8 | 0.1020 | N36 | -0.1178 |
|  | C9 | -0.0223 | N37 | -0.1532 |
|  | C10 | -0.0282 | C38 | 0.1020 |
|  | C11 | -0.0352 | N39 | -0.1178 |
|  | C12 | -0.0351 | C40 | -0.0223 |
|  | C13 | -0.0282 | H41 | 0.0493 |
|  | C14 | -0.0223 | H42 | 0.0446 |
|  | C15 | 0.1020 | H43 | 0.0446 |
|  | N16 | -0.1179 | H44 | 0.0493 |
|  | N17 | -0.1531 | H45 | 0.0492 |
|  | C18 | 0.1019 | H46 | 0.0446 |
|  | C19 | -0.0223 | H47 | 0.0446 |
|  | C20 | -0.0282 | H48 | 0.0492 |
|  | C21 | -0.0352 | H49 | 0.0492 |
|  | C22 | -0.0352 | H50 | 0.0446 |
|  | C23 | -0.0282 | H51 | 0.0446 |
|  | C24 | -0.0223 | H52 | 0.0492 |
|  | C25 | 0.1019 | H53 | 0.0492 |
|  | N26 | -0.1178 | H54 | 0.0446 |
|  | N27 | -0.1532 | H55 | 0.0446 |
|  | C28 | 0.1019 | H56 | 0.0492 |
|  |  |  | Co57 | 0.2038 |
| CoTAPc | C1 | -0.0294 | C34 | -0.0223 |
|  | C2 | -0.0659 | C35 | 0.0982 |
|  | C3 | 0.0510 | N36 | -0.1220 |
|  | C4 | -0.0634 | N37 | -0.1607 |
|  | C5 | -0.0223 | C38 | 0.0974 |
|  | C6 | 0.0982 | N39 | -0.1220 |
|  | N7 | -0.1607 | C40 | -0.0421 |
|  | C8 | 0.0974 | H41 | 0.0472 |
|  | C9 | -0.0421 | H42 | 0.0358 |
|  | C10 | -0.0294 | H43 | 0.0405 |
|  | C11 | -0.0659 | H44 | 0.0472 |
|  | C12 | 0.0510 | H45 | 0.0358 |
|  | C13 | -0.0634 | H46 | 0.0405 |
|  | C14 | -0.0223 | H47 | 0.0472 |
|  | C15 | 0.0982 | H48 | 0.0358 |
|  | N16 | -0.1220 | H49 | 0.0405 |
|  | N17 | -0.1607 | H50 | 0.0472 |
|  | C18 | 0.0974 | H51 | 0.0358 |
|  | C19 | -0.0421 | H52 | 0.0405 |
|  | C20 | -0.0294 | Co53 | 0.1971 |
|  | C21 | -0.0659 | N54 | -0.1614 |
|  | C22 | 0.0510 | H55 | 0.1232 |
|  | C23 | -0.0634 | H56 | 0.1247 |
|  | C24 | -0.0223 | N57 | -0.1614 |
|  | C25 | 0.0982 | H58 | -0.0294 |
|  | N26 | -0.1220 | H59 | -0.0659 |
|  | N27 | -0.1607 | N60 | 0.0510 |
|  | C28 | 0.0974 | H61 | -0.0634 |
|  | C29 | -0.0421 | H62 | -0.0223 |
|  | C30 | -0.0294 | N63 | 0.0982 |
|  | C31 | -0.0659 | H64 | -0.1607 |
|  | C32 | 0.0510 | H65 | 0.0974 |
|  | C33 | -0.0634 |  |  |
| CoTCPc | C1 | -0.0236 | C35 | 0.1056 |
|  | C2 | -0.0255 | N36 | -0.1151 |
|  | C3 | -0.0168 | N37 | -0.1482 |
|  | C4 | -0.0110 | C38 | 0.1046 |
|  | C5 | -0.0200 | N39 | -0.1151 |
|  | C6 | 0.1056 | C40 | -0.0134 |
|  | N7 | -0.1482 | H41 | 0.0545 |
|  | C8 | 0.1046 | H42 | 0.0478 |
|  | C9 | -0.0134 | H43 | 0.0557 |
|  | C10 | -0.0236 | H44 | 0.0545 |
|  | C11 | -0.0255 | H45 | 0.0478 |
|  | C12 | -0.0168 | H46 | 0.0557 |
|  | C13 | -0.0110 | H47 | 0.0545 |
|  | C14 | -0.0200 | H48 | 0.0478 |
|  | C15 | 0.1056 | H49 | 0.0557 |
|  | N16 | -0.1151 | H50 | 0.0545 |
|  | N17 | -0.1482 | H51 | 0.0478 |
|  | C18 | 0.1046 | H52 | 0.0557 |
|  | C19 | -0.0134 | Co53 | 0.2084 |
|  | C20 | -0.0236 | C54 | 0.2095 |
|  | C21 | -0.0255 | O55 | -0.2781 |
|  | C22 | -0.0168 | O56 | -0.1666 |
|  | C23 | -0.0110 | H57 | 0.1885 |
|  | C24 | -0.0200 | C58 | 0.2095 |
|  | C25 | 0.1056 | O59 | -0.2781 |
|  | N26 | -0.1151 | O60 | -0.1666 |
|  | N27 | -0.1482 | H61 | 0.1885 |
|  | C28 | 0.1046 | C62 | 0.2095 |
|  | C29 | -0.0134 | O63 | -0.2781 |
|  | C30 | -0.0236 | O64 | -0.1666 |
|  | C31 | -0.0255 | H65 | 0.1885 |
|  | C32 | -0.0168 | C66 | 0.2095 |
|  | C33 | -0.0110 | O67 | -0.2781 |
|  | C34 | -0.0200 | O68 | -0.1666 |
|  |  |  | H69 | 0.1885 |
| CoTDMAPc | C1 | -0.0317 | H46 | 0.0373 |
|  | C2 | -0.0683 | H47 | 0.0457 |
|  | C3 | 0.0460 | H48 | 0.0330 |
|  | C4 | -0.0652 | H49 | 0.0373 |
|  | C5 | -0.0241 | H50 | 0.0457 |
|  | C6 | 0.0977 | H51 | 0.0330 |
|  | N7 | -0.1616 | H52 | 0.0373 |
|  | C8 | 0.0966 | Co53 | 0.1959 |
|  | C9 | -0.0436 | N54 | -0.0419 |
|  | C10 | -0.0317 | N55 | -0.0419 |
|  | C11 | -0.0683 | N56 | -0.0419 |
|  | C12 | 0.0460 | N57 | -0.0419 |
|  | C13 | -0.0652 | C58 | -0.0316 |
|  | C14 | -0.0241 | H59 | 0.0420 |
|  | C15 | 0.0977 | H60 | 0.0327 |
|  | N16 | -0.1224 | H61 | 0.0327 |
|  | N17 | -0.1616 | C62 | -0.0315 |
|  | C18 | 0.0966 | H63 | 0.0340 |
|  | C19 | -0.0436 | H64 | 0.0413 |
|  | C20 | -0.0317 | H65 | 0.0340 |
|  | C21 | -0.0683 | C66 | -0.0316 |
|  | C22 | 0.0460 | H67 | 0.0420 |
|  | C23 | -0.0652 | H68 | 0.0327 |
|  | C24 | -0.0241 | H69 | 0.0326 |
|  | C25 | 0.0977 | C70 | -0.0317 |
|  | N26 | -0.1224 | H71 | -0.0683 |
|  | N27 | -0.1616 | H72 | 0.0460 |
|  | C28 | 0.0966 | H73 | -0.0652 |
|  | C29 | -0.0436 | C74 | -0.0241 |
|  | C30 | -0.0317 | H75 | 0.0977 |
|  | C31 | -0.0683 | H76 | -0.1616 |
|  | C32 | 0.0460 | H77 | 0.0966 |
|  | C33 | -0.0652 | C78 | -0.0436 |
|  | C34 | -0.0241 | H79 | -0.0317 |
|  | C35 | 0.0977 | H80 | -0.0683 |
|  | N36 | -0.1224 | H81 | 0.0460 |
|  | N37 | -0.1616 | C82 | -0.0652 |
|  | C38 | 0.0966 | H83 | -0.0241 |
|  | N39 | -0.1224 | H84 | 0.0977 |
|  | C40 | -0.0436 | H85 | -0.1224 |
|  | H41 | 0.0457 | C86 | -0.1616 |
|  | H42 | 0.0330 | H87 | 0.0966 |
|  | H43 | 0.0373 | H88 | -0.0436 |
|  | H44 | 0.0457 | H89 | -0.0317 |
|  | H45 | 0.0330 |  |  |
| CoTSPc | C1 | -0.0146 | N37 | -0.1458 |
|  | C2 | -0.0174 | C38 | 0.1068 |
|  | C3 | -0.0239 | N39 | -0.1137 |
|  | C4 | -0.0172 | C40 | -0.0110 |
|  | C5 | -0.0164 | H41 | 0.0592 |
|  | C6 | 0.1070 | H42 | 0.0596 |
|  | N7 | -0.1458 | H43 | 0.0573 |
|  | C8 | 0.1068 | H44 | 0.0592 |
|  | C9 | -0.0110 | H45 | 0.0596 |
|  | C10 | -0.0146 | H46 | 0.0573 |
|  | C11 | -0.0174 | H47 | 0.0592 |
|  | C12 | -0.0239 | H48 | 0.0596 |
|  | C13 | -0.0172 | H49 | 0.0573 |
|  | C14 | -0.0164 | H50 | 0.0592 |
|  | C15 | 0.1070 | H51 | 0.0596 |
|  | N16 | -0.1137 | H52 | 0.0573 |
|  | N17 | -0.1458 | Co53 | 0.2122 |
|  | C18 | 0.1068 | S54 | 0.5453 |
|  | C19 | -0.0110 | O55 | -0.3119 |
|  | C20 | -0.0146 | O56 | -0.2953 |
|  | C21 | -0.0174 | S57 | 0.5453 |
|  | C22 | -0.0239 | O58 | -0.3119 |
|  | C23 | -0.0172 | O59 | -0.2953 |
|  | C24 | -0.0164 | S60 | 0.5453 |
|  | C25 | 0.1070 | O61 | -0.3119 |
|  | N26 | -0.1137 | O62 | -0.2953 |
|  | N27 | -0.1458 | S63 | 0.5453 |
|  | C28 | 0.1068 | O64 | -0.3119 |
|  | C29 | -0.0110 | O65 | -0.2953 |
|  | C30 | -0.0146 | O66 | -0.2095 |
|  | C31 | -0.0174 | H67 | 0.1886 |
|  | C32 | -0.0239 | O68 | -0.2095 |
|  | C33 | -0.0172 | H69 | 0.1886 |
|  | C34 | -0.0164 | O70 | -0.0146 |
|  | C35 | 0.1070 | H71 | -0.0174 |
|  | N36 | -0.1137 | O72 | -0.0239 |
|  |  |  | H73 | -0.0172 |

Appendix II: DFT optimized coordinates of CuBCP and CuPBCP in the ground state using the BP86 functional and the atom-pairwise Grimme dispersion correction with the Becke-Johnson damping scheme (D3BJ).

CuBCP - ground state:

Cu  6.19407390151465     11.33976968151509      5.49160968333885

P   4.38127148632952     11.75134286268871      4.26245004578418

P   7.71239011254823     12.98664718217361      5.80308266707333

O   6.45783249316850     13.61418261855334      3.30121296717779

N   7.39035701626705      9.71557181898222      5.04800647744349

N   6.27457222199436     10.48324719282593      7.37280220055931

C   4.74341394014226     12.16811623301850      2.51079965427434

C   4.08789120920097     11.56374935226785      1.42770855336803

H   3.26735528454702     10.87163845328859      1.61388249071285

C   4.50610177857821     11.81542623199546      0.12102764259034

H   3.99324183083241     11.33443355671841     -0.71160346267897

C   5.58109091731734     12.67332291325509     -0.12859435837028

H   5.89843688808451     12.84797801135940     -1.15580006520257

C   6.24764176531402     13.31133117281508      0.92259695950475

C   5.80420198075829     13.03862110945507      2.22164419494776

C   8.60711021509081     13.52295609085497      4.30379353399114

C   9.99634100087134     13.67692073623327      4.19097966586548

H   10.62967466086083     13.52099427809139      5.06397437302637

C   10.56710970909626     13.99501962542137      2.95804805595207

H   11.64885179773639     14.10418772826225      2.87541101624456

C   9.76506296996280     14.17207523700969      1.82610629623002

H   10.23445318033534     14.41116150192444      0.87296610400648

C   8.37234315970399     14.06237452169094      1.90754961037509

C   7.83030486020682     13.74836566379800      3.15767363595622

C   7.39756420672884     14.30840444148621      0.75519258109038

C   8.07381562185106     14.18199540959793     -0.61302439535907

H   8.47999946513057     13.17418469983090     -0.77661491935379

H   8.89203794277441     14.90706246344362     -0.70980875296481

H   7.36058539222001     14.40498372448306     -1.41742875806063

C   6.82124319478793     15.74286908456361      0.90729333934463

H   6.07632225870538     15.93405439083741      0.12244885633612

H   7.62848115654972     16.48329746933885      0.81860041612859

H   6.33817590273217     15.87766371432853      1.88395518977019

C   3.24617947018549     10.32889000423899      4.13719448249563

C   3.76883955911912      9.05515079041112      4.40672119565939

H   4.81094282347803      8.96264267503704      4.71964143019207

C   2.95947686013717      7.92376934030055      4.28780400896574

H   3.37107378161456      6.93615916895774      4.49933427633973

C   1.62102778682640      8.05965266278223      3.91094057276085

H   0.98680308527485      7.17672950893653      3.82407558879087

C   1.09068937448522      9.32834298916553      3.65343946735418

H   0.04466974704296      9.43515194513473      3.36408314974124

C   1.89864212057078     10.45999766125024      3.76376784701319

H   1.48327137638350     11.44915222310524      3.56585014217952

C   3.29581171687257     13.12171271428971      4.80150598617170

C   2.45361003937404     12.92503003413840      5.90955366868844

H   2.37305012195615     11.93451912032688      6.36074885111273

C   1.70224576537075     13.98219844421505      6.42199433593558

H   1.04640838505246     13.81471310124127      7.27732674755865

C   1.78410968194583     15.24971113935847      5.83645237273979

H   1.19677092377991     16.07630060767266      6.23736031403486

C   2.60941559350447     15.44839406769302      4.72748841324719

H   2.66967522021301     16.43128400475634      4.25894453604500

C   3.36090215373337     14.39141291878890      4.21028115592953

H   4.00236413347946     14.55831930824490      3.34623277874116

C   7.19636268172033     14.56900367788008      6.54869994988303

C   5.82990924793863     14.85639469038418      6.64364900698119

H   5.10193176699868     14.12733347714659      6.29234093249218

C   5.40319504816940     16.07984937153003      7.16607267879818

H   4.33575990135990     16.29411505919746      7.22689583915165

C   6.34181083085884     17.01805527338259      7.59916337002472

H   6.01032362068240     17.97248868600038      8.00959325724499

C   7.71021679080838     16.73792752917963      7.50122653986376

H   8.44392033988312     17.47339257505804      7.83305639698403

C   8.13815186486453     15.52114110314236      6.97296130999994

H   9.20530449833321     15.30765020013160      6.89063093345134

C   8.97711679440191     12.30849288302650      6.92245594451229

C   9.88720092133140     11.34489837168471      6.45169141146754

H   9.94678618626372     11.12565274416195      5.38434835933014

C   10.70691375233374     10.65309593159390      7.34189489352994

H   11.41215910428771      9.91545310261366      6.95762987377752

C   10.61471162963309     10.89195363232662      8.71534570626575

H   11.25915861208765     10.34930629051596      9.40781332282208

C   9.69903031648506     11.83211312423551      9.19420939953067

H   9.61600696245298     12.01978487484484     10.26549155500176

C   8.88729449209647     12.53806676847465      8.30563165402804

H   8.17614764723012     13.27100743618495      8.68780350070163

C   7.94674098712161      9.37952446873216      3.87212399729946

C   8.92265222340838      8.37175017948002      3.79271738715483

H   9.37732842229956      8.15501611596145      2.82629702926018

C   9.35525737183606      7.68537532271332      4.92254917821263

C   8.75077470123578      8.01756497596332      6.16919242512839

C   7.78056872456250      9.05574203054915      6.17671286200104

C   7.53342043460502     10.14754263088753      2.65792716632519

H   6.44049693588674     10.16487659406541      2.55398079306845

H   7.97138210031224      9.72112059721662      1.74821728444284

H   7.86373947828877     11.19401398576047      2.74086096475982

C   5.75702183593146     10.94677179518655      8.51849403709262

C   6.15529985457698     10.42611015076200      9.76287421834993

H   5.73997447271532     10.86161246042550     10.67239727602157

C   7.09629144129156      9.40982020353794      9.85798926689951

C   7.62590411994870      8.88589813100648      8.64114622219138

C   7.19953911669308      9.48217455347558      7.42549016537547

C   4.78080320928567     12.07586806374316      8.44260692369285

H   4.39086061602853     12.17266778570910      7.42457444636528

H   5.27026185365655     13.02751801089882      8.70180216119595

H   3.94644276522284     11.93373939908006      9.14249400888908

C   9.05641991823819      7.35350516512572      7.39792435528794

H   9.72383395383874      6.49352628606031      7.37343476881169

C   8.52252019290161      7.77365313324945      8.58323452493251

H   8.76190231949232      7.24775422247170      9.50587686238161

C   10.41734496965326      6.66459664643803      4.80006086680839

C   10.30187602828113      5.64493636809568      3.84079620288181

H   9.40279126997671      5.58945378574815      3.22490416617076

C   11.30941072825219      4.69162933580636      3.69436803151607

H   11.19926154098410      3.89667149674930      2.95578071669742

C   12.45420636635556      4.75202173232051      4.49307868198163

H   13.24391569596394      4.00913690273551      4.37473792054559

C   12.58576571463724      5.76971636677390      5.44156668023234

H   13.48383833591579      5.83091643561227      6.05732296868959

C   11.57337272861292      6.71574866088553      5.59867382666267

H   11.69002546724692      7.52023521657227      6.32673324777413

C   7.52834752676180      8.92717656242451     11.18551400040751

C   6.57338608718498      8.59572906456652     12.16175206622313

H   5.51232061143420      8.64732032750736     11.91169367188730

C   6.97237224434580      8.17373169270613     13.42988836218286

H   6.22034353109867      7.90597045418691     14.17274046054826

C   8.33083925282934      8.08955970172486     13.74590463361303

H   8.64289817088620      7.76268345824042     14.73794911952156

C   9.28884847728590      8.42766194924573     12.78618721894103

H   10.35027115937391      8.37589757991175     13.03219864903611

C   8.89248975177824      8.83878866064038     11.51398381457652

H   9.63847603919915      9.12377893419495     10.77228671132004

CuPBCP - ground state:

Cu  6.19319641918515     11.33944461256316      5.48660326851596

P   4.37945684459323     11.75100466239125      4.25440591639471

P   7.70922343520119     12.98808972463782      5.80684232707927

O   6.45855025071019     13.61704230773308      3.30510345096700

N   7.39350105547990      9.71769704419578      5.03927481045234

N   6.27759623675138     10.47732748143003      7.36696120392737

C   4.74536068179106     12.17441360402978      2.50575186644072

C   4.09078985760369     11.57469886407761      1.41942206724909

H   3.26976001689359     10.88212076050098      1.60153553998493

C   4.51042533262360     11.83235464084873      0.11438194092235

H   3.99828228107386     11.35543782634058     -0.72099155466541

C   5.58587895209614     12.69120586410831     -0.13009096886822

H   5.90428286419910     12.87047710523033     -1.15614342148467

C   6.25141234815422     13.32459677148270      0.92457207845950

C   5.80638904991802     13.04627448693814      2.22183212558849

C   8.60655178557337     13.52511084340133      4.31005221372063

C   9.99580428900153     13.68154683794380      4.20041459910794

H   10.62809339067909     13.52542993389237      5.07410521994399

C   10.56797411957664     14.00424642586785      2.96932639042710

H   11.64960032415534     14.11576164288365      2.88882766839816

C   9.76739251160846     14.18376136303473      1.83671605172264

H   10.23804283665866     14.42691480570290      0.88525052943132

C   8.37461544850348     14.07225541585091      1.91538872034061

C   7.83100266851255     13.75304120527285      3.16349311207893

C   7.40148371006768     14.32245418950609      0.76249641683613

C   8.07968108408004     14.20125632998457     -0.60521158867218

H   8.48627700672852     13.19415887774086     -0.77213133232124

H   8.89787005628986     14.92681831812713     -0.69844525616153

H   7.36763104127133     14.42723923567959     -1.40978459601064

C   6.82460636704873     15.75619947617377      0.91941126730575

H   6.08164365488685     15.95046366159416      0.13352847160325

H   7.63181704741861     16.49718076937204      0.83553840204535

H   6.33911087014345     15.88696145715290      1.89540717209790

C   3.24795469104351     10.32665893291108      4.12424849357243

C   3.77201232406854      9.05233832678448      4.38824650521814

H   4.81420242230964      8.95935501627540      4.70062193012536

C   2.96410999377279      7.92047075452533      4.26445034539722

H   3.37664641305475      6.93232368648967      4.47154931715092

C   1.62554278069023      8.05647618387992      3.88804464070406

H   0.99238290763508      7.17323108105828      3.79725677014041

C   1.09377051363139      9.32563017383547      3.63597538448775

H   0.04768788708539      9.43241335192590      3.34699264175251

C   1.90025197663284     10.45780277449826      3.75124901805358

H   1.48358283038455     11.44722895146050      3.55754359177533

C   3.29239191692686     13.11750707755127      4.79869066191779

C   2.45064956168957     12.91523015261496      5.90607681252956

H   2.37206866705641     11.92303853918703      6.35402721460969

C   1.69575529204105     13.96881713125322      6.42072306937052

H   1.03961623270823     13.79733255548831      7.27501362372301

C   1.77374951569670     15.23783432165541      5.83786685694771

H   1.18313430541964     16.06143909205629      6.24006079701309

C   2.59880329046443     15.44189464696787      4.72970129770819

H   2.65559729595185     16.42595691568464      4.26325938422937

C   3.35405626572105     14.38862315335068      4.21034600205011

H   3.99510518625565     14.55932011051886      3.34672083038033

C   7.18469889118642     14.56712481376350      6.55195549622384

C   5.81704849740065     14.84840700809152      6.64788459148236

H   5.09178993818243     14.11696453199595      6.29592279481321

C   5.38557170740220     16.06979219873775      7.17123120836525

H   4.31735250991535     16.27970228860670      7.23284695529012

C   6.32050605753738     17.01193980388079      7.60371066420719

H   5.98523782786763     17.96474186712183      8.01478375986847

C   7.69005718232285     16.73820043454651      7.50392514592407

H   8.42079685458242     17.47697957819558      7.83480391201085

C   8.12293585713170     15.52353679244418      6.97489591990741

H   9.19103079102905     15.31555920698315      6.89070739841020

C   8.97222185540470     12.31328129862645      6.93044029865726

C   9.88647081271213     11.35157489011419      6.46349197496788

H   9.94659510813231     11.12882371027621      5.39689046743685

C   10.71335118093805     10.67105396862206      7.35584914442939

H   11.42496418456928      9.93773891636915      6.97494869168514

C   10.62474635495479     10.91944005132293      8.72795469430960

H   11.27883118718189     10.38959411234767      9.42132882653109

C   9.70419193703874     11.85670221705782      9.20320122439302

H   9.62627400797294     12.05456782969486     10.27304468748068

C   8.88460100655864     12.55092966122754      8.31239335199160

H   8.17224476963827     13.28434546913119      8.69142130122680

C   7.94641146140570      9.38457067768135      3.86090732523055

C   8.91876056671881      8.37257781262759      3.77692936537493

H   9.36577431746185      8.15060534687353      2.80813646694139

C   9.35271612215937      7.68870036725111      4.90637348203437

C   8.76001245844789      8.02195850194513      6.15662260739606

C   7.78667175656637      9.05735297749409      6.16627035118229

C   7.53209073572178     10.15529308855226      2.64955925283420

H   6.43918750870462     10.17247380740883      2.54514514342141

H   7.97108637515029      9.73321617637266      1.73844795181059

H   7.86089864689461     11.20191248124684      2.73729095746739

C   5.75980187174093     10.93906696580511      8.51316845413653

C   6.16111404306956     10.41701698739143      9.75699271846856

H   5.74215570778201     10.84548454059138     10.66814187230730

C   7.10723559880731      9.40638636979318      9.84539493127851

C   7.64150632018188      8.88686781573416      8.63046172726446

C   7.20723501498403      9.48074746554899      7.41643154540103

C   4.77840429799487     12.06300419693428      8.43986612152135

H   4.38268867770300     12.15654358430681      7.42371583194289

H   5.26573107752662     13.01707857369216      8.69429945021745

H   3.94870047665370     11.91931543632080      9.14488564064081

C   9.08160256574569      7.36582533259892      7.38555932143966

H   9.75971295877044      6.51411757392872      7.36235784088334

C   8.55094751167294      7.78503824783525      8.57243796321905

H   8.80493801026948      7.26593904784776      9.49499478896072

C   10.41247606565249      6.66508628008635      4.77908852651831

C   10.29113888377973      5.62255858998026      3.85004625205701

H   9.39295425169622      5.52736266479039      3.23812379495809

C   11.32460816970131      4.69050376297151      3.73858544919661

H   11.24318333401867      3.86209878836145      3.02939337151391

N   12.45060974575499      4.73655216389844      4.46562848308123

C   12.56773684659880      5.74237290526140      5.34502775184911

H   13.49641329744285      5.77251654432280      5.92134214367998

C   11.58849239812129      6.71723302750268      5.54239944000294

H   11.75121374205866      7.52009670766035      6.26294085160961

C   7.54423837267465      8.92530627970436     11.17264730581948

C   6.60799924218985      8.56182725956890     12.15082691064936

H   5.53954080195553      8.58033602319071     11.93060037074779

C   7.06353084672543      8.14720853207474     13.40394461480720

H   6.34993919253551      7.84860647111946     14.17663154398624

N   8.36011372081954      8.08390942096654     13.74150428678389

C   9.25165785550185      8.44195314778575     12.80508775446100

H   10.30382136523001      8.39418336547368     13.09971530033557

C   8.90200025333794      8.86026699065627     11.52058167382087

H   9.66898190369162      9.15742357402025     10.80582025141941

Appendix III: DFT optimized coordinates of CuBCP and CuPBCP in the ground state using the BP86 functional, the PCM method assuming solvent effects of acetonitrile, and the atom-pairwise Grimme dispersion correction with the Becke-Johnson damping scheme (D3BJ).

CuBCP - ground state:

Cu  6.19108689626378     11.34005303322046      5.49473453988362

P   4.37872590643634     11.75217788786902      4.26715438518565

P   7.71149787312079     12.98510521116816      5.80118400434029

O   6.45355631485203     13.60786429088622      3.29768026246737

N   7.38807317548113      9.71847787140871      5.04750135716375

N   6.27173660082518     10.48153288451048      7.37350612112790

C   4.73492256264133     12.16457986738080      2.51345387566862

C   4.07249637577526     11.56267553260923      1.43294123836822

H   3.24810439952433     10.87518153650947      1.61998575208753

C   4.48774977182053     11.81174806203492      0.12383666470774

H   3.97004757886970     11.33206384555581     -0.70694964780649

C   5.56782636052278     12.66352787854720     -0.12998470330094

H   5.88304148775652     12.83644405618481     -1.15829850347594

C   6.24016947415573     13.29882105714395      0.91975937678416

C   5.79812375824398     13.03096344195538      2.22015737701655

C   8.60316706807022     13.52457533423682      4.30060437879577

C   9.99232134513678     13.68233881124481      4.18778560838739

H   10.62739744075537     13.53166996865437      5.06037215430261

C   10.56232671207165     13.99830318006075      2.95295303585298

H   11.64431639935274     14.10787485982233      2.86991422760527

C   9.75985099178097     14.16808620924671      1.81903450932699

H   10.22840393047989     14.40540318960775      0.86489638691201

C   8.36701579607097     14.05328240296002      1.90140813756852

C   7.82579431155395     13.74353350321511      3.15301599319459

C   7.39433705221090     14.28919985994563      0.74525943676527

C   8.07345367831483     14.14477838941876     -0.61993107343923

H   8.47457216834817     13.13244618161513     -0.76849208367116

H   8.89618708445874     14.86447456435383     -0.71829314827062

H   7.36027722544108     14.35990575894101     -1.42656386004612

C   6.82193572253782     15.72697213932588      0.88097171914094

H   6.08203896860793     15.91058737897719      0.08922992995685

H   7.63450849014112     16.46137333226901      0.78710418333013

H   6.33343429407715     15.87266528231014      1.85384918926557

C   3.24412643808209     10.32748166855114      4.14750996444803

C   3.77524011345520      9.05373557578922      4.40292914265004

H   4.82227690274087      8.95973201537562      4.69873191325382

C   2.96811379642328      7.91916903339389      4.29014796395853

H   3.38781541145752      6.93237894445239      4.49024358210263

C   1.62256117078371      8.05279640474547      3.93361753402818

H   0.98995757048083      7.16789190147284      3.85120478150114

C   1.08454275401702      9.32195294778245      3.68932911505898

H   0.03447691474010      9.42749049652504      3.41350004831282

C   1.89127862407312     10.45622561168186      3.79337734681301

H   1.46902805051161     11.44369763295075      3.60204107179275

C   3.29910308317752     13.12783727990954      4.80416610155853

C   2.47577751573150     12.94547491112807      5.92900963023737

H   2.40111657008702     11.96251817779671      6.39703317727413

C   1.74198818413467     14.01307947466764      6.44719144143210

H   1.10743998643787     13.85781877082375      7.32088298285660

C   1.82224930625488     15.27617860940122      5.84993715988234

H   1.25587127984814     16.11273262544985      6.26074314747574

C   2.62679686970027     15.45972656147341      4.72213155996540

H   2.68909539923192     16.43919449397961      4.24617606356418

C   3.36088673305619     14.39218776448214      4.19978857172782

H   3.98758367449485     14.54978888096358      3.32309866512878

C   7.20109035546260     14.57304849088766      6.54421556795445

C   5.83602500329974     14.86757736064067      6.63969534758184

H   5.10417519969610     14.13971047419724      6.29370466576674

C   5.41515035245976     16.09543481367957      7.15871640245069

H   4.34901529518965     16.31627174500287      7.22217054502366

C   6.35923948864285     17.03117400340505      7.58851824956623

H   6.03211856061721     17.98867428947766      7.99599124021264

C   7.72717649346910     16.74273754516068      7.49170302547345

H   8.46562982093420     17.47427440915834      7.82271325959914

C   8.14845624065443     15.52084729373891      6.96706213028025

H   9.21482853732495     15.30127065234343      6.88799952018934

C   8.97261483106685     12.30529968657379      6.92252373428487

C   9.88792859819852     11.34606557745286      6.45245543913140

H   9.96384261261131     11.13733840869055      5.38402704368368

C   10.69140748940504     10.63898204729609      7.34665612798975

H   11.39597471710690      9.89924424209173      6.96492840498103

C   10.57780996829210     10.85957049836620      8.72238689334693

H   11.20143489763056     10.29641652092561      9.41775902495809

C   9.65860794658717     11.79868572396849      9.19920368061256

H   9.55429045565728     11.96951891802163     10.27168306988838

C   8.86242069610165     12.51902712752480      8.30727621227097

H   8.14247674904464     13.24244519795548      8.69141304447323

C   7.94492988196772      9.38619309850229      3.87106268761083

C   8.92485176342341      8.38220965780143      3.78840442893500

H   9.37646455693438      8.17019700309748      2.81981972911458

C   9.35932943361044      7.69835372641117      4.91812167860963

C   8.75154668592095      8.02181613007919      6.16522784129690

C   7.77763164629496      9.05633526834814      6.17472014503839

C   7.53002229297487     10.15234538534501      2.65705162464772

H   6.43699247856793     10.16349176594633      2.55260842910625

H   7.97465358663449      9.72889140689090      1.74955171549295

H   7.85413097897570     11.20031168470564      2.74442490245929

C   5.75323121899699     10.94386671402650      8.51926450839456

C   6.14441335349240     10.41564351206948      9.76341285176230

H   5.72337756587181     10.84915587858486     10.67083482777212

C   7.08295328526671      9.39760133139441      9.85482142786005

C   7.61748810432152      8.87710758705097      8.63849915605699

C   7.19425358487338      9.47793611678311      7.42394070979756

C   4.78648688000801     12.07974249436677      8.44846661629742

H   4.40950176165664     12.19334301722412      7.42754190136227

H   5.28362717463408     13.02054811375311      8.73165054132429

H   3.94463248969931     11.93245719529798      9.13770072088533

C   9.05859991384819      7.35604504769429      7.39262201494615

H   9.73549529428192      6.50344797245610      7.37238656674428

C   8.51894810687454      7.76883327092560      8.57835327219551

H   8.76565926794538      7.24076532255586      9.49766652035802

C   10.43267823964364      6.68824536062793      4.79468504878984

C   10.33188456464165      5.67380481156862      3.82735198899483

H   9.43855371274763      5.61585468402545      3.20333102621733

C   11.35208471386754      4.73259686248440      3.67825217642356

H   11.25420292473705      3.94278949684036      2.93176255659679

C   12.49398716995595      4.80037443643601      4.48308360970521

H   13.29345022613799      4.06754984726054      4.36281416168120

C   12.60948233648794      5.81420658707639      5.43962549476188

H   13.50345457804087      5.88261276785013      6.06116246119250

C   11.58497865946159      6.74857857551557      5.59866786064332

H   11.69187001688959      7.54854347157143      6.33303678931440

C   7.51059997181483      8.91201972031411     11.18397589915149

C   6.55014470127252      8.59161440262063     12.15967162399262

H   5.48991047821125      8.65878350645039     11.90971447220028

C   6.94337918581323      8.16898004105615     13.43075095735211

H   6.18663943784119      7.91197589476021     14.17325320494888

C   8.30182547233811      8.07261466916461     13.74991530453551

H   8.60967335615406      7.74509220372439     14.74360124489967

C   9.26480220113863      8.40085190222024     12.79001437310627

H   10.32618149235375      8.34051036844932     13.03556058696034

C   8.87358960497596      8.81344974759174     11.51547488701139

H   9.62644877432584      9.08778832853375     10.77709403351333

CuPBCP - ground state:

Cu  6.19056921475358     11.33880022716705      5.48972065370891

P   4.37695077823355     11.75114448420441      4.26047450207833

P   7.70795647518649     12.98579938335849      5.80544976066144

O   6.45304134110340     13.61023483267049      3.30165994246042

N   7.39173823888119      9.72050331529960      5.03771317788942

N   6.27401997166165     10.47444858936701      7.36651814297669

C   4.73587985773007     12.16985577181235      2.50934019044722

C   4.07423434367018     11.57237776278816      1.42595525283994

H   3.24955164171792     10.88432277243076      1.60948987994149

C   4.49064755549354     11.82704860196674      0.11834425205375

H   3.97363678152497     11.35096852912024     -0.71491126811146

C   5.57099050790080     12.67984009317249     -0.13085036012430

H   5.88710981239609     12.85696151451305     -1.15814661583130

C   6.24255360451133     13.31079145845823      0.92203799411506

C   5.79916947817872     13.03766255004756      2.22080968114126

C   8.60132859346505     13.52710904411677      4.30710952664466

C   9.99041762639945     13.68732450663695      4.19733756170507

H   10.62442948950198     13.53570081199359      5.07049825888714

C   10.56175821271919     14.00782700457554      2.96430781237330

H   11.64366151247907     14.11940229893455      2.88332404132743

C   9.76074442240237     14.17980129693800      1.82970447356150

H   10.23051497650914     14.42083619417936      0.87711751135872

C   8.36790463670259     14.06273144934363      1.90934709168718

C   7.82520516024073     13.74817205360424      3.15906344124950

C   7.39691267416224     14.30178938089646      0.75243756397552

C   8.07822239141369     14.16139364409799     -0.61208843659543

H   8.47989039575081     13.14959782920798     -0.76276683963210

H   8.90086211188429     14.88162092741841     -0.70731295317116

H   7.36617829419023     14.37847166415846     -1.41917348703732

C   6.82399917084046     15.73902461479991      0.89167810306853

H   6.08603305600380     15.92512736168216      0.09874063871225

H   7.63665162752506     16.47388843690216      0.80227031863162

H   6.33302241784157     15.88128487553440      1.86381731514278

C   3.24598526893853     10.32450119547118      4.13593642389328

C   3.77859359075374      9.05076304479353      4.38806649354103

H   4.82531427296247      8.95665865858045      4.68471650377754

C   2.97332301377472      7.91539638885345      4.27070309353635

H   3.39424108319014      6.92865156917485      4.46833164349576

C   1.62811286239926      8.04826440129195      3.91268553088792

H   0.99692047100971      7.16272336536748      3.82661966484845

C   1.08863463347690      9.31736798106308      3.67145342336641

H   0.03886389377524      9.42225859964096      3.39433283549307

C   1.89348095904224     10.45252220492784      3.78013866371002

H   1.47022395992699     11.43993439589153      3.59089056565191

C   3.29579596118996     13.12336263552236      4.80198061064398

C   2.47284858106525     12.93632238501506      5.92628062815986

H   2.40010976711565     11.95207899751856      6.39187591636836

C   1.73646264084951     14.00108448077320      6.44661879837269

H   1.10213162001712     13.84248878056536      7.31984459770716

C   1.81366193044376     15.26551902534314      5.85181804006214

H   1.24508706232437     16.09978185053554      6.26421967350619

C   2.61777645176860     15.45349079617133      4.72443505163289

H   2.67747578757422     16.43402956560516      4.25040029789297

C   3.35470469799450     14.38894664931073      4.20001779704414

H   3.98081157946829     14.54968784121010      3.32347229842945

C   7.19063546150478     14.57062800082936      6.54904467510440

C   5.82467998516892     14.86073534086875      6.64472025116688

H   5.09483892404223     14.13152639400875      6.29744195084672

C   5.40015202789465     16.08665324369555      7.16530824337725

H   4.33341195658866     16.30424761450669      7.22912101255892

C   6.34144621611921     17.02476770558605      7.59598661239801

H   6.01139916822981     17.98077381481028      8.00456850155076

C   7.71024943379818     16.74082535774966      7.49849775802420

H   8.44650430774950     17.47429161418020      7.83005037108423

C   8.13531316650021     15.52087368535674      6.97255001785865

H   9.20238352802527     15.30500100141578      6.89295513483656

C   8.96716414008860     12.30762557338225      6.92990797030531

C   9.88716824509461     11.35161876709604      6.46202350829121

H   9.96661783727721     11.14330968254884      5.39376714497721

C   10.69350572525959     10.65000945928818      7.35804485689164

H   11.40355668125031      9.91439098851913      6.97849498550659

C   10.57809160648086     10.87275592858504      8.73338008433463

H   11.20582472162662     10.31549754450284      9.42981368084729

C   9.65390581776277     11.80814861837437      9.20789751721923

H   9.54922788226130     11.98222163343218     10.27982757297190

C   8.85460037227032     12.52297699934256      8.31418004581898

H   8.13208715971446     13.24467782206912      8.69667259856138

C   7.94682560241293      9.39314372751785      3.85922996826404

C   8.92580259281558      8.38755988356890      3.77213911509187

H   9.37277935649207      8.17293453707977      2.80214450878132

C   9.36066237392819      7.70677592758784      4.90188542495840

C   8.76255322808050      8.02778176125642      6.15234978892545

C   7.78416663477312      9.05801471176278      6.16339436371273

C   7.52962321328995     10.16103168045941      2.64792971722695

H   6.43642142048444     10.17165756864908      2.54563630493700

H   7.97315726862909      9.73999590769876      1.73892083680251

H   7.85354026456378     11.20885643488181      2.73774243580420

C   5.75522950983265     10.93522380731456      8.51252492613398

C   6.14939776607891     10.40597555195864      9.75626238315850

H   5.72582110547119     10.83307042956530     10.66535337887744

C   7.09311048678283      9.39381918799582      9.83994964655384

C   7.63267673729891      8.87682975885780      8.62629791197621

C   7.20149042427142      9.47555467347508      7.41363111944081

C   4.78302184260035     12.06559615247572      8.44468311050448

H   4.40475572729780     12.17945823189830      7.42434125451132

H   5.27613876550583     13.00780713046256      8.73022861211379

H   3.94283734176470     11.91239793609633      9.13456018943588

C   9.08406929969849      7.36826116214629      7.37916836392329

H   9.77050450133684      6.52327381630300      7.36034295814681

C   8.54640189901326      7.77891450038593      8.56633423559409

H   8.80583173015944      7.25564360552545      9.48480923046994

C   10.43436558396212      6.69800838928150      4.77328365016595

C   10.33627633301676      5.66820629738696      3.82690400414679

H   9.44936590080659      5.57261872597571      3.19967288189832

C   11.38089051195605      4.75136007039375      3.71132447003433

H   11.31365543880853      3.93605251577968      2.98600904973454

N   12.50169310316122      4.79903286742337      4.45408049797504

C   12.59476474268061      5.79658427953465      5.35195179423282

H   13.51341544213651      5.83454949779096      5.94291386754839

C   11.60104480307033      6.75481256025291      5.55023425234861

H   11.75007722525276      7.54688559154862      6.28466982019197

C   7.52596886374371      8.91287617238574     11.16891292884035

C   6.58351173127873      8.57305476594932     12.15041953277107

H   5.51546792197994      8.61399342339044     11.93394586201849

C   7.02947560352112      8.16060115111603     13.40598443655084

H   6.30663380213615      7.88341491262072     14.17771960411258

N   8.32857949287668      8.07545422128849     13.74626064361305

C   9.22741715555720      8.41273422500583     12.80325428291301

H   10.28018851976725      8.35059781860974     13.09116660339557

C   8.88225650530944      8.82801493289686     11.51778884718181

H   9.65895039965030      9.10372061227086     10.80600201029096

Appendix IV: DFT optimized coordinates of CuBCP and CuOBCO in the excited state using the B3LYP functional, the PCM method assuming solvent effects of acetonitrile, and the atom-pairwise Grimme dispersion correction with the Becke-Johnson damping scheme (D3BJ).

CuBCP - excited state:

Cu  6.14987715104097     11.26723483029526      5.55807803955590

P   4.38882091370741     11.73806062466126      4.14374129013960

P   7.62857806595300     13.07079287758812      5.87734768899177

O   6.42288618169321     13.61990846735489      3.28092827219976

N   7.29389893447026      9.62124383942365      5.05101313679094

N   6.32973419911234     10.50576725418553      7.41161605827988

C   4.75608742091429     12.17593919110142      2.40442151624437

C   4.11704394250264     11.59214371843415      1.29867618383123

H   3.29873694934746     10.89364620766352      1.44870283791062

C   4.55805150190387     11.88687162158838      0.00512407653468

H   4.06338385469546     11.42963790648548     -0.84874071335836

C   5.63991338625999     12.75354341506944     -0.20214852273671

H   5.97150029757954     12.95336826007823     -1.21692089577124

C   6.28997503162479     13.36655496295654      0.87886977977858

C   5.81285230354804     13.06266825958611      2.15827823228604

C   8.53720218621700     13.57371764201406      4.36555613857098

C   9.92940556011090     13.76897868066279      4.31300733100856

H   10.53278921568539     13.62789862543736      5.20438923455672

C   10.53766885655852     14.12598071380667      3.10739334419151

H   11.61526819435417     14.27192083818054      3.07177798632703

C   9.77543415196798     14.29186543934626      1.94243834262829

H   10.27686554806575     14.55948002941450      1.01723375608460

C   8.38265645277500     14.13282958151973      1.96268021367294

C   7.80178722474771     13.78591454381618      3.18922243194358

C   7.45167489782622     14.36716135779665      0.76117724285143

C   8.19457278540304     14.22962893827358     -0.58062182786577

H   8.61859955249538     13.22582029494667     -0.70375087935262

H   9.00604434345854     14.96179267419776     -0.64940287519905

H   7.51326882916692     14.42594425957059     -1.41554607937397

C   6.86354587514114     15.80908841094511      0.87690757697718

H   6.16737406361225     15.99389253463461      0.04964120259365

H   7.67517998562746     16.54577460010847      0.83211539737546

H   6.32305573289939     15.94299750767274      1.82108904351382

C   3.30763897303906     10.26582883080865      4.04246512950282

C   3.87216449729144      8.99421515393201      4.25017931097941

H   4.92504448778390      8.90215159852859      4.50775508437292

C   3.07916790938190      7.84735161055351      4.13706880263922

H   3.52290480937890      6.86708079727015      4.30057126940175

C   1.71945704236778      7.96278863957971      3.82379703209752

H   1.10268597627508      7.07006902398617      3.73910189637634

C   1.15081052291247      9.22858172350878      3.62405813925746

H   0.09426392634985      9.32136151600093      3.37995151749641

C   1.93875565998323     10.37728958388551      3.73385502082295

H   1.49190513657701     11.35630084566370      3.57809479494533

C   3.30109214135243     13.07833937623088      4.74501985397518

C   2.55864928151253     12.86526440043343      5.92370847779338

H   2.56012701004406     11.88783192456888      6.40147149828339

C   1.80405960331224     13.90196214377157      6.47722212095670

H   1.23637089881733     13.72739407923235      7.38898806845219

C   1.78235746401463     15.16135206104789      5.86254157038295

H   1.20165402635988     15.97127004470716      6.29939276939372

C   2.50698017620672     15.37381157458129      4.68358480569529

H   2.48713816078746     16.34692777457361      4.19687194318472

C   3.26446231272078     14.33917078139556      4.12536726546202

H   3.82180665754047     14.51873964404729      3.21120276750102

C   7.10344373919241     14.66258071061440      6.60659378522528

C   5.74123123868358     14.99513416400727      6.63456068975864

H   5.00354778313058     14.28915171115047      6.27139987001943

C   5.33199349076973     16.24005721398557      7.12527619121140

H   4.27344808714092     16.49010601273261      7.13918762999784

C   6.28191185194288     17.15478973694615      7.59292091593960

H   5.96318046943559     18.12196551427743      7.97667458322287

C   7.64570382190985     16.82737146444392      7.56401407216744

H   8.38711255314817     17.53845786386505      7.92331164088772

C   8.05871788471791     15.58845320337042      7.06841455282473

H   9.11833495909868     15.34321558945451      7.04202223857030

C   8.88567997335509     12.34434908363550      6.97890838906619

C   9.76336260482234     11.36502085618084      6.47077022119436

H   9.77403104394393     11.13763467666986      5.40795368417542

C   10.60946566545685     10.66228045189961      7.33016520363331

H   11.27598551609328      9.90506877106318      6.92328287087383

C   10.57566163518323     10.90866983820615      8.70744405956471

H   11.22506843671706     10.34866268705511      9.37702176782270

C   9.69296211621359     11.86703006559265      9.22171993106400

H   9.65051810421031     12.05152226071258     10.29332531075205

C   8.85091264733539     12.58113482952730      8.36625192103912

H   8.16302400455275     13.31261207705063      8.78107433140244

C   7.82098445856857      9.23605327349572      3.85621488678001

C   8.78828253158516      8.23900909255379      3.76546308746713

H   9.20633579774336      8.00619168709625      2.79045295509323

C   9.26965051399785      7.56370157096275      4.91512510957385

C   8.69562865849075      7.91679021233582      6.16702458358914

C   7.72384498917954      8.96958007497358      6.20509557640970

C   7.34932072758712      9.95394619325681      2.62342321062670

H   6.26605946662467      9.84365489542080      2.49097177256592

H   7.84770624199178      9.56642036288256      1.73016304466751

H   7.55895402460962     11.02768842619692      2.69971597381424

C   5.83404282525657     10.98791211136479      8.58287233251930

C   6.16890999576571     10.41742337246836      9.80537035439018

H   5.75925664900688     10.85808005358376     10.71037629505733

C   7.12544495071914      9.37267360970527      9.89838356692301

C   7.63056116986941      8.84106120386106      8.67900127494863

C   7.21532905389697      9.43191436799881      7.44392504586775

C   4.97080082978373     12.21627700953286      8.53024191430259

H   4.45142809392737     12.29523776783057      7.57254166090171

H   5.58471018087813     13.11849927829902      8.64997568668392

H   4.23007123274473     12.21127341633469      9.33762913785377

C   9.00453542651010      7.26479920142704      7.40267105171295

H   9.65276432402901      6.39404306690688      7.39122993877970

C   8.48580625450353      7.69701333453717      8.59845961179547

H   8.71222457234361      7.14409438360082      9.50503428725643

C   10.34034709356029      6.55701220597937      4.76910396361724

C   10.27775523413677      5.59849107271270      3.73304411497244

H   9.40989332279213      5.58030178519268      3.07620749807884

C   11.29740257146249      4.65937643718095      3.55992227604361

H   11.21971307614210      3.92048663312884      2.76347380011006

C   12.41475643752673      4.66387675040470      4.40725098246768

H   13.21237383191396      3.93587659285396      4.26817397467177

C   12.50092159460920      5.62016565399595      5.42810643342370

H   13.37354592108756      5.64667900240271      6.07923671711174

C   11.47775694704769      6.55468048247507      5.60809821040214

H   11.57467937419469      7.31042996881047      6.38453225370115

C   7.58643265862244      8.93653706226682     11.22679752881924

C   6.66596208505422      8.79462166437340     12.29241643156937

H   5.60594787552948      8.95704393615075     12.10646491344740

C   7.09409397346527      8.41972195002134     13.56725199370442

H   6.36481564479375      8.30010745346094     14.36704121914588

C   8.45520611057203      8.19267427935131     13.81892920514128

H   8.78900455215713      7.90369230949017     14.81370706655808

C   9.38325437654321      8.34939425815186     12.77992867257593

H   10.44475982893358      8.19573951804888     12.96886333123541

C   8.95690475790994      8.71672467434618     11.50197107509266

H   9.68986087080203      8.87148432300845     10.71558441796166

CuPBCP – excited state:

Cu  6.18194638184136     11.27749887716117      5.54125347892553

P   4.40910762677141     11.73389396363141      4.13730393574406

P   7.64396407785601     13.10577674978655      5.85172336649645

O   6.41460079386598     13.63214742486159      3.25917807277440

N   7.28661303084316      9.61564806698816      5.05628507782167

N   6.35722663945390     10.53072029300657      7.41376168914739

C   4.75841319805347     12.16933974386182      2.39678020898690

C   4.11687701833576     11.57504913069678      1.29799935731935

H   3.30593879070675     10.86985504532704      1.45636408186958

C   4.54677302151814     11.87044950271691      0.00095559645491

H   4.05084090508990     11.40630286452234     -0.84834443425830

C   5.61968712153295     12.74603145706310     -0.21598440593026

H   5.94255056086807     12.94528377836371     -1.23373815082897

C   6.27187852402489     13.36871654159119      0.85845015720287

C   5.80483866918106     13.06552871902472      2.14134515991508

C   8.53479707713051     13.61096529141094      4.33266407709659

C   9.92448660430099     13.82370460152310      4.27523160879070

H   10.53259919258932     13.69395812944107      5.16514178849048

C   10.52283482183663     14.18358607458527      3.06585954963249

H   11.59822825021785     14.34314175481733      3.02507571148774

C   9.75360027568497     14.33444369751220      1.90331924541902

H   10.24818493693598     14.60403847344546      0.97505701308531

C   8.36290042854918     14.15887722091793      1.92927056030689

C   7.79123655675362     13.81090905267900      3.15962545733780

C   7.42490539810660     14.37820617194023      0.73027876260556

C   8.16345118993080     14.23841413555773     -0.61366875435354

H   8.59542343725263     13.23748380328266     -0.73235997415027

H   8.96823758517836     14.97710212385056     -0.69048903093818

H   7.47704473447471     14.42413449475380     -1.44675883474773

C   6.82569536038613     15.81603358008584      0.84020582956205

H   6.12494181263952     15.99069699685025      0.01465190195205

H   7.63169565361676     16.55834780620110      0.78789366621447

H   6.28826884985422     15.95131697447298      1.78589874586130

C   3.33504062764912     10.25631503298097      4.06148903015728

C   3.90167488832718      8.98510193161228      4.26557263646385

H   4.95753735901910      8.89189560357232      4.50856509460015

C   3.10517912568309      7.83923394753558      4.17016173026631

H   3.55011653529683      6.85918626007978      4.33131825846223

C   1.74095431834772      7.95525607220989      3.87776009748732

H   1.12182526306111      7.06304069993472      3.80654115016214

C   1.17057855489780      9.22094384100630      3.68204517876879

H   0.11047625100513      9.31420616798838      3.45408186346883

C   1.96091384830898     10.36914491208950      3.77570518927039

H   1.51286273399219     11.34806062495045      3.62333173552113

C   3.32915419104654     13.06586873717647      4.76347486925782

C   2.64341224387570     12.85387018096662      5.97658042324688

H   2.69597932444328     11.88721833483079      6.47210071592512

C   1.88855950634189     13.88139116857753      6.54544137276542

H   1.36743746673997     13.71003482116710      7.48498386602627

C   1.80940189405240     15.12892479617835      5.91110635477194

H   1.22836790759992     15.93226442354111      6.35951924940920

C   2.47666918967397     15.33888341763699      4.69820394813216

H   2.41037385202528     16.30239039979584      4.19683330846231

C   3.23564641160828     14.31384875973632      4.12418282542032

H   3.74692100952266     14.49026982068390      3.18276826854272

C   7.13179825065500     14.68778279118658      6.60776548132979

C   5.78077144166963     15.06355975199291      6.57500378674041

H   5.04164533437953     14.39803461469353      6.14382355392600

C   5.38439180324655     16.30459197125978      7.08476040123531

H   4.33502690424592     16.58897009805655      7.05101039488722

C   6.33591634054742     17.17294160973486      7.63129469294060

H   6.02716057010913     18.13716743335647      8.03003416883807

C   7.68871931735232     16.80316418616802      7.66086445587961

H   8.43187663975110     17.47873475222238      8.07993097855366

C   8.08993152531723     15.56774917112760      7.14711949018409

H   9.14149636334288     15.29035069509977      7.16627957264182

C   8.90148908796119     12.35252061427545      6.93205173632442

C   9.78311213591208     11.38974968256495      6.39894246326658

H   9.79853286799552     11.19207767111560      5.33019384076003

C   10.62725031432300     10.66403354949766      7.24096663594731

H   11.29787756243136      9.92122150715076      6.81491854895943

C   10.58836258992599     10.87128037826352      8.62461789139538

H   11.23735069010547     10.29373357034242      9.27961424871116

C   9.70190550807449     11.81339668589530      9.16325200935841

H   9.65696976952714     11.96946968962024     10.23928137171806

C   8.86077971634647     12.54894984608374      8.32613418934355

H   8.16743428405797     13.26403932590381      8.76020803805566

C   7.80593185597127      9.21727672146800      3.85583841106819

C   8.76466988298737      8.21798105638536      3.77151491190576

H   9.17563445287157      7.97760665994278      2.79550066203347

C   9.26001373995922      7.55218239014174      4.92596449735521

C   8.69024924616984      7.92040969193873      6.18235756987054

C   7.72421319494217      8.97195458343813      6.20995703250100

C   7.33123026418346      9.93057566551503      2.62210603245662

H   6.24864998564536      9.81502012118294      2.48723593345469

H   7.83198752455130      9.54264329216580      1.73041109244311

H   7.53631493992361     11.00584833602844      2.69480846436589

C   5.85694381566805     11.02297918905143      8.56534187168965

C   6.19425283773558     10.46267073421278      9.80287827686389

H   5.79163577238783     10.91633070730690     10.70436932563996

C   7.12014742596781      9.40688938502656      9.89758370404272

C   7.63157005773125      8.85826615221252      8.68843452319311

C   7.22289987553630      9.44533903772877      7.45132945285185

C   4.95445093438672     12.22284512375436      8.50076997495692

H   4.86372292305048     12.58662269286354      7.47705565089170

H   5.33926108344838     13.03582423701740      9.12772028983100

H   3.95114595178465     11.96884401237337      8.86709037631792

C   8.99500511788670      7.27398517636380      7.42437823939995

H   9.63264334477139      6.39608461334615      7.41903708724785

C   8.48457024844090      7.71372119381249      8.62019858290665

H   8.71485670844939      7.16676631689317      9.52904343967383

C   10.33021554029566      6.55952407254246      4.77485862656700

C   10.34731944286645      5.67174885564208      3.67285072051357

H   9.53410410685807      5.67438582486124      2.95020765660107

C   11.39402688478634      4.76514874787526      3.52564804163838

H   11.39585346891664      4.07110444115913      2.68334180032382

N   12.44211566857039      4.67445702179237      4.37685279905257

C   12.43802598571210      5.53561813565559      5.42016974509762

H   13.29273465388254      5.47807053320976      6.09616115524933

C   11.43287708982998      6.47115770168371      5.65701786469306

H   11.52951164840185      7.14952247247442      6.50037597502228

C   7.54988305908245      8.94758274245275     11.23209101204163

C   6.61451070920108      8.76963721946262     12.27194977084926

H   5.55201863288942      8.91860377239045     12.09204095291116

C   7.05530263937388      8.37397189879809     13.53442519662016

H   6.33477377227559      8.22138257835770     14.33914927083728

N   8.35268898692741      8.15654110467577     13.84357854648599

C   9.24887034409132      8.34344805448668     12.85101667808153

H   10.29657256998234      8.18097945223592     13.10814507023424

C   8.90485366803280      8.73095773118525     11.55565199561572

H   9.68518889839532      8.89192745709383     10.81815508572377