Supplementary Information

In situ observation of cracking and self-healing of solid electrolyte interphases during lithium deposition

Tingting Yang,1,6 Hui Li,1,6 Yongfu Tang,1,3,6* Jingzhao Chen,1 Hongjun Ye,1 Baolin Wang,5 Yin Zhang,5 Congcong Du,1 Jingming Yao,1 Baiyu Guo,1 Tongde Shen,1 Liqiang Zhang,1,4* Ting Zhu,5* Jianyu Huang1,2*

1Clean Nano Energy Center, State Key Laboratory of Metastable Materials Science and Technology, Yanshan University, Qinhuangdao 066004, P. R. China

2Key Laboratory of Low Dimensional Materials and Application Technology of Ministry of Education, School of Materials Science and Engineering, Xiangtan University, Xiangtan, Hunan 411105, P. R. China.

3Hebei Key Laboratory of Applied Chemistry, School of Environmental and Chemical Engineering, Yanshan University, Qinhuangdao, 066004, P. R. China.

4State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an 710049, China.

5Woodruff School of Mechanical Engineering, Georgia Institute of Technology, Atlanta, GA, 30332, USA

6These authors contributed equally

*Correspondence to: jyhuang8@hotmail.com; tangyongfu@ysu.edu.cn; lqzhang@ysu.edu.cn;

ting.zhu@me.gatech.edu

1. Description of the Supplementary Videos

Supplementary Video 1 An in-situ TEM movie showing the growth of a Li whisker under a CO2 atmosphere (corresponding to Fig. 1). Upon applying a negative potential at the CNT cathode, a Li sphere emerged at the MWCNT, Li2CO3 and CO2 three-phase point. With the enlarging of the Li spheres, a crack appeared on the rigid SEI film. When two symmetric cracks near the bottom of the lithium sphere were present, a straight Li whisker started to grow with cyclic crack formation/repairing near the root of the lithium whisker. The movie was recorded at 30 frames per second and played at 31× speed.

Supplementary Video 2 An in-situ TEM movie showing the growth of a Li whisker with kinks under a CO2 atmosphere (corresponding to Supplementary Fig. 3). The movie was recorded at 30 frames per second and played at 369× speed.

Supplementary Video 3 An in-situ TEM movie showing the growth of a Li sphere, which evolved into a whisker with kinks under a CO2 atmosphere (corresponding to Supplementary Fig. 5). The movie was recorded at 30 frames per second and played at 129× speed.

Supplementary Video 4 An in-situ TEM movie showing the growth of a Li whisker with kinks under a CO2 atmosphere (corresponding to Supplementary Fig. 6). The movie was recorded at 30 frames per second and played at 164× speed.

Supplementary Video 5 An in-situ TEM movie showing the growth of a Li sphere, which evolved into a whisker under a CO2 atmosphere (corresponding to Supplementary Fig. 7). The movie was recorded at 30 frames per second and played at 50× speed.

Supplementary Video 6 An in-situ TEM movie showing the growth of a Li sphere accompanying with the cracking and self-healing of the Li2CO3 SEI shell at low voltage (corresponding to Fig. 2). When the MWCNT contacted with the Li2CO3 coated bulk metallic Li, sphere-like Li was formed at low voltage. Then four cycles of the cracking and self-healing of Li2CO3 SEI film were clearly observed in the movie. The arrowheads with different colors (red, green, blue and yellow for the first to the fourth cycles, respectively) point out the cracks formed by the diffusion induced stress during the electroplating, while the arrows with different colors mark the growth directions of metallic Li driven by the electroplating when the SEI crack was present. The movie was recorded at 30 frames per second and played at 165× speed.

Supplementary Video 7 An in-situ TEM movie showing the growth of a metallic Li sphere accompanying with the cracking and self-healing of the Li2CO3 SEI shell at low voltage (corresponding to Supplementary Fig. 8). Two SEI cracks formation and self-healing cycles were observed in the movie. The red and blue arrowheads represent the cracks formed at the first and second cycles, respectively. The movie was recorded at 30 frames per second and played at 119× speed.

Supplementary Video 8 An in-situ TEM movie showing the growth of a metallic Li sphere under the confinement of Li2CO3 SEI shell at low voltage (corresponding to Supplementary Fig. 9). Three cycles of the SEI crack formation/self-healing were observed during the growth of the Li sphere. The movie was recorded at 30 frames per second and played at 38× speed.

Supplementary Video 9 An in-situ TEM movie showing the growth of a metallic Li sphere accompanying cracking and self-healing of Li2CO3 SEI shell at low voltage (corresponding to Supplementary Fig. 10). Before the presence of the crack, a lithium sphere grew with well-defined morphology. The video was recorded at 30 frames per second and played at 120× speed.

Supplementary Video 10 An in-situ movie showing the growth of a well-defined Li sphere in a CO2 atmosphere under ultralow voltage (corresponding to Fig. 3). No cracks were observed most of the time, and even if a crack emerged (red arrowheads), it was efficiently self-healed. The movie was recorded at 30 frames per second and played at 81× speed.

Supplementary Video 11 An in-situ movie showing the growth of two well-defined Li spheres in a CO2 atmosphere under ultralow voltage (corresponding to Supplementary Fig. 11). No cracks were observed most of the time, and even if crack emerged, it was efficiently self-healed. The video was recorded at 30 frames per second and played at 74× speed.

Supplementary Video 12 An in-situ movie showing the transformation of a lithium whisker into a Li sphere in a CO2 atmosphere when the voltage was reduced (corresponding to Fig. 4). The movie was recorded at 30 frames per second and played at 8× speed.

Supplementary Video 13 An in-situ movie showing the growth of the Li spheres in an O2 atmosphere under high voltage (corresponding to Fig. 5). Lithium whisker was not present even under high voltage due to the formation of Li2O as the surface SEI layer and the absence of crack during the growth process. The movie was recorded at 30 frames per second and played at 170× speed.

Supplementary Video 14 An in-situ movie showing the growth of the Li spheres in an O2 atmosphere under high voltage (corresponding to Supplementary Fig. 12). Lithium whisker was not present even under high voltage due to the formation of Li2O as the surface SEI layer and the absence of crack during the growth process. The movie was recorded at 30 frames per second and played at 269× speed.

## 2. Supplementary Figures

Supplementary Fig. 1 Schematic of the experimental set up. The experiment was carried out in an aberration corrected environmental transmission electron microscopy under a CO2 atmosphere.

Supplementary Fig. 2 Morphology and crystalline structure of a Li whisker. (a-c) TEM bright field, electron diffraction pattern (EDP), and dark field images of a Li whisker. The dark-field image in (c) was obtained by choosing the sharp diffraction spot marked by a red circle in (b), demonstrating that the straight Li whisker is a single crystal. The EDP indicates the newly formed Li with a [011] zone axis growing along the <111> direction (b).

Supplementary Fig. 3 In situ growth of a Li whisker with kinks in a CO2 atmosphere (-0.3 V from a-e, -1.0 V from f-j, and -1.5 V from k-u). (a-u) Time lapse TEM images showing the formation of a Li whisker with kinks covered with a SEI shell of Li2CO3. Before the formation of kinks, the newly formed SEI film on one side is thinner than on the other side (blue arrowheads in h-k, and yellow arrowheads in n-t).

Supplementary Fig. 4 Morphology and crystalline structure of a Li whisker with kinks. (a-c) Bright field, the corresponding EDP, and dark field TEM images of a Li whisker. The dark field image (c) was obtained by choosing the diffraction spot marked by a red circle in (b), indicating the same growth direction of the different segments of the kinks. The Li whisker growth direction is <111>.

Supplementary Fig.5 In situ growth of the formation of a Li sphere, which evolved into whisker with kinks in a CO2 atmosphere (-0.3 V from a-i, -1.5 V from j-y). (a-y) Time lapse TEM images showing the formation of a Li whisker with kinks covered with a SEI shell of Li2CO3. Before the formation of kinks, the newly formed SEI film on one side is thinner than on the other side (blue arrowheads in t-w).

Supplementary Fig. 6 In situ growth of the formation of a Li whisker with kinks in a CO2 atmosphere (-0.3 V from a-d, -0.5 V from e-g, and -1.0 V from h-t). (a-t) Time lapse TEM images showing the formation of a Li whisker with kinks covered with a SEI shell of Li2CO3. Before the formation of kinks, the newly formed SEI film was thicker on one side than on the other side.

Supplementary Fig. 7 The growth process of a Li whisker with a Li2CO3 SEI layer (-0.8 V from a-j, -4.0 V from k-l). (a-l) Time lapse TEM images of the growth of a Li sphere, which evolved into a whisker in a CO2 atmosphere.

Supplementary Fig. 8 In situ growth of the formation of an irregular Li sphere in a CO2 environment under low voltage (-0.5 V (a-d), -0.8 V (e-f), and -0.5 V (g-h)). (a-h) Time lapse TEM images showing the formation of an irregular Li sphere covered with a SEI shell of Li2CO3. Both one crack (red arrowheads, b-c) and two cracks (blue arrowheads, f) can be quickly self-healed if the Li deposition is slow under low voltage. The arrows point out Li growth direction.

Supplementary Fig. 9 In situ growth of an elongated Li sphere in a CO2 environment under low voltage (-0.3 V from a-e, -0.6 V from f-o). (a-o) Time lapse TEM images showing the formation of an electroplated Li sphere covered with a SEI shell of Li2CO3. Both one crack (red arrowheads in d-e, yellow arrowheads in k-l) and two cracks (blue arrowhead in j) can be quickly self-healed if the Li deposition is slow under low voltage. The arrowheads denote the cracks formed during the Li growth. The arrows point out the growth direction of the deposited Li.

Supplementary Fig. 10 Time lapse TEM images of the growth of an elongated Li sphere in a CO2 environment under low voltage (-0.2 V from a-h, -0.5 V from i-l). (a-h) A well-defined Li sphere gradually grew with the absence of cracks at first. (i-l) After the formation and self-healing of a crack (point out by red arrowheads), an elongated sphere was formed.

Supplementary Fig. 11 The growth process of Li spheres with Li2CO3 shell (-0.2 V). (a-f) Time lapse TEM images of the morphology evolution of two Li spheres without cracking and self-healing of the Li2CO3 SEI during their growth under ultra-low voltage.

Supplementary Fig. 12 The growth process of a Li sphere with Li2O shell (-0.4 V from a-e, -1.2 V from f-h). (a-h) Time lapse TEM images of the morphology evolution of a Li sphere grown in an O2 atmosphere under high voltage. The Li2O shell layer is more loose and thicker than the Li2CO3 shell layer formed in the CO2 gas. The sphere surface is relatively smooth and no cracks are present during the growth process.

Supplementary Fig. 13 Characterization of the Li/Li2O core-shell sphere. (a-d) A TEM bright-field image, a corresponding EDP, and dark field images obtained by choosing a sharp diffraction spot corresponding to metallic Li (c, obtained from a yellow circle in b) and the diffraction ring corresponding to Li2O (d, obtained from a red ring in b), respectively. (e-f) Low-loss and core-loss electron energy loss spectroscopies of the Li2O shell (blue) and Li core (red).

Supplementary Fig. 14 A comparison of Li2O SEI layer and Li2CO3 SEI layer formed on the surface of the Li spheres. (a) The Li sphere with a Li2O layer. (b) Local magnification of the Li2O layer in (a) with a thickness of the layer of about 24 nm. (c) The Li sphere with a Li2CO3 layer. (d) Local magnification of the Li2CO3 layer in (c) with a thickness of about 7 nm.