Supplementary section

Figure S1. FTIR spectra of (1) and its ligand

Figure S2. FTIR spectra of (2) and its ligand

Figure S3.  Simulated and experimental PXRD patterns of (1)

Figure S4.  Simulated and experimental PXRD patterns of (2)

Table S1: Experimental bond lengths (Å) and angles (ο) in (1) and (2)

| Bond lengths of (1) |  | Bond lengths of (2) |  |
| --- | --- | --- | --- |
| Experimental | Theoretical | Experimental | Theoretical |
| Ca1–N 2.561(2) | 2.74766 | Ca1–O1 2.5049(15) | - |
| Ca1–N11 2.561(2) | 2.74806 | Ca1–O2 2.3753(15) | 2.36775 |
| Ca1–O8 2.4446(15) | 2.41309 | Ca1–O3 2.3706(15) | 2.36421 |
| Ca1–O81 2.4445(15) | 2.30391 | Ca1– O1011 2.3725(16) | 2.35928 |
| Ca1–O11 2.6891(17) | 3.10462 | Ca1– N1072 2.6142(18) | 2.60094 |
| Ca1–O111 2.6890(17) | 3.1052 | Ca1– O1092 2.4140(15) | 2.4068 |
| Ca1–O13 2.3177(16) | 2.2874 | Ca1– O110 2.4044(16) | 2.40939 |
| Ca1–O131 2.3177(16) | 2.2873 | Ca2– O1 2.5411(16) | 2.54318 |
|  |  | Ca2– O4 2.4784(16) | 2.48034 |
|  |  | Ca2– O5 2.3750(17) | 2.38055 |
|  |  | Ca2–O6 2.3396(17) | 2.3472 |
|  |  | Ca2– O201 2.2724(17) | 2.28263 |
|  |  | Ca2– N2073 2.5694(18) | 2.55898 |
|  |  | Ca2–O2103 2.3658(15) | 2.35651 |
| Bond angles of (1) |  | Bond angles of (2) |  |
| N11–Ca1–N1 173.79(8) | 165.37 | O1–Ca1–O2 72.07(6) | - |
| N11–Ca1–O111 58.40(5) | 53.3585 | O1–Ca1–O3 149.00(5) | 148.6150 |
| N1–Ca1–O111 115.51(5) | 112.0141 | O1–Ca1–O110 88.40(5) | 88.5039 |
| O81–Ca1–O8 68.95(7) | 63.3202 | O1–Ca1–O101 100.50(5) | 100.6616 |
| N1–Ca1–O11 58.40(5) | 53.3585 | O1–Ca1–NIO7 130.26(6) | 129.8239 |
| O81–Ca1–N1 122.58(5) | 129.8532 | O1–Ca1–O109 68.99(5) | 70.2349 |
| O81–Ca1–N11 63.30(5) | 63.3202 | O2–Ca1–O3 77.75(6) | 77.8153 |
| O8–Ca1–O11 115.35(5) | 113.2579 | O2–Ca1–O110 91.45(6) | 91.2683 |
| O8–Ca1–O111 173.40(5) | 163.5680 | O2–Ca1–O101 93.56(6) | 93.5176 |
| O111–Ca1–O11 60.87(7) | 58.8311 | O1–Ca2–O4 70.34(5) | 70.3902 |
| O13–Ca1–N11 81.47(6) | 82.2498 | O1–Ca2–O5 92.98(5) | 93.1078 |
| O131–Ca1–N11 97.19(6) | 96.5513 | O1–Ca2–O6 146.70(6) | 146.6870 |
| O131–Ca1–N1 81.48(6) | 81.0888 | O1–Ca2–O201 79.22(5) | 79.2661 |
| O13–Ca1–N1 97.19(6) | 96.0505 | O1–Ca2–N207 130.25(6) | 129.9013 |
| O131–Ca1–O8 111.94(6) | 112.3713 | O1–Ca2–O210 71.74(5) | 72.3944 |
| O13–Ca1–O8 88.66(5) | 885.3018 | O4–Ca2–O5 76.04(5) | 76.2092 |
| O13–Ca1–O11 73.74(5) | 79.6905 | O4–Ca2–O6 77.50(6) | 77.4116 |
| O131–Ca1–O11 85.05(5) | 85.3018 | O4–Ca2–O201 97.47(5) | 97.0565 |
| O131–Ca1–O111 73.74(5) | 74.2219 |  |  |
| O13–Ca1–O131 155.47(8) | 158.7818 |  |  |

# Symmetry codes: (1): 13/2-x,3/2-y,+z (2): +x,1-y,-1/2+z; 2 +x,1-y,1/2+z;  +x,+y,1+z; +x,2-y,1/2+z; +x,2-y,-1/2+z

Table S2: Selected hydrogen bonding parameters of (1)

| #### Compound | #### D-H∙∙∙∙A | D-H (Å) | D∙∙∙∙A (Å) | H∙∙∙∙A (Å) | D-H∙∙∙∙A (ο) |
| --- | --- | --- | --- | --- | --- |
| (1) | O11–H11···O81 | 0.846(18) | 2.573(2) | 1.728(19) | 176(3) |
|  | O13–H13A···O92 | 0.845(17) | 2.834(2) | 1.989(2) | 160(3) |
|  | O13–H13B···O91 | 0.838(17) | 2.724(2) | 1.886(17) | 176(3) |

Table S3: Showing the π···π interactions distances in (1)

| #### Compound |  | π···π (Å) |
| --- | --- | --- |
| (1) | i1···i2 | 4.082(8) |

Table S4: Selected hydrogen bonding parameters of (2)

| #### Compound | #### D-H∙∙∙∙A | D-H (Å) | D∙∙∙∙A (Å) | H∙∙∙∙A (Å) | D-H∙∙∙∙A (ο) |
| --- | --- | --- | --- | --- | --- |
| (2) | C105‒H105···O202 | 0.950(3) | 3.458(4) | 2.508(5) | 133.7 |
|  | O1–H1B···O209 | 0.881(6) | 2.652(2) | 1.787(9) | 167(3) |
|  | O1–H1A···O109 | 0.880(6) | 2.787(2) | 2.33(3) | 113(2) |
|  | O1–H1A···O4 | 0.880(6) | 3.081(2) | 2.232(11) | 162(3) |
|  | O2–H2A···O101 | 0.85 | 2.969(2) | 2.13 | 168.1 |
|  | O2–H2B···O210 | 0.84 | 2.764(2) | 1.95 | 164.9 |
|  | O3–H3A···O102 | 0.89 | 2.771(2) | 1.88 | 178.1 |
|  | O3–H3B···O102 | 0.89 | 2.690(2) | 1.81 | 172.9 |
|  | O4–H4A···O109 | 0.88 | 2.778(2) | 1.93 | 164.4 |
|  | O4–H4B···O5 | 0.88 | 2.911(2) | 2.14 | 145.8 |
|  | O5–H5A···O209 | 0.85 | 2.605(2) | 1.83 | 149.9 |
|  | O5–H5B···O110 | 0.87 | 2.769(2) | 2.00 | 145.9 |
|  | O6–H6B···O202 | 0.87 | 2.685(2) | 1.84 | 160.4 |
|  | O6–H6A···O201 | 0.89 | 2.827(2) | 1.95 | 168.2 |

Table S5: Showing the π···π interactions distances in (2)

| #### Compound |  | π···π (Å) |
| --- | --- | --- |
| (2) | i1···i2 | 3.647(8) |
|  | i9···i10 | 3.711(7) |

(a)

(b)

(a)

(b)

Figure S5. Optimised structure of (a) Ca(H(2,6-pyr))2(H2O)2 (1) and (b) [Ca2(2,3-pyr)2(H2O)6]n (2)