# Supporting Information

#### Table S.1. Life cycle inventory for the LCA of the studied beams. Note that the inventory is documented for a reference flow of 1 for simplicity. In the comparison of product systems, a reference flow of 0.87 is applied for the grid 3DCP beams

|  | Solid 3DCP on-site | Solid 3DCP prefab | Grid 3DCP on-site | Grid 3DCP prefab | Cast beam on-site | Cast beam prefab |
| --- | --- | --- | --- | --- | --- | --- |
| Reference flow | 1 | 1 | 1 | 1 | 1 | 1 |
| Transportation All scenarios: Transport, freight, lorry >32 metric ton, euro6 {RER}¦ market for transport, freight, lorry >32 metric ton, EURO6 ¦ Cut-off, U | Scenario 1 | Scenario 2 | Scenario 1 | Scenario 2 | Scenario 3 | Scenario 2 |
|  | 250km, supply of raw materials from import center | 250 km, prefab beam to construction site |  |  | 250km, supply of raw materials from import center |  |
|  | 50 km, materials to construction site |  |  |  | 50 km, materials to construction site |  |
|  | 100 km, robot and pump to construction site and back (5 beams printed per construction site). |  |  |  | 50km, formwork to construction site (5 beams casted per construction site). |  |
| Values entered | 52996 kg*km | 10900 kg*km | 75590kg*km | 15100 kg*km | 45110 kg*km | 8080 kg*km |
|  | Import transport of raw materials automatically included by database processes |  |  |  |  |  |
| Raw materials | 5.65 kg Reinforcing steel {GLO}¦ market for ¦ Cut-off, U 302 kg 3DCP concrete mix 45 Mpa (see the modeled 3DCP mixture unit process below) |  | 5.65 kg Reinforcing steel {GLO}¦ market for ¦ Cut-off, U 231 kg 3DCP concrete mix 45 Mpa (see the modeled 3DCP mixture unit process below) |  | 5.65kg Reinforcing steel {GLO}¦ market for ¦ Cut-off, U 217 kg Concrete, 40MPa {RoW}¦ concrete production 40MPa ¦ Cut-off, U |  |
| 3DCP mixture | Material Content; Amount; Unit. Acetic acid, without water, in 98% solution state {GLO}¦ market for ¦ Cut-off, U; 0,000881; kg. Portland Cement 95% (modified process); 0,275238; Kg. Concrete mixing factory {GLO}¦ market for ¦ Cut-off, U; 2,18E-10; Units. Ethylene oxide {RER}¦ market for ethylene oxide ¦ Cut-off, U; 0,003519; Kg. Gravel, round {CH}¦ market for gravel, round ¦ Cut-off, U; 0,298095; Kg. Sand {BR}¦ market for sand ¦ Cut-off, U; 0,211905; Kg. Tap water {Europe without Switzerland}¦ market for ¦ Cut-off, U; 0,019524; Kg. Tap water {Europe without Switzerland}¦ market for ¦ Cut-off, U; 0,165238; Kg. Silica fume, densified {GLO}¦ market for ¦ Cut-off, U; 0,045; Kg. Fibre, polyester {GLO}¦ market for fibre, polyester ¦ Cut-off, U; 0,0001; kg. Material per kg of 3DCP concrete mix 45MPA |  |  |

| Manufacturing equipment | Pump: PFT ZP3XXL (240 kg). Material content; Amount; Unit. Electric motor, vehicle {RER}¦ production ¦ Cut-off, U; 55; kg. Inverter, 2.5kW {GLO}¦ market for ¦ Cut-off, U; 3; Units. Steel, low-alloyed {GLO}¦ market for ¦ Cut-off, U; 114; kg. Acrylonitrile-butadiene-styrene copolymer {RER}¦ production ¦ Cut-off, U; 20; kg. Metal working, average for steel product manufacturing {RoW}¦ processing ¦ Cut-off, U; 114; kg. Injection moulding {RoW}¦ processing ¦ Cut-off, S; 20; kg. Robot: ABB IRB6650S (2250 kg). Material content; Amount; Unit. Steel, low-alloyed {GLO}¦ market for ¦ Cut-off, U; 2100; kg. Cable, unspecified {GLO}¦ market for ¦ Cut-off, U; 30; kg. Powertrain, for electric scooter {GLO}¦ market for electric ¦ Cut-off, U; 50; kg. Electronics, for control units {GLO}¦ market for ¦ Cut-off, U; 20; kg. Casting, steel, lost-wax {GLO}¦ market for ¦ Cut-off, U; 1600; kg. Steel removed by milling, large parts {RER}¦ steel milling, large parts ¦ Cut-off, U; 10; kg. Deep drawing, steel, 38000 kN press, single stroke {GLO}¦ market for ¦ Cut-off, U; 500; kg. Welding, arc, steel {GLO}¦ market for ¦ Cut-off, U; 20; kg. | Wooden formwork: 0.0016m3 Plywood, for outdoor use {RER}¦ market for ¦ Cut-off, U 0.01hr Power sawing, with catalytic converter {RER}¦ processing ¦ Cut-off, U | Steel formwork: 200kg Steel, chromium steel 18/8, hot rolled {GLO}¦ market for ¦ Cut-off, U 200kg Metal working, average for chromium steel product manufacturing {GLO}¦ market for ¦ Cut-off, U |
| --- | --- | --- | --- |
| Manufacturing equipment lifetime and use | Lifetime: 35 000 hours Print time: 0.43 hours (26 minutes) 81 395 “reuses” | Lifetime: 35 000 hours Print time: 0.23 hours (14 minutes) 156 174 “reuses” | 5 reuses | 5000 reuses |
| Manufacturing energy | Robot: 0.768 kW Electricity, medium voltage {DK}¦ market for ¦ Cut-off, U Pump: 2.4 kW Electricity, medium voltage {DK}¦ market for ¦ Cut-off, U |  |  |  |
| Use stage | Carbon sequestration from the atmosphere for 50 years in indoor exposure conditions. Calculation method based on literature review and parameters for carbon sequestration listed below. No maintenance assumed (i.e., 50 year lifetime) |  |  |  |
| Parameters for carbon sequestration | Surface area: 2.86 m2 Clinker content: 549 kg/m3 Silica fume content 4.5% 13.1 kg CO2 sequestration from air (negative emission) | Surface area: 7.15 m2 Clinker content: 549 kg/m3 Silica fume content 4.5% 21.8 kg CO2 sequestration from air (negative emission) | Surface area: 2.07 m2 Clinker content: 227 kg/m3 Silica fume content 0% 4.90 kg CO2 sequestration from air (negative emission) |  |

| Disposal of concrete | Year of disposal: 2071 (50 year lifetime of beam). Calculations are relative to weight of cement, rebar or beam Inputs: 100% Rock crushing {RER}¦ processing ¦ Cut-off, U 100% Sorting facility, for construction waste {GLO}¦ market for ¦ Cut-off, U 100% Sorting facility, for construction waste {GLO}¦ market for ¦ Cut-off, U 50kg*km Transport, freight, lorry 16-32 metric ton, euro6 {RoW}¦ market for transport, freight, lorry 16-32 metric ton, EURO6 ¦ Cut-off, U Output 50% weigh -Gravel, crushed {RoW}¦ market for gravel, crushed ¦ Cut-off, U 27% Gravel, round {CH}¦ market for gravel, round ¦ Cut-off, U 19% Sand {BR}¦ market for sand ¦ Cut-off, U 100% Pig iron {RoW}¦ pig iron production ¦ Cut-off, U |  |  |
| --- | --- | --- | --- |
| Disposal of manufacturing equipment | Year of disposal: 2033 (35 000 hours lifetime = 12 years based on 8 production hours per day on average). Robot and pump refurbished with 75% efficiency. Avoided production of 0.75 new robots and pumps. 100% weigh Manual treatment facility, waste electric and electronic equipment {GLO}¦ construction ¦ Cut-off, U 250km Transport, freight, lorry 16-32 metric ton, euro6 {RoW}¦ market for transport, freight, lorry 16-32 metric ton, EURO6 ¦ Cut-off, U | Year of disposal: 2021 Formwork incinerated after 5 uses. Avoided heat and power production. 332MJ Heat, district or industrial, other than natural gas {DK}¦ heat and power co-generation, wood chips, 6667 kW, state-of-the-art 2014 ¦ Cut-off, U 50 km Transport, freight, lorry 16-32 metric ton, euro6 {RoW}¦ market for transport, freight, lorry 16-32 metric ton, EURO6 ¦ Cut-off, U | Year of disposal: 2046 Formwork recycled after 5 000 uses. Avoided production of pig iron. 50 km Transport, freight, lorry 16-32 metric ton, euro6 {RoW}¦ market for transport, freight, lorry 16-32 metric ton, EURO6 ¦ Cut-off, U |

##### Table S.2: Compared beam systems in the LCA

|  |  | B1 3DCP | B2 Grid | B3 Cast |
| --- | --- | --- | --- | --- |
| Metrics | Volume (m3) | 0.144 | 0.11 | 0.096 |
|  | Concrete (Kg) | 302 | 231 | 217 |
|  | Surface area (m2) | 2.86 | 7.15 | 2.46 |
|  | Exposed surface area (m2)* | 2.28 | 6.57 | 2.07 |
| Concrete mix | Aggregates size | 0-2 mm | 0-2 mm | 8 mm |
|  | Strength (MPa) | 45 | 45 | 40 |
|  | Density (Kg/m3) | 2100 | 2100 | 2270 |
| Failure Load | kN | 43.7** | 50.1** | 43.7*** |
| Lifetime (assumption) | Years | 50 | 50 | 50 |
| Reference Flow LCA | n | 1 | 0.87 | 1 |
| *Assume only two sides and underside of the beam will be exposed to air after construction, i.e. not covered by other construction materials such as slabs and pillars. ** Experimental test data. *** Calculated value due to cast beam being theoretical. |  |  |  |  |

##### Table S.3: Impact categories reported in the LCA

| Impact category | Unit |
| --- | --- |
| Climate change | Kg CO2 eq |
| Ozone depletion | Kg CFC-11 eq |
| Ionizing radiation | kBq U-235 eq |
| Photochemical ozone formation | Kg NMVOC eq |
| Particulate matter | Disease inc. |
| Human toxicity, non-cancer | CTUh |
| Human toxicity, cancer | CTUh |
| Acidification | Mol H+ eq |
| Eutrophication, freshwater | Kg P eq |
| Eutrophication, marine | Kg N eq |
| Eutrophication, terrestrial | Mol N eq |
| Land use | Pt |
| Resource use, fossils | MJ |
| Resource use, minerals, and metals | Kg Sb eq |

##### Table S.4. Assumed 3DCP mix for the case study, based on literature review and experimental data

| Type of material | Quantity (%) |
| --- | --- |
| Cement | 27.5 |
| Fly Ash | 5 |
| Silica fume | 4.5 |
| Aggregates | 51 |
| Water | 16.5 |
| Admixtures | 0.44 |
| PE microfibers | 0.01 |
| Density | 2100 Kg/m3 |
| Compressive strength | 45 MPa |

Supporting Content S.5

Carbonation sensitivity (1) was performed by selecting lower and higher constant values (k) during the calculation, resulting in lower or higher carbonation depth as a result. Differing situations were selected where  Clinker Content (1) in the cement was changed based on commonly observed clinker values in concrete (62-95%) while still containing the same cement amount. Transportation distance (3) scenarios were modified based on the maximum transportation distance (500km) in the assumed scenario. Reuse of manufacturing equipment (4) scenarios were made for the manufacturing equipment. The plywood formwork ranged from 1-100 uses, the reusable steel formwork from 1000-10000 uses, and the 3DCP cell (robot and pump) ranged from 10.000-100.000 hours. End-of-Life (5) scenarios were modeled based on the findings on disposal of concrete in Section 3.2.5, and by modifying the recovery potential of the equipment. Energy use (6) was based on the assumption of 20% and 100% maximum power rating of equipment from the manufacturers' technical documentation  for the robot and pump.

##### Table S.6: LCIA results for impact categories of all beams at midpoint

| Impact category | Unit | B1 on-site | B1 prefab | B2 on-site | B2 prefab | B3 on-site | B3 prefab |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Climate change | kg CO2eq | 97.96 | 95.73 | 54.54 | 56.91 | 31.13 | 38.81 |
| Ozone depletion | kg CFC11 eq | 9.5E-06 | 8.6E-06 | 5.92E-06 | 6.74E-06 | 6.1E-06 | 5.2E-06 |
| Ionizing radiation | kBq U-235 eq | 4.339 | 4.20 | 2.98 | 3.14 | 3.23 | 2.38 |
| Photoche. ozone formation | kg NMVOC eq | 0.30 | 0.30 | 0.20 | 0.21 | 0.17 | 0.13 |
| Particulate matter | disease inc. | 4.1E-06 | 4.1E-06 | 2.83E-06 | 2.94E-06 | 4.2E-06 | 2.3E-06 |
| Human toxicity, non-cancer | CTUh | 1.3E-06 | 1.5E-06 | 1.17E-06 | 1.07E-06 | 9.2E-07 | 9.0E-07 |
| Human toxicity, cancer | CTUh | 4.5E-08 | 5.7E-08 | 4.72E-08 | 3.93E-08 | 6.1E-08 | 3.8E-08 |
| Acidification | mol H+ eq | 0.35 | 0.36 | 0.24 | 0.24 | 0.19 | 0.16 |
| Eutrophication, freshwater | kg P eq | 0.015 | 0.017 | 0.017 | 0.012 | 0.009 | 0.008 |
| Eutrophication, marine | kg N eq | 0.098 | 0.098 | 0.07 | 0.07 | 0.051 | 0.043 |
| Eutrophication, terrestrial | mol N eq | 1.09 | 1.10 | 0.75 | 0.752589 | 0.59 | 0.48 |
| Ecotoxicity, freshwater | CTUe | 1480.29 | 1571.03 | 1080.85 | 1032.069 | 753.80 | 694.85 |
| Land use | Pt | 645.07 | 674.68 | 457.30 | 454.18 | 1605.57 | 461.96 |
| Water use | m3 depriv. | 10.88 | 11.57 | 9.68 | 9.27 | 11.99 | 6.33 |
| Resource use, fossils | MJ | 903.94 | 866.89 | 592.74 | 631.83 | 537.68 | 449.63 |
| Resource use, minerals and metals | kg Sb eq | 0.006 | 0.006 | 0.004 | 0.004 | 0.002 | 0.002 |