Visualization of the Process of a Nanocarrier-Mediated Gene Delivery: Stabilization, Endocytosis, Endosomal Escape and Exocytosis of Genes for Intercellular Spreading

Zhongzheng Ma1,2, Yang Zheng3, Zijian Chao1, Hongtao Chen4, Yunhui Zhang1, Meizhen Yin4, Jie Shen1, Shuo Yan1*

Corresponding authors: Shuo Yan, yanshuo2011@foxmail.com

Zhongzheng Ma and Yang Zheng have contributed equally to this work.

1 Department of Plant Biosecurity and MOA Key Laboratory of Pest Monitoring and Green Management, College of Plant Protection, China Agricultural University, Beijing 100193, People’s Republic of China

2 Institute of Plant and Environmental Protection, Beijing Academy of Agricultural and Forestry Sciences, Beijing 100097, People’s Republic of China

3 College of Horticulture and Plant Protection, Yangzhou University, Yangzhou 225002, Jiangsu, People’s Republic of China

4 State Key Laboratory of Chemical Resource Engineering, Beijing Lab of Biomedical Materials, Beijing University of Chemical Technology, Beijing 100029, People’s Republic of China

Figure S1. Enhanced stability of SPc-complexed dsRNA treated with insect hemolymph. (A) The dseGFP degradation by the hemolymph of S. frugiperda. One μg dseGFP was incubated with various dilutions of hemolymph for 1.5 h at room temperature. M: DNA Marker. (B-B’) Gel electrophoresis assay (B) and relative band density (B’) of SPc-complexed dseGFP treated with the hemolymph of S. frugiperda. Different amounts of dseGFP/SPc complex were incubated with 12.5% of hemolymph for 1.5 h at room temperature. The dseGFP/SPc complex was decomplexed in 0.3% SDS solution and analyzed using agarose gel electrophoresis. The relative band density was determined using ImageJ. (C) Relative dsRNA amount of SPc-complexed dseGFP treated with the hemolymph of S. frugiperda. Statistical analysis was conducted using independent t-test at the P=0.05 level of significance.

Figure S2. Enhanced stability of G2-complexed dsRNA treated with RNase A. (A) Gel electrophoresis assay of dseGFP retardation by G2 at various mass ratios. M: DNA marker. (B) Absorption changes of dseGFP at 260 nm after the treatment of 100 ng RNase A. Asterisk indicates significant difference according to independent t-test (*P<0.05 and **P<0.01). (C) Changes in fluorescence intensity of G2 with the addition of dseGFP (Ex=590 nm). (D) Absorption changes of dseGFP/G2 complex at 590 nm after the treatment of 100 ng RNase A.

Figure S3. Enhanced stability of G2-complexed dsRNA treated with insect hemolymph. (A-A’) Gel electrophoresis assay (A) and relative band density (A’) of G2-complexed dseGFP treated with the hemolymph of S. frugiperda. Different amounts of dseGFP/G2 complex were incubated with 12.5% of hemolymph for 1.5 h at room temperature. The dseGFP/G2 complex was decomplexed in 0.3% SDS solution and analyzed using agarose gel electrophoresis. The relative band density was determined using ImageJ. M: DNA Marker. (B) Relative dsRNA amount of G2-complexed dseGFP treated with the hemolymph of S. frugiperda. Statistical analysis was conducted using independent t-test at the P=0.05 level of significance.

Figure S4. Changes in fluorescence intensity of dsRNA complexed by SPc and G2. (A) The spectral analysis of SPc, fluorescent dseGFP, dseGFP/SPc complex, G2 and dseGFP/G2 complex was conducted using NanoDrop 2000 spectrophotometer. The dseGFP was mixed with SPc and G2 at the mass ratio of 1:1 and 1:1.5, respectively (final concentration for dseGFP: 100 ng/μL). (B) The absorbance comparison of G2 and dseGFP/G2 complex at 590 nm was conducted using independent t-test (***P< 0.001). (C) The absorbance comparison of dseGFP and dseGFP/SPc complex at 488 nm was conducted using independent t-test at the P=0.05 level of significance.

Figure S5. Cellular uptake of naked dsRNA and dsRNA/SPc complex. The fluorescent dseGFP was mixed with SPc at the mass ratio of 1:1. The cell medium was added with fluorescent dseGFP and dseGFP/SPc complex, respectively (dseGFP: 500 ng). Blue: DAPI. Green: dseGFP.

Figure S6. Cellular uptake of naked siRNA and siRNA/SPc complex. The fluorescent sieGFP was mixed with SPc at the mass ratio of 1:1. The cell medium was added with fluorescent sieGFP and sieGFP/SPc complex, respectively (sieGFP: 500 ng). Blue: DAPI. Green: sieGFP.

Figure S7. Cytoplasm release of SPc/dseGFP vesicle in one cell by real-time imaging. The fluorescent dseGFP was mixed with SPc at the mass ratio of 1:1. A surface plot test was conducted using ImageJ. Three typical regions were marked.

Figure S8. SPc-mediated exocytosis of dsRNA. The medium of cells incubated with fluorescent dseGFP for 6 h, was replaced with the fresh medium. The fluorescent signal of dseGFP/SPc complex was accumulated and located close to the inner membrane of cells. A surface plot test was conducted using ImageJ. Four typical regions were marked.