TOWARDS VIABLE ECO-FRIENDLY MATRICES FOR CONTROLLED PESTICIDE DELIVERY: ADSORPTIVE BEHAVIOUR OF COW DUNG ASH AND STARCH TOWARDS ORGANOPHOSPHORUS PESTICIDES

Chinyere Emmanuella Okafor1,2 & Ikenna Onyido1*

1Department of Pure and Industrial Chemistry, Nnamdi Azikiwe University, Awka, Nigeria

1,2Department of Science Education, Chukwuemeka Odumegwu Ojukwu University,

Uli, Anambra State, Nigeria

SUPPLEMENTARY MATERIAL

Table S1. Experimental data for the adsorption of diazinon on CDA surface at pHs 4, 7 and 9

| pH 4 | Co (mg/L) | Ce (mg/L) |  | Co-Ce | qe (mg/g) | 1/qe |  | 1/Ce |  | Log qe | Log Ce |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.3587 2.0440 2.7202 2.9248 3.1853 4.4651 |  | 0.6413 2.956 7.2798 12.0752 16.8147 20.5349 | 0.1283 0.5912 1.4560 2.4150 3.3629 4.1070 | 7.7942 1.6915 0.6868 0.4141 0.2974 0.2435 |  | 2.7878 0.4892 0.3676 0.3419 0.3139 0.2240 |  | -0.8918 -0.2282 0.1632 0.3829 0.5267 0.6135 | -0.4453 0.3105 0.4346 0.4661 0.5032 0.6498 |  |
| pH 7 | Co (mg/L) | Ce (mg/L) | Co-Ce |  | qe (mg/g) | 1/qe | 1/Ce |  | Log qe |  | Log Ce |  |  |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.3835 1.8067 2.0629 3.0468 3.5688 4.9853 | 0.6165 3.1933 7.9371 11.9532 16.4312 20.0147 |  | 0.1233 0.6387 1.5874 2.3906 3.2863 4.0029 | 8.1103 1.5657 0.6300 0.4183 0.3043 0.2498 | 2.6076 0.5535 0.4848 0.3282 0.2802 0.2006 |  | -0.1990 -0.1947 0.2007 0.3785 0.5167 0.6024 |  | -0.4162 0.2569 0.3145 0.4838 0.5525 0.6977 |  |  |

| pH 9 | Co (mg/L) | Ce (mg/L) | Co-Ce | qe (mg/g) | 1/qe | 1/Ce | Log qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.4073 1.9501 2.7000 3.0349 3.7083 4.6755 | 0.5927 3.0499 7.3000 11.9651 16.2917 20.3245 | 0.1185 0.6100 1.4600 2.3930 3.2583 4.0649 | 8.4388 1.6393 0.6849 0.4179 0.3069 0.2460 | 2.4552 0.5128 0.3704 0.3295 0.2697 0.2139 | -0.9263 -0.2147 0.1644 0.3789 0.5130 0.6090 | -0.3901 0.2901 0.4314 0.4821 0.5692 0.6698 |

Table S2. Experimental data for the adsorption of dichlorvos on CDA surface at pH 4, 7 and 9

| pH 4 | Co (mg/L) | Ce (mg/L) | Co-Ce | qe (mg/g) | 1/qe | 1/Ce | Log qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.5987 3.0423 7.0154 9.7231 11.0872 12.1423 | 0.4014 1.9577 2.9846 5.2769 8.9128 12.8577 | 0.0803 0.3915 0.5969 1.0554 1.7826 2.5715 | 12.4579 2.5540 1.6753 0.9475 0.5610 0.3889 | 1.6703 0.5108 0.1425 0.1029 0.0902 0.0824 | -1.0953 -0.4073 -0.2241 0.0234 0.2511 0.4102 | -0.2228 0.4832 0.8461 0.9878 1.0448 1.0843 |

| pH 7 | Co (mg/L) | Ce (mg/L) | Co-Ce | qe (mg/g) | 1/qe | 1/Ce | Log qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.4638 1.8987 3.2167 3.6718 5.5308 6.4179 | 0.8526 3.1013 6.7833 11.3282 14.4692 18.5821 | 0.1190 0.6203 1.3567 2.2656 2.8938 3.7164 | 2.4765 0.5351 0.3109 0.2724 0.1808 0.1558 | 8.4034 1.6121 0.7371 0.4414 0.3456 0.2691 | -0.3938 0.2785 0.5074 0.5649 0.7428 0.8074 | -0.9245 -0.2074 0.1325 0.3552 0.4615 0.5701 |

| pH 9 | Co (mg/L) | Ce (mg/L) | Co-Ce | qe (mg/g) | 1/qe | 1/Ce | Log qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.1379 1.7297 3.7423 5.7808 6.2051 7.2256 | 0.8603 3.2603 6.2577 9.2192 13.7949 17.7744 | 0.1721 0.6521 1.2515 1.8439 2.7549 3.5549 | 5.8122 1.5336 0.7990 0.5424 0.3625 0.2813 | 7.1582 0.5748 0.2672 0.1730 0.1612 0.1384 | -0.7642 -0.1857 0.0974 0.2657 0.4408 0.5508 | -0.8548 0.2405 0.5731 0.7620 0.7927 0.8689 |

Table S3. Experimental data for the adsorption of diazinon on starch at pH 4, 7 and 9 and 27oC

| pH 4 | Co (mg/L) | Ce (mg/L) | Co-Ce | Qe (mg/g) | 1/Qe | 1/Ce | Log Qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.1647 0.2857 0.6679 0.7688 1.0743 1.9849 | 0.8353 4.7143 9.3321 14.2312 18.9257 23.0151 | 0.1671 0.9429 1.8664 2.8462 3.7851 4.8030 | 6.0716 3.5002 1.4972 1.3007 0.9308 0.5038 | 5.9844 1.0606 0.5358 0.3513 0.2642 0.2172 | -0.7833 -0.5441 -0.1753 -0.1142 0.03113 0.2977 | -0.7770 -0.5441 -0.1753 -0.1142 0.0311 0.2977 |

| pH 7 | Co (mg/L) | Ce (mg/L) | Co-Ce | Qe (mg/g) | 1/Qe | 1/Ce | Log Qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.2752 0.5459 0.9835 1.3193 1.5596 1.7385 | 0.7248 4.4541 9.0165 13.6807 18.4404 23.2615 | 0.1445 0.8908 1.8033 2.7361 3.6881 4.6523 | 3.6337 1.8318 1.0168 0.7580 0.6412 0.5752 | 6.8985 1.1226 0.5545 0.3655 0.2711 0.2149 | -0.8401 -0.0502 0.2561 0.4371 0.5668 0.6677 | 0.0588 0.1734 0.2561 0.3296 0.3959 0.4552 |

| pH 9 | Co (mg/L) | Ce (mg/L) | Co-Ce | Qe (mg/g) | 1/Qe | 1/Ce | Log Qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.3706 0.7431 1.0459 1.2844 1.7220 2.2569 | 0.6294 4.2569 8.9541 13.7156 18.2780 22.7461 | 0.1259 0.8514 1.7909 2.7431 3.6556 4.5486 | 2.6983 1.3457 0.9561 0.7786 0.5807 0.4431 | 7.9428 1.1745 0.5584 0.3646 0.2736 0.2198 | -0.4311 -0.1290 0.0195 0.1087 0.2360 0.3535 | -0.9000 -0.0699 0.2531 0.4382 0.5630 0.6579 |

Table S4. Experimental data for the adsorption of dichlorvos on starch at pH 4, 7 and 9 and 27oC

| pH 4 | Co (mg/L) | Ce (mg/L) | Co-Ce | Qe (mg/g) | 1/Qe | 1/Ce | Log Qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.3654 1.9936 5.8269 7.3936 8.9782 10.0782 | 0.6346 3.0064 4.1731 7.6064 11.0218 14.9218 | 0.1269 0.6013 0.8346 1.5213 2.2044 2.9844 | 7.8790 1.6631 1.1982 0.6573 0.4537 0.3351 | 2.7367 0.5016 0.1716 0.1353 0.1114 0.0992 | -0.8965 -0.2209 -0.0785 0.1822 0.3433 0.4749 | -0.4372 0.2996 0.7654 0.8689 0.9532 1.0034 |

| pH 7 | Co (mg/L) | Ce (mg/L) | Co-Ce | Qe (mg/g) | 1/Qe | 1/Ce | Log Qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.1051 1.9051 2.6897 4.7205 5.7462 6.3526 | 0.8949 3.0949 7.3103 10.2795 14.2538 18.6474 | 0.1790 0.6190 1.4621 2.0559 2.8508 3.7295 | 9.5147 0.5128 0.3718 0.2118 0.1740 0.1574 | 5.5866 1.6155 0.6839 0.4864 0.3508 0.2681 | -0.9784 0.2901 0.4297 0.6740 0.7594 0.8030 | -0.47 -0.2083 0.1650 0.3130 0.4550 0.5717 |

| pH 9 | Co (mg/L) | Ce (mg/L) | Co-Ce | Qe (mg/g) | 1/Qe | 1/Ce | Log Qe | Log Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0 5.0 10.0 15.0 20.0 25.0 | 0.3244 0.6590 0.9192 1.1321 1.1590 1.6321 | 0.6756 4.3410 9.0808 13.8680 18.8410 23.3680 | 0.1351 0.8682 1.8162 2.7736 3.7682 4.6736 | 7.4004 1.1518 0.5506 0.3605 0.2654 0.2140 | 3.8261 1.5175 1.0879 0.8833 0.8628 0.6127 | -0.7314 0.0141 0.2799 0.4557 0.5798 0.6788 | -1.8277 -0.7951 -0.3239 -0.1408 -0.0013 0.0553 |

Table S5. Data for the modelling of the adsorption kinetics of (a) diazinon and (b) dichlorvos on CDA surface according to zero-, first- and second-order behaviour at pH 7 and 270C.

- Adsorbate = diazinon

| Time, t (mins) | (c-b)a ln (c/c-b)a t/(c-b)a |
| --- | --- |
| 20 40 60 90 120 150 | 1.369 0.314 14.609 1.519 0.418 26.342 1.937 0.661 30.981 2.121 0.752 42.425 2.321 0.842 51.697 2.547 0.935 58.900 |

aSee the text for the definition of these notations.

- Adsorbate = dichlorvos

| Time, t (mins) | ( c-b)a ln (c/c-b)a t/(c-b)a |
| --- | --- |
| 20 40 60 90 120 150 | 2.673 0.983 14.209 4.332 1.466 25.642 6.555 1.880 29.951 6.940 1.932 32.969 7.602 2.029 45.697 8.725 2.161 50.193 |

aSee the text for the definition of these notations.

Table S6. Data for the modelling of the adsorption kinetics of (a) diazinon and (b) dichlorvos on starch surface according to zero-, first- and second-order behaviour at pH 7 and 270C.

- Adsorbate = diazinon

| Time, t (mins) | ( c-b)a ln (c/c-b)a t/(c-b)a |
| --- | --- |
| 0.10 10 20 40 60 90 120 150 | 1.090 0.086 0.092 1.238 0.214 8.075 1.301 0.263 15.376 1.451 0.372 27.567 1.713 0.538 35.020 1.978 0.682 45.512 2.031 0.708 59.099 2.058 0.722 72.883 |

aSee the text for the definition of these notations.

- Adsorbate = dichlorvos

| Time, t (mins) | ( c-b)a ln (c/c-b)a t/(c-b)a |
| --- | --- |
| 0.1 10 20 40 60 90 120 150 | 1.193 0.177 0.084 1.250 0.223 8.003 1.333 0.287 15.005 1.600 0.470 24.995 1.733 0.550 34.630 1.878 0.630 47.918 1.900 0.642 63.171 1.951 0.668 72.883 |

aSee the text for the definition of these notations.

Table S7. Data for the desorption of diazinon and dichlorvos from CDA surface at 27oC and pH 7

- Desorbate = Diazinon

| Time (hrs.) | Abs Ce |
| --- | --- |
| 0.5 2.0 5.0 8.0 12.0 24.0 48.0 96.0 144.0 168.0 192.0 | 0.0254 0.0318 0.0272 0.0478 0.0293 0.0671 0.0300 0.0733 0.0312 0.0845 0.0322 0.094 0.0333 0.1045 0.0342 0.1121 0.0346 0.1163 - 0.1191 0.3630 0.1317 |

- Desorbate = Dichlorvos

| Time (hrs) | Abs Ce |
| --- | --- |
| 0.5 2.0 5.0 8.0 12.0 24.0 48.0 96.0 144.0 168.0 192.0 | 0.1244 0.0055 0.1245 0.0073 0.1249 0.0116 0.1252 0.0156 0.1262 0.0284 0.1269 0.0369 0.1276 0.0455 0.1279 0.0503 0.1288 0.0616 0.1291 0.0659 0.1292 0.0671 |

Table S8. Data for the desorption of diazinon and dichlorvos from starch surface at 27oC and pH 7

- Desorbate = Diazinon

| Time (hrs.) | Abs Ce |
| --- | --- |
| 0.5 2.0 5.0 8.0 12.0 24.0 48.0 96.0 144.0 168.0 192.0 | 0.0292 0.0664 0.0309 0.0817 0.0344 0.1139 0.0365 0.1331 0.0392 0.1583 0.0402 0.1674 0.0414 0.1785 0.0432 0.1946 0.0452 0.2128 0.0458 0.2184 - 0.2230 |

- Desorbate = Dichlorvos

| Time (hrs.) | Abs Ce |
| --- | --- |
| 0.5 2.0 5.0 8.0 12.0 24.0 48.0 96.0 144.0 168.0 192.0 | 0.1265 0.0332 0.1291 0.0658 0.1316 0.0982 0.1333 0.1201 0.1343 0.1332 0.1351 0.1433 0.1359 0.1519 0.1368 0.1635 0.1378 0.1772 0.1385 0.1864 0.1394 0.1967 |

Figure S1. Freundlich isotherms for the adsorption of (A) diazinon and (B) dichlorvos on CDA and for the adsorption of (C) diazinon and (D) dichlorvos on starch at 27oC and pHs 4, 7 and 9 at 27oC and pHs 4, 7 and 9  .

Figure S2. Zero-order kinetic plots for the adsorption of diazinon and dichlorvos on CDA surface at pH 7 and 27oC.

Figure S3. First-order kinetic plots for the adsorption of diazinon and dichlorvos on CDA  surface at pH 7 and 27oC.

Figure S4. Zero-order kinetic plots for the desorption of diazinon and dichlorvos from CDA surface into water at pH 7 and 27oC.

Figure S5. First-order kinetic plots for the desorption of (a) diazinon and (b) dichlorvos from CDA surface into water at pH 7 and 27oC.