A comparative study on Fe(III)-chitosan and Fe(III)-chitosan-CTAB complexes for As(V) removal from water: preparation, characterization and reaction mechanism

Changjin Jianga, Ting Zhanga,b,*, Shuhui Lia, Zhaoguang Yanga,b

a College of Chemistry and Chemical Engineering, Central South University, Changsha 410083, Hunan, People’s Republic of China

b Key Laboratory of Hunan Province for Water Environment and Agriculture Product Safety, Central South University, Changsha 410083, Hunan, People’s Republic of China

* Corresponding author.

Corresponding author at: College of Chemistry and Chemical Engineering, Central South University, Changsha 410083, Hunan, People’s Republic of China.

E-mail address: zhangting@csu.edu.cn (T. Zhang).

Table S1.

Operating parameters for ICP-MS.

| Parameter | Setting |
| --- | --- |
| Plasma RF power | 1550 W |
| Plasma gas flow rate | 15.0 L min–1 |
| Carrier gas flow rate | 0.9 L min–1 |
| Auxiliary gas flow rate | 0.9 L min–1 |
| Collision cell gas and flow rate | He, 4.3 L min–1 |
| Monitored ion (m/z) | 75As |
| Dwell time | 1.0 s (As) |

Table S2.

Removal efficiency of As(V) from real water samples using Fe(III)-chitosan-CTAB.

| Sample | pH | Initial As(V) concentration (μg L–1) | Residual As(V) concentration (μg L–1) | As(V) removal (%) |
| --- | --- | --- | --- | --- |
| Tap water | 7.91 | 2.85 | 0.57 | 80.0 |
| Lake water | 7.95 | 17.69 | 0.79 | 95.5 |
| River water | 8.01 | 12.08 | 1.39 | 88.5 |

Table S3.

As(V) removal efficiency and Fe(III) concentration at different pH.

| pH | Fe(III)-chitosan |  |  | Fe(III)-chitosan-CTAB |  |
| --- | --- | --- | --- | --- | --- |
|  | As(V) removal (%) | Fe(III) concentration (mg L–1) |  | As(V) removal (%) | Fe(III) concentration (mg L–1) |
| 2 | 23.2 ± 0.6g | 137.21 ± 1.54 |  | 15.4 ± 0.8f | 119.96 ± 1.54 |
| 3 | 98.4 ± 0.6a | 0.05 ± 0.05 |  | 89.0 ± 0.1d | 10.16 ± 1.82 |
| 4 | 86.0 ± 0.9b | 0 |  | 99.1 ± 0.1a | 0 |
| 5 | 64.8 ± 1.1c | 0 |  | 97.7 ± 0.4ab | 0 |
| 6 | 59.4 ± 0.8d | 0 |  | 96.5 ± 1.0b | 0 |
| 7 | 46.2 ± 0.9e | 0 |  | 93.6 ± 0.2c | 0 |
| 8 | 29.9 ± 1.0f | 0 |  | 89.1 ± 0d | 0 |
| 9 | 10.4 ± 0.6h | 0.01 ± 0 |  | 77.2 ± 0.8e | 0 |
| 10 | 3.9 ± 1.3i | 0 |  | 76.6 ± 2.0e | 0 |

All values are means ± SD (n =3). Different letters indicate significant differences (P < 0.05).

Table S4.

Removal efficiency of As(V) by Fe(III)-chitosan and Fe(III)-chitosan-CTAB at different contact time.

| Contact time (min) | Fe(III)-chitosan |  |  | Fe(III)-chitosan-CTAB |  |
| --- | --- | --- | --- | --- | --- |
|  | As(V) concentration (mg L–1) | As(V) removal (%) |  | As(V) concentration (mg L–1) | As(V) removal (%) |
| 0 | 10.51 ± 0 | 0 |  | 10.51 ± 0 | 0 |
| 1 | 6.13 ± 0.48 | 41.7 ± 4.6 |  | 6.33 ± 0.27 | 39.8 ± 2.6 |
| 2 | 4.22 ± 0.45 | 59.8 ± 4.3 |  | 5.03 ± 0.24 | 52.1 ± 2.3 |
| 3 | 2.97 ± 0.35 | 71.8 ± 3.3 |  | 4.21 ± 0.32 | 59.9 ± 3.1 |
| 4 | 2.32 ± 0.26 | 77.9 ± 2.5 |  | 3.84 ± 0.12 | 63.5 ± 1.1 |
| 5 | 1.75 ± 0.15 | 83.3 ± 1.5 |  | 3.33 ± 0.17 | 68.3 ± 1.6 |
| 10 | 0.92 ± 0.47 | 91.2 ± 4.5 |  | 2.22 ± 0.19 | 78.9 ± 1.8 |
| 15 | 0.64 ± 0.10 | 93.9 ± 0.9 |  | 1.77 ± 0.13 | 83.1 ± 1.2 |
| 20 | 0.49 ± 0.06 | 95.3 ± 0.5 |  | 1.30 ± 0.06 | 87.6 ±0.6 |
| 25 | 0.44 ± 0.06 | 95.8 ± 0.6 |  | 1.19 ± 0.12 | 88.6 ± 1.1 |
| 30 | 0.33 ± 0.02 | 96.9 ±0.2 |  | 1.01 ± 0.06 | 90.4 ± 0.6 |
| 45 | 0.31 ± 0.05 | 97.1 ± 0.4 |  | 0.75 ± 0.04 | 92.9 ± 0.4 |
| 60 | 0.27 ± 0.01 | 97.4 ± 0.1 |  | 0.56 ± 0.11 | 94.6 ± 1.1 |
| 90 | 0.24 ± 0.03 | 97.7 ± 0.3 |  | 0.35 ± 0.05 | 96.7 ± 0.4 |
| 120 | 0.25 ± 0.02 | 97.6 ± 0.2 |  | 0.32 ± 0.03 | 97.0 ± 0.3 |
| 180 | 0.20 ± 0.01 | 98.1 ± 0.1 |  | 0.22 ± 0.03 | 97.9 ± 0.2 |
| 300 | 0.16 ± 0.01 | 98.5 ± 0.2 |  | 0.20 ± 0.03 | 98.1 ± 0.3 |