Supporting Information

High Stability and Recyclable Cellulose-based Fluorescent Paper Derived from Waste Bagasse for Anti-counterfeiting

Lei Guoa, Hongchen Liua, b *, Fang Penga, Jian Kang c *, Haisong Qia *

a State Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou 510641, China

b College of Textiles, Zhongyuan University of Technology, Zhengzhou 450007, China

c State Key Laboratory of NBC Protection for Civilian, Beijing, 100191, China.

E-mail: liuhongchen.beyond@163.com; larance0130@163.com; qihs@scut.edu.cn

*Corresponding authors:

Haisong Qi: qihs@scut.edu.cn

Hongchen Liu: liuhongchen.beyond@163.com

Jian Kang: larance0130@163.com

Table. S1. Elemental analysis of bagasse and CAA-FA paper

| Sample | Elements contents (%) |  |  |
| --- | --- | --- | --- |
|  | C | H | N |
| Bagasse | 41.76 | 6.621 | 0 |
| CAA-FA | 44.11 | 6.271 | 0.19 |

Fig. S1. (a) C1s (b) O1s and (c) N1s peak of CAA-FA paper.

Fig. S2. XRD of bagasse and CAA-FA paper.

Fig. S3. Photographs of CAA-FA paper under UV light

Fig. S4. The fluorescence (a) excitation and (b) emission of CAA-FA paper after different recycling times.

Fig. S5. (a) The fluorescence spectrum and (b) photograph of CAA-FA paper store for 120 days.

Fig. S6. The photo of CAA-FA paper after 24 h treatment with different organic reagents.

Fig. S7. The fluorescence (a) excitation and (b) emission of CAA-FA paper after different solvents treated with 24 h.

Fig. S8. The photo of CAA-FA paper after 24 h treatment with acid and alkali solutions.

Fig. S9. The fluorescence spectrum of CAA-FA paper after (a) acid and (b) alkali treated with 24 h.