Supplementary Information

Van der Waals heterostructure of BixIy for ultra-sensitive x-ray detection

Renzhong Zhuang1, 2, Songhua Cai3, Zengxia Mei1, Huili Liang1, Ningjiu Zhao1, Haoran Mu1, Wenzhi Yu1, 4, Yan Jiang1, Jian Yuan1, Shuping Lau3, Shiming Deng5, Mingyue Han1, Peng Jin6, Cailin Wang1, Guangyu Zhang1, 4, *, Shenghuang Lin1, *

1 State Key Laboratory of Modern Optical Instrumentation

College of Optical Science and Engineering

Zhejiang University

Hangzhou, Zhejiang 310027, China

1 State Key Laboratory of Modern Optical Instrumentation

College of Optical Science and Engineering

Zhejiang University

Hangzhou, Zhejiang 310027, China

1Songshan Lake Materials Laboratory, Dongguan 523808, Guangdong, P. R. China.

2Fujian Provincial Key Laboratory of Welding Quality Intelligent Evaluation, Longyan University, Longyan, Fujian, P. R. China.

3Department of Applied Physics, The Hong Kong Polytechnic University, Hunghom, Kowloon, Hong Kong, P. R. China.

4Institute of Physics, Chinese Academy of Science, Beijing, 100190, P. R. China.

5HAMAMATSU Photonics (China) Co., LTD., Beijing, 100020, P. R. China.

6State Key Laboratory of Modern Optical Instrumentation, College of Optical Science and Engineering, Zhejiang University, Hangzhou, Zhejiang, China.

*Email Address: linshenghuang@sslab.org.cn (S. Lin) & gyzhang@sslab.org.cn, gyzhang@iphy.ac.cn (G. Zhang)

State Key Laboratory of Modern Optical Instrumentation

College of Optical Science and Engineering

Zhejiang University

Hangzhou, Zhejiang 310027, China

Figure caption

Fig. S1 ｜Morphology characterization of BixIy. a, A typical as-grown crystal with the stripped surface. b, c, Complete and flexible slices exfoliated by PDMS, respectively. d, SEM image of an exfoliated flake transferred onto a conductive tape. e, f, AFM image (e) and corresponding surface profile (f) of a freshly exfoliated flake.

Fig. S2 ｜XRD pattern of BixIy with (001) surface, the red arrows point to a minor secondary diffraction.

Fig. S3 ｜XPS spectra of valance band BE of BixIy and commercial BiI3.

Fig. S4 ｜Thermogravimetric analysis curves of BixIy and commercial BiI3.

Fig. S5 ｜Cross-sectional HAADF-STEM images of stripped BixIy slices. a, SEM image of BixIy slices for FIB. b-d, Alternate stacking of thin bright Bi-rich layers and thick dark BiI3 layers with 670 nm (b), 163 nm (c) and 154 nm (d) thickness. e-g, STEM-EDS mapping of Bi (f) and I (g) in a region with bright Bi-rich phase and dark BiI3 (e).

Fig. S6 ｜a-d, HAADF-STEM images of BiI3 and BiI structure viewed along the [100] zone axis (a, b) and the [010] zone axis (c, d).

Fig. S7 ｜HAADF-STEM image of an exfoliated BiI film with 7 I-Bi-Bi-I layers.

Fig. S8 ｜Absorption spectrum of BixIy.

Fig. S9 ｜Photoluminescence spectrum of the BiI3 and BixIy.

Fig. S10 ｜Raman spectrum of the BixIy.

Fig. S11 ｜photo response of the BixIy. a, A planar-type Ag/BixIy/Ag photodetector made on the (001) surface of BixIy. b, Infrared on/off responses from 1100-1900 nm. c, On/off responses under ambient light.

Fig. S12 ｜Transient absorption spectra of BixIy (a) and BiI3 (b).

Fig. S13 ｜On/off x-ray responses of the lateral device (a) and vertical device (b) at different dose rates measured by cavity-edge configuration at room temperature.

Fig. S14 ｜Room temperature self-powered device. a, A Si/BixIy/Bi detector configuration. The Si and Bi electrodes were prepared by mixed the ground Si and Bi powders with the supernatant of silver paste. b, On/off responses of the Si/BixIy/Bi detector at different dose rates under zero bias measured by cavity-edge configuration. c, X-ray photocurrent densities of self-powered device at different dose rates measured by cavity-edge configuration. The sensitivity of 7.5 μC Gy-1 cm-2 was obtained from the current-dose rate relations.

Fig. S15 ｜Comparison of the x-ray detection sensitivities of the BixIy detector in this work with some traditional (CdZnTe, PbI2, HgI2, α-Se38) and recently reported (MAPbBr339, MAPbBr3/Si40, CsPbBr3, Cs2AgBiBr641, MAPbI38, BDAPbI442, Cs3Bi2I99, (NH4)3Bi2I97) detectors. Data for CdZnTe, PbI2, HgI2 and CsPbBr3 were extracted from ref. 43.

Fig. S1 ｜Morphology characterization of BixIy. a, A typical as-grown crystal with the stripped surface. b, c, Complete and flexible slices exfoliated by PDMS, respectively. d, SEM image of an exfoliated flake transferred onto a conductive tape. e, f, AFM image (e) and corresponding surface profile (f) of a freshly exfoliated flake.

Fig. S2 ｜XRD pattern of BixIy with (001) surface, the red arrows point to a minor secondary diffraction.

Fig. S3 ｜XPS spectra of valance band BE of BixIy and commercial BiI3.

Fig. S4 ｜Thermogravimetric analysis curves of BixIy and commercial BiI3.

Fig. S5 ｜Cross-sectional HAADF-STEM images of stripped BixIy slices. a, SEM image of BixIy slices for FIB. b-d, Alternate stacking of thin bright Bi-rich layers and thick dark BiI3 layers with 670 nm (b), 163 nm (c) and 154 nm (d) thickness. e-g, STEM-EDS mapping of Bi (f) and I (g) in a region with bright Bi-rich phase and dark BiI3 (e).

Fig. S6 ｜a-d, HAADF-STEM images of BiI3 and BiI structure viewed along the [100] zone axis (a, b) and the [010] zone axis (c, d).

Fig. S7 ｜HAADF-STEM image of an exfoliated BiI film with 7 I-Bi-Bi-I layers.

Fig. S8 ｜Absorption spectrum of BixIy.

Fig. S9 ｜Photoluminescence spectrum of the BiI3 and BixIy.

Fig. S10 ｜Raman spectrum of the BixIy.

Fig. S11 ｜photo response of the BixIy. a, A planar-type Ag/BixIy/Ag photodetector made on the (001) surface of BixIy. b, Infrared on/off responses from 1100-1900 nm. c, On/off responses under ambient light.

Fig. S12 ｜Transient absorption spectra of BixIy (a) and BiI3 (b).

Fig. S13 ｜On/off x-ray responses of the lateral device (a) and vertical device (b) at different dose rates measured by cavity-edge configuration at room temperature.

Fig. S14 ｜Room temperature self-powered device. a, A Si/BixIy/Bi detector configuration. The Si and Bi electrodes were prepared by mixed the ground Si and Bi powders with the supernatant of silver paste. b, On/off responses of the Si/BixIy/Bi detector at different dose rates under zero bias measured by cavity-edge configuration. c, X-ray photocurrent densities of self-powered device at different dose rates measured by cavity-edge configuration. The sensitivity of 7.5 μC Gy-1 cm-2 was obtained from the current-dose rate relations.

Fig. S15 ｜Comparison of the x-ray detection sensitivities of the BixIy detector in this work with some traditional (CdZnTe, PbI2, HgI2, α-Se38) and recently reported (MAPbBr339, MAPbBr3/Si40, CsPbBr3, Cs2AgBiBr641, MAPbI38, BDAPbI442, Cs3Bi2I99, (NH4)3Bi2I97) detectors. Data for CdZnTe, PbI2, HgI2 and CsPbBr3 were extracted from ref. 43.