Supplementary material:

Bio-inspired, strong, flexible lignin/cellulose film with UV-blocking，water-stable and antioxidant properties

Liangxian Liu1a, Boyu Cui1a, Shuang Li, Chaodong Liu, Lei Tan, Weihong Wang*

Key Laboratory of Bio-Based Material Science and Technology (Ministry of Education), Material Science and Engineering College, Northeast Forestry University, Harbin 150040, China

* Correspondence: weihongwang2001@mefu.edu.cn  (Weihong Wang).

| Sample code | Process parameters |  |  | Ultrasonic treatment |
| --- | --- | --- | --- | --- |
|  | Cellulose (g) | Lignin/acetone (mg/ml) | ZnCl2/H2O (g/100g) |  |
| C UC UCZn-15 UCL UCLZn-15 UCLZn-30 UCLZn-45 | 0.5 0.5 0.5 0.5 0.5 0.5 0.5 | 0 0 0 30 30 30 30 | 0 0 15 0 15 30 45 | No Yes Yes Yes Yes Yes Yes |

Table S1. Films with different process parameters.

Figure S1. The basic length range of C and UC determined by L&W Fiber tester plus (Sweden).

The MFC length ranges were mainly 1–200 μm (approximately 48.9483%) and 200–400 μm (approximately 37.7%). After ultrasonic treatment, the MFC ranges were mainly 1–200 μm (approximately 52.4%) and 200–400 μm (approximately 34.7%).

Figure S2 X-ray diffraction pattern (a) and Crl of C, UC, UCL, and UCLZn-15 (b).

To characterize the crystallization of the films, we performed XRD tests. The crystallinity of the cellulose film was 72.75%, whereas the UC films exhibited a high degree of crystallinity of up to 77.52% after ultrasound treatment, which was attributed to the transformation of amorphous cellulose to cellulose microcrystals. After the addition of lignin, the non-crystalline lignin attenuated the crystallinity of the material. With the addition of Zn2+, the crystallinity of the film decreased to 72.86%, illustrating that the crystal structure of the material was changed, which may be attributed to the coordination interactions of cellulose hydroxyl groups and lignin oxygen-containing groups with Zn2+.

Figure S2 XPS spectra of UCLZn15 and UCL.

Compared to UCL, UCLZn-15 produced a new peak at 1021.7 eV, attributed to the Zn 2p2/3 binding energy after the addition of Zn2+.

Figure S3 SEM micrographs and corresponding surface layer element scanning results (EDS) of the UCLZn-15.

The characteristic element “Zn” (red spots) was uniformly distributed on the film surface. The relative amounts of C, O, and Zn were 60.10%, 38.61%, and 1.29%, respectively.