Supplementary Information

Selection of oxygen reduction catalysts for secondary tri-electrode zinc-air batteries

Adeline Loh1, David P. Trudgeon1, Xiaohong Li1*, Mao-Cheng Liu2, Ling-Bin Kong2, Frank C. Walsh3

1 Renewable Energy Group, College of Engineering, Mathematics and Physical Sciences, University of Exeter, Penryn Campus, Cornwall TR10 9FE, UK

2 State Key Laboratory of Advanced Processing and Recycling of Non-Ferrous Metals, School of Materials Science and Engineering, Lanzhou University of Technology, Lanzhou 730050, China

3 Electrochemical Engineering Laboratory, Energy Technology Group, Department of Mechanical Engineering, University of Southampton, SO17 1BJ, UK.

* Corresponding author. Email: X.Li@exeter.ac.uk Tel: 0044 (0)1326 255769

Data availability ​ statements

- The datasets used and/or analysed during the current study available from the corresponding author on reasonable request.

- All data generated or analysed during this study are included in this published article [and its supplementary information files].

Figure S1. Schematic illustration of electrodes in a jacketed glass cell, connected to Raspberry Pi-microcontroller and relay for galvanostatic cycling.

(a)

(b)

Figure S2. Tafel slope plots for various ORR catalysts (a) without XC-72R and (b) with XC-72R, in O2 saturated 1 M NaOH at 298 K taken from LSVs measured at 400 rpm and scan rate of 5 mV s-1.

(a)

(b)

Figure S3. Koutecky-Levich plots j-1 versus ω-1/2 for (a) catalysts and (b) catalysts with Vulcan XC-72R taken from the mass transfer controlled region of -0.4 V for rotation rates 100, 400, 900, 1600 and 2500 rpm.

Table S1. Corresponding performance data of oxygen electrodes at different current densities as shown in Fig. 6a

| j/ mA cm-2 | Charge / V |  |  | Discharge / V |  |  | Δ E / mV |  | Energy efficiency / % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | ORR and OER | Zn |  |
| 10 | -1.903 | 0.532 | -1.371 | 1.281 | -0.070 | -1.351 | 606 | 20 | 67 |
| 20 | -1.926 | 0.551 | -1.375 | 1.238 | -0.108 | -1.346 | 659 | 29 | 64 |
| 50 | -1.956 | 0.571 | -1.385 | 1.140 | -0.204 | -1.344 | 775 | 41 | 58 |
| 100 | -2.011 | 0.596 | -1.415 | 0.978 | -0.346 | -1.324 | 942 | 91 | 49 |

Table S2. Corresponding performance data of oxygen electrodes at different electrolyte molarities as shown in Fig. 6b

| Electrolyte molarity / M | Charge / V |  |  | Discharge / V |  |  | Δ E / mV |  | Energy efficiency / % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | ORR and OER | Zn |  |
| 2 | -1.944 | 0.590 | -1.354 | 1.195 | -0.126 | -1.321 | 716 | 33 | 62 |
| 4 | -1.926 | 0.551 | -1.375 | 1.238 | -0.108 | -1.346 | 659 | 29 | 64 |
| 6 | -1.927 | 0.535 | -1.392 | 1.247 | -0.117 | -1.364 | 652 | 28 | 65 |
| 8 | -1.939 | 0.525 | -1.414 | 1.241 | -0.140 | -1.381 | 665 | 33 | 64 |

Table S3. Corresponding performance data of oxygen electrodes at different operating temperature as shown in Fig. 6c

| Temperature / ºC | Charge / V |  |  | Discharge / V |  |  | Δ E / mV |  | Energy efficiency / % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | ORR and OER | Zn |  |
| 25 | -1.993 | 0.604 | -1.389 | 1.159 | -0.189 | -1.348 | 793 | 42 | 58 |
| 40 | -1.955 | 0.575 | -1.380 | 1.200 | -0.147 | -1.347 | 722 | 33 | 61 |
| 60 | -1.926 | 0.551 | -1.375 | 1.238 | -0.108 | -1.346 | 659 | 29 | 64 |
| 80 | -1.904 | 0.526 | -1.378 | 1.260 | -0.094 | -1.354 | 620 | 24 | 66 |

Table S4. Corresponding performance data of oxygen electrodes with effect of oxygen purity as shown in Fig. 6d

| O2 purity | Charge / V |  |  | Discharge / V |  |  | Δ E / mV |  | Energy efficiency / % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | Ecell | Ewe vs Hg/HgO | Ece vs Hg/HgO | ORR and OER | Zn |  |
| Bottled O2 | -1.926 | 0.551 | -1.375 | 1.238 | -0.108 | -1.346 | 659 | 29 | 64 |
| Air | -1.925 | 0.553 | -1.372 | 1.180 | -0.164 | -1.344 | 718 | 28 | 61 |
| Air (alt. arrangement) | -1.934 | 0.560 | -1.374 | 1.192 | -0.135 | -1.327 | 695 | 47 | 62 |

Table S5. Conductivities of selected NaOH electrolyte concentrations

| Electrolyte | Conductivity / S cm-1 |
| --- | --- |
| 2 M NaOH + 0.3 M ZnO | 0.266 |
| 4 M NaOH + 0.3 M ZnO | 0.353 |
| 6 M NaOH + 0.3 M ZnO | 0.362 |
| 8 M NaOH + 0.3 M ZnO | 0.369 |

Figure S4. Comparison of ORR electrodes at 20 mA cm-2 in static electrolyte 4 M NaOH + 0.3 M ZnO at 333 K and O2 flow rate 200 cm3 min-1.

Figure S5. Comparison of Zn electrode performance at 20 mA cm-2 in static electrolyte of varying NaOH concentration. A constant concentration of 0.3 M ZnO was added to the electrolyte and experiments were run at 333 K.

Figure S6. Comparison of the conductivity1 and viscosity2 of NaOH over a range of concentrations at 333 K.

The reported conductivities of different NaOH molarities at 338.15 K are much greater than that of the NaOH + 0.3 M ZnO electrolytes measured in this work which indicates that the addition of ZnO reduces the conductivity3. In Fig. S6, conductivities of 4 M NaOH + 0.3 M ZnO and 6 M NaOH + 0.3 M ZnO electrolytes at 333 K are observed to be similar at around 0.36 S cm-1, however the viscosity of 6 M NaOH is much greater than 4 M NaOH.

(a)						   (b)

(c)

Figure S7. Changes in overpotential at the ORR and OER electrode versus (a) current density, (b) electrolyte molarity and (c) temperature.

Figure S8. Galvanostatic cycling performance of MnOx + Ni-Fe-Co(OH)2 electrodes (―) and commercial QSI-Nano® ORR and Magneto OER electrodes (―) in a tri-electrode Zn-air set-up over 50 h at 20 mA cm-2 with 30 min cycle periods, in static electrolyte of 4 M NaOH + 0.3 M ZnO at 333 K. Compressed air was supplied at 200 cm3 min-1.

Table S6. Performance of tri-electrode secondary Zn-air systems in the literature

| Cathode | Anode | Electrolyte | Cycling conditions and stability | Voltage polarisation at 20 mA cm-2 / V | Ref. |
| --- | --- | --- | --- | --- | --- |
| ORR: MnO2 on C paper OER: NiFeCo hydroxide coated SS mesh | Zn foil | 4 M NaOH + 0.3 M ZnO, static | - 10-50 mA cm-2, 30 min cycle periods for 50 h - 58-61 % energy efficiency at 20 mA cm-2 | 0.69 at 20 mA cm-2 | This work |
| ORR: CoO or MnO2 OER: 316 L SS mesh | 3D metal foam current collector filled with Zn, TiN and polymer binder | Commercial electrolyte mainly consisting of 7 M KOH, static | - 5-15 mA cm-2, 24-30 h cycle periods for ~120 h (4 cycles) - 50 % energy efficiency | > 0.90 at 5-15 mA cm-2 | 4 |
| ORR: CoO/ N-CNT on carbon fibre paper OER: NiFe LDH on Ni foam | Zn foil | 6 M KOH + 0.2 M zincate, static | - 20-50 mA cm-2, 4-20 h cycle periods for > 200 h (10 cycles) - 65 % energy efficiency at 20 mA cm-2 | 0.70 at 20 mA cm-2 | 5 |
| ORR: macro/ meso-NC-NH3 OER: Co3O4 on Ni foam | Zn foil | 6 M KOH + 0.2 M ZnCl2, static | - 10 mA cm-2, 4 h cycle periods for ~800 h (200 cycles) - 60-65 % voltage efficiency at 10 mA cm-2 | 0.75 at 10 mA cm-2 | 6 |
| ORR: Commercial GDE OER: RuO2 on Ti net | Zn coated C felt on porous Cu foam | 6 M KOH + 0.4 M ZnO, static | - 20 mA cm-2, ~2 h cycle periods for 1917 h (1000 cycles) - 40 % energy efficiency | 1.1 V to 1.4 V at 20 mA cm-2 | 7 |
| ORR: Ag-based catalyst OER: Ni foam | Cu foam soldered on Zn (not in contact with electrolyte) | 30 wt% KOH + 2 wt% ZnO, 30ºC, flowing 0.4 L min-1 | - 50 mA cm-2, ~8 min cycle periods, (>600 cycles) with short circuits - ~58 % voltage efficiency at 20 mA cm-2 | 1.2 V at 50 mA cm-2 (0.75 V at 20 mA cm-2) | 8 |

References

1.	Woo, A.L.W. Conductance studies of concentrated solutions of sodium hydroxide and potassium hydroxide electrolytes in Chemistry (South Dakota State University: South Dakota, USA, 1968).

2.	O'Brien, T. F., Bommaraju, T.V. & Hine, F. Handbook of Chlor-Alkali Technology (Boston, 2005).

3.	Liu, M. B. et al. Conductivity of KOH electrolyte supersaturated with zincate. J. Electrochem. Soc. 128, 2049-2052. https://doi.org/10.1149/1.2127187 (1981).

4.	Toussaint, G., Stevens, P., Moureau, F., Rouget, R. & Fourgeot, F. Development of a rechargeable zinc-air battery. ECS Trans. 28, 25-34. https://doi.org/10.1149/MA2010-01/12/757 (2010).

5.	Li, Y. et al. Advanced zinc-air batteries based on high-performance hybrid electrocatalysts. Nat. Commun. 4, 1805. https://doi.org/10.1038/ncomms2812 (2013).

6.	Li, L., Liu, C., He, G., Fan, D. & Manthiram, A. Hierarchical pore-in-pore and wire-in-wire catalysts for rechargeable Zn– and Li–air batteries with ultra-long cycle life and high cell efficiency. Energy Environ. Sci. 8, 3274-3282. https://doi.org/10.1039/C5EE02616D (2015).

7.	Hong, W., Li, H. & Wang, B. A horizontal three-electrode structure for zinc-air batteries with long-term cycle life and high performance. Int. J. Electrochem. Sci. 11, 3843-3851. https://doi.org/10.20964/110384 (2016).

8.	Bockelmann, M., Kunz, U. & Turek, T. Electrically rechargeable zinc-oxygen flow battery with high power density. Electrochem. Commun. 69, 24-27. https://doi.org/10.1016/j.elecom.2016.05.013 (2016).