Supporting Information

The Depletable Peroxidase-like Activity of Fe3O4 Nanozymes Accompanied with Phase Transformation Triggered by Separate Migration of Electrons and Iron Ions

Haijiao Dong a, Wei Du a, Jian Dong a, Fei Kong a, Wenlong Cheng b, Ming Ma a, *, Ning Gu a, * and Yu Zhang a, *

a State Key Laboratory of Bioelectronics, Jiangsu Key Laboratory for Biomaterials and Devices, School of Biological Science and Medical Engineering & Collaborative Innovation Center of Suzhou Nano Science and Technology, Southeast University, Nanjing 210096, P. R. China

b Department of Chemical Engineering, Faculty of Engineering, Monash University, Clayton, Victoria, Australia. The Melbourne Centre for Nanofabrication, Clayton, Victoria, Australia.

* Corresponding author:

Yu Zhang, Ph.D    Professor

Ning Gu, Ph.D     Professor

Ming Ma, Ph.D     Associate professor

State Key Laboratory of Bioelectronics, Jiangsu Key Laboratory for Biomaterials and Devices,

School of Biological Science and Medical Engineering, Southeast University

87 Dingjiaqiao, District Gulou, Nanjing 210009, China

Tel: (86) 25-8327 2496.

E-mail: zhangyu@seu.edu.cn; guning@seu.edu.cn; maming@seu.edu.cn

Supplementary Fig. 1 (a) TEM image and size distribution (inset) of Fe3O4 NPs synthesized by chemical co-precipitation method. (b) XRD patterns of as-synthesized Fe3O4 NPs, γ-Fe2O3 NPs and α-Fe2O3 NPs in comparison with the standard diffraction peaks. (c) Ramam spectra of as-synthesized IONPs. (d) Hydrodynamic diameter and Zeta potential of these three IONPs in aqueous solution of pH 3. Inset: the digital photographs of the three IONPs aqueous solution.

XRD patterns of these three iron oxide NPs (IONPs) were in agreement with the corresponding standard diffraction peaks, indicating the acceptable purity and crystallinity (Supplementary Fig. 1b).1-3 From the Raman spectra, Fe3O4 NPs and γ-Fe2O3 NPs were further identified by the A1g mode band near 660 and 700 cm-1, respectively (Supplementary Fig. 1c).1,2,4-6 Magnetite (Fe3O4) has three dominant Raman bands at 313 (T2g mode), 542 (T2g mode), 660 (A1g mode) cm-1. Maghemite (γ-Fe2O3) can be characterized by three broad structures around 360 (T2g), 504 (Eg mode) and 700 cm-1 (A1g mode). Hematite (α-Fe2O3) belongs to the D63d crystal space group and seven phonon lines are expected in the Raman spectrum, namely two A1g modes (229 and 503 cm-1) and five Eg modes (247, 295, 299, 412 and 612 cm-1).4-6 To avoid affecting the enzymatic-like activity, all particles were free of surface coating. Thus their hydrodynamic diameters increased duo to slight aggregation, but with similar surface positive potentials (Supplementary Fig. 1d).

Supplementary Fig. 2 The POD-like activity of as-synthesized Fe3O4 NPs, γ-Fe2O3 NPs, and α-Fe2O3 NPs with (a) TMB, (b) ABTS, and (c) OPD as colorimetric substrates under the presence of H2O2 in 0.2 M acetate buffer (pH = 3.6).

Supplementary Fig. 3 ESR spectra of spin adducts DMPO/·OH produced by Fe3O4 NPs (10 ug/mL) in the presence or absence of H2O2 (0.165 M ) in 0.2 M acetate buffer (pH = 3.6).

Supplementary Fig. 4 (a) Reaction scheme for the oxidation of TMB. (b and c) The changes of UV-vis spectra during the oxidation of TMB catalyzed by Fe3O4 NPs in the presence of H2O2 in 0.2 M acetate buffer (pH = 3.6). (d-f) The absorbance changes at 650 nm catalyzed by Fe3O4 NPs, γ-Fe2O3 NPs, and α-Fe2O3 NPs (0.625 μg Fe/mL) with different concentration of TMB in the presence of H2O2 (7 mM) at pH 3.6. (g) The color changes of POD-like reaction solution catalyzed by Fe3O4 NPs, γ-Fe2O3 NPs, and α-Fe2O3 NPs.

The oxidation of TMB by peroxidase involves two successive one-electron transfer processes (Supplementary Fig. 4a).7 At the beginning of oxidation reaction, colorless TMB loses one electron to form the blue charge-transfer complex with maximum absorbance peaks at 370 and 650 nm. In the second stage, this blue complex continues to lose an electron, forming the final yellow diimine with maximum absorbance peaks of 450 nm. Since the peak at 370 nm overlaps with the diimine peak at 450 nm, the absorption at 650 nm was used to follow the kinetics of catalytic reaction.

Supplementary Fig. 5 The anano of Fe3O4 NPs and γ-Fe2O3 NPs before and after 5 days of cyclic catalysis.

Supplementary Fig. 6 XRD pattern of the recycled Fe3O4 NPs after 5 days of cyclic catalysis. Black lines represent the standard pattern of γ-Fe2O3.

Supplementary Fig. 7 (a) Illustration of the synthesis process of Fe3O4 NPs by thermal decomposition methods (named TD-Fe3O4 NPs) and the aeration oxidization of TD-Fe3O4 NPs. (b-d) TEM image, size distribution, and digital photo of NPs at each synthesis stage. Inset: HRTEM and corresponding SAED pattern.

Supplementary Fig. 8 (a) Comparison of the hydrodynamic diameter and Zeta potential of cc-Fe3O4 NPs and TD-Fe3O4 NPs. (b) Comparison of annao of Fe3O4 NPs synthesized by two methods before and after aeration oxidation of 12 h.

Supplementary Fig. 9 Changes in hydrodynamic diameter and zeta potential of (a) cc-Fe3O4 NPs and (b) TD-Fe3O4 NPs during the aeration oxidation .

Supplementary Fig. 10 The characterization of LiFePO4 NPs. (a) The element mapping of as-synthesized LiFePO4 NPs. (b) XRD, (c) FTIR and (d) XPS spectra of as-synthesized LiFePO4 NPs. The core XPS spectra of (e) Li 1s, P 2p, and (f) Fe 2p of as-synthesized LiFePO4 NPs.

Element mapping of the LiFePO4 powders indicate the presence of Fe, P, and O elements in the prepared samples (Supplementary Fig. 10a). The sharp XRD diffraction peak, shown in Supplementary Fig. 10b, is identified as the orthorhombic olivine structure (JCPDS NO. 40-1499) of LiFePO4, suggesting the phase purity and the high crystallinity of the samples.8 Additionally, the FTIR spectrum in the ranges of 1150-950 cm-1 and 650-450 cm-1 are characteristic for the absorption of PO43- in LiFePO4 NPs (Supplementary Fig. 10c), and their corresponding vibration models were summarized in Table S1, agreeing well with the results reported in the literature.9,10 The XPS full spectrum of as-synthesized LiFePO4 NPs and the core spectra in the binding energy range of Li 1s, P 2p, and Fe 2p were shown in Supplementary Fig. 10d-f. Detailed information was listed in Table S2. Notably, the Fe 2p spectrum contains two main peaks (710.98 and 724.50 eV) and their satellite peak at corresponding high binding energies position. The spin-orbital split energy is about 13.5 eV. These imply that the chemical oxidation state of Fe in the as-synthesized LiFePO4 NPs is divalent.8,11,12 Furthermore, the ICP analysis shows that the molar ratio of Li: Fe: P in the prepared LiFePO4 is 1: 1.04: 1.02, which approximately matched its stoichiometric formula.13 The above characterization results indicate that LiFePO4 NPs have been successfully synthesized.

Supplementary Fig. 11 The POD-like activity of LiFePO4 NPs with (a) ABTS and (b) OPD as colorimetric substrates in the presence of H2O2 at pH 3.6.

Supplementary Fig. 12 (a) pH, (b) temperature, and (d) NPs concentration-dependence of the POD-like activity of LiFePO4 NPs.

Supplementary Fig. 13 Steady-state kinetic assay of LiFePO4 NPs with (a) TMB and (b) H2O2 as substrates. Insets are the Lineweaver–Burk fitting.

Supplementary Fig. 14 The POD-like activity of LiFePO4 NPs and cc-Fe3O4 NPs at the same concentration (0.4 μg Fe/mL) for (a) TMB (1.7 mM) and (b) ABTS (0.75 mM) coloration in the presence of H2O2 (0.8 M) at pH 3.6.

Supplementary Fig. 15 Cyclic voltammograms of (a) LiFePO4 NPs and (c) recycled LiFePO4 NPs at various scan rate (0.2-2 mV·s-1). Plot of peak currents (ipa and ipc) vs. square root of scan rates (v1/2) of (b) LiFePO4 NPs and (d) recycled LiFePO4 NPs.

The electrochemical characteristics of the control and recycled LiFePO4 NPs were evaluated by cyclic voltammetry (CV) at various scan rates in the voltage range of 0.2 to 0.5 V. The increase in peak currents (ipa and ipc) was proportional to the square root of scan rate (v1/2), implying a diffusion-controlled process of Li+ extraction and insertion.14

Supplementary Fig. 16 (a-c) SEM image, element mapping, and EDS analysis, (d) XRD patterns, and (e) hydrodynamic diameter and (inset) Zeta potential of NaLiFePO4-1, NaLiFePO4-5, and NaLiFePO4-10.

Based on the synthetic strategy of LiFePO4 NPs,10 Na-doped LiFePO4 NPs with similar physicochemical properties were prepared by replacing 1%, 5%, and 10% of the Li source with Na source, named as NaLiFePO4-1, NaLiFePO4-5, and NaLiFePO4-10, respectively. EDS (Supplementary Fig. 16a-c) and ICP (Table S3) results show that the amount of Na and the molar ratio of Na: Li in NPs increased with the feeding amount of Na. In addition, the doping of Na did not affect the original orthorhombic olivine structure of LiFePO4 (Supplementary Fig. 16d). They have an approximate hydrodynamic dimension and surface negative potential, compared with LiFePO4 NPs (Supplementary Fig. 16e).

Supplementary Fig. 17 SEM image and EDS analysis of (a) KLiFePO4-1, (b) KLiFePO4-5, and (c) KLiFePO4-10.

Supplementary Fig. 18 (a) Hydrodynamic diameter and (b) Zeta potential of commercial LiFePO4, Fe3(PO4)2, and FePO4 aqueous solution.

Table S1. FTIR spetrum of LiFePO4 NPs.9,10

| - Vibration Model | - Wavenumber (cm-1) |
| --- | --- |
| Stretching mode of O-P-O | 1136.3 |
| Anti-symmetric stretching mode of P-O | 1073.5 |
| Symmetric stretching mode of P-O | 965.6 |
|  | 634.4 |
| Anti-symmetric bending mode of O-P-O | 579.5 |
| symmetric bending mode of O-P-O | 549.1 |
|  | 501.9 |
| Mixture of symmetric and anti-symmetric bending mode of O-P-O | 472.1 |

Table S2. XPS binding energy of various atoms for LiFePO4 NPs.8,11,12

| Atom | Emission peak | Binding energy (eV) | Assignation |
| --- | --- | --- | --- |
| Li | 1s | 55.49 | Li+ |
| Fe | 2p3/2 | 710.98 | Fe2+ |
|  |  | 714.71 | Satellite |
|  | 2p1/2 | 724.50 | Fe2+ |
|  |  | 728.61 | Satellite |
| P | 2p3/2 | 133.38 | [PO4]3- |
|  | 2p1/2 | 134.40 |  |
| O | 1s | 531.08 |  |

- Table S3. ICP analysis results of the Na and K-doped LiFePO4 NPs.

| - Nanozymes |  | - Molar ratio of Na or K : Li |
| --- | --- | --- |
| Na-doped LiFePO4 NPs | NaLiFePO4-1 | 0.25 : 1 |
|  | NaLiFePO4-5 | 0.80 : 1 |
|  | NaLiFePO4-10 | 1.33 : 1 |
| K-doped LiFePO4 NPs | KLiFePO4-1 | 0.04 : 1 |
|  | KLiFePO4-5 | 0.05: 1 |
|  | KLiFePO4-10 | 0.04: 1 |

- References

1.	Zhang, L. et al. Facile synthesis of iron oxides/reduced graphene oxide composites: application for electromagnetic wave absorption at high temperature. Sci. Rep.-UK. 5, (2015).

2.	Gao, J. et al. One-step solvothermal synthesis of highly water-soluble, negatively charged superparamagnetic Fe3O4 colloidal nanocrystal clusters. Nanoscale. 5, 7026 (2013).

3.	Sun, Y., Ma, M., Zhang, Y. & Gu, N. Synthesis of nanometer-size maghemite particles from magnetite. Colloids Surf., A. 245, 15-19 (2004).

4.	Shebanova, O. N. & Lazor, P. Raman study of magnetite (Fe3O4): laser-induced thermal effects and oxidation. J. Raman Spectrosc. 34, 845-852 (2003).

5.	Guo, C., Hu, Y., Qian, H., Ning, J. & Xu, S. Magnetite (Fe3O4) tetrakaidecahedral microcrystals: synthesis, characterization, and micro-Raman study. Mater. Charact. 62, 148-151 (2011).

6.	Jubb, A. M. & Allen, H. C. Vibrational spectroscopic characterization of hematite, maghemite, and magnetite thin films produced by vapor deposition. ACS Appl. Mater. Inter. 2, 2804-2812 (2010).

7.	Gu, S., Risse, S., Lu, Y. & Ballauff, M. Mechanism of the oxidation of 3, 3', 5, 5' -tetramethylbenzidine catalyzed by peroxidase-like Pt nanoparticles immobilized in spherical polyelectrolyte brushes: a kinetic study. ChemPhysChem. 21, (2020).

8.	Ma, J., Li, B., Du, H., Xu, C. & Kang, F. Inorganic-based sol-gel synthesis of nano-structured LiFePO4/C composite materials for lithium ion batteries. J. Solid State Electr. 16, 1353-1362 (2012).

9.	Salah, A. et al. Local structure and redox energies of lithium phosphates with olivine- and nasicon-like structures. J. Power Sources. 140, 370-375 (2005).

10.	Wang, L. et al. Crystal orientation tuning of LiFePO4 nanoplates for high rate lithium battery cathode materials. Nano Lett. 12, 5632-5636 (2012).

11.	Bhuvaneswari, M. S., Bramnik, N. N., Ensling, D., Ehrenberg, H. & Jaegermann, W. Synthesis and characterization of carbon nano fiber/LiFePO4 composites for Li-ion batteries. J. Power Sources. 180, 553-560 (2008).

12.	Caballero, A., Cruz Yusta, M., Morales, J., Santos Peña, J. & Rodríguez Castellón, E. A new and fast synthesis of nanosized LiFePO4 electrode materials. Eur. J. Inorg. Chem. 2006, 1758-1764 (2006).

13.	Kim, J. et al. Enhancement of electrochemical performance of lithium iron phosphate by controlled sol-gel synthesis. Electrochim. Acta. 53, 8258-8264 (2008).

14.	Tang, K., Yu, X., Sun, J., Li, H. & Huang, X. Kinetic analysis on LiFePO4 thin films by CV, GITT, and EIS. Electrochim. Acta. 56, 4869-4875 (2011).