Table 1

Literature absorption data, computed excitation wavelength ( in nm), oscillator strength (f) and orbitals configuration of the C1-1 dye were performed in ethanol solution with TD-DFT method.

| Methods | (nm) | Oscillator Strength (f) | Main configuration (%) |
| --- | --- | --- | --- |
| B3LYP | 579 | 1.383 | HOMO→LUMO (100%) |
| CAM-B3LYP | 477 | 1.790 | HOMO→LUMO (87%) |
| ωB97XD | 463 | 1.843 | HOMO→LUMO (80%) |
| Literature data (C1-1) | 468 | Taken from reference [18] |  |

Table 2

The HOMOs, LUMOs and energy gap () of the C1-1 and A1-A4 dyes were calculated by the B3LYP/6-31G(d) level of theory.

| Dyes | HOMOs | LUMOs | Energy gap () |
| --- | --- | --- | --- |
|  | in (eV) |  |  |
| C1-1 | -5.03 | -2.50 | 2.53 |
| A1 | -4.98 | -2.48 | 2.50 |
| A2 | -5.20 | -2.58 | 2.62 |
| A3 | -5.35 | -2.60 | 2.75 |

Table 3

Computed maximum absorption wavelengths corresponding excitation energy ( in nm and E in eV), Oscillator strength (f in a.u.), Light harvesting efficiency (LHE) and major orbitals transition of the studied dyes were calculated by the TD-ωB97XD/6-31G(d) theory with ethanol medium.

| Dyes | Wavelength |  | Oscillator strength (f) | LHE | Major Transitions |
| --- | --- | --- | --- | --- | --- |
|  | Energy (eV) | (nm) |  |  |  |
| C1-1 | 2.67 | 463 | 1.843 | 0.985 | HOMO→LUMO (80%) |
| A1 | 2.53 | 489 | 1.918 | 0.987 | HOMO→LUMO (78%) |
| A2 | 2.90 | 426 | 1.767 | 0.982 | HOMO→LUMO (80%) |
| A3 | 3.13 | 396 | 1.907 | 0.987 | HOMO→LUMO (80%) |

Table 4

The calculated redox potential of the ground state ( in eV), oxidation potential of the dye (in eV), absorption energy ( in eV), free energy change for electron injection 
( in eV), dye regeneration ( in eV), open-circuit photovoltage ( in eV), exciton binding energy (), chemical hardness (η) and dipole moment ( in Debye) of the studied dye molecules at the TD-ωB97XD/6-31G(d) level of theory in ethanol medium.

| Dyes |  |  |  |  |  |  |  | η | (Debye) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (in eV) |  |  |  |  |  |  |  |  |
| C1-1 | 5.03 | 2.67 | 2.36 | -1.64 | 0.23 | 1.50 | 0.14 | 1.03 | 10.94 |
| A1 | 4.98 | 2.53 | 2.45 | -1.55 | 0.18 | 1.52 | 0.13 | 0.98 | 16.58 |
| A2 | 5.20 | 2.90 | 2.30 | -1.70 | 0.40 | 1.42 | 0.28 | 1.20 | 12.87 |
| A3 | 5.35 | 3.13 | 2.23 | -1.77 | 0.55 | 1.40 | 0.38 | 1.10 | 6.64 |