Supplementary Information for

Facile synthesis of magnetic ZnFe2O4/AC composite to activate peroxydisulfate for dye degradation under visible light irradiation

Tingting Song1, Quanbao He1, Xiaoyan Meng1, Zhangxing He1,2,*, Ming Ge1,*

1College of Chemical Engineering, North China University of Science and Technology, Tangshan 063210, China

2Tangshan Sanyou Group Co., Ltd., Tangshan 063305, China

Fig. S1 The TG curves of the as-obtained catalysts in air.

Fig. S2 Decolorization of RhB under different conditions. Experimental conditions: 20 mg/L RhB solution, 0.30 g/L catalyst, 1.5 g/L PDS, 25 °C.

Fig. S3 XPS survey of ZnFe2O4/AC nanocomposites before and after t reaction.

Fig. S4 The second order kinetic on RhB degradation by the Vis/ZnFe2O4/AC/PDS system.

Table S1 The molecule structure of dyes, the pH value of dye solution and the surface charge of ZnFe2O4/AC

| dye | Structural formula | pH of dye solution | charge of ZnFe2O4/AC |
| --- | --- | --- | --- |
| MO |  | 7.72 | negative charge |
| CR |  | 7.31 | negative charge |
| RhB |  | 6.15 | positive charge |
| MB |  | 7.17 | positive charge |