Table 1

The value of bulk conductivity (σb), total conductivity (σt) measured at 25℃, and relative density (ρrd) for LLTO-Fx solid electrolyte films

| Sample | σb (S/cm) | σt (S/cm) | ρrd (%) |
| --- | --- | --- | --- |
| LLTO-F0 | 2.74×10-4 | 1.57×10-5 | 94.2 |
| LLTO-F2 | 2.78×10-4 | 1.02×10-4 | 95.4 |
| LLTO-F4 | 3.03×10-4 | 2.46×10-5 | 95.1 |
| LLTO-F6 | 6.53×10-4 | 2.25×10-5 | 94.7 |

Table 2

Ionic conductivities of LLTO reported in literatures.

| Methods | Electrolyte | Sintering temperature | σ (S/cm) | Activation Energy Ea (eV) | Reference |
| --- | --- | --- | --- | --- | --- |
| Solid-state reaction method | 1wt% Li2O-B2O3-SiO2 doped Li0.5La0.5TiO3 | 1200 ℃ for 6 h | σb = 1.12×10-3 | － | [2] |
| Pechini method | Li3xLa2/3-x□1/3-2xTiO3 | 1400℃ | σt = 2.0×10-4 | 0.453 | [18] |
| Sol-gel | Li0.33La0.56TiO3 | 1165℃ for 20 h | σt = 1.31×10-4 | － | [19] |
| Glycine nitrate combustion process | Li0.30(La0.50Ln0.50)0.567TiO3 (Ln=La, Pr, Nd) | 1200 ℃ for 10 h | σb = 9×10-4 | 0.27, 0.35 and 0.36 for La, Pr and Nd | [20] |
| Solid-state reaction method | Li0.33La0.555Nd0.005TiO3 | 1250 ℃ for 8 h | σb = 1.26×10-3 | － | [21] |
| Sol-gel | Li0.35La0.55TiO3-Li7La3Zr2O12 | 1350 °C for 6 h. | σt = 1.2×10-4 | 0.32 | [10] |
| Solid-state reaction method | Li0.35La0.55TiO3-2wt% LiF | 1100℃ for 10 h | σt = 1.02×10-4 | 0.26 | Present work |