Supplementary Information

Effects of external field wavelength and solvation on the photophysical property and optical nonlinearity of 1,3-thiazolium-5-thiolates mesoionic compound

Shugui Hua1, Xia Wang2, Zeyu Liu2,, Tian Lu3,, and Mengdi Zhao4

1College of Life Science and Chemistry, Jiangsu Key Laboratory of Biological Functional Molecules, Jiangsu Second Normal University, Nanjing 210013, People’s Republic of China

2School of Environmental and Chemical Engineering, Jiangsu University of Science and Technology, Zhenjiang 212018, People’s Republic of China

3Beijing Kein Research Center for Natural Sciences, Beijing 100022, People’s Republic of China

4Department of Materials Science and Engineering, Suzhou University of Science and Technology, Suzhou 215009, People’s Republic of China

Contents:

Detailed formulas for calculating molecular response properties……………………S3

Table S1 Optimized Cartesian coordinates (in Å) for ground-state MIC at the PBE0/def-TZVP level in C2H6OS solution…………………………………………S5

Table	S2 Selected data related to electron transitions for the MIC at the TD-PBE0/def2-TZVP level in various environments……………………………………S7

Figure S1 HOMOs and LUMOs (isovalue = 0.03 au) for MIC in various environments…………………………………………………………………………S8

Table S3 Selected parameters related to the HRS study of the MIC at the CAM-B3LYP/aug-cc-pVTZ(-f,-d) level in various environments…………………………S9

Figure S2 Harmonic light intensity () for the MIC as a function of the polarization angle (Ψ) by polar representation in different environments at various fundamental wavelength of external field…………………………………………S12

Table S4 Selected parameters related to the EFISHG technique of the studied MIC at the CAM-B3LYP/aug-cc-pVTZ(-f,-d) level in various environments……………S13

Figure S3 Plots of (hyper)polarizability density functions of the MIC under the zero-frequency limit in vacuum: (a)  for the polarizability (isovalue = 0.2 au), (b)  for the first-order hyperpolarizability (isovalue = 2.0 au), and (c)  for the second-order hyperpolarizability (isovalue = 20.0 au)…………………………S16

Table S5 Components of the (hyper)polarizability [, , and , i = x, y, and z] of the constituent units of the MIC under the zero-frequency limit in vacuum…………………………………………………………S17

Detailed formulas for calculating molecular response properties:

For the static case, Taylor expansion of total energy  of a system with respect to the external electric field F is conducted as [S1,S2]:

(S1)

where , , , and  are the tensor components of the dipole moment, polarizability, first-order hyperpolarizability, and second-order hyperpolarizability, respectively.

For the analytic derivative of system energy (the coupled perturbed Kohn-Sham method, CPKS) [S3], T-convention of Willetts et al [S4] was adopted for molecular (hyper)polarizabilities. Formulas of some terms related to molecular response properties are given below:

The isotropic average polarizability [], Hyper-Rayleigh scattering (HRS)-derived first-order hyperpolarizabilities projection of first-order hyperpolarizability on dipole moment [], and scalar component of second-order hyperpolarizability [] are described as:

(S2)

(S3)

(S4)

(S5)

Meanwhile, the electron density of a system  can be defined with respect to the external field F:

(S6)

The components of (hyper)polarizability are expressed by:

(S7)

(S8)

(S9)

where the (hyper)polarizability density  are written as:

(S10)

(S11)

(S12)

The (hyper)polarizability density is obtained by finite difference method using the electron density generated under different applied electric fields. The stepsize of finite difference was set to be 0.003 au, which can get numerically stable results according to our tests [S5,S6].

References

[S1] Buckingham, A. D. Permanent and Induced Molecular Moments and Long-Range Intermolecular Forces. Adv. Chem. Phys. 1967, 12, 107−142.

[S2] Mclean, A. D.; Yoshimine, M. Theory of Molecular Polarizabilities. J. Chem. Phys. 1967, 47, 1927−1935.

[S3] Jensen F. Introduction to computational chemistry. John Wiley & Sons, West Sussex, 2017.

[S4] Willetts, A.; Rice, J. E.; Burland, D. M.; Shelton, D. P. Problems in the Comparison of Theoretical and Experimental Hyperpolarizabilities. J. Chem. Phys. 1992, 97, 7590−7599.

[S5] Liu, Z.; Lu, T. Controllable Photophysical and Nonlinear Properties in Conformation Isomerization of Macrocyclic [32]Octaphyrin(1.0.1.0.1.0.1.0) Involving Hückel and Möbius Topologies. J. Phys. Chem. C 2020, 124, 845–853.

[S6] Liu, Z.; Lu, T. Optical Properties of Novel Conjugated Nanohoops: Revealing the Effects of Topology and Size. J. Phys. Chem. C 2020, 124, 7353−7360.

Table S1 Optimized Cartesian coordinates (in Å) for ground-state MIC at the PBE0/def-TZVP level in C2H6OS solution

| 2-(4-trifluoromethophenyl)-3-methyl-4-(4-methoxyphenyl)-1,3-thiazole-5-thiolate charge = 0, spin multiplicity = 1) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| atom |  | x |  | y |  | z |
| C |  | 0.80386380 |  | 0.00000000 |  | -0.55012303 |
| C |  | -1.40632572 |  | -0.39957766 |  | -1.04522708 |
| C |  | -0.89756745 |  | -0.56094532 |  | -2.32319494 |
| S |  | 0.84275677 |  | -0.29386106 |  | -2.24056384 |
| N |  | -0.43843322 |  | -0.10634703 |  | -0.09446535 |
| C |  | -0.77022483 |  | -0.03262958 |  | 1.32785471 |
| H |  | 0.11268917 |  | -0.27943512 |  | 1.91156919 |
| H |  | -1.11946228 |  | 0.96664090 |  | 1.58469556 |
| H |  | -1.55512829 |  | -0.75715736 |  | 1.53203284 |
| C |  | 1.99998815 |  | 0.33041083 |  | 0.21557828 |
| C |  | 3.18001238 |  | -0.38528700 |  | -0.01175930 |
| C |  | 2.00894824 |  | 1.39281096 |  | 1.12422404 |
| C |  | 4.33831461 |  | -0.05848209 |  | 0.66866806 |
| H |  | 3.18854984 |  | -1.21695827 |  | -0.70725465 |
| C |  | 3.16760229 |  | 1.71675468 |  | 1.80730788 |
| H |  | 1.11647788 |  | 1.98548525 |  | 1.28354026 |
| C |  | 4.32863453 |  | 0.98750156 |  | 1.58412180 |
| H |  | 5.24322207 |  | -0.62802874 |  | 0.49136763 |
| H |  | 3.16201925 |  | 2.54389070 |  | 2.50706379 |
| C |  | -2.82259733 |  | -0.50853440 |  | -0.67289964 |
| C |  | -3.52223134 |  | 0.58515869 |  | -0.15111669 |
| C |  | -3.51273432 |  | -1.70221256 |  | -0.86395704 |
| C |  | -4.85857391 |  | 0.48102945 |  | 0.17926040 |
| H |  | -3.01354181 |  | 1.53277553 |  | -0.00767200 |
| C |  | -4.85693409 |  | -1.82132822 |  | -0.53849378 |
| H |  | -2.99134453 |  | -2.56025809 |  | -1.27292444 |
| C |  | -5.53837953 |  | -0.72463976 |  | -0.01212699 |
| H |  | -5.39807692 |  | 1.33168385 |  | 0.58086116 |
| H |  | -5.35910831 |  | -2.76730817 |  | -0.69599270 |
| S |  | -1.65983031 |  | -0.91076969 |  | -3.80629298 |
| O |  | -6.84130154 |  | -0.73446823 |  | 0.33585868 |
| C |  | -7.57269646 |  | -1.93514177 |  | 0.14336724 |
| H |  | -7.16249153 |  | -2.75452041 |  | 0.74179284 |
| H |  | -8.58823938 |  | -1.72396836 |  | 0.47527487 |
| H |  | -7.59245260 |  | -2.22694086 |  | -0.91120017 |
| C |  | 5.59772587 |  | 1.35823637 |  | 2.29201514 |
| F |  | 6.33866688 |  | 0.28180374 |  | 2.60226940 |
| F |  | 6.38250788 |  | 2.15399113 |  | 1.53658053 |
| F |  | 5.37088664 |  | 2.02082911 |  | 3.43559125 |

Table S2 Selected data related to electron transitions for the MIC at the TD-PBE0/def2-TZVP level in various environments

| environment | nstate | λ (in nm) | f | major transition | μT (in au) |
| --- | --- | --- | --- | --- | --- |
| in vacuum | S2 | 548 | 0.2531 | H → L (92.7%), H-1 → L (5.7%) | 2.14 |
| in CH2Cl2 | S1 | 481 | 0.3450 | H → L (98.6%) | 2.34 |
| in (CH2)2CO | S1 | 470 | 0.3417 | H → L (98.7%) | 2.30 |
| in C2H3N | S1 | 466 | 0.3414 | H → L (98.8%) | 2.29 |
| in C2H6OS | S1 | 466 | 0.3519 | H → L (98.9%) | 2.32 |

Figure S1 HOMOs and LUMOs (isovalue = 0.03 au) for MIC in various environments, blue and red regions denote positive and negative orbital phases, respectively. The numbers inside and outside the parentheses denote the contributions of HOMO-LUMO transitions to the maximum absorptions and the HOMO-LUMO energy gaps (in eV), respectively.

Table S3 Selected parameters related to the HRS study of the MIC at the CAM-B3LYP/aug-cc-pVTZ(-f,-d) level in various environments

| in vacuum |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| incident wavelength (λ, in nm) | (in 10-30 esu) | DRa | ¦<βJ=1>¦b | ¦<βJ=3>¦c | ρd | ΦJ=1e | ΦJ=3f |
| 99999 | 27.9 | 4.456 | 5.03E-29 | 4.76E-29 | 0.947 | 0.514 | 0.486 |
| 1907 | 40.5 | 4.607 | 7.38E-29 | 6.70E-29 | 0.908 | 0.524 | 0.476 |
| 1460 | 56.6 | 4.733 | 1.04E-28 | 9.14E-29 | 0.877 | 0.533 | 0.467 |
| 1340 | 68.1 | 4.798 | 1.26E-28 | 1.09E-28 | 0.862 | 0.537 | 0.463 |
| 1180 | 104.6 | 4.930 | 1.95E-28 | 1.62E-28 | 0.832 | 0.546 | 0.454 |
| 1064 | 209.7 | 5.089 | 3.94E-28 | 3.14E-28 | 0.797 | 0.556 | 0.444 |
| in CH2Cl2 |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | (in 10-30 esu) | DRa | ¦<βJ=1>¦b | ¦<βJ=3>¦c | ρd | ΦJ=1e | ΦJ=3f |
| 99999 | 24.0 | 4.330 | 4.29E-29 | 4.20E-29 | 0.981 | 0.505 | 0.495 |
| 1907 | 32.3 | 4.469 | 5.84E-29 | 5.51E-29 | 0.944 | 0.515 | 0.485 |
| 1460 | 41.5 | 4.581 | 7.55E-29 | 6.90E-29 | 0.915 | 0.522 | 0.478 |
| 1340 | 47.0 | 4.635 | 8.60E-29 | 7.75E-29 | 0.901 | 0.526 | 0.474 |
| 1180 | 61.2 | 4.743 | 1.13E-28 | 9.86E-29 | 0.875 | 0.533 | 0.467 |
| 1064 | 85.1 | 4.864 | 1.58E-28 | 1.34E-28 | 0.847 | 0.541 | 0.459 |
| in (CH2)2CO |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | (in 10-30 esu) | DRa | ¦<βJ=1>¦b | ¦<βJ=3>¦c | ρd | ΦJ=1e | ΦJ=3f |
| 99999 | 21.0 | 4.281 | 3.74E-29 | 3.72E-29 | 0.995 | 0.501 | 0.499 |
| 1907 | 28.0 | 4.418 | 5.03E-29 | 4.81E-29 | 0.957 | 0.511 | 0.489 |
| 1460 | 35.4 | 4.529 | 6.42E-29 | 5.96E-29 | 0.928 | 0.519 | 0.481 |
| 1340 | 39.9 | 4.583 | 7.26E-29 | 6.64E-29 | 0.914 | 0.522 | 0.478 |
| 1180 | 51.0 | 4.690 | 9.35E-29 | 8.30E-29 | 0.888 | 0.530 | 0.470 |
| 1064 | 68.9 | 4.810 | 1.27E-28 | 1.09E-28 | 0.859 | 0.538 | 0.462 |
| in C2H3N |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | (in 10-30 esu) | DRa | ¦<βJ=1>¦b | ¦<βJ=3>¦c | ρd | ΦJ=1e | ΦJ=3f |
| 99999 | 20.2 | 4.264 | 3.58E-29 | 3.58E-29 | 1.000 | 0.500 | 0.500 |
| 1907 | 26.7 | 4.400 | 4.79E-29 | 4.61E-29 | 0.962 | 0.510 | 0.490 |
| 1460 | 33.6 | 4.510 | 6.09E-29 | 5.68E-29 | 0.933 | 0.517 | 0.483 |
| 1340 | 37.8 | 4.564 | 6.87E-29 | 6.32E-29 | 0.919 | 0.521 | 0.479 |
| 1180 | 48.1 | 4.670 | 8.80E-29 | 7.86E-29 | 0.893 | 0.528 | 0.472 |
| 1064 | 64.4 | 4.790 | 1.19E-28 | 1.03E-28 | 0.864 | 0.536 | 0.464 |
| in C2H6OS |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | (in 10-30 esu) | DRa | ¦<βJ=1>¦b | ¦<βJ=3>¦c | ρd | ΦJ=1e | ΦJ=3f |
| 99999 | 21.0 | 4.264 | 3.72E-29 | 3.72E-29 | 1.000 | 0.500 | 0.500 |
| 1907 | 27.8 | 4.401 | 4.99E-29 | 4.80E-29 | 0.962 | 0.510 | 0.490 |
| 1460 | 35.1 | 4.512 | 6.35E-29 | 5.92E-29 | 0.932 | 0.518 | 0.482 |
| 1340 | 39.5 | 4.566 | 7.17E-29 | 6.59E-29 | 0.918 | 0.521 | 0.479 |
| 1180 | 50.2 | 4.673 | 9.20E-29 | 8.21E-29 | 0.892 | 0.529 | 0.471 |
| 1064 | 67.4 | 4.793 | 1.24E-28 | 1.07E-28 | 0.863 | 0.537 | 0.463 |

aDepolarization ratio. bDipolar tensorial component. cOctupolar tensorial component. dNonlinear anisotropy parameter. eRatio of the dipolar contribution to the hyperpolarizability tensor. fRatio of the octupolar contribution to the hyperpolarizability tensor.

Figure S2 Harmonic light intensity () for the MIC as a function of the polarization angle (Ψ) by polar representation in different environments at various fundamental wavelength of external field.

Table S4 Selected parameters related to the EFISHG technique of the studied MIC at the CAM-B3LYP/aug-cc-pVTZ(-f,-d) level in various environments

| in vacuum |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| incident wavelength (λ, in nm) | polarizability (in 10-23 esu) |  |  |  | first-order hyperpolarizability (in 10-30 esu) |  |  |  | second-order hyperpolarizability (in 10-36 esu) |  |  |  |
| 99999 | 6.54 | 3.14 | 4.11 | 4.60 | -43.3 | 1.2 | -2.5 | -20.8 | 396 | 23 | 59 | 159 |
| 1907 | 6.65 | 3.16 | 4.15 | 4.65 | -61.4 | 1.1 | -5.3 | -32.9 | 593 | 25 | 83 | 238 |
| 1460 | 6.73 | 3.17 | 4.19 | 4.69 | -84.3 | 1.0 | -9.3 | -48.9 | 881 | 28 | 121 | 358 |
| 1340 | 6.76 | 3.17 | 4.21 | 4.71 | -100.3 | 0.8 | -12.3 | -60.4 | 1111 | 29 | 153 | 455 |
| 1180 | 6.84 | 3.18 | 4.24 | 4.75 | -151.0 | 0.4 | -22.1 | -97.4 | 1994 | 34 | 280 | 836 |
| 1064 | 6.92 | 3.19 | 4.27 | 4.79 | -295.7 | -1.2 | -51.7 | -205.6 | 5923 | 50 | 885 | 2573 |
| in CH2Cl2 |  |  |  |  |  |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | polarizability (in 10-23 esu) |  |  |  | first-order hyperpolarizability (in 10-30 esu) |  |  |  | second-order hyperpolarizability (in 10-36 esu) |  |  |  |
| 99999 | 6.99 | 3.64 | 4.71 | 5.11 | -37.5 | 2.0 | -0.2 | -20.9 | 504 | 37 | 91 | 216 |
| 1907 | 7.08 | 3.66 | 4.75 | 5.16 | -49.3 | 2.1 | -2.0 | -31.3 | 681 | 41 | 116 | 290 |
| 1460 | 7.14 | 3.67 | 4.79 | 5.20 | -61.9 | 2.2 | -4.3 | -43.1 | 888 | 44 | 146 | 378 |
| 1340 | 7.17 | 3.68 | 4.81 | 5.22 | -69.6 | 2.2 | -5.8 | -50.3 | 1023 | 46 | 166 | 436 |
| 1180 | 7.23 | 3.69 | 4.84 | 5.25 | -88.8 | 2.2 | -9.6 | -69.1 | 1390 | 50 | 221 | 595 |
| 7 | 7.29 | 3.70 | 4.87 | 5.29 | -120.9 | 2.2 | -16.6 | -101.1 | 2101 | 55 | 331 | 908 |
| in (CH2)2CO |  |  |  |  |  |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | polarizability (in 10-23 esu) |  |  |  | first-order hyperpolarizability (in 10-30 esu) |  |  |  | second-order hyperpolarizability (in 10-36 esu) |  |  |  |
| 99999 | 6.86 | 3.57 | 4.62 | 5.02 | -33.1 | 1.9 | 0.7 | -17.4 | 465 | 37 | 89 | 202 |
| 1907 | 6.94 | 3.59 | 4.66 | 5.06 | -43.0 | 2.1 | -0.8 | -26.1 | 617 | 41 | 111 | 266 |
| 1460 | 7.00 | 3.60 | 4.69 | 5.10 | -53.4 | 2.2 | -2.6 | -35.8 | 789 | 44 | 137 | 340 |
| 1340 | 7.03 | 3.61 | 4.71 | 5.12 | -59.5 | 2.2 | -3.7 | -41.7 | 898 | 46 | 153 | 386 |
| 1180 | 7.08 | 3.62 | 4.74 | 5.15 | -74.7 | 2.3 | -6.6 | -56.4 | 1185 | 50 | 196 | 511 |
| 1064 | 7.14 | 3.63 | 4.77 | 5.18 | -98.8 | 2.3 | -11.7 | -80.7 | 1706 | 54 | 278 | 740 |
| in C2H3N |  |  |  |  |  |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | polarizability (in 10-23 esu) |  |  |  | first-order hyperpolarizability (in 10-30 esu) |  |  |  | second-order hyperpolarizability (in 10-36 esu) |  |  |  |
| 99999 | 6.83 | 3.56 | 4.60 | 4.99 | -31.8 | 1.9 | 0.9 | -16.4 | 454 | 38 | 89 | 198 |
| 1907 | 6.91 | 3.57 | 4.64 | 5.04 | -41.2 | 2.1 | -0.4 | -24.6 | 599 | 42 | 110 | 260 |
| 1460 | 6.97 | 3.59 | 4.67 | 5.07 | -50.9 | 2.2 | -2.0 | -33.7 | 762 | 45 | 135 | 329 |
| 1340 | 6.99 | 3.59 | 4.69 | 5.09 | -56.6 | 2.2 | -3.1 | -39.2 | 863 | 46 | 150 | 373 |
| 1180 | 7.05 | 3.60 | 4.72 | 5.12 | -70.7 | 2.3 | -5.8 | -52.9 | 1129 | 50 | 190 | 488 |
| 1064 | 7.10 | 3.61 | 4.75 | 5.15 | -92.7 | 2.3 | -10.3 | -75.1 | 1601 | 55 | 264 | 696 |
| in C2H6OS |  |  |  |  |  |  |  |  |  |  |  |  |
| incident wavelength (λ, in nm) | polarizability (in 10-23 esu) |  |  |  | first-order hyperpolarizability (in 10-30 esu) |  |  |  | second-order hyperpolarizability (in 10-36 esu) |  |  |  |
| 99999 | 6.92 | 3.63 | 4.69 | 5.08 | -33.0 | 2.0 | 0.8 | -17.2 | 473 | 39 | 93 | 207 |
| 1907 | 7.00 | 3.65 | 4.73 | 5.13 | -42.7 | 2.2 | -0.6 | -25.9 | 625 | 43 | 116 | 272 |
| 1460 | 7.06 | 3.66 | 4.76 | 5.16 | -52.8 | 2.3 | -2.3 | -35.4 | 795 | 47 | 142 | 345 |
| 1340 | 7.09 | 3.67 | 4.78 | 5.18 | -58.8 | 2.3 | -3.5 | -41.2 | 902 | 48 | 158 | 391 |
| 1180 | 7.14 | 3.68 | 4.81 | 5.21 | -73.4 | 2.4 | -6.3 | -55.6 | 1181 | 52 | 201 | 513 |
| 1064 | 7.20 | 3.69 | 4.84 | 5.24 | -96.5 | 2.4 | -11.2 | -79.1 | 1678 | 57 | 280 | 733 |

Figure S3 Plots of (hyper)polarizability density functions of the MIC under the zero-frequency limit in vacuum: (a)  for the polarizability (isovalue = 0.2 au), (b)  for the first-order hyperpolarizability (isovalue = 2.0 au), and (c)  for the second-order hyperpolarizability (isovalue = 20.0 au). Blue and red regions denote positive and negative contributions, respectively.

Table S5 Components of the (hyper)polarizability [, , and , i = x, y, and z] of the constituent units of the MIC under the zero-frequency limit in vacuuma

| (in 10-23 esu) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| i = x |  |  |  |  |  |  | i = y |  |  |  |  |  |  | i = z |  |  |  |  |  |
| overall | RD | BD | BM | BA | RA |  | overall | RD | BD | BM | BA | RA |  | overall | RD | BD | BM | BA | RA |
| 6.56 | 1.82 | 0.95 | 1.25 | 1.27 | 1.27 |  | 3.14 | 0.30 | 0.93 | 0.85 | 0.76 | 0.31 |  | 4.10 | 0.23 | 0.45 | 2.30 | 0.65 | 0.47 |
| (in 10-30 esu) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| i = x |  |  |  |  |  |  | i = y |  |  |  |  |  |  | i = z |  |  |  |  |  |
| overall | RD | BD | BM | BA | RA |  | overall | RD | BD | BM | BA | RA |  | overall | RD | BD | BM | BA | RA |
| -43.9 | -7.0 | -3.9 | -9.1 | -14.4 | -9.6 |  | 1.1 | 0.5 | 0.2 | 1.1 | -0.3 | -0.3 |  | -2.7 | -0.0 | -0.2 | 0.5 | -1.6 | -1.5 |
| (in 10-36 esu) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| i = x |  |  |  |  |  |  | i = y |  |  |  |  |  |  | i = z |  |  |  |  |  |
| overall | RD | BD | BM | BA | RA |  | overall | RD | BD | BM | BA | RA |  | overall | RD | BD | BM | BA | RA |
| 417 | 77 | 90 | 16 | 152 | 83 |  | 22 | 2 | 5 | 10 | 4 | 1 |  | 60 | 1 | 2 | 41 | 9 | 7 |

aThe stepsize of finite difference, Fi (i = x, y, and z), was set to be 0.003 au.

Email: liuzy@just.edu.cn  (Zeyu Liu), sobereva@sina.com (Tian Lu).