Appendix A. Supplementary Data

Fig.S1. Powder of gIONPs dried at 70 °C.

Table S1. Experimental design runs for synthesis of gIONPs with the corresponding responses (hydrodynamic size and PDI values of DLS measurements).

| No | Extract Concentration (w/w %) | Iron Ion (M) | Time (h) | Temp (°C) | RPM | pH | Hydrodynamic Size (nm) | PDI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 5 | 0,07 | 1 | 25 | 200 | 5 | 302.6±13 | 6.4±0.4 |
| 2 | 5 | 0.07 | 1 | 25 | 400 | 8 | 401±27 | 5.6±0.1 |
| 3 | 5 | 0.07 | 1 | 25 | 600 | 11 | 448.8±16.9 | 5.3±1 |
| 4 | 5 | 0.14 | 2 | 55 | 200 | 5 | 384.7±8.5 | 3.7±0.3 |
| 5 | 5 | 0.14 | 2 | 55 | 400 | 8 | 256.3±9.7 | 4.3±0.1 |
| 6 | 5 | 0.14 | 2 | 55 | 600 | 11 | 254.1±9 | 4.1±0.1 |
| 7 | 5 | 0.28 | 3 | 85 | 200 | 5 | 317.9±5.7 | 2.4±0.4 |
| 8 | 5 | 0.28 | 3 | 85 | 400 | 8 | 330±7.8 | 3.3±0.1 |
| 9 | 5 | 0.28 | 3 | 85 | 600 | 11 | 384±7.8 | 3.1±0.2 |
| 10 | 10 | 0.07 | 2 | 85 | 200 | 8 | 268.3±7.8 | 3.1±0.1 |
| 11 | 10 | 0.07 | 2 | 85 | 400 | 11 | 279.7±9 | 2.9±0.02 |
| 12 | 10 | 0.07 | 2 | 85 | 600 | 5 | 277.2±14.5 | 2.9±0.2 |
| 13 | 10 | 0.14 | 3 | 25 | 200 | 8 | 237.6±5 | 0.6±0.06 |
| 14 | 10 | 0.14 | 3 | 25 | 400 | 11 | 288±3 | 0.4±0.08 |
| 15 | 10 | 0.14 | 3 | 25 | 600 | 5 | 278.2±7.2 | 0.7±0.1 |
| 16 | 10 | 0.28 | 1 | 55 | 200 | 8 | 373.5±11 | 7.5±0.4 |
| 17 | 10 | 0.28 | 1 | 55 | 400 | 11 | 372.7±24 | 8.5±1.2 |
| 18 | 10 | 0.28 | 1 | 55 | 600 | 5 | 325.8±9 | 8.4±1 |
| 19 | 20 | 0.07 | 3 | 55 | 200 | 11 | 800.6±39.5 | 7.5±0.4 |
| 20 | 20 | 0.07 | 3 | 55 | 400 | 5 | 661±8 | 4.9±1 |
| 21 | 20 | 0.07 | 3 | 55 | 600 | 8 | 721.4±30 | 7.1±0.6 |
| 22 | 20 | 0.14 | 1 | 85 | 200 | 11 | 1074.1±7.8 | 5.0±1 |
| 23 | 20 | 0.14 | 1 | 85 | 400 | 5 | 645.7±5.8 | 3.1±0.3 |
| 24 | 20 | 0.14 | 1 | 85 | 600 | 8 | 826.9±3 | 4.4±0.3 |
| 25 | 20 | 0.28 | 2 | 25 | 200 | 11 | 766±3.8 | 3.9±0.5 |
| 26 | 20 | 0.28 | 2 | 25 | 400 | 5 | 472.5±2.5 | 3.0±0.4 |
| 27 | 20 | 0.28 | 2 | 25 | 600 | 8 | 714.9±5 | 5.7±0.6 |

Table S2. JCPDS card for Hematite

Name and formula

Reference code:	00-013-0534

Mineral name:	Hematite, syn

Compound name:	Iron Oxide

PDF index name:	Iron Oxide

Empirical formula:	Fe2O3

Chemical formula:	Fe2O3

Crystallographic parameters

Crystal system:	Rhombohedral

Space group:	R-3c

Space group number:	167

a (Å):	  5.0310

b (Å):	  5.0310

c (Å):	 13.7370

Alpha (°):	 90.0000

Beta (°):	 90.0000

Gamma (°):	120.0000

Calculated density (g/cm^3):	  5.27

Measured density (g/cm^3):	  5.26

Volume of cell (10^6 pm^3):	301.11

Z:	  6.00

RIR:	  2.60

Status, subfiles and quality

Status:	Marked as deleted by ICDD

Subfiles:	Alloy, metal or intermetalic

Forensic

Inorganic

Mineral

Pharmaceutical

Quality:	Blank (B)

References

Primary reference:	Aravindaksham, Ali, Council of Sci. and Ind. Res., Central Fuel Res. Inst., Bimat, India., Private Communication

Unit cell:	Kastalsky, et al., Aust. J. Chem., 21, 1061, (1968)

Peak list

No.    h    k    l      d [A]     2Theta[deg] I [%]

1    0    1    2      3.66000    24.299      25.0

2    1    0    4      2.69000    33.280     100.0

3    1    1    0      2.51000    35.744      50.0

4    0    0    6      2.28500    39.402       2.0

5    1    1    3      2.20100    40.972      30.0

6    2    0    2      2.07000    43.694       2.0

7    0    2    4      1.83800    49.555      40.0

8    1    1    6      1.69000    54.233      60.0

9    2    1    1      1.63400    56.253       4.0

10    0    1    8      1.59600    57.716      16.0

11    2    1    4      1.48400    62.540      35.0

12    3    0    0      1.45200    64.080      35.0

13    2    0    8      1.34900    69.642       4.0

14    1    0   10      1.31000    72.033      20.0

15    2    2    0      1.25800    75.515       8.0

16    0    3    6      1.22600    77.850       2.0

17    2    2    3      1.21300    78.845       4.0

18    1    2    8      1.18900    80.760       8.0

19    0    2   10      1.16200    83.044      10.0

20    1    3    4      1.14100    84.925      12.0

21    2    2    6      1.10200    88.694      14.0

22    0    4    2      1.07600    91.433       2.0

23    2    1   10      1.05500    93.797      18.0

24    1    1   12      1.04200    95.335       2.0

25    4    0    4      1.03800    95.821       2.0

26    2    3    2      0.98900   102.314      10.0

27    2    2    9      0.97150   104.914       2.0

28    3    2    4      0.96010   106.703      18.0

29    0    1   14      0.95780   107.074       6.0

30    4    1    0      0.95120   108.157      12.0

31    4    1    3      0.93140   111.591       6.0

32    0    4    8      0.92040   113.632       6.0

33                     0.90800   116.065      25.0

Table S3. Kirby Bauer Interpretation chart for test antibiotics

| Antibiotics | Abbreviation | Disc potency µg/ Disc | Zone of Inhibition in mm |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Resistant | Intermediate | Susceptible |
| Cefotaxime | CTX | 30 | ≤ 14 | 15 – 22 | ≥ 23 |
| Tetracycline | TE | 30 | ≤ 14 | 15 – 18 | ≥ 19 |
| Gentamicin | CN | 10 | ≤ 12 | 13 – 14 | ≥ 15 |
| Cefoxitin | FOX | 30 | ≤ 21 | - | ≥ 22 |