Supplementary Information

Omnidirectional printing of elastic conductors for 3D-structured stretchable electronics

Lee et al.

Supplementary Figures

Supplementary Fig. 1 | Extrusion stability of the dilution-based and emulsion-based inks. The dilution-based ink contained 15-wt% CHCl3, and the emulsion-based ink contained 10-wt% CHCl3 and 5-wt% DEG. The emulsion-based ink was stably extruded until the ink was completely depleted, while the dilution-based ink shortly clogged the nozzle.

Supplementary Fig. 2 | Ink stability over time. a,b Photographs of the dilution-based ink (a) and emulsion-based ink (b) in a vial over time. The dilution-based ink contained 15-wt% CHCl3, and the emulsion-based ink contained 10-wt% CHCl3 and 5-wt% DEG. After 24 hours, both inks were poured by a spatula.

Supplementary Fig. 3 | Rheological properties of the dilution-based and emulsion-based inks. a-d, Storage and loss moduli of the 85-wt% (a) and 89-wt% (b) dilution-based inks and 85-wt% (c) and 89-wt% (d) emulsion-based inks.

Supplementary Fig. 4 | Rheological behaviours of the dilution-based and emulsion-based inks. a,d, Photographs of the as-fabricated inks based on dilution (a) and emulsion (b) that were poured by a spatula. The dilution-based ink contained 15-wt% CHCl3, and the emulsion-based ink contained 10-wt% CHCl3 and 5-wt% DEG.

Supplementary Fig. 5 | Simulation models for self-supporting filaments. Modelling details for the 3D FEA simulation calculating the von Mises stress (σvm) and first principal strain (ε1) applied to the self-supporting filaments.

Supplementary Fig. 6 | Self-supporting filament bridging noncoplanar surfaces. a, Schematic illustration of the direct writing process for oblique filaments that bridge two surfaces having a large height difference. b, Photograph showing the direct writing of the out-of-plane segment. c, Photograph of the printed self-supporting out-of-plane filaments.

Supplementary Fig. 7 | Scalability of our printing method. a, Optical microscopy images showing the scalability of our printing method using emulsion-based ink. b,c, Scanning electron microscopy (SEM) image of the lines printed with a 27-gauge needle (b) and a 30-gauge needle (c). d, SEM image of the printed line with a width <100 μm.

Supplementary Fig. 8 | Complex patterns printed on elastomeric substrates. a, Photographs of complex patterns printed on elastomeric substrates under various tensile deformations. b, Optical microscopy images of the printed patterns.

Supplementary Fig. 9 | Comparison of self-supporting structures printed using dilution-based and emulsion-based inks. a,b, Sequential photographs showing the printing process fabricating a self-supporting arch-shaped filament using dilution-based (a) and emulsion-based (b) inks.

Supplementary Fig. 10 | Cross-sectional morphology of the dilution-based and emulsion-based composites. a,b, SEM images showing the cross-sectional morphology of the dilution-based composites (a) and emulsion-based composites (b).

Supplementary Fig. 11 | Electrical conductivity as a function of Ag volume fraction for the dilution-based and emulsion-based composites.

Supplementary Fig. 12 | Critical exponents in percolation theory. a,b, Plots for fitting equation (1) with the experimental results to find the critical exponent (t) for the dilution-based and emulsion-based inks.

Supplementary Fig. 13 | Electrical conductivity of printed elastic conductors with different feature sizes. a, Electrical conductivity as a function of line width. b, Dimensions, measured resistance, and calculated conductivity for each line. c, SEM image showing the cross-sections of the printed elastic conductors. The yellow regions denote the cross-sectional areas of the printed lines calculated using image analysis software.

Supplementary Fig. 14 | Effect of encapsulation on strained elastic conductors. a, SEM images showing the cross-section of the emulsion-based elastic conductors under tensile strain. b, SEM images showing the cross-section of the encapsulated elastic conductors under tensile strain.

Supplementary Tables

Supplementary Table 1 | Comparison of direct ink writing methods for elastic conductors

| Ref. | Strategy | Viscosity (Pa s) |  | Storage modulus (Pa) | Yield Stress (Pa) | Minimum feature size (µm) | Electrical conductivity (S cm-1) | Stretchability (%) | 3D deposition |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Low shear rate | High shear rate |  |  |  |  |  |  |
| This work | Emulsion of Ag particles /MWCNTs/PDMS and DEG | 209000 (0.012 s-1) | 29 (131 s-1) | ~2300000 | ~5000 | 98 | 6177 | 160 | Omnidirectional printing |
| 1 | Ag flakes/fluorine rubber with solvent dilution1 | - |  | - | - | 50 | 738 | 220 | 2D plane only |
| 2 | Ag flakes/TPU with solvent dilution2 | ~3000 (0.01 s-1) | ~50 (20 s-1) | 10000 | 20 | 100 | ~10000 | 30 | 2D plane only |
| 3 | Ag flakes/PDMS/lubricant with solvent dilution3 | ~200 (0.1 s-1) | 2.45 (100 s-1) | ~20000 | <100 | 260 | 1933.3 | 300 | 2D plane only |
| 4 | AgNPs/PU with solvent dilution4 | 70 (0.1 s-1) | ~1.5 (100 s-1) | - | - | 3 | 8846 | 100 | 2D plane only |
| 5 | MWNTs/RGO/SIS with solvent dilution5 | 600 |  | 3150 | 42 | 161 | - | 70 | Layer-wise |
| 6 | Ag particles/PDMS with solvent dilution6 | - |  | - | - | 200 | 1000 | 400 | Layer-wise |
| 7 | Ag flakes/PDMS with solvent dilution7 | 363.9 |  | 607 | - | 510 | 85.91 | 150 | Layer-wise |
| 8 | Ag flakes/CNTs/SIS with solvent dilution8 | - |  | 17836 | 145.6 | 200 | >1000 | 70 | Layer-wise |

Supplementary References

1.	Matsuhisa, N. et al. Printable elastic conductors with a high conductivity for electronic textile applications. Nat. Commun. 6, 7461 (2015).

2.	Valentine, A. D. et al. Hybrid 3D Printing of Soft Electronics. Adv. Mater. 29, 1703817 (2017).

3.	Hwang, Y. et al. Lubricant-Added Conductive Composite for Direct Writing of a Stretchable Electrode. ACS Appl. Mater. Interfaces 11, 48459–48465 (2019).

4.	Kang, Y. et al. High-Resolution Printable and Elastomeric Conductors from Strain-Adaptive Assemblies of Metallic Nanoparticles with Low Aspect Ratios. Small 16, 2004793 (2020).

5.	Kim, J. Y. et al. 3D printable composite dough for stretchable, ultrasensitive and body-patchable strain sensors. Nanoscale 9, 11035–11046 (2017).

6.	Guo, S.-Z., Qiu, K., Meng, F., Park, S. H. & McAlpine, M. C. 3D Printed Stretchable Tactile Sensors. Adv. Mater. 29, 1701218 (2017).

7.	Yoon, I. S. et al. 3D Printing of Self‐Wiring Conductive Ink with High Stretchability and Stackability for Customized Wearable Devices. Adv. Mater. Technol. 4, 1900363 (2019).

8.	Lee, H. S. et al. Three-Dimensionally Printed Stretchable Conductors from Surfactant-Mediated Composite Pastes. ACS Appl. Mater. Interfaces 11, 12622–12631 (2019).