Surface bio-interactions stand at the base of the short-term nano CuO-induced cell oxidative stress: insights for a safe(r)-by-design approach

ADDITIONAL FILE 2

Elisa Moschini1,4, Graziano Colombo2, Giuseppe Chirico3, Giancarlo Capitani1, Isabella Dalle-Donne2, Paride Mantecca1*

1 Department of Earth and Environmental Sciences, Research Center POLARIS, University of Milano Bicocca, 1 Piazza della Scienza - 20126 Milan, Italy

2 Department of Biosciences, Università degli Studi di Milano, 26 via Celoria - 20133 Milan, Italy

3 Department of Physic, University of Milano Bicocca, 2 Piazza della Scienza - 20126 Milano, Italy

4 Luxembourg Institute of Science and Technology (LIST), Environmental Research and Innovation (ERIN) Department, 41, rue du Brill, L-4422 Belvaux, Grand-Duchy of Luxembourg

1. Cell viability

The viability was assessed by MTT assay in cells exposed to cCuO and sCuO at 10-100 mg/ml for 1h, 3h and 6h. At the end of exposure, culture medium was replaced with new medium containing MTT solution (0.3 mg/ml) and incubated for 2.5 hours at 37°C. Formazan crystals formed were dissolved in dimethyl sulfoxide (DMSO). The plates were shacked for 10 minutes at room temperature and optical density was recorded at 570 nm (using 690 nm as a reference) using a multiplate reader (Multiskan Ascent, Thermo Electron Corporation, Vantaa, Finland). Untreated cells were used as negative control.

The data, shown in Additional Figure 3, are representative of at least three independent experiments. Statistical comparisons were performed by one-way ANOVA followed by Fischer’s LSD test.

The contribution to cytotoxicity of copper ions dissolved from NPs was also evaluated at the maximum theoretical dissolving concentration for the higher NP concentration tested (100mg/ml).

Additional Figure 3. Cell viability results by MTT assay of A549 cells exposed to CuO NPs (6 h).

Dark grey bars= cCuO; light grey bars= sCuO; black bar= 80 mg/ml Cu++ (from CuSO4·5H2O). *Significantly different from control (ANOVA + Fisher LSD Method, p < 0.05).