Surface bio-interactions stand at the base of the short-term nano CuO-induced cell oxidative stress: insights for a safe(r)-by-design approach

ADDITIONAL FILE 1

Elisa Moschini1,4, Graziano Colombo2, Giuseppe Chirico3, Giancarlo Capitani1, Isabella Dalle-Donne2, Paride Mantecca1*

1 Department of Earth and Environmental Sciences, Research Center POLARIS, University of Milano Bicocca, 1 Piazza della Scienza - 20126 Milan, Italy

2 Department of Biosciences, Università degli Studi di Milano, 26 via Celoria - 20133 Milan, Italy

3 Department of Physic, University of Milano Bicocca, 2 Piazza della Scienza - 20126 Milano, Italy

4 Luxembourg Institute of Science and Technology (LIST), Environmental Research and Innovation (ERIN) Department, 41, rue du Brill, L-4422 Belvaux, Grand-Duchy of Luxembourg

1. Dynamic Light Scattering characterization of the nanoparticles.

1.1 Analysis of the second order correlation function of the light scattered by suspensions of the cCuO and sCuO nanoparticles.

The NP suspensions were studied on a home-made DLS spectrometer [60] The laser source was a He-Ne laser (HNL210L, Thorlabs, USA) emitting at 633 nm with average power 21 mW. The scattering_angle was set at 90°. A cylindrical quartz cell (Hellma GmbH & Co, Germany) was thermostated (Thermo Haake GmbH, Germany) at 37 °C. The temperature monitored by a thermocouple placed just below the scattering cell had fluctuations smaller than 0.1 °C. The normalized intensity (second order) autocorrelation functions (ACFs) were computed by an ISS FCS

board (ISS Inc. Urbana, IL, USA) and they were fit to a multi-exponential decay law according to the following relation [61]:

(1)

Additional Table 1. Best fit parameters of the double Exponential analysis of the second order ACFs.

| Sample | Radius first component (nm) | Radius first component (nm) | Relative amplitude first component |
| --- | --- | --- | --- |
| sCuO 25 mg/ml | 210 2 | 6300 600 | 88% |
| sCuO 50 mg/ml | 190 2 | 790 200 | 77% |
| cCuO 25 mg/ml | 270 10 | 4500 1200 | 77% |
| cCuO 50 mg/ml | 770 70 |  | 100% |

The hydrodynamic radii were computed according to the Stokes-Einstein relation , where KB is the Boltzmann constant, T and  are the solution temperature and viscosity and  is the hydrodynamic radius of the k-th species.

Additional Figure1. The double exponential fit of the second order (intensity) ACFs for the sCuO (panel A) and the cCuO (panel B) NPs. For each concentration (either 25 or 50 mg/ml two distinct ACF acquisition (open symbols) with the corresponding best fit functions (colored solid lines) are plotted.

1.2 Maximum Entropy analysis of the first order ACFs.

As a second approach to the analysis of the ACFs from the nanoparticle suspensions, the first order ACFs g(1)τ were computed from the measured second order ACF, g(2)τ, as g(1)τ= g(2)τ-1, and the analysis was performed on g(1)τ up to the first largest lag-time, τ*, for which g(2)τ*< 1. The first order correlation function was fit to a regularized distribution of relaxation rates () according to [63]:

(2)

In this second approach, a single component was always found in the distributions of relaxation rates Γ. However, the distributions always displayed a marked skewness at high radii value that is accounted for by additional minor components (up to 4 components in total). The distributions PΓ were then fit to a composition of up to 4 log-normal functions .

We have then obtained a weighted average of the hydrodynamic radius according to the relation:

(3)

Additional Table 2. Best fit average hydrodynamic radii of the maximum entropy analysis of the first order ACFs for the copper oxide NPs.

| Sample | Average Radius (nm) |
| --- | --- |
| sCuO25 mg/ml |  |
| sCuO50 mg/ml |  |
| cCuO25 mg/ml |  |
| cCuO50 mg/ml |  |

The uncertainties in the radii were computed according to the relation:

1σ2= i1σi2						(4)

The super. and subscripts in Table 2 correspond to the minimum and maximum variability of the radius according to the average log-normal distribution.

Additional Figure 2. Exemplary distributions of radii for the suspension of Nanoparticles. T=37 °C. The solid line is a multicomponent lognormal fit to the data. The ACFs for the 25 and 50 mg/ml suspensions are reported in filled and open symbols, respectively. Panel A: sCuO NPs. Panel B: cCuO NPs.