Supporting Information:

Enhanced Macroporous Cationic Chitosan Hydrogel by Freezing and Thawing Method with Superadsorption Capacity for Anionic Dyes

Zahraa H. Athab1, Ahmed F. Halbus2*, Ahmed S. Abbas2, Jasim M. Salman3 and

Abbas J. Atiyah2

1Environmental Research and Studies Center, University of Babylon, Hilla, IRAQ;

2Department of Chemistry, College of Science, University of Babylon, Hilla, IRAQ;

3Department of Biology, College of Science, University of Babylon, Hilla, IRAQ;

*Corresponding author e-mail: ahmed.halbus@uobabylon.edu.iq

Contents

Photographs of a cylindrical monolithic FCS hydrogel	2

Photograph images demonstrates using FCS monolithic hydrogel for adsorption of anionic dyes	3

Photograph images demonstrates using FCS monolithic hydrogel for adsorption of cationic dyes	4

Table S1. Freundlich and Langmuir Isotherms parameters for CR and SFL dyes adsorption onto FCS hydrogel at 293 K and pH 6.	5

Table S2. Kinetic parameters using pseudo-first order, pseudo-second order and intraparticle kinetic models CR dye adsorption onto FCS hydrogel at 293 K and pH 6.	6

Table S3. Kinetic parameters using pseudo-first order, pseudo-second order and intraparticle kinetic models SFL dye adsorption onto FCS hydrogel at 293 K and pH 6.	6

# Photographs of a cylindrical monolithic FCS hydrogel

Fig. S1 Photographs of a cylindrical monolithic FCS hydrogel show change the hydrogel color after gelation as a function of time (A) 30 min after gelation (B) 6 hours after gelation and (C) after 24 hours after gelation, which also confirms the formation of cross-links between CS and GA.

# Photograph images demonstrates using FCS monolithic hydrogel for adsorption of anionic dyes

Fig. S2 Photograph images demonstrates using FCS monolithic hydrogel for adsorption of anionic dyes (A) CR dye; (B) SFL dye.

# Photograph images demonstrates using FCS monolithic hydrogel for adsorption of cationic dyes

Fig. S3 Photograph images demonstrates using FCS monolithic hydrogel for adsorption of cationic dyes (A) MB dye; (B) R6G dye.

# Table S1. Freundlich and Langmuir Isotherms parameters for CR and SFL dyes adsorption onto FCS hydrogel at 293 K and pH 6.

| Dye | Isotherm model | Isotherm model constant |  |
| --- | --- | --- | --- |
| CR | Freundlich | R2 | 0.994 |
|  |  | KF[(mg/g)(mg*L-1/n] | 1.457 |
|  |  | n | 1.919 |
|  | Langmuir | R2 | 0.908 |
|  |  | KL(L/mg) | 0.226 |
|  |  | Qmax (mg/g) | 136.986 |
| SFL | Freundlich | R2 | 0.989 |
|  |  | KF | 1.330 |
|  |  | n | 1.646 |
|  | Langmuir | R2 | 0.896 |
|  |  | KL | 0.148 |
|  |  | Qmax | 142.857 |

# Table S2. Kinetic parameters using pseudo-first order, pseudo-second order and intraparticle kinetic models CR dye adsorption onto FCS hydrogel at 293 K and pH 6.

| Co mg/L | pseudo-first order kinetic model |  |  |  | pseudo-second order kinetic model |  |  | Intraparticale diffusion model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qe,exp (mg/g) | qe,cal (mg/g) | k1 (min-1) | R2 | qe,cal (mg/g) | k2 (g/mg min) | R2 | C (mg/g) | kp (mg/g min1/2) | R2 |
| 10 | 19.128 | 20.833 | 16.689 | 0.981 | 19.920 | 0.077 | 0.999 | 12.372 | 0.421 | 0.698 |
| 20 | 37.029 | 39.525 | 15.722 | 0.993 | 38.461 | 0.074 | 0.999 | 23.642 | 0.817 | 0.753 |
| 30 | 53.06931 | 56.497 | 1.2906 | 0.964 | 54.945 | 0.096 | 0.999 | 37.488 | 0.964 | 0.682 |
| 40 | 68.43564 | 72.463 | 1.3522 | 0.987 | 70.921 | 0.074 | 0.999 | 47.052 | 1.292 | 0.710 |
| 50 | 86.49505 | 92.592 | 17.091 | 0.991 | 89.285 | 0.072 | 0.999 | 57.762 | 1.775 | 0.728 |
| 60 | 103.4059 | 112.359 | 17.713 | 0.985 | 107.526 | 0.070 | 0.999 | 64.597 | 2.370 | 0.714 |

| Co mg/L | pseudo-first order kinetic model |  |  |  | pseudo-second order kinetic model |  |  | Intraparticale diffusion model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qe,exp (mg/g) | qe,cal (mg/g) | k1 (min-1) | R2 | qe,cal (mg/g) | k2 (g/mg min) | R2 | C (mg/g) | kp (mg/g min1/2) | R2 |
| 10 | 18.925 | 21.786 | 23.376 | 0.935 | 19.920 | 0.081 | 0.998 | 11.145 | 0.490 | 0.624 |
| 20 | 36.337 | 47.393 | 37.794 | 0.905 | 39.062 | 0.078 | 0.992 | 17.847 | 1.173 | 0.572 |
| 30 | 51.452 | 62.500 | 27.908 | 0.921 | 54.347 | 0.102 | 0.996 | 29.136 | 1.441 | 0.568 |
| 40 | 65.738 | 73.529 | 20.273 | 0.968 | 68.027 | 0.080 | 0.998 | 40.168 | 1.595 | 0.638 |
| 50 | 83.345 | 90.909 | 17.002 | 0.973 | 86.956 | 0.077 | 0.998 | 52.978 | 1.9132 | 0.679 |
| 60 | 99.536 | 109.890 | 18.254 | 0.971 | 103.092 | 0.075 | 0.998 | 63.365 | 2.292 | 0.642 |

# Table S3. Kinetic parameters using pseudo-first order, pseudo-second order and intraparticle kinetic models SFL dye adsorption onto FCS hydrogel at 293 K and pH 6.