Appendix

A. Progressive failure criteria for modelling 3D-printed CCF/PA composites

When modelling the continuous fibre, i.e., CCF/PA composites, the material constitutive relations is presumed to be a plane stress orthotropic material with linear elasticity, by which the constitutive response of the material can be calculated based on continuum damage mechanics as follows:

(A1)

where ε is the elastic strain and ε = (ε11, ε22, ε12)T, σ is the stress vector and σ = (σ11, σ22, σ12)T, and Cd is the damage-variable based stiffness matrix,

(A2)

where df, dm and ds = 1−(1–df)(1–dm)v12v21 are the continuous fibre, matrix and shear damage variables, respectively, varying from 0 (undamaged) to 1 (completely damaged) to reflect the material modulus degradation. E11, E22 and G12 are the Young’s moduli while v12 and v21 are the Poisson ratios. Thus, the damage variables determine the reduction of elastic properties and influence the stress propagation and residual strength in the plies. For the failure calculation, based on Hashin’s method [21, 22], the initiation failure criteria in the progressive failure modelling are presented below.

Table A1 Hashin damage initiation criteria for 3D-printed CCF/PA composites in the modelling.

| Description | Stress condition | Damage initiation |
| --- | --- | --- |
| Fibre tensile mode |  |  |
| Fibre compressive mode |  |  |
| Matrix tensile mode |  |  |
| Matrix compressive mode |  |  |

*XT and XC are the strengths along the fibre direction under uniaxial tensile and compressive loading, respectively, YT and YC are the strengths of the matrix normal to the fibre direction under uniaxial tensile and compressive loading, respectively, S12L and S12T denote shear strengths in the longitudinal and transverse directions, respectively with S12L = S12L = S12, α is the coefficient determining the contribution of shear stress to the fibre tensile mode and it is defined as 1 to fully include shear stress, Fft , Ffc , Fmt or Fmc are the assessment values, by which if it is equal to or higher than 1, the damage initiation criteria are met and afterwards the damage evaluation process will begin.

Once any the four failure initiation modes in Table A1 have been reached, the corresponding damage are evaluated by calculating equivalent stress and strain in a linear degradation as follows:

Fibre tension (,)

(A3)

Fibre compression (,)

(A4)

Matrix tension (,)

(A5)

Matrix compression (,)

(A6)

where Lc, the characteristic length, is determined by the element geometry and introduced to normalise the elements with different size ranges and ε11, ε22 and ε12 are the elastic strain. Accordingly, such a bilinear equivalent stress-strain model for the failure initiation and evolution of the 3D-printed CCF/PA composites is then applied with continuum damage mechanics in current modelling.