Table 4: Vibration modes and mode assignments for the ATR FT-IR spectra (Melissa et al., 2018).

| Polymer | Chemical structure | Absorption bands (cm-1) | Assignment |
| --- | --- | --- | --- |
| Polypropylene (PP) |  | 2950 | C-H stretch |
|  |  | 2915 | C-H stretch |
|  |  | 2838 | C-H stretch |
|  |  | 1455 | CH2 bend |
|  |  | 1377 | CH3 bend |
|  |  | 1166 | CH bend, CH3 rock, C-C stretch |
|  |  | 997 | CH3 rock, CH3 bend, CH bend |
|  |  | 972 | CH3 rock, C-C stretch |
|  |  | 840 | CH2 rock, C-CH3 stretch |
|  |  | 808 | CH2 rock, C-C stretch, C-CH stretch |
| Polyethylene (PE) |  | 2915 | C-H stretch |
|  |  | 2845 | C-H stretch |
|  |  | 1467 | CH2 bend |
|  |  | 1462 | CH2 bend |
|  |  | 1377 | CH3 bend |
|  |  | 730 | CH2 rock |
|  |  | 717 | CH2 rock |
| Polyethylene terephthalate (PET) |  | 1713 | C=O stretch |
|  |  | 1241 | C-O stretch |
|  |  | 1094 | C-O stretch |
|  |  | 720 | Aromatic CH out of plane bend |
| Ethylene vinyl acetate (EVA) |  | 2917 | C-H stretch |
|  |  | 2848 | C-H stretch |
|  |  | 1740 | C=O stretch |
|  |  | 1464 | CH2 bend, CH3bend |
|  |  | 1241 | C(=O)O stretch |
|  |  | 1020 | C-O stretch |
|  |  | 720 | CH2 rock |
| Nylon (all polyamides) |  | 3298 | N-H stretch |
|  |  | 2932 | CH stretch |
|  |  | 2858 | CH stretch |
|  |  | 1634 | C=O stretch |
|  |  | 1538 | NH bend, C-N stretch |
|  |  | 1464 | CH2 bend |
|  |  | 1372 | CH2 bend |
|  |  | 1274 | NH bend, C-N stretch |
|  |  | 1199 | CH2 bend |
|  |  | 687 | NH bend, C=O bend |

Table 5: ATR FT-IR result for selected microplastic.

| Absorption band | ATR FT-IR Result |
| --- | --- |
| S1: Polypropylene (PP) - 2951.05 cm-1 - 2918.44 cm-1 - 2840.72 cm-1 - 1456.21 cm-1 - 1375.96 cm-1 - 1166.81 cm-1 - 998.50 cm-1 - 973.54 cm-1 - 841.12 cm-1 - 808.84 cm-1 | (j) (i) (h) (g) (f) (c) (e) (d) (b) (a) |
| S2: Polyethylene (PE) - 2915.83 cm-1 - 2848.14 cm-1 - 1465.05 cm-1 - 1378.43 cm-1 - 717.33 cm-1 | (a) (e) (d) (c) (b) PE |
| S3: Polyethylene terephthalate (PET) - 1713.25 cm-1 - 1243.68 cm-1 - 1093.66 cm-1 - 724.43 cm-1 | PET (c) (d) (b) (a) |
| S4: Ethylene vinyl acetate (EVA) - 2922.10 cm-1 - 2853.11 cm-1 - 1710.59 cm-1 - 1454.29 cm-1 - 1242.25 cm-1 - 1018.08 cm-1 - 724.93 cm-1 | (g) (f) (e) (d) (b) (c) (a) EVA |
| S5: Nylon (all polyamides) - 3273.41 cm-1 - 2922.69 cm-1 - 2853.06 cm-1 - 1623.85 cm-1 - 1528.54 cm-1 | (e) (d) (c) (b) (a) Nylon |