Supplementary Materials: In vitro degradation and erosion behavior of commercial PLGAs used for controlled drug delivery

Jennifer Walkera, Jason Alberta, Desheng Lianga, Jing Suna, Richard Schutzmana, Raj Kumara, Cameron Whitea, Moritz Beck-Broichsitterb and Steven P. Schwendemana, c*

a Department of Pharmaceutical Sciences and the Biointerfaces Institute, University of Michigan, North Campus Research Complex, 2800 Plymouth Road, Ann Arbor, MI, 48109, United States;

b MilliporeSigma a Business of Merck KGaA, Frankfurter Strasse 250, D-64293, Darmstadt, Germany;

c Department of Biomedical Engineering, University of Michigan, 2200 Bonisteel Ave., Ann Arbor, MI, 48109, United States.

*Corresponding author. Department of Pharmaceutical Sciences and the Biointerfaces Institute, University of Michigan, North Campus Research Complex, 2800 Plymouth Road, Ann Arbor, MI, 48109, United States. E-mail address: schwende@umich.edu (S.P. Schwendeman).

Supplementary Fig. 1. Lactic content remaining in 50/50 acid- and ester-terminated PLGA films as a function of incubation time. The remaining lactic content was determined by 1HNMR and actual differences relative to their raw polymer starting %lactic content were used for statistical analyses. Data represents mean ± standard error (SE), n=3. Day 21 was used in place of day 28 for Resomer® RG 502H and Expansorb® DLG 50-2A due to significant film mass loss. Statistics represent unpaired t-test, *p<0.05.