Supplementary Information

Rapid, quantitative, and high-sensitivity detection of anti-phospholipase A2 receptor antibodies using novel CdSe/ZnS-based fluorescence immunosorbent assay

Chenxi Li1, Manyun Qian2, Qiaozhen Hong3, Xiaohong Xin2, Zichun Sun4, Yafeng Li2*, Bo Tang1,4*, Bing Gu1,5*

1Medical Technology School of Xuzhou Medical University, Xuzhou Key Laboratory of Laboratory Diagnostics, Xuzhou 221004, China

2Department of nephrology, The Shanxi People’s Hospital, Shanxi Medical University, Taiyuan, Shanxi 030001, China

3Department of Laboratory Medicine, Quzhou Kecheng People's Hospital, Quzhou 324000, China

4Nanjing Vazyme Medical Technology Co. Ltd., Nanjing 210046, China

5Department of Laboratory Medicine, The Affiliated Hospital of Xuzhou Medical University, Xuzhou 221006, China

*Corresponding authors

Bing Gu, Medical Technology School of Xuzhou Medical University, Xuzhou Key Laboratory of Laboratory Diagnostics, Xuzhou 221004, China; Department of Laboratory Medicine, Affiliated Hospital of Xuzhou Medical University, Xuzhou 221006, China. E-mail: binggu2015@xzhmu.edu.cn

Bo Tang, Medical Technology School of Xuzhou Medical University, Xuzhou Key Laboratory of Laboratory Diagnostics, Xuzhou 221004, China. Nanjing Vazyme Medical Technology Co. Ltd., Nanjing 210046, China. E-mail: tangbo@vazyme.com

Yafeng Li, Department of Nephrology, The Shanxi People’s Hospital, Shanxi Medical University, Taiyuan, Shanxi 030001, China. E-mail: Dr.yafengli@gmail.com

Optimization of the coupling ratio between QDs and mAb

The QD-ICA test strip prepared previously (see “Fabrication of the QD-based immunochromatography assay”) was used to identify the optimal coupling ratio between hydrophilic QDs and mAb. Different concentrations of a commercial PLA2R antigen (0.5, 1, and 2 mg/mL) and different coupling ratios of the QD-mAb conjugate (1:0.1, 1:0.15, 1:0.2, 1:0.25, 1:0.3) were coated on test strips. Standard serum (100 RU/mL; EUROIMMUN) was added and incubated with QD-mAb conjugates with different coupling ratios for the same time. Under excitation and emission wavelengths of 356 and 615 nm, respectively, the T/C fluorescence of QD-mAb conjugates with different coupling ratios was measured simultaneously (10-20 min).

Analytical performance of QD-ICA

LoB was used to determine the highest concentration of anti-PLA2R antibodies detected from blank samples and LoD was used to determine the lowest concentration that the method could reliably detect to establish the presence or absence of anti-PLA2R antibodies [1]. LoB and LoD was calculated according to the CLSI EP17 document [1]. Physiological saline (blank control) was tested 60 times and the values for anti-PLA2R antibodies were recorded. If the detection values were normally distributed, the LoB threshold of the anti-PLA2R antibody corresponded to:

LoB = µB + 1.645 σB

where µB is the detection mean of blank control, σB is the standard deviation (SD) of blank control.

If the values showed asymmetric distributions, the LoB corresponded to the 95th percentile of the detected data. Three samples containing low levels of anti-PLA2R antibodies were selected and 12 replicates were performed to determine the SD for the LoD. The calculation formula was:

LoD = LoB + 1.645 σs

where σS is the SD of the low sample measurement population.

References

- Tholen, D.W., et al. Protocols for determination of limits of detection and limits of quantitation; approved guideline—second edition. CLSI EP17-A 2004; 24.